Steam Activated Hydrochar from Wine Waste for the Removal of Pharmaceutical Micropollutants from Water

Lucio Zaccarielloa, Annarita Travaglinob, Angelo Fentib*, Giovanni Falcoa, Simona Galoppob, Domenico Palmaa, Antonella Giarrac, Maria Toscanesic, Marco Trifuoggic,d, Pasquale Iovinoa

a Department of Environmental, Biological and Pharmaceutical Sciences and Technologies, University of Campania “Luigi Vanvitelli”, Via Vivaldi 43, 81100 Caserta, Italy

b Department of Engineering, University of Campania “Luigi Vanvitelli”, Via Roma 29, 81031 Aversa (CE), Italy

c Department of Chemical Sciences, University of Naples Federico II, Via Vicinale Cupa Cintia 26, 80126 Naples, Italy

d CeSMA – Advanced Metrological and Technological Services Centre, University of Naples Federico II, Corso Nicolangelo Protopisani, 80146 Naples, Italy

*Corresponding author:

Angelo Fenti, Department of Engineering, University of Campania “Luigi Vanvitelli”, Via Roma 29, 81031 Aversa, Italy; Tel: +39 0823274148; E-mail: angelo.fenti@unicampania.it.

Table S1. DCF adsorption test on hydrochar produced during HTC treatments conducted at different operative conditions, and physically activated by steam.

| Exp. runs # | HTC T (°C) | Steam activation* | Mass of hydrochar (mg) | Volume (ml) | Adsorbent dosage (g L-1) |
| --- | --- | --- | --- | --- | --- |
| 1 | 200 | / | 10 | 50 | 0.2 |
| 2 | 200 | / | 20 | 50 | 0.4 |
| 3 | 200 | / | 30 | 50 | 0.6 |
| 4 | 200 | / | 40 | 50 | 0.8 |
| 5 | 200 | / | 50 | 50 | 1.0 |
| 6 | 230 | / | 10 | 50 | 0.2 |
| 7 | 230 | / | 20 | 50 | 0.4 |
| 8 | 230 | / | 30 | 50 | 0.6 |
| 9 | 230 | / | 40 | 50 | 0.8 |
| 10 | 230 | / | 50 | 50 | 1.0 |
| 11 | 260 | / | 10 | 50 | 0.2 |
| 12 | 260 | / | 20 | 50 | 0.4 |
| 13 | 260 | / | 30 | 50 | 0.6 |
| 14 | 260 | / | 40 | 50 | 0.8 |
| 15 | 260 | / | 50 | 50 | 1.0 |
| 16 | 230 | yes | 10 | 50 | 0.2 |
| 17 | 230 | yes | 20 | 50 | 0.4 |
| 18 | 230 | yes | 30 | 50 | 0.6 |
| 19 | 230 | yes | 40 | 50 | 0.8 |
| 20 | 230 | yes | 50 | 50 | 1.0 |

*Steam activation conditions: steam flow rate of 5 g min-1 at a temperature of 900 °C for 15 minutes.

Fig. S1. Hydrochar steam activation apparatus.

Fig. S2. Plot of the point of zero charge of i) HC-230 (red line), ii) steam-activated HC-230 (blue line).

Table S2. BET analyses of the HC-200, HC-230, HC-260, and of steam-activated HC-230 samples.

| Sample | SBET (m²/g) | Error (± m²/g) |
| --- | --- | --- |
| HC-200 | 17.44 | ± 0.20 |
| HC-230 | 49.41 | ± 0.51 |
| HC-260 | / | / |
| SA-HC-230 | 728 | ± 0.5 |

Fig. S3. The effect of HTC temperature on DCF removal efficiencies (%) and adsorption capacity (mg g-1); initial DCF concentration = 5.0 mg L−1; pH = 9.0 ± 0.1; adsorbent dosage = 1.0 g L-1.

Fig. S4. Pseudo-first and pseudo-second order fitting procedures for the DCF adsorption experimental data onto steam-activated HC-230 at different adsorbent dosage.

Fig. S5. Intra-particle diffusion and Elovich fitting procedures for the DCF adsorption experimental data onto steam-activated HC-230 at different adsorbent dosage.

Table S3. Adsorption isotherm parameters for DCF adsorption onto steam-activated HC-230.

| Adsorbent | qe (mg g-1) | Lanngmuir |  |  | Freundlich |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qmax (mg g-1) | kL (L mg-1) | R2 | kF (mg1-1/n L1/n g-1) | 1/n |  | R2 |  | qmax(1) (mg g-1) |
| Steam-activated HC-230 | 22.01 | 25.19 | 8.97 | 0.971 | 23.6 | 0.347 |  | 0.896 |  | 42.89 |
|  |  | Dubinin-Radushkevich |  |  | Temkin |  |  |  |  |  |
|  |  | qmax (mg g-1) | BD-R (mol2 kJ−2) | R2 | B (J mol−1) |  | KT (L g−1) |  | R2 |  |
|  |  | 25.91 | 2.15x10-2 | 0.964 | 5.236 |  | 88.11 |  | 0.954 |  |

- qmax=kFC01/n