Supplementary Table S1. Tukey’s multiple comparisons test for all experimental groups.
P values are shown for comparisons of flexural strength, Vickers hardness, degree of conversion (DC), color difference (ΔE), and surface roughness (Ra). Statistically significant differences (P < 0.05) are indicated for each pairwise comparison.
	Tukey's multiple comparisons test
	P Value
(Flexural strength)
	P Value
(Vickers hardness)
	P Value
(DC)
	P Value
(ΔE)
	P Value
(Ra)

	Control vs. 1%S
	0.8313
	<0.0001
	0.0144
	<0.0001
	<0.0001

	Control vs. 2%S
	0.7839
	0.6556
	0.0003
	<0.0001
	<0.0001

	Control vs. 1%L
	0.7327
	<0.0001
	0.9938
	<0.0001
	<0.0001

	Control vs. 2%L
	0.0995
	<0.0001
	>0.9999
	<0.0001
	<0.0001

	1%S vs. 2%S
	0.2046
	0.0004
	0.8025
	<0.0001
	0.0151

	1%S vs. 1%L
	0.9997
	0.5551
	0.0053
	<0.0001
	<0.0001

	1%S vs. 2%L
	0.5667
	<0.0001
	0.0175
	<0.0001
	<0.0001

	2%S vs. 1%L
	0.1437
	<0.0001
	<0.0001
	<0.0001
	<0.0001

	2%S vs. 2%L
	0.0057
	<0.0001
	0.0003
	<0.0001
	<0.0001

	1%L vs. 2%L
	0.6814
	<0.0001
	0.9893
	<0.0001
	<0.0001



