Supplementary Table S1. Tukey’s multiple comparisons test for all experimental groups.

P values are shown for comparisons of flexural strength, Vickers hardness, degree of conversion (DC), color difference (ΔE), and surface roughness (Ra). Statistically significant differences (P < 0.05) are indicated for each pairwise comparison.

| Tukey's multiple comparisons test | P Value (Flexural strength) |  | P Value (Vickers hardness) |  | P Value (DC) |  | P Value (ΔE) |  | P Value (Ra) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Control vs. 1%S |  | 0.8313 |  | <0.0001 |  | 0.0144 |  | <0.0001 | <0.0001 |
| Control vs. 2%S |  | 0.7839 |  | 0.6556 |  | 0.0003 |  | <0.0001 | <0.0001 |
| Control vs. 1%L |  | 0.7327 |  | <0.0001 |  | 0.9938 |  | <0.0001 | <0.0001 |
| Control vs. 2%L |  | 0.0995 |  | <0.0001 |  | >0.9999 |  | <0.0001 | <0.0001 |
| 1%S vs. 2%S |  | 0.2046 |  | 0.0004 |  | 0.8025 |  | <0.0001 | 0.0151 |
| 1%S vs. 1%L |  | 0.9997 |  | 0.5551 |  | 0.0053 |  | <0.0001 | <0.0001 |
| 1%S vs. 2%L |  | 0.5667 |  | <0.0001 |  | 0.0175 |  | <0.0001 | <0.0001 |
| 2%S vs. 1%L |  | 0.1437 |  | <0.0001 |  | <0.0001 |  | <0.0001 | <0.0001 |
| 2%S vs. 2%L |  | 0.0057 |  | <0.0001 |  | 0.0003 |  | <0.0001 | <0.0001 |
| 1%L vs. 2%L |  | 0.6814 |  | <0.0001 |  | 0.9893 |  | <0.0001 | <0.0001 |