Experimental and Machine Learning Prediction of Compressive Strength of Chemically Activated RHA based RAC using SHAP and PDP Analysis

Supplementary File

- Data Source References with Access Links

This provides a detailed list of the original dataset sources used in this study. Each reference includes a direct link to publicly available data for easy access.

- Current Study

- Fadi Althoey et. al. [59]. Available at: https://doi.org/10.1016/j.jobe.2022.104610

- Chao Liu et. al. [60]. Available at: https://doi.org/10.1016/j.conbuildmat.2022.128934

S2. Dataset:

| Sr. No. | Cement (kg/m3) | RHA (kg/m3) | FA (kg/m3) | RCA (kg/m3) | NCA (kg/m3) | Water (kg/m3) | SP (kg/m3) | Sodium Sulfate (kg/m3) | Age (days) | CS (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 3 | 15.9 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 3 | 16.8 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 3 | 17.62 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 3 | 16.52 |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 7 | 31.12 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 7 | 33.34 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 7 | 35.03 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 7 | 33.9 |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 14 | 40.82 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 14 | 42.73 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 14 | 43.68 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 14 | 42.06 |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 28 | 50.66 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 28 | 52.11 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 28 | 54.04 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 28 | 53.01 |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 56 | 53.64 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 56 | 54.51 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 56 | 55.86 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 56 | 54.22 |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 90 | 55.97 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 90 | 56.08 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 90 | 57.77 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 90 | 56.33 |
|  | 550 | 0 | 680 | 0 | 880 | 176 | 12 | 0 | 120 | 56.67 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 0 | 120 | 57.34 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 0 | 120 | 58.76 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 0 | 120 | 57.35 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 3 | 18.6 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 3 | 18.94 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 3 | 19.02 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 7 | 36.39 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 7 | 38.59 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 7 | 37.07 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 14 | 52.07 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 14 | 53.26 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 14 | 52.75 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 28 | 58.65 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 28 | 60.47 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 28 | 58.62 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 56 | 59.55 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 56 | 60.95 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 56 | 59.33 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 90 | 60.33 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 90 | 61.38 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 90 | 59.18 |
|  | 495 | 55 | 680 | 0 | 880 | 176 | 12 | 13.75 | 120 | 62.85 |
|  | 440 | 110 | 680 | 0 | 880 | 176 | 12 | 13.75 | 120 | 65.95 |
|  | 385 | 165 | 680 | 0 | 880 | 176 | 12 | 13.75 | 120 | 63.64 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 3 | 14.52 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 3 | 15.93 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 3 | 16.54 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 3 | 15.18 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 7 | 27.56 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 7 | 28.45 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 7 | 30.14 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 7 | 29.22 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 14 | 40.73 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 14 | 41.63 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 14 | 44.01 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 14 | 42.7 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 28 | 46.12 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 28 | 47.46 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 28 | 49.93 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 28 | 46.12 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 56 | 47.97 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 56 | 49.12 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 56 | 50.52 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 56 | 49.73 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 90 | 48.64 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 90 | 50.64 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 90 | 51.94 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 90 | 50.16 |
|  | 550 | 0 | 680 | 352 | 528 | 176 | 12 | 0 | 120 | 53.38 |
|  | 495 | 55 | 680 | 352 | 528 | 176 | 12 | 13.75 | 120 | 54.33 |
|  | 440 | 110 | 680 | 352 | 528 | 176 | 12 | 13.75 | 120 | 56.17 |
|  | 385 | 165 | 680 | 352 | 528 | 176 | 12 | 13.75 | 120 | 55.13 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 3 | 13.58 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 3 | 14.94 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 3 | 15.91 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 3 | 14.53 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 7 | 22.54 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 7 | 23.70 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 7 | 24.39 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 7 | 23.66 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 14 | 33.17 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 14 | 34.76 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 14 | 36.65 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 14 | 33.06 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 28 | 36.95 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 28 | 40.11 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 28 | 41.85 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 28 | 39.58 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 56 | 39.56 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 56 | 41.09 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 56 | 42.81 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 56 | 41.39 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 90 | 40.02 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 90 | 42.88 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 90 | 44.62 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 90 | 42.08 |
|  | 550 | 0 | 680 | 528 | 352 | 176 | 12 | 0 | 120 | 45.29 |
|  | 495 | 55 | 680 | 528 | 352 | 176 | 12 | 13.75 | 120 | 46.99 |
|  | 440 | 110 | 680 | 528 | 352 | 176 | 12 | 13.75 | 120 | 47.81 |
|  | 385 | 165 | 680 | 528 | 352 | 176 | 12 | 13.75 | 120 | 49.24 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 3 | 10.53 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 3 | 11.58 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 3 | 12.37 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 3 | 13.45 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 7 | 18.24 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 7 | 19.02 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 7 | 20.59 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 7 | 19.29 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 14 | 25.86 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 14 | 27.91 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 14 | 29.78 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 14 | 26.22 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 28 | 29.12 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 28 | 31.45 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 28 | 32.83 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 28 | 30.65 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 56 | 31.81 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 56 | 33.28 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 56 | 34.47 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 56 | 32.26 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 90 | 33.32 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 90 | 34.96 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 90 | 35.94 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 90 | 33.42 |
|  | 550 | 0 | 680 | 704 | 176 | 176 | 12 | 0 | 120 | 38.26 |
|  | 495 | 55 | 680 | 704 | 176 | 176 | 12 | 13.75 | 120 | 39.43 |
|  | 440 | 110 | 680 | 704 | 176 | 176 | 12 | 13.75 | 120 | 41.02 |
|  | 385 | 165 | 680 | 704 | 176 | 176 | 12 | 13.75 | 120 | 40.67 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 3 | 9.87 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 3 | 8.23 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 3 | 7.45 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 3 | 6.32 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 7 | 16.78 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 7 | 15.49 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 7 | 14.64 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 7 | 13.71 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 14 | 23.18 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 14 | 22.68 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 14 | 21.43 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 14 | 20.12 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 28 | 27.56 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 28 | 26.51 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 28 | 25.89 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 28 | 24.23 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 56 | 29.36 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 56 | 28.33 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 56 | 27.78 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 56 | 26.22 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 90 | 30.34 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 90 | 29.56 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 90 | 28.19 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 90 | 27.88 |
|  | 550 | 0 | 680 | 880 | 0 | 176 | 12 | 0 | 120 | 35.34 |
|  | 495 | 55 | 680 | 880 | 0 | 176 | 12 | 13.75 | 120 | 34.91 |
|  | 440 | 110 | 680 | 880 | 0 | 176 | 12 | 13.75 | 120 | 31.67 |
|  | 385 | 165 | 680 | 880 | 0 | 176 | 12 | 13.75 | 120 | 28.75 |
|  | 495 | 0 | 675 | 0 | 870 | 205 | 5.44 | 0 | 28 | 62 |
|  | 495 | 0 | 675 | 0 | 870 | 205 | 5.44 | 0 | 56 | 74 |
|  | 495 | 0 | 675 | 0 | 870 | 205 | 5.44 | 0 | 90 | 83 |
|  | 272.25 | 222.75 | 675 | 0 | 870 | 205 | 5.44 | 0 | 28 | 36 |
|  | 272.25 | 222.75 | 675 | 0 | 870 | 205 | 5.44 | 0 | 56 | 66 |
|  | 272.25 | 222.75 | 675 | 0 | 870 | 205 | 5.44 | 0 | 90 | 72 |
|  | 272.25 | 222.75 | 675 | 0 | 870 | 205 | 5.44 | 14.85 | 28 | 57 |
|  | 272.25 | 222.75 | 675 | 0 | 870 | 205 | 5.44 | 14.85 | 56 | 79 |
|  | 272.25 | 222.75 | 675 | 0 | 870 | 205 | 5.44 | 14.85 | 90 | 88 |
|  | 495 | 0 | 675 | 304.5 | 565.5 | 205 | 5.44 | 0 | 28 | 59 |
|  | 495 | 0 | 675 | 304.5 | 565.5 | 205 | 5.44 | 0 | 56 | 76 |
|  | 495 | 0 | 675 | 304.5 | 565.5 | 205 | 5.44 | 0 | 90 | 82 |
|  | 272.25 | 222.75 | 675 | 304.5 | 565.5 | 205 | 5.44 | 0 | 28 | 39 |
|  | 272.25 | 222.75 | 675 | 304.5 | 565.5 | 205 | 5.44 | 0 | 56 | 64 |
|  | 272.25 | 222.75 | 675 | 304.5 | 565.5 | 205 | 5.44 | 0 | 90 | 73 |
|  | 272.25 | 222.75 | 675 | 304.5 | 565.5 | 205 | 5.44 | 14.85 | 28 | 55 |
|  | 272.25 | 222.75 | 675 | 304.5 | 565.5 | 205 | 5.44 | 14.85 | 56 | 81 |
|  | 272.25 | 222.75 | 675 | 304.5 | 565.5 | 205 | 5.44 | 14.85 | 90 | 93 |
|  | 495 | 0 | 675 | 609 | 261 | 205 | 5.44 | 0 | 28 | 58 |
|  | 495 | 0 | 675 | 609 | 261 | 205 | 5.44 | 0 | 56 | 71 |
|  | 495 | 0 | 675 | 609 | 261 | 205 | 5.44 | 0 | 90 | 76 |
|  | 272.25 | 222.75 | 675 | 609 | 261 | 205 | 5.44 | 0 | 28 | 35 |
|  | 272.25 | 222.75 | 675 | 609 | 261 | 205 | 5.44 | 0 | 56 | 59 |
|  | 272.25 | 222.75 | 675 | 609 | 261 | 205 | 5.44 | 0 | 90 | 67 |
|  | 272.25 | 222.75 | 675 | 609 | 261 | 205 | 5.44 | 14.85 | 28 | 60.5 |
|  | 272.25 | 222.75 | 675 | 609 | 261 | 205 | 5.44 | 14.85 | 56 | 68.5 |
|  | 272.25 | 222.75 | 675 | 609 | 261 | 205 | 5.44 | 14.85 | 90 | 90 |
|  | 495 | 0 | 675 | 870 | 0 | 205 | 5.44 | 0 | 28 | 49 |
|  | 495 | 0 | 675 | 870 | 0 | 205 | 5.44 | 0 | 56 | 56 |
|  | 495 | 0 | 675 | 870 | 0 | 205 | 5.44 | 0 | 90 | 66 |
|  | 272.25 | 222.75 | 675 | 870 | 0 | 205 | 5.44 | 0 | 28 | 30.5 |
|  | 272.25 | 222.75 | 675 | 870 | 0 | 205 | 5.44 | 0 | 56 | 52 |
|  | 272.25 | 222.75 | 675 | 870 | 0 | 205 | 5.44 | 0 | 90 | 55 |
|  | 272.25 | 222.75 | 675 | 870 | 0 | 205 | 5.44 | 14.85 | 28 | 51 |
|  | 272.25 | 222.75 | 675 | 870 | 0 | 205 | 5.44 | 14.85 | 56 | 56.5 |
|  | 272.25 | 222.75 | 675 | 870 | 0 | 205 | 5.44 | 14.85 | 90 | 81.5 |
|  | 410 | 0 | 825 | 0 | 1080 | 164 | 8.5 | 0 | 7 | 40 |
|  | 410 | 0 | 825 | 0 | 1080 | 164 | 8.5 | 0 | 28 | 54 |
|  | 410 | 0 | 825 | 0 | 1080 | 164 | 8.5 | 0 | 90 | 61 |
|  | 369 | 41 | 825 | 0 | 1080 | 164 | 9.5 | 0 | 7 | 42 |
|  | 369 | 41 | 825 | 0 | 1080 | 164 | 9.5 | 0 | 28 | 57.5 |
|  | 369 | 41 | 825 | 0 | 1080 | 164 | 9.5 | 0 | 90 | 66 |
|  | 328 | 82 | 825 | 0 | 1080 | 164 | 11.5 | 0 | 7 | 43.5 |
|  | 328 | 82 | 825 | 0 | 1080 | 164 | 11.5 | 0 | 28 | 59 |
|  | 328 | 82 | 825 | 0 | 1080 | 164 | 11.5 | 0 | 90 | 68 |
|  | 287 | 123 | 825 | 0 | 1080 | 164 | 12 | 0 | 7 | 38 |
|  | 287 | 123 | 825 | 0 | 1080 | 164 | 12 | 0 | 28 | 52 |
|  | 287 | 123 | 825 | 0 | 1080 | 164 | 12 | 0 | 90 | 59.5 |
|  | 410 | 0 | 825 | 540 | 540 | 176.3 | 8.5 | 0 | 7 | 37.5 |
|  | 410 | 0 | 825 | 540 | 540 | 176.3 | 8.5 | 0 | 28 | 52 |
|  | 410 | 0 | 825 | 540 | 540 | 176.3 | 8.5 | 0 | 90 | 56.5 |
|  | 369 | 41 | 825 | 540 | 540 | 176.3 | 9.5 | 0 | 7 | 40 |
|  | 369 | 41 | 825 | 540 | 540 | 176.3 | 9.5 | 0 | 28 | 53 |
|  | 369 | 41 | 825 | 540 | 540 | 176.3 | 9.5 | 0 | 90 | 60 |
|  | 328 | 82 | 825 | 540 | 540 | 176.3 | 11.5 | 0 | 7 | 41 |
|  | 328 | 82 | 825 | 540 | 540 | 176.3 | 11.5 | 0 | 28 | 53.5 |
|  | 328 | 82 | 825 | 540 | 540 | 176.3 | 11.5 | 0 | 90 | 61 |
|  | 287 | 123 | 825 | 540 | 540 | 176.3 | 12 | 0 | 7 | 36 |
|  | 287 | 123 | 825 | 540 | 540 | 176.3 | 12 | 0 | 28 | 48.5 |
|  | 287 | 123 | 825 | 540 | 540 | 176.3 | 12 | 0 | 90 | 55 |
|  | 410 | 0 | 825 | 1080 | 0 | 186 | 8.5 | 0 | 7 | 36 |
|  | 410 | 0 | 825 | 1080 | 0 | 186 | 8.5 | 0 | 28 | 45 |
|  | 410 | 0 | 825 | 1080 | 0 | 186 | 8.5 | 0 | 90 | 49 |
|  | 369 | 41 | 825 | 1080 | 0 | 186 | 9.5 | 0 | 7 | 37.5 |
|  | 369 | 41 | 825 | 1080 | 0 | 186 | 9.5 | 0 | 28 | 45.5 |
|  | 369 | 41 | 825 | 1080 | 0 | 186 | 9.5 | 0 | 90 | 49.8 |
|  | 328 | 82 | 825 | 1080 | 0 | 186 | 11.5 | 0 | 7 | 38 |
|  | 328 | 82 | 825 | 1080 | 0 | 186 | 11.5 | 0 | 28 | 47 |
|  | 328 | 82 | 825 | 1080 | 0 | 186 | 11.5 | 0 | 90 | 49.8 |
|  | 287 | 123 | 825 | 1080 | 0 | 186 | 12 | 0 | 7 | 33 |
|  | 287 | 123 | 825 | 1080 | 0 | 186 | 12 | 0 | 28 | 43 |
|  | 287 | 123 | 825 | 1080 | 0 | 186 | 12 | 0 | 90 | 46 |