Table S1. Overview of curcumin-loaded nanocomposites, summarizing their composition, target cell lines, key physicochemical properties (particle size and zeta potential), cytotoxicity toward normal cells, and drug loading and encapsulation efficiencies.

| Drug | Type of nanocomposite | Normal cell line | Cancer cell line | Size of nanocarriers (nm) | Zeta Potential (mV) | Normal cell Cytotoxicity | Loading Efficiency (%) | Encapsulation Efficiency (%) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Curcumin | Starch/Agarose/ZnO (Triple-component) | --- | MCF-7 | 218.6 | -36.4 | --- | --- | --- | (1) |
| Curcumin | Curcumin-loaded zein nanoparticles (CR-ZN-NPs) | --- | --- | 184 | -66.8 | biocompatible drug delivery system | 51 | 0.64 | (2) |
| Curcumin | Carboxymethyl cellulose-coated curcumin-loaded zein NPs (CR-ZN-CMC-NPs) | --- | --- | 277.5 | −48.1 | biocompatible drug delivery system | 70 | 0.58 | (2) |
| Curcumin | PLGA nanoparticles loaded with Cur | --- | MDA-MB-231 (breast cancer) | 177.13 ± 2.81 | −16.26 ± 2.15 | more effective in inducing cell cytotoxicity | 6.3–8.9 | 50 | (3) |
| Curcumin | HbPG-PTHF-HbPG ABA Triblock Copolymer Micelles | --- | U-87 Glioblastoma | 15–20 | --- | No toxicity observed | 16.2 ± 1.1 | --- | (4) |
| Curcumin | MOF-based nanoparticles with carbon QDs + pH-sensitive chitosan/PEG hydrogel | --- | MCF-7 (breast cancer) | 110 to 220 | +45 | Biocompatible (no toxicity reported) | 31 | 85 | (5) |
| Curcumin | Fucoidan/Nano-Curcumin/Selenium Nanoparticles (Fu/NCur/SeNPs) | --- | CaCo-2, HT-29 (colorectal) | 34.67 ± 4.32 (NCur) | −36.5 | --- | --- | --- | (6) |
| Curcumin | Mg-Al-Ca LDH@Fe3O4 coated with PEG/DOX/CUR (LDH@Fe3O4-PEG-DOX-CUR) | L929 (mouse fibroblast) | HepG2 (human liver cancer) | Not explicitly stated | --- | Low cytotoxicity, good biocompatibility | --- | --- | (7) |
| Curcumin | Chitosan–Alginate Gel | Peripheral blood cells (rabbits) | --- | 521 | --- | Cytotoxicity at highest concentration (10 mg/mL) | Highest loading | Highest encapsulation | (8) |
| Curcumin | Gelatin/Agarose/Mg-CQD@Cur | L929 fibroblast cells | U-87 MG glioma | 193.5 | −42 | Minimal toxicity | 85.5 | 45.75 | (9) |
| Curcumin | Gelatin/Carboxymethylcellulose/CNT@Cur | L929 fibroblast cells | MCF-7 | --- | --- | Significant cytotoxicity (MTT assay) | 46 ± 0.25 | 87 ± 0.3 | (10) |
| Curcumin | Chitosan/Sodium Alginate/CeO₂@Cur | Healthy astrocytes | U-87 MG2 glioma | --- | Positive charge | Minimal toxicity | --- | ~86 | (11) |
| Curcumin | Curcumin-loaded Bovine Serum Albumin Nanoparticles (CUR-BSA NPs) | --- | MCF-7 | ~170 | −36 ± 2.7 | Low cytotoxicity without PDT | --- | 47.5 | (12) |
| Curcumin | curcumin-loaded Niosomes (Span 60/Cholesterol) | --- | --- | 139.7 | --- | --- | --- | ~37 | (13) |
| Curcumin | Fe3O4@Zn-doped Hydroxyapatite (Zn-HA) | Normal fibroblasts | MCF-7 | 14.1 ± 3.4 | -23.34 (after loading) | Excellent cytocompatibility (unloaded) | 251.09 | --- | (14) |
| Curcumin | Reduced Graphene Oxide/Carboxymethyl Tamarind Gum (rGO/CMTG) Nanofibers | --- | MDA-MB-231 human breast cancer cells | --- | --- | High (exact % ---) | --- | --- | (15) |
| Curcumin | Polyelectrolyte Complex (Trimethylchitosan/Carboxymethylkaraya gum) with Silver NPs | MCF-10A | MCF-7 | 712 ± 46.1 | 5.2 ± 0.67 | Confirmed biocompatibility | 0.051 g g−1 | 81.86 | (16) |
| Curcumin | Zein–Methylcellulose Nanoconjugate loaded with Curcumin (ZMC@Cur) | --- | MCF-7, HepG2 | 190 ± 28.2 | --- | --- | --- | 92 | (17) |
| Curcumin | Amine-functionalized Magnetic Nanocellulose Fiber Composites (NH2–MFNCs) | --- | MCF-7 | --- | --- | --- | --- | --- | (18) |
| Curcumin | Ag@LEC-PVA-CUR-NPs | --- | MCF-7, MDA-MB-231, A549 | 10–15 | --- | IC50: 25.6 μg/mL | --- | 90.28 | (19) |
| Curcumin | Linoleic acid (LA)-loaded niosomes | --- | Hep-3B hepatoma | 266.9 | −26.1 | --- | --- | --- | (20) |
| Curcumin | ZnO-decorated Bacterial Cellulose/HPEC Hydrogel (Cc/Pp50@BCZO/HPEC) | Human skin fibroblasts (HFB-4) | --- | < 10 | --- | Excellent cell viability (cytocompatible) | 20 | 100 | (21) |
| Curcumin | Fe3O4@Chitosan/MIL-100(Fe) loaded with Curcumin | Human dermal fibroblasts (HDF) | MCF-7 | --- | −15.7 | Low toxicity | 95.36 | 48.81 | (22) |
| Curcumin | Luteolin-loaded Graphene Quantum Dot–Hyaluronic Acid Nanocomposites (GQD-HA-Lu NCs) | --- | PANC-1 pancreatic | 207.19 | --- | --- | --- | 86.61 | (23) |
| Curcumin | Hollow Cu9S8@PCM@Cur Nanoplatform | --- | --- | --- | --- | Minimal systemic toxicity | --- | --- | (24) |
| Curcumin | PTX/CUR-FA-PLU-127/Ag-β-CD | --- | --- | --- | --- | Hemolysis <3%; safe and nontoxic | CUR: 46.05 ± 1.38 | CUR: 92.02 ± 2.76 | (25) |
| Curcumin | Zein/γ-PGA Nanocomposite loaded with Curcumin (zein/γ-PGA4:1/Cur) | HaCaT, GES1 | --- | 150 | -20 | Assessed cytocompatibility showed safety | 3.84 – 11.41 | 71.28 – 95.93 | (26) |
| Curcumin | Gelatin-Oleic acid-Carboxymethyl chitosan Nanoparticles (GOCNPs) | --- | MCF-7 | --- | --- | Hemocompatibility tested | 78.0 ± 2.34 | 94.0 ± 2.8 | (27) |
| Curcumin | Folic Acid Functionalized Carbon Nanotubes loaded with Curcumin (Cur-FA-OMC) | NIH/3T3 fibroblasts | Not applicable | 217.7 ± 3.05 | −21.5 ± 2.37 | High biocompatibility (low cytotoxicity) | High entrapment | 79.44 ± 0.42 | (28) |
| Curcumin | Curcumin-loaded PEO-PPO-PEO Polymer Nanomicelles (Cur@M) in PLA Fibers | RAW 264.7 macrophage | Murine fibroblast cell line L292 | 160 | −8.7 ± 0.4 | Excellent biocompatibility (patch) | 6.5 ± 1.06 | 55 ± 1.9 | (29) |
| Curcumin | DA-LAC-NH2-ZnO/DOX/CUR/Layered Double Hydroxide (LDH) System | L929 | HepG2 | --- | --- | >90% biocompatibility | CUR: --- | CUR: 36.2 ± 0.5 | (30) |
| Curcumin | Casein Nanoparticles co-loaded with Curcumin and Fluorouracil Acetic Acid (CUR-FUA NPs) | --- | --- | 182.34 ± 22.36 | --- | Hemolysis ~3.5% at 500 µg/mL | CUR: 54.2% | CUR: 96.45% | (31) |
| Curcumin | Sodium Alginate/Polyvinylpyrrolidone/γ-Al₂O₃ Nanoparticles (SA/PVP/γ-Al₂O₃) | --- | Colon cancer cells | --- | --- | Minimal impact on healthy cells | --- | --- | (32) |
| Curcumin | Curcumin-loaded ZnO, Ag2O Nanoparticles and ZnO/Ag2O Nanocomposite (NC) | --- | MDA-MB-231 | --- | --- | IC50 (Antidiabetic, μM): 10.17 | --- | --- | (33) |
| Curcumin | Graphene Quantum Dot-Hyaluronic Acid-Quinoline Nanocomposites (GQD-HA-Qu NCs) | --- | MCF-7, HT-29, A2780, PANC-1, HeLa | 224.96 (Z-average) | −43.38 ± 19.64 | --- | 98.02% | 90.32% | (34) |
| Curcumin | Alginate-encapsulated Curcumin-loaded ZIF-8/ZrO₂ Nanocomposite (Alg-CUR-ZIF-8/ZrO₂-C) | --- | MDA-MB-231 | Increased hydrodynamic size | --- | IC50: Cell viability reduced to 18.04% | --- | --- | (35) |
| Curcumin | CUR-MWCNT-COOH-PEG | PC12 neuronal cells | Alzheimer's disease model | 310 ± 7.92 | −31.1 ± 1.05 | Inhibits apoptosis at 18.75 µg/mL | --- | 91.4 ± 0.8 | (36) |
| Curcumin | Halloysite Nanotubes (HNTs) loaded with CuO NPs and Curcumin (CHC) | --- | HMVII, HepG2, MCF-7 | 252.69 | --- | IC50 value of 10.43 μg/mL | 3–5 | 15–20 | (37) |
| Curcumin | Lactoferrin-conjugated Curcumin-loaded Polycaprolactone Nanoparticles (M-PCL-Cur-Lf) | HBME cells | U-87MG glioblastoma cells | --- | --- | Outperformed non-conjugated NPs | --- | --- | (38) |
| Curcumin | Curcumin-loaded Nanostructured Lipid Carrier in PLA Scaffold (PLA/CNLC) | Fibroblast cells | Not applicable | 292 | --- | Non-cytotoxic | 6.59 ± 1.61 | 81.37 ± 0.85 | (39) |
| Curcumin | MWCNT-COOH-CA | --- | MCF-7 | 371 | -25.2 | --- | --- | 77.86 | (40) |
| Curcumin | Amoxicillin-loaded Montmorillonite Nanoclay in Tri-Calcium Phosphate Cement (AMX-MMT-CPC) | --- | Escherichia coli, Streptococcus mutans... | --- | --- | >95% cell viability (except slight reduction) | --- | 70 | (41) |
| Curcumin | BVZ:PCF:CuNP | --- | UM-SCC-1 (oral malignant keratinocyte) | CuNPs: 40–100 | --- | --- | --- | --- | (42) |
| Curcumin | Cur-FeONPs combined with IFNα-PLGANPs | NIH-3T3 fibroblast cells | A375 melanoma skin cancer cells | Cur-FeONPs: 111.0 | Cur-FeONPs: -29.6 ± 9.51 | High cell viability (>70%); non-cytotoxic | 78.9% ± 0.3 | 93.83% ± 0.1 | (43) |
| Curcumin | Lysozyme (Lys) - Tannic Acid (TA) - Curcumin Complex (Lys-TA-Cur) | Caco-2 cells (intestinal model) | --- | 337 | --- | --- | --- | 92.41 | (44) |
| Curcumin | CS/CUR@UWO-1 | --- | HeLa, SH-SY5Y (cancer cells) | --- | --- | --- | 30.7 | 94.9 | (45) |
| Curcumin | Curcumin-loaded PLGA nanoparticles in thermoresponsive hydrogel | HaCaT (human keratinocytes) | --- | 296.4 ± 3.1 | −7.1 ± 0.8 | Non-cytotoxic on HaCaT cells | --- | 82.5 ± 2.3 | (46) |
| Curcumin | G/PEG/Cu.CQDs@CUR | L929 fibroblasts | U87-MG glioblastoma | 165 | −50 | >90% viability (L929 fibroblasts) | --- | --- | (47) |
| Curcumin | ZnO-MET-FA | --- | A375 (melanoma), T24 (bladder cancer) | < 20 | +3.04 | --- | 3% and 5% | 95–98 | (48) |
| Curcumin | CPA-Fe₃O₄-NPs | --- | U-87 glioblastoma cells | --- | −13.05 | Biocompatible (negative zeta potential) | 15.8 | 79.4 | (49) |
| Curcumin | BaO₂-SA-Cur | L929 fibroblast cells | MG-63 osteosarcoma cells | 139.50 ± 7.8 | --- | >85% cell viability | --- | --- | (50) |
| Curcumin | ConA-Cur-SLNs | --- | A549 human lung cancer | 287.9 ± 3.066 | −17.11 ± 4.21 | --- | 4.43 ± 1.05 | 88 ± 1.285 | (51) |
| Curcumin | Silver-Chitosan Nanocomposites (AgCS-NCs) | HEK-293 (human embryonic kidney cells) | MCF-7 (breast cancer) | 308 | --- | Safe, significant viability | --- | 60 | (52) |
| Curcumin | CUR NPs | --- | BT-474 human breast cancer | 187 | -13.3 | IC50: Better cytotoxicity than free CUR | --- | --- | (53) |
| Curcumin | Piperine-loaded Polycaprolactone Nanoparticles (PPN-PCL-NPs) | --- | MCF-7 breast cancer cells | ~108 | −20.42 ± 1.82 | Stable under different temperatures | --- | 79.53 ± 5.22 | (54) |
| Curcumin | CS-PVP-CQDs@DOX | --- | MCF-7 breast cancer cells | 218 | --- | Biocompatible (CS alone non-toxic) | 47.75 ± 2.17 | 86.42 ± 1.39 | (55) |
| Curcumin | PEGylated Graphene Oxide Sol-Gel Nanoparticles (SJ-go) | BEAS-2B human bronchial epithelial cells | --- | --- | --- | IC50: 318.86 μg/mL (lower toxicity) | --- | --- | (56) |
| Curcumin | Dual-Encapsulation Hydrogel | VERO CCL-81 epithelial cells | --- | diameter 47 mm | --- | >80% viability (0.2–20 ppm) | 0.29 | 78.33 ± 0.44 | (57) |
| Curcumin | Fe-Cur Coordination Polymer Nanodots (Fe-Cur CPNs) | --- | Target: Corneal tissue | Ultra-small (< 10) | −5.82 | No cytotoxicity observed | --- | --- | (58) |
| Curcumin | MgO/Fe2O3–CS–Cur NC | Normal cells | A549 human lung cancer cells | --- | --- | Low cytotoxicity (biocompatible) | --- | --- | (59) |
| Curcumin | Sodium Alginate/Silica-ZnO Composite Hydrogel Beads (Ss/CMC-ZnO) | biocompatibility confirmed | --- | --- | --- | Good biocompatibility (low hemolysis) | --- | --- | (60) |
| Curcumin | CS/HA/P407@Cyc@Cur Nanosystem | --- | MCF-7 breast cancer | 182.6 ± 10.7 | -30 | Exceptional hemocompatibility (hemolysis <2%) | 90.42–93.09 | 4.17–4.73 | (61) |
| Curcumin | SA/PVP/GO@5-FU | L929 fibroblast cells | HCT-116 colorectal cancer cells | 297 | -39 | 90% cell survival | 46 | 85 | (62) |
| Curcumin | Chios Mastic Gum in PCL nanofibers | HEK293 (human embryonic kidney) | HepG2 (human hepatocarcinoma) | 1.5 μm | --- | Cytotoxicity increases with higher concentration | 3-9 | 85-89 | (63) |
| Curcumin | PEG-functionalized UiO-66 Metal–Organic Framework loaded with Vincristine | --- | MDA-MB-231 (breast), A2780 (ovarian) | 223.5 ± 7.45 | --- | stable | --- | 65.24 ± 1.72 | (64) |
| Curcumin | cGQDs-PEG-curcumin nano-composite | HeLa cell line | HeLa cell line | 60 | -11 | Low toxicity without irradiation | --- | --- | (65) |
| Curcumin | CS-GL/Cu-MOF-CUR-CHR | Human epidermal keratinocytes | --- | 302–380 | --- | > 90% cell survival at 1% and 5% concentration | --- | 99.2 | (66) |
| Curcumin | Nanohydrogel encapsulating Curcumin/Berberine (CUR/BBR) co-crystals | --- | HEC-59 endometrial cancer cells | 637.3 | 35.1 | Minimal toxicity of blank nanohydrogel | --- | 99.68 | (67) |
| Curcumin | Dual-responsive alginate-coated mesoporous silica nanohybrid | --- | HT29 colorectal cancer cells | < 50 | -30.71 ± 0.71 | --- | 20.49 | --- | (68) |
| Curcumin | Mesoporous Silica Nanoparticles with Curcumin–Palladium complex (MSN-AP-PdCur) | --- | Triple-negative breast cancer (TNBC) cells | 144 ± 7 | --- | IC50: 40.2 and 33.6 μM | 50% | 32% | (69) |
| Curcumin | Various curcumin-loaded nanocarriers | Various (e.g., keratinocytes) | Various cancer cells | 40-250 (size varies) | Varied; often negative | Low to moderate toxicity in normal cells | High (varies) | Not always specified | (70) |
| Curcumin | Curcumin-Lignin Nanoparticles (CLLNPs) with Eudragit-L100 film spray | --- | --- | 119.2 ± 2.1 | -21.5 | --- | 97.58 ± 0.67 | High | (71) |
| Curcumin | Chrysin-Piperine loaded chitosan-lecithin nanoparticles (CHR-PIP-LCS-NPs) | HFF (human foreskin fibroblast) | PANC, MCF-7, A2780 | 214.59 | +30.45 | No significant effect on HFF cells (IC50 > 500) | CHR: 79.2, PIP: 90.5 | --- | (72) |
| Curcumin | Ch@Au-MXNSs@Cur | --- | MCF-7 breast cancer cells | (likely ~100-200) | +65 ± 1.65 | Confirmed biocompatibility with low nanotoxicity | High | 88.5 % | (73) |
| Curcumin | Nalidixic acid–Curcumin complex loaded on Cerium Oxide Nanoparticles (Nla/Cn-CNPs) | Vero cells | --- | 45–60 | --- | >90% cell viability at 400 µg/mL | --- | High | (74) |
| Curcumin | LDH-DOX-CUR/Serine-Chitosan (LDH-DOX-CUR/Ser-CS) bio-carriers | L929 normal liver cells | HepG2 liver cancer cells | Not explicitly specified | --- | Biocompatible with selective toxicity | --- | CUR ~83.6% | (75) |

References

1.	Rajabpour M, Pourmadadi M, Yazdian F, Hallajisani A, Fazeli A. Treatment of breast cancer with curcumin-loaded hydrogel nanocomposite containing starch/agarose/zinc oxide. International Journal of Biological Macromolecules. 2025:144492.

2.	Öztekin M, Açıkel YS. Novel pH-Responsive Folic Acid-Conjugated Zein-Carboxymethyl Cellulose Nanoparticles for Enhanced and Controlled Curcumin Release. Journal of Pharmaceutical Innovation. 2025;20(3):89.

3.	Ghaly HSA, Seyedasli N, Varamini P. Enhanced Nanoprecipitation Method for the Production of PLGA Nanoparticles for Oncology Applications. The AAPS Journal. 2025;27(5):1-20.

4.	Fecske D, Kasza G, Gyulai G, Horváti K, Szabó M, Wacha A, et al. Self-Assembling Amphiphilic ABA Triblock Copolymers of Hyperbranched Polyglycerol with Poly (tetrahydrofuran) and Their Nanomicelles as Highly Efficient Solubilization and Delivery Systems of Curcumin. International Journal of Molecular Sciences. 2025;26(12):5866.

5.	Kunde A, Bhatia D. Synthesis of Metal-Organic Framework (MOF) Based Composites for pH-Responsive Drug Delivery. bioRxiv. 2025:2025.06. 18.660385.

6.	Al-Duais MA, El Rabey HA, Mohammed GM, Al-Awthan YS, Althiyabi AS, Attia ES, et al. The anticancer activity of fucoidan coated selenium nanoparticles and curcumin nanoparticles against colorectal cancer lines. Scientific Reports. 2025;15(1):287.

7.	Karimi S, Namazi H. Magnetic LDH coated with DOX and CUR physically Co-loaded onto PEG for targeted and controlled Co-delivery of drugs to liver cancer cells. Journal of Polymers and the Environment. 2025;33(1):269-84.

8.	Kuchta-Gładysz M, Wojciechowska-Puchałka J, Grzesiakowska-Dul A, Kmiecik M, Khachatryan K, Khachatryan G. The In Vitro Toxicity Profile of Nanoencapsulated Curcumin in a Chitosan–Alginate Gel Carrier Using Rabbit Lymphocytes: Preliminary Research. International Journal of Molecular Sciences. 2025;26(17):8577.

9.	Pourmadadi M, Hafezi AR, Yaghoobi R, Rahmaninodeh A, Hosseini N, Alibabaie A, et al. pH-responsive Gelatin/Agarose/Magnesium-doped carbon quantum dot hydrogel nanocomposite for targeted curcumin delivery in brain cancer therapy. Reactive and Functional Polymers. 2025:106403.

10.	Mousavi MS, Pourmadadi M, Abdouss M, Mazinani S, Rahdar A, Fathi-Karkan S, et al. Gelatin/Carboxymethylcellulose Incorporated CNTs Nanocarrier Synthesis Targeted Delivery of Curcumin. BioNanoScience. 2025;15(3):375.

11.	Shabestari SM, Pourmadadi M, Abdouss H, Ghanbari T, Abdouss M, Rahdar A, et al. pH-Responsive Chitosan-Sodium Alginate Nanocarriers for Curcumin Delivery Against Brain Cancer. Colloids and Surfaces B: Biointerfaces. 2025:114875.

12.	Ranjbaran H, Maboudi SA, Moshtaghioun SM, Shojaosadati SA. Evaluation of curcumin (CUR) loaded BSA nanoparticles for in-vitro photodynamic therapy on MCF-7 cell line. Drug Development and Industrial Pharmacy. 2025:1-13.

13.	Jaber SA, Saadh M, Abuhassan Q, Obeid MA. Curcumin-loaded Niosomes Prepared by Microfluidic Mixing; Characterization and Cytotoxicity Evaluation. Journal of Pharmaceutical Innovation. 2025;20(4):125.

14.	Doan VD, Hoang HY, Nguyen TTT, Mai BD, Tran VA, Le VT. The Role of Zinc Doping in Hydroxyapatite-Coated Fe3O4 Nanoparticles for Targeted Curcumin Delivery in Breast Cancer Therapy. Ceramics International. 2025.

15.	Orsu P, CH V. Fabrication and characterization of Curcumin and Piperine loaded CMTG/rGO Electrospun for breast cancer treatment. BioNanoScience. 2025;15(2):260.

16.	Anjar R, Mahadev M, Charyulu RN, Badalamoole V. Development of a novel polyelectrolyte complex nanocomposite of modified chitosan and karaya gum for co-delivery of 5-fluorouracil and curcumin for cancer therapy. Journal of Materials Chemistry B. 2025;13(11):3602-17.

17.	Abaza SF, Elbialy NS, Mohamed N. Binary nanoconjugation of zein–methylcellulose for improving curcumin properties: solubility, controlled release and anticancer activity. Polymer International. 2025;74(2):118-26.

18.	Chatap V, Vanjari P, Bhilare NV. Curcumin loaded magnetic nanocellulose fiber composites with con-a cap for theranostics application in breast cancer. Cellulose. 2025:1-22.

19.	Krishnaveni S, Parvathi K, Ayyanaar DS. Design and Characterization of Ros-Responsive Curcumin Encapsulated Ag@ Lecithin/Polyvinyl Alcohol Nanoparticles for Targeted Drug Delivery Applications. Polyvinyl Alcohol Nanoparticles for Targeted Drug Delivery Applications.

20.	Ghasemzad M, Bakhshandeh H, Naserkhaki R, Ghoytasi I, Shokoohian B, Fotouhi A, et al. Synthesis, characterization and evaluation of linoleic acid-loaded nano-carriers: a novel drug delivery system for efficient treatment of hepatocellular carcinoma. Anti-Cancer Drugs. 2025:10.1097.

21.	Dawwam GE, El-Sayed NS, Al-Shemy MT. Bacterial cellulose doped with ZnO as a multifunctional bioactive platform for curcumin and propolis immobilization: synthesis, characterization, and wound healing potential. Microbial Cell Factories. 2025;24(1):196.

22.	Parsa F, Setoodehkhah M, Atyabi SM. Design, fabrication and characterization of a magnetite-chitosan coated iron-based metal–organic framework (Fe 3 O 4@ chitosan/MIL-100 (Fe)) for efficient curcumin delivery as a magnetic nanocarrier. RSC advances. 2025;15(23):18518-34.

23.	Faezi M, Motavalizadehkakhky A, Tabrizi MH, Dolatabadi S, Es-haghi A. Efficacy of Luteolin-loaded quantum graphene-hyaluronic acid nanocomposites as a drug delivery system against PANC-1 pancreatic cancer cells. Inorganic Chemistry Communications. 2025:115141.

24.	Ji A, Yang P, Ma B, Li J, Yu Y, Zhang X, et al. Photothermal-responsive curcumin-loaded copper-based nanocomposites for targeted drug release and combined immunotherapy. Journal of Colloid and Interface Science. 2025:138042.

25.	Suriya R, Rajeev MR, Lekshmi GS, Anirudhan TS. A novel silver entangled synergistic effect induced dual drug loaded Pluronic-127/Beta-cyclodextrin nano composite hydrophobic carrier for lung cancer therapy. Applied Surface Science. 2025:164310.

26.	Mei J, Li Y, Feng Y, Zhao B, Yang C, Sun Y, et al. Preparation of Stable Zein/Poly (γ‐glutamic acid) Nanocomposite Particles for Improved Encapsulation of Curcumin. Advanced Materials Interfaces. 2025;12(13):2500362.

27.	Sivasankaran LG, Rahim S, Sreenivasan AT. Synthesis and Anticancer Activity Evaluation of Self-assembled Curcumin Loaded Gelatin− Oleic acid–Carboxymethyl Chitosan Nanoparticles on MCF-7 cells. European Journal of Pharmaceutics and Biopharmaceutics. 2025;211:114718.

28.	Gul J, Jabbar A, Perveen S, Awan AN, Shah MR. Development of Folic Acid Functionalized Carbon Nanotubes for Efficient Delivery of Curcumin and Quercetin Against Pathogenic Bacteria. Journal of Cluster Science. 2025;36(1):10.

29.	Qi F, Zhang S, Zhang M, Xu Y, Yu D-G, Chu L, et al. Structure, performance and tissue repair evaluation of biodegradable core-sheath fiber patch loaded with curcumin nano-micelles. Biomaterials Advances. 2025:214432.

30.	Karimi S, Namazi H. Doxorubicin-curcumin-co loaded layered double hydroxide coated with dialdehyde lactose/ZnO via Schiff-base bonding for simultaneous and targeted delivery of drugs to Hepatocellular carcinoma cells. Colloids and Surfaces A: Physicochemical and Engineering Aspects. 2025;715:136628.

31.	Chaudhary A, Behera A, Sahoo J. Design and evaluation of casein nanoparticles for co-delivery of curcumin and fluorouracil acetic acid in cancer therapy. Medical Oncology. 2025;42(8):1-17.

32.	Pourmadadi M, Hafezi AR, Mafirad S, Nouri M, Shirazi M, Younesi M, et al. Development and evaluation of SA/PVP/γ-Al₂O₃ nanocarriers for targeted delivery of curcumin in colon cancer therapy. Journal of Drug Delivery Science and Technology. 2025;105:106632.

33.	Mukhtar A, Aruge S, Tariq A, Tabassam L, Arif S, Haq S, et al. Enhanced Role of Flower Shaped Curcumin Loaded ZnO/Ag2O Nanocomposites for Biological Applications. BioNanoScience. 2025;15(1):11.

34.	Soltani M, Ahmadzadeh N, Rajabi S, Besharati N, Khatamian N, Homayouni Tabrizi M. Efficacy of graphene quantum dot-hyaluronic acid nanocomposites containing quinoline for target therapy against cancer cells. Scientific Reports. 2025;15(1):8494.

35.	Shanmugam S, Ranjith H, Santhanam A. Insights into the potential of polymer-encapsulated ZIF/ZrO₂ nanocomposite with curcumin for Anticancer Therapy. Emergent Materials. 2025:1-17.

36.	Pawar S, Suvarna V. Curcumin-loaded PEG-functionalized carbon nanotubes: a novel strategy for Alzheimer’s management. Therapeutic Delivery. 2025:1-9.

37.	Adams I, Adi-Dako O, Appiah-Opong R, Ofori-Attah E, Aning A, Ofori EK, et al. In Vitro Anticancer Activities of Curcumin‐Loaded Copper Oxide–Halloysite Nanotubes Composite. Journal of Nanotechnology. 2025;2025(1):7535486.

38.	Ramesh S, Heggannavar GB, Kariduraganavar MY, Durgannavar AK. Design and Evaluation of Lactoferrin-Conjugated Cur-M-PCL Nanocarriers for Targeted Glioblastoma Multiforme Therapy. BioNanoScience. 2025;15(3):1-23.

39.	Vijayaraghavan R, Vidyavathi M, Kumar RS, Loganathan S, Valapa RB. 3D bioprinted poly (lactic acid) scaffolds infused with curcumin-loaded nanostructured lipid carriers: a promising approach for skin regeneration. Biomaterials Science. 2025;13(5):1286-303.

40.	Morparia S, Suvarna V. Development and Optimization of Curcumin-Loaded Citric Acid Functionalized Multi-Walled Carbon Nanotubes for Enhanced Breast Cancer Treatment Using Design of Experiment. Journal of Pharmaceutical Innovation. 2025;20(2):35.

41.	Elmergawy FH, Fathy IA, Amer MA, Hamdi S, Ibrahim MS. Evaluation of Amoxicillin loaded Montmorillonite nanocomposite as drug delivery system in dental calcium phosphate bone cement; in vitro study. Journal of Drug Delivery Science and Technology. 2025:107413.

42.	Senthil R. Bevacizumab-conjugated curcumin nanoparticles promote cytotoxicity and apoptosis in human malignant oral keratinocytes in vitro. Journal of Oral and Maxillofacial Surgery. 2025.

43.	Abobaker M, Govender M, Choonara YE. Co-Formulation of Iron Oxide and PLGA Nanoparticles to Deliver Curcumin and IFNα for Synergistic Anticancer Activity in A375 Melanoma Skin Cancer Cells. Pharmaceutics. 2025;17(7):860.

44.	Liang H, Chen F, Shan M, Dai J, Cao L. Structural mechanisms and transmembrane delivery performance of a polyphenol-lysozyme synergistically regulated curcumin nano-delivery system. Journal of Molecular Liquids. 2025:128435.

45.	Nabipour H, Aliakbari F, Volkening K, Strong MJ, Rohani S. Development of metal-organic framework biocomposites from chitosan as drug delivery vehicles: In vitro evaluation on HeLa and SH-SY5Y cell lines. International Journal of Biological Macromolecules. 2025;291:138878.

46.	Slavkova M, Voycheva C, Popova T, Tzankov B, Tzankova D, Spassova I, et al. Ophthalmic In Situ Nanocomposite Gel for Delivery of a Hydrophobic Antioxidant. Gels. 2025;11(2):105.

47.	Afshari M, Pourmadadi M, Shabestari SM, Abdouss H, Abdouss M. Development and Characterization of biocompatible Gelatin/Polyethylene Glycol/Copper-Doped carbon quantum Dots@ Curcumin nanocarriers for pH-Sensitive curcumin delivery in glioblastoma treatment. Inorganic Chemistry Communications. 2025:114782.

48.	Ezzat N, Emadeldien N, Ali MK, Fahd S, Shebl S, Elshishiny M, et al. In vitro evaluation of zinc oxide-metformin folic acid nanocomposite as a targeted drug delivery system for cancer therapy. Asian Pacific Journal of Cancer Prevention: APJCP. 2025;26(2):443.

49.	Bibi A, Azmat A, Zafar S. Green-synthesized cyclophosphamide-loaded magnetite nanocomposites for in vitro anti-cancer activity against U-87 glioblastoma cells. Results in Chemistry. 2025:102513.

50.	Bhalla V, Sahu CP, Shashikala A, Singh S, Thangavelu I, Tadepalli S, et al. Synthesis and Multifunctional Evaluation of BaO₂-Sodium Alginate-Curcumin Nanocomposite: Improved Antibacterial, Antioxidant, and Osteosarcoma Cell Inhibition. Journal of Inorganic and Organometallic Polymers and Materials. 2025:1-20.

51.	Nikwade V, Choudhary N, Solanki R, Patel A, Yadav VK, Salmen SH, et al. Fabrication and characterization of ConA-conjugated curcumin-loaded solid lipid nanoparticles for theranostic applications in lung cancer treatment. Nanoscale. 2025;17(6):3203-10.

52.	Bashir S, Iram G, Rafique S, Bashir M, Ghani T, Tanveer A, et al. Encapsulation of Moringa oleifera aqueous extract in silver chitosan metallopolymer nanocomposites for anti-cancer activity. International Journal of Biological Macromolecules. 2025;297:139683.

53.	Zahid A, Khurshid A, Rehman SU, Hassan SMU, Akhtar R. Enhanced intracellular delivery of curcumin using polymeric nanocarriers: a natural photosensitizing agent for anti-cancer photodynamic therapy. Journal of Fluorescence. 2025:1-13.

54.	Kumar G, Ruivinho B, Virmani T, Brandão P, Choudhary P, Kumar Chouhan N, et al. Unlocking the full potential of piperine-loaded nanocarriers for cancer treatment. Therapeutic Delivery. 2025:1-21.

55.	Ghadami A, Pourmadadi M, Yazdian F, Kazemi A, Mirshafiei M, Bastami SH. Chitosan/Carbon Quantum Dots/Polyvinylpyrrolidone Nanocarrier for Enhanced Anticancer Efficacy of Doxorubicin. Carbohydrate Polymer Technologies and Applications. 2025:100883.

56.	Cagil EM, Ozcan F, Korucu EN, Kuvvet KY, Menevse E. Curcumin and quercetin modulate oxidative stress and inflammation of healthy lung cells treated with sol-gel graphene oxide nanoparticles. Biochemical and Biophysical Research Communications. 2025:152584.

57.	Herrera-Alonso AE, Rodríguez-Chávez DF, Toxqui-Terán A, Rubio-Valle JF, Martín-Alfonso JE, Longoria-García S, et al. pH-Sensitive Chitosan-Based Hydrogels Trap Poloxamer Micelles as a Dual-Encapsulating Responsive System for the Loading and Delivery of Curcumin. Polymers. 2025;17(10):1335.

58.	Huo Y, Song L, Han Z, Yang Y, Wang T, Chen Z, et al. Efficacy and safety of Fe-curcumin coordination polymer nanodots to prevent corneal neovascularization in alkali burn models. Journal of Nanobiotechnology. 2025;23(1):518.

59.	Elmetwalli A, Abdelsayed S, Elsayed A, El-Hersh MS, Hassan MG, Gad LA, et al. Next-generation nanoformulation: Glycyrrhiza glabra-based chitosan–curcumin MgO/Fe2O3 nanocomposite for targeted lung cancer therapy with dual antioxidant action. Medical Oncology. 2025;42(9):1-27.

60.	Zhang X, Xiao Y, Guo S, Wang H, Gao X, Niu B, et al. pH-sensitive zinc oxide nanoparticle-controlled sodium alginate/silica hydrogel beads: For controlled curcumin release. Journal of Molecular Structure. 2025;1324:140967.

61.	Nguyen TD, Tran TT, Pham SH, Dang TT. Dual Anticancer and Antimicrobial Activity of A Novel Dual-Drug Nanosystem for Co-Delivery of Curcumin and Cyclotides Derived from Viola Dalatensis Gagnep. Journal of Cluster Science. 2025;36(5):166.

62.	Pourmadadi M, Ajalli N, Nouri M, Shirazi M, Hashemipour M, Hosseini N, et al. Enhanced Drug Delivery of 5-Fluorouracil Using a GO-PVP-SA Nanocomposite for Targeted Colorectal Cancer Treatment. BioNanoScience. 2025;15(1):194.

63.	Mastorakis PM, Marras SI, Tsioptsias C, Zaoutsos SP, Leonidas DD, Tsivintzelis I, et al. Novel Bio-Functional Electrospun Membranes by Chios Mastic Gum Encapsulation. Fibers. 2025;13(9):116.

64.	Sadeghi Jam Z, Tafvizi F, Khodarahmi P, Jafari P, Baghbani-Arani F. PEG-functionalized UiO-66 MOFs for targeted vincristine delivery: enhanced cytotoxicity in breast and ovarian cancer cell lines. Cancer Nanotechnology. 2025;16(1):10.

65.	Dilenko H, Tománková KB, Hinde E, Válková L, Kolaříková M, Kolářová H. Illuminating the dark: PEGylated carboxylated graphene quantum dots and curcumin in nucleolar activity and PDT-induced DNA damage in cancer. Biomedicine & Pharmacotherapy. 2025;187:118096.

66.	Yeoh SG, Liew YK, Lim WM, Rahman NA, Then YY. The Preparation and Characterization of Electrospun Chitosan-Gelatin Nanofibers Containing Copper–Metal–Organic Frameworks Loaded with Curcumin and Chrysin as Antibacterial Wound Dressings. ACS omega. 2025.

67.	Yan F, Wang Y, Chen L, Cheng W, Oduro‐Kwateng E, Soliman ME, et al. Nanohydrogel of Curcumin/Berberine Co‐Crystals Induces Apoptosis via Dual Covalent/Noncovalent Inhibition of Caspases in Endometrial Cancer Cell Lines: The Synergy Between Pharmacokinetics and Pharmacodynamics. Journal of Molecular Recognition. 2025;38(2):e70004.

68.	Alallam B, Abdkadir E, Hayati A, Keong YY, Lim V. Alginate coated mesoporous silica nanoparticles as oral delivery carrier of curcumin and quercetin to colon cancer: preparation, optimization, characterization, and anticancer activity. Drug Delivery and Translational Research. 2025:1-42.

69.	Nayila I, Sharif S, Zaheer S. A COMPREHENSIVE REVIEW ON THE THERAPEUTIC EFFICACY OF CURCUMIN AND ITS NANOFORMULATIONS: Bioactive role of curcumin in diseases prevention. BIOTROPIA. 2025;32(2):266-76.

70.	Najafi M, Omidi MH, Hajebi S, Khoddam Z, Chamanara M, Ramezanpour S, et al. Synthesis and Characterization of pH-Responsive Sodium Alginate/Zein/γ-Alumina Nanocarriers for Targeted Curcumin Delivery in Lung Cancer. Nano LIFE. 2026;16(03):2550004.

71.	Goyal M, Batra N, Vishkarma H, Siddiqui L, Mittal S, Sharma G, et al. QbD-optimized curcumin-lignin nanoparticle spray for targeted wound infection therapy against Escherichia coli and Mycobacterium smegmatis. Journal of Biomaterials Science, Polymer Edition. 2025:1-33.

72.	Pourali P, Alowaidi JSA, Beyramabdi P, Hosseini Torshiz G, Taslim T, Ghahramani S, et al. Synergistic anticancer, inflammatory, and antioxidant effect of piperine and chrysin combination loaded on lipid-polymer hybrid nanoparticles. Polymer Bulletin. 2025:1-24.

73.	Elbialy NS, Salam MA, Mohamed N. Chitosan-MXene-gold-curcumin: quaternary nanohybrid platform: A Chemo/Photothermal onco-strategy for improved cancer therapy. Carbohydrate Polymer Technologies and Applications. 2025;10:100795.

74.	Man Y, Xie Z. Smart Delivery of Nalidixic Acid–Curcumin Complex Via Cerium Oxide Nanoparticles for Urinary Tract Infection and its Management. Journal of Cluster Science. 2025;36(5):167.

75.	Karimi S, Namazi H, Aghazadeh M. Simultaneous Release of Hydrophilic and Hydrophobic Drugs by a pH-sensitive Bio-carrier Based on Layered Double Hydroxides Decorated with l-serine-chitosan. Journal of Polymers and the Environment. 2025:1-18.