Supplementary Information S1

Kinetic, Equilibrium, and Thermodynamic Study of Methylene Blue Adsorption on Orange Peel Biochar Prepared by Microwave-Assisted Pyrolysis

Jhonny Correa-Abrila, Elvia V. Cabreraa, Nilo Roblesa,b, J. L. López Terána, and Ullrich Stahla,*

a Universidad Central del Ecuador, Facultad de Ingeniería Química, Grupo de Investigación en Alimentos, Compuestos Orgánicos, Materiales, Microbiología aplicada, y Energía - ACMME. Enrique Ritter s/n y Bolivia, Quito, Ecuador.

b Instituto de Investigación Geológico y Energético - IIGE, Quito EC-170518, Ecuador.

*  Correspondence: ustahl@uce.edu.ec

Highlights:

• Pristine biochar from orange peel waste is an effective adsorbent for Methylene Blue.

• pH control is critical: constant pH 4 yields a qmax of 25.57 mg g⁻¹, more than double that of the unregulated system (11.24 mg g⁻¹).

• High Methylene Blue removal (83 %) occurs at pH 4, despite electrostatic repulsion with the positively charged biochar surface (pHpzc = 11.20).

• The adsorption process is spontaneous, endothermic (ΔH° > 0), and dominated by physisorption mechanisms like hydrogen bonding and π-π interactions.

• The Elovich kinetic model provides the best fit (R² > 0.99), confirming a complex adsorption process on a heterogeneous surface.

- Figures:

Figure S1. Resonance structures of the MB cation.

Figure S2. The schematic diagram of the microwave-assisted pyrolysis apparatus

Figure S3. Schematic of the synthesis process of BC-OP via MAP, characterization, and adsorption study of MB on BC-OP.)

Figure S4. Pore size distribution evaluation of BC-OP with PoreVision software1.

Figure S5. Determination of the pHpzc value for BC-OP.

Figure S6. Determination of ZP at pH 9.

Figure S7. Schematic illustrating the Boehm titration principle of selective neutralization of oxygen functional groups according to their acidity using multiple bases 2.

Figure S8. Residual plots of the kinetic adsorption model of MB on BC-OP under controlled (constant pH 4) and unregulated conditions.

Figure S9. Residual plots of the adsorption isotherm of MB on BC-OP under controlled (constant pH 4) and unregulated conditions.

Figure S10. Residual plots of the adsorption isotherm of MB on BC-OP at 293 K under controlled (constant pH 4) and unregulated conditions.

Figure S11. Residual plots of the adsorption isotherm of MB on BC-OP at 308 K under controlled (constant pH 4) and unregulated conditions.

Figure S12. Residual plots of the adsorption isotherm of MB on BC-OP at 323 K under controlled (constant pH 4) and unregulated conditions.

- TABLES

Table S1. Production yield of BC-OP

| Yield MAP (%) |  |  |  |
| --- | --- | --- | --- |
| # | OP (g) | BC-OP (g) | Yield (%) |
| 1 | 40.002 | 8.948 | 22.369 |
| 2 | 40.162 | 9.043 | 22.516 |
| 3 | 42.618 | 9.520 | 22.338 |
| 4 | 42.108 | 9.168 | 21.773 |
| 5 | 43.004 | 9.272 | 22.561 |
| 6 | 40.747 | 8.921 | 22.894 |
| 7 | 41.415 | 9.324 | 22.514 |
| 8 | 42.354 | 8.944 | 22.317 |
| 9 | 42.285 | 9.402 | 22.235 |
| 10 | 40.347 | 9.004 | 22.316 |
| 11 | 40.471 | 8.751 | 22.223 |
| 12 | 40.137 | 8.796 | 21.915 |
|  |  | Average | 22.331 |
|  |  | SD | 2.931 |

Table S2. Electrical conductivity of BC-OP.

| EC (mS cm-1) |  |
| --- | --- |
| 1 | 4.40 |
| 2 | 4.42 |
| 3 | 4.32 |
| Average | 4.38 |
| SD | 0.05 |

Table S3. Effect of pH on the removal of MB in BC-OP.

| Effect of solution pH |  |  |
| --- | --- | --- |
| pH | %R | SD |
| 2 | 61.643 | 3.544 |
| 4 | 82.703 | 3.872 |
| 6 | 70.223 | 4.444 |
| 8 | 71.091 | 0.223 |
| 10 | 72.798 | 4.712 |

Table S4. Effect of adsorbent dosage on the removal of MB in BC-OP under controlled (constant pH 4) and unregulated conditions.

| DOSAGE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| CONSTANT | Adsorbent dosage (g 100 mL-1) | Removal MB (%) | SD | qe (mg g-1) | SD |
|  | 0.5 | 94.730 | 1.248 | 9.429 | 0.118 |
|  | 1.0 | 98.185 | 0.671 | 4.790 | 0.038 |
|  | 1.5 | 99.563 | 0.670 | 3.317 | 0.022 |
|  | 2.0 | 99.564 | 0.747 | 2.398 | 0.011 |
|  | 3.0 | 99.563 | 0.363 | 1.638 | 0.016 |
| UN REGULATED | Adsorbent dosage (g 100 mL-1) | Removal MB (%) | SD | qe (mg g-1) | SD |
|  | 0.5 | 62.035 | 0.465 | 8.728 | 0.020 |
|  | 1.0 | 66.281 | 1.285 | 4.155 | 0.030 |
|  | 1.5 | 70.510 | 0.834 | 2.842 | 0.014 |
|  | 2.0 | 82.226 | 0.643 | 2.277 | 0.007 |
|  | 3.0 | 83.113 | 2.312 | 1.525 | 0.018 |

Table S5. Effect of contact time on the removal of MB in BC-OP under controlled (constant pH 4) and unregulated conditions.

| KINETICS |  |  |  |
| --- | --- | --- | --- |
| CONSTANT | Time (min) | qt (mg g-1) | SD |
|  | 15 | 6.908 | 0.055 |
|  | 30 | 7.430 | 0.470 |
|  | 60 | 7.760 | 0.001 |
|  | 120 | 7.911 | 0.001 |
|  | 180 | 9.173 | 0.000 |
| UN REGULATED | Time (min) | qt (mg g-1) | SD |
|  | 15 | 3.523 | 0.172 |
|  | 30 | 3.884 | 0.201 |
|  | 60 | 3.989 | 0.000 |
|  | 120 | 4.304 | 0.000 |
|  | 180 | 4.546 | 0.113 |

Table S6. Study of the effect of the initial adsorbate concentration at 293 K on the removal of MB in BC-OP under controlled (constant pH 4) and unregulated conditions.

| INITIAL CONCENTRATION AT 293 K |  |  |  |  |
| --- | --- | --- | --- | --- |
| CONSTANT | C0 (mg L-1) | Ce (mg L-1) | qe (mg g-1) | SD |
|  | 50 | 5.621 | 2.214 | 0.022 |
|  | 100 | 21.363 | 3.924 | 0.320 |
|  | 200 | 40.901 | 7.939 | 0.095 |
|  | 300 | 86.227 | 10.667 | 0.038 |
|  | 500 | 197.604 | 15.089 | 0.688 |
| UN REGULATED | C0 (mg L-1) | Ce (mg L-1) | qe (mg g-1) | SD |
|  | 50 | 1.842 | 1.203 | 0.015 |
|  | 100 | 2.910 | 2.425 | 0.001 |
|  | 200 | 21.721 | 4.453 | 0.055 |
|  | 300 | 49.397 | 6.378 | 0.000 |
|  | 500 | 121.534 | 9.052 | 0.000 |

Table S7. Study of the effect of the initial adsorbate concentration at 308 K on the removal of MB in BC-OP under controlled (constant pH 4) and unregulated conditions.

| INITIAL CONCENTRATION AT 308 K |  |  |  |  |
| --- | --- | --- | --- | --- |
| CONSTANT | C0 (mg L-1) | Ce (mg L-1) | qe (mg g-1) | SD |
|  | 50 | 5.769 | 2.207 | 0.038 |
|  | 100 | 7.243 | 4.629 | 0.022 |
|  | 200 | 10.457 | 9.458 | 0.030 |
|  | 300 | 11.281 | 14.407 | 0.094 |
|  | 500 | 50.138 | 22.448 | 2.294 |
| UN REGULATED | C0 (mg L-1) | Ce (mg L-1) | qe (mg g-1) | SD |
|  | 50 | 4.464 | 1.137 | 0.015 |
|  | 100 | 5.933 | 2.349 | 0.026 |
|  | 200 | 45.789 | 3.851 | 0.403 |
|  | 300 | 57.107 | 6.067 | 0.067 |
|  | 500 | 125.369 | 9.356 | 0.159 |

Table S8. Study of the effect of the initial adsorbate concentration at 323 K on the removal of MB in BC-OP under controlled (constant pH 4) and unregulated conditions.

| INITIAL CONCENTRATION AT 323 K |  |  |  |  |
| --- | --- | --- | --- | --- |
| CONSTANT | C0 (mg L-1) | Ce (mg L-1) | qe (mg g-1) | SD |
|  | 50 | 4.606 | 2.265 | 0.040 |
|  | 100 | 4.427 | 4.769 | 0.029 |
|  | 200 | 7.180 | 9.622 | 0.150 |
|  | 300 | 6.996 | 14.621 | 0.057 |
|  | 500 | 29.528 | 23.477 | 0.568 |
| UN REGULATED | C0 (mg L-1) | Ce (mg L-1) | qe (mg g-1) | SD |
|  | 50 | 5.875 | 1.102 | 0.001 |
|  | 100 | 7.428 | 2.312 | 0.002 |
|  | 200 | 20.333 | 4.487 | 0.001 |
|  | 300 | 30.596 | 6.728 | 0.000 |
|  | 500 | 105.684 | 9.848 | 0.003 |

References

1.	Olevsky, L. M., Jacques, M. G. & Hixon, K. R. PoreVision: A Program for Enhancing Efficiency and Accuracy in SEM Pore Analyses of Gels and Other Porous Materials. Gels 11, 132 (2025).

2. Sen, T. K. Adsorptive Removal of Dye (Methylene Blue) Organic Pollutant from Water by Pine Tree Leaf Biomass Adsorbent. Processes, 11(7), 1877 (2023).