Supplementary Table 1
Point-of-breakage analysis showing the percentage of suture failures occurring away from the knot across groups, media, and time intervals.
	Group
	Medium
	Day 1
	Day 3
	Day 7
	Day 14

	A (PGA 3-0)
	Dipotassium Glycyrrhizinate
	40% away
	100% knot
	20% away
	100% knot

	A (PGA 3-0)
	Propolis
	100% knot
	20% slippage
	100% knot
	100% knot

	A (PGA 3-0)
	Artificial Saliva
	20% away
	100% knot
	100% knot
	100% knot

	B (PGA 4-0)
	Dipotassium Glycyrrhizinate
	20% away
	100% knot
	100% knot
	100% knot

	B (PGA 4-0)
	Propolis
	100% knot
	20% slippage
	100% knot
	40% slippage

	B (PGA 4-0)
	1:1 Mixture
	100% knot
	100% knot
	100% knot
	40% away

	B (PGA 4-0)
	Artificial Saliva
	100% knot
	100% knot
	100% knot
	20% near knot

	B (PGA 4-0)
	Chlorhexidine
	20% near/far
	100% knot
	100% knot
	100% knot

	C (PGCL 3-0)
	Dipotassium Glycyrrhizinate
	20% near / 40% far
	80% slippage
	60% far
	20% slippage

	C (PGCL 3-0)
	Propolis
	20% far
	60% slippage + 20% far
	40% far
	20% slippage

	C (PGCL 3-0)
	1:1 Mixture
	20% far
	40% far
	20% near + 20% far
	20% near + 40% far

	C (PGCL 3-0)
	Artificial Saliva
	100% knot
	100% knot
	20% slippage + 40% far
	20% slippage + 60% far

	C (PGCL 3-0)
	Chlorhexidine
	40% near
	20% near/far/slippage
	100% knot
	100% knot

	D (PGCL 4-0)
	Dipotassium Glycyrrhizinate
	20% far
	20% slippage
	20% far
	100% knot

	D (PGCL 4-0)
	Propolis
	20% far
	20% slippage
	40% near
	100% knot

	D (PGCL 4-0)
	1:1 Mixture
	20% far
	100% knot
	20% near
	100% knot

	D (PGCL 4-0)
	Artificial Saliva
	20% far
	20% far
	40% far
	100% knot



