[bookmark: _GoBack]Table S1: UV-vis spectra of the synthesized silver nanoparticle sample at 1:2, 1:4, 1:6, and 1:10 ratios at 30 min. Here, 1:2 ratios produce the highest concentration and size of Ag NPs, represents raw data of Table 4A.
	SPR Wavelength (nm)
	Absorbance at 1:2 (30 min)
	Absorbance at 1:4 (30 min)
	Absorbance at 1:6 (30 min)
	Absorbance at 1:10 (30 min)

	325
	0.359
	0.243
	0.174
	0.108

	326
	0.371
	0.241
	0.161
	0.096

	327
	0.384
	0.231
	0.156
	0.097

	328
	0.41
	0.233
	0.163
	0.113

	329
	0.429
	0.251
	0.187
	0.147

	330
	0.456
	0.268
	0.218
	0.165

	331
	0.464
	0.297
	0.24
	0.192

	332
	0.483
	0.312
	0.269
	0.206

	333
	0.493
	0.34
	0.285
	0.222

	334
	0.501
	0.352
	0.302
	0.229

	335
	0.508
	0.373
	0.315
	0.239

	336
	0.516
	0.384
	0.327
	0.248

	337
	0.523
	0.407
	0.335
	0.258

	338
	0.528
	0.413
	0.341
	0.267

	339
	0.533
	0.415
	0.348
	0.278

	340
	0.537
	0.423
	0.357
	0.288

	341
	0.548
	0.426
	0.363
	0.298

	342
	0.547
	0.429
	0.373
	0.311

	343
	0.558
	0.429
	0.379
	0.322

	344
	0.552
	0.429
	0.386
	0.33

	345
	0.555
	0.429
	0.392
	0.342

	346
	0.552
	0.429
	0.397
	0.348

	347
	0.549
	0.428
	0.403
	0.361

	348
	0.548
	0.429
	0.409
	0.37

	349
	0.538
	0.426
	0.415
	0.376

	350
	0.53
	0.427
	0.419
	0.387

	351
	0.52
	0.425
	0.426
	0.393

	352
	0.51
	0.424
	0.429
	0.401

	353
	0.503
	0.423
	0.435
	0.407

	354
	0.493
	0.424
	0.44
	0.415

	355
	0.484
	0.424
	0.445
	0.424

	356
	0.476
	0.424
	0.449
	0.43

	357
	0.466
	0.422
	0.452
	0.437

	358
	0.461
	0.426
	0.459
	0.443

	359
	0.454
	0.424
	0.462
	0.45

	360
	0.47
	0.452
	0.473
	0.465

	361
	0.466
	0.454
	0.478
	0.472

	362
	0.462
	0.455
	0.484
	0.479

	363
	0.459
	0.458
	0.49
	0.486

	364
	0.456
	0.461
	0.495
	0.494

	365
	0.454
	0.464
	0.502
	0.502

	366
	0.453
	0.467
	0.508
	0.509

	367
	0.452
	0.47
	0.514
	0.517

	368
	0.451
	0.473
	0.52
	0.524

	369
	0.452
	0.477
	0.526
	0.532

	370
	0.452
	0.481
	0.533
	0.539

	371
	0.453
	0.485
	0.539
	0.547

	372
	0.455
	0.489
	0.545
	0.554

	373
	0.456
	0.493
	0.551
	0.561

	374
	0.458
	0.498
	0.557
	0.569

	375
	0.46
	0.502
	0.564
	0.576

	376
	0.462
	0.506
	0.569
	0.583

	377
	0.464
	0.51
	0.576
	0.589

	378
	0.466
	0.514
	0.581
	0.596

	379
	0.468
	0.519
	0.587
	0.603

	380
	0.47
	0.522
	0.592
	0.609

	381
	0.473
	0.526
	0.597
	0.615

	382
	0.475
	0.529
	0.602
	0.62

	383
	0.477
	0.533
	0.607
	0.626

	384
	0.479
	0.536
	0.612
	0.631

	385
	0.481
	0.539
	0.616
	0.637

	386
	0.482
	0.542
	0.62
	0.641

	387
	0.484
	0.545
	0.624
	0.646

	388
	0.486
	0.548
	0.628
	0.651

	389
	0.488
	0.551
	0.631
	0.656

	390
	0.489
	0.554
	0.635
	0.66

	391
	0.491
	0.556
	0.638
	0.665

	392
	0.492
	0.559
	0.641
	0.669

	393
	0.493
	0.561
	0.644
	0.673

	394
	0.494
	0.563
	0.647
	0.676

	395
	0.496
	0.566
	0.65
	0.68

	396
	0.497
	0.568
	0.653
	0.684

	397
	0.498
	0.57
	0.656
	0.688

	398
	0.499
	0.572
	0.659
	0.691

	399
	0.5
	0.574
	0.661
	0.694

	400
	0.501
	0.576
	0.664
	0.698

	401
	0.502
	0.579
	0.667
	0.701

	402
	0.503
	0.581
	0.67
	0.705

	403
	0.504
	0.583
	0.672
	0.708

	404
	0.505
	0.585
	0.675
	0.711

	405
	0.505
	0.587
	0.678
	0.715

	406
	0.506
	0.589
	0.68
	0.717

	407
	0.507
	0.591
	0.683
	0.72

	408
	0.508
	0.593
	0.685
	0.723

	409
	0.509
	0.595
	0.687
	0.726

	410
	0.509
	0.597
	0.69
	0.729

	411
	0.51
	0.599
	0.693
	0.732

	412
	0.511
	0.601
	0.695
	0.735

	413
	0.512
	0.603
	0.698
	0.738

	414
	0.512
	0.605
	0.7
	0.741

	415
	0.513
	0.607
	0.703
	0.743

	416
	0.514
	0.609
	0.705
	0.746

	417
	0.515
	0.612
	0.708
	0.749

	418
	0.515
	0.613
	0.711
	0.752

	419
	0.516
	0.615
	0.714
	0.755

	420
	0.542
	0.656
	0.765
	0.805

	421
	0.543
	0.658
	0.768
	0.808

	422
	0.544
	0.66
	0.771
	0.811

	423
	0.544
	0.663
	0.774
	0.814

	424
	0.545
	0.665
	0.777
	0.817

	425
	0.546
	0.667
	0.78
	0.82

	426
	0.546
	0.669
	0.783
	0.823

	427
	0.547
	0.672
	0.786
	0.826

	428
	0.548
	0.674
	0.789
	0.829

	429
	0.548
	0.676
	0.792
	0.831

	430
	0.549
	0.677
	0.794
	0.834

	431
	0.549
	0.68
	0.797
	0.836

	432
	0.55
	0.681
	0.8
	0.839

	433
	0.55
	0.683
	0.802
	0.841

	434
	0.55
	0.686
	0.806
	0.844

	435
	0.551
	0.688
	0.808
	0.846

	436
	0.551
	0.69
	0.81
	0.848

	437
	0.551
	0.691
	0.813
	0.85

	438
	0.551
	0.693
	0.815
	0.852

	439
	0.551
	0.694
	0.817
	0.853

	440
	0.551
	0.696
	0.819
	0.855

	441
	0.551
	0.697
	0.822
	0.856

	442
	0.551
	0.699
	0.823
	0.857

	443
	0.55
	0.7
	0.825
	0.858

	444
	0.55
	0.702
	0.827
	0.86

	445
	0.55
	0.703
	0.829
	0.861

	446
	0.55
	0.704
	0.831
	0.862

	447
	0.549
	0.706
	0.833
	0.863

	448
	0.549
	0.707
	0.835
	0.864

	449
	0.549
	0.708
	0.837
	0.864

	450
	0.548
	0.709
	0.838
	0.865

	451
	0.548
	0.71
	0.84
	0.866

	452
	0.548
	0.711
	0.842
	0.866

	453
	0.547
	0.712
	0.843
	0.866

	454
	0.546
	0.713
	0.845
	0.867

	455
	0.546
	0.714
	0.846
	0.867

	456
	0.545
	0.715
	0.848
	0.867

	457
	0.545
	0.715
	0.849
	0.867

	458
	0.544
	0.716
	0.85
	0.867

	459
	0.543
	0.717
	0.852
	0.867

	460
	0.543
	0.718
	0.853
	0.868

	461
	0.542
	0.718
	0.854
	0.868

	462
	0.542
	0.719
	0.856
	0.868

	463
	0.541
	0.72
	0.857
	0.867

	464
	0.54
	0.72
	0.858
	0.867

	465
	0.54
	0.721
	0.859
	0.867

	466
	0.539
	0.721
	0.86
	0.867

	467
	0.538
	0.722
	0.861
	0.867

	468
	0.537
	0.722
	0.862
	0.866

	469
	0.536
	0.722
	0.863
	0.866

	470
	0.536
	0.722
	0.864
	0.865

	471
	0.535
	0.723
	0.865
	0.865

	472
	0.534
	0.723
	0.865
	0.864

	473
	0.533
	0.723
	0.866
	0.863

	474
	0.532
	0.723
	0.866
	0.863

	475
	0.531
	0.723
	0.867
	0.862

	476
	0.53
	0.722
	0.867
	0.861

	477
	0.529
	0.722
	0.867
	0.86

	478
	0.528
	0.722
	0.867
	0.859

	479
	0.527
	0.722
	0.868
	0.858

	480
	0.526
	0.721
	0.868
	0.856

	481
	0.524
	0.721
	0.868
	0.855

	482
	0.523
	0.72
	0.868
	0.854

	483
	0.522
	0.72
	0.868
	0.853

	484
	0.52
	0.719
	0.867
	0.851

	485
	0.519
	0.719
	0.867
	0.85

	486
	0.518
	0.718
	0.867
	0.848

	487
	0.516
	0.717
	0.867
	0.847

	488
	0.515
	0.716
	0.866
	0.845

	489
	0.513
	0.716
	0.865
	0.843

	490
	0.512
	0.715
	0.865
	0.842

	491
	0.51
	0.714
	0.864
	0.84

	492
	0.508
	0.713
	0.863
	0.838

	493
	0.507
	0.712
	0.863
	0.836

	494
	0.505
	0.711
	0.862
	0.834

	495
	0.503
	0.71
	0.861
	0.832

	496
	0.501
	0.708
	0.859
	0.83

	497
	0.499
	0.707
	0.858
	0.827

	498
	0.498
	0.706
	0.857
	0.826

	499
	0.496
	0.704
	0.856
	0.823

	500
	0.471
	0.666
	0.805
	0.773

	501
	0.47
	0.664
	0.804
	0.771

	502
	0.468
	0.663
	0.802
	0.769

	503
	0.465
	0.661
	0.8
	0.766

	504
	0.463
	0.66
	0.799
	0.764

	505
	0.461
	0.658
	0.797
	0.761

	506
	0.459
	0.656
	0.795
	0.759

	507
	0.457
	0.654
	0.793
	0.756

	508
	0.455
	0.652
	0.791
	0.753

	509
	0.453
	0.65
	0.789
	0.75

	510
	0.45
	0.648
	0.787
	0.747

	511
	0.448
	0.646
	0.784
	0.744

	512
	0.446
	0.644
	0.782
	0.741

	513
	0.443
	0.642
	0.78
	0.738

	514
	0.441
	0.639
	0.777
	0.735

	515
	0.438
	0.636
	0.774
	0.732

	516
	0.435
	0.633
	0.771
	0.728

	517
	0.433
	0.631
	0.768
	0.724

	518
	0.431
	0.628
	0.765
	0.721

	519
	0.428
	0.625
	0.761
	0.717

	520
	0.425
	0.622
	0.758
	0.713

	521
	0.422
	0.619
	0.755
	0.71

	522
	0.42
	0.616
	0.751
	0.706

	523
	0.417
	0.612
	0.748
	0.702

	524
	0.415
	0.609
	0.744
	0.699

	525
	0.412
	0.606
	0.741
	0.695

	526
	0.409
	0.602
	0.737
	0.691

	527
	0.406
	0.598
	0.733
	0.687

	528
	0.403
	0.595
	0.729
	0.683

	529
	0.401
	0.591
	0.725
	0.679

	530
	0.397
	0.587
	0.72
	0.674

	531
	0.394
	0.583
	0.716
	0.67

	532
	0.391
	0.579
	0.711
	0.666

	533
	0.388
	0.575
	0.707
	0.662

	534
	0.385
	0.57
	0.702
	0.657

	535
	0.382
	0.566
	0.697
	0.653

	536
	0.379
	0.561
	0.692
	0.648

	537
	0.376
	0.557
	0.687
	0.643

	538
	0.373
	0.552
	0.682
	0.638

	539
	0.37
	0.548
	0.677
	0.634

	540
	0.366
	0.543
	0.672
	0.629

	541
	0.364
	0.539
	0.668
	0.625

	542
	0.361
	0.534
	0.663
	0.62

	543
	0.358
	0.53
	0.658
	0.616

	544
	0.355
	0.525
	0.653
	0.611

	545
	0.352
	0.521
	0.648
	0.607

	546
	0.349
	0.516
	0.643
	0.602

	547
	0.346
	0.511
	0.638
	0.597

	548
	0.343
	0.506
	0.633
	0.593

	549
	0.34
	0.501
	0.627
	0.588

	550
	0.337
	0.497
	0.623
	0.583

	551
	0.334
	0.492
	0.617
	0.579

	552
	0.331
	0.487
	0.612
	0.574

	553
	0.328
	0.482
	0.606
	0.569

	554
	0.325
	0.477
	0.601
	0.564

	555
	0.322
	0.472
	0.596
	0.559

	556
	0.319
	0.467
	0.59
	0.554

	557
	0.316
	0.462
	0.585
	0.55

	558
	0.313
	0.457
	0.579
	0.545

	559
	0.31
	0.452
	0.574
	0.54

	560
	0.308
	0.447
	0.568
	0.535

	561
	0.305
	0.442
	0.563
	0.53

	562
	0.302
	0.437
	0.558
	0.525

	563
	0.299
	0.432
	0.552
	0.52

	564
	0.296
	0.427
	0.547
	0.515

	565
	0.294
	0.422
	0.542
	0.511

	566
	0.291
	0.417
	0.537
	0.506

	567
	0.289
	0.413
	0.532
	0.501

	568
	0.286
	0.408
	0.526
	0.497

	569
	0.283
	0.403
	0.52
	0.491

	570
	0.28
	0.398
	0.515
	0.486

	571
	0.278
	0.393
	0.51
	0.481

	572
	0.275
	0.388
	0.504
	0.476

	573
	0.273
	0.383
	0.499
	0.471

	574
	0.27
	0.378
	0.493
	0.467

	575
	0.267
	0.373
	0.488
	0.461

	576
	0.265
	0.369
	0.483
	0.456

	577
	0.262
	0.364
	0.477
	0.451

	578
	0.26
	0.359
	0.472
	0.447

	579
	0.257
	0.355
	0.467
	0.442

	580
	0.255
	0.35
	0.461
	0.437

	581
	0.253
	0.345
	0.457
	0.432

	582
	0.25
	0.341
	0.452
	0.427

	583
	0.248
	0.336
	0.446
	0.423

	584
	0.246
	0.332
	0.442
	0.418

	585
	0.244
	0.328
	0.437
	0.413

	586
	0.241
	0.323
	0.432
	0.409

	587
	0.239
	0.319
	0.427
	0.404

	588
	0.237
	0.315
	0.422
	0.4

	589
	0.235
	0.311
	0.417
	0.395

	590
	0.233
	0.307
	0.413
	0.391

	591
	0.231
	0.303
	0.408
	0.386

	592
	0.229
	0.298
	0.403
	0.382

	593
	0.227
	0.294
	0.399
	0.378

	594
	0.224
	0.29
	0.394
	0.373

	595
	0.222
	0.287
	0.389
	0.369

	596
	0.22
	0.282
	0.385
	0.364

	597
	0.218
	0.278
	0.38
	0.36

	598
	0.216
	0.274
	0.375
	0.355

	599
	0.214
	0.271
	0.371
	0.351

	600
	0.212
	0.267
	0.366
	0.347

	601
	0.21
	0.263
	0.362
	0.342

	602
	0.208
	0.26
	0.358
	0.338

	603
	0.206
	0.256
	0.353
	0.334

	604
	0.204
	0.252
	0.349
	0.33

	605
	0.202
	0.249
	0.345
	0.326

	606
	0.2
	0.245
	0.34
	0.322

	607
	0.199
	0.242
	0.336
	0.318

	608
	0.197
	0.239
	0.332
	0.314

	609
	0.195
	0.235
	0.328
	0.31

	610
	0.193
	0.232
	0.324
	0.306

	611
	0.192
	0.229
	0.32
	0.302

	612
	0.19
	0.226
	0.316
	0.299

	613
	0.188
	0.222
	0.312
	0.295

	614
	0.186
	0.219
	0.308
	0.291

	615
	0.185
	0.216
	0.304
	0.287

	616
	0.183
	0.213
	0.301
	0.284

	617
	0.181
	0.21
	0.297
	0.28

	618
	0.179
	0.207
	0.293
	0.277

	619
	0.178
	0.204
	0.29
	0.273

	620
	0.176
	0.202
	0.286
	0.27

	621
	0.175
	0.199
	0.283
	0.266

	622
	0.173
	0.196
	0.279
	0.263

	623
	0.171
	0.193
	0.275
	0.259

	624
	0.17
	0.19
	0.272
	0.256

	625
	0.168
	0.188
	0.268
	0.252

	626
	0.166
	0.185
	0.265
	0.249

	627
	0.165
	0.182
	0.261
	0.246

	628
	0.163
	0.18
	0.258
	0.243

	629
	0.162
	0.178
	0.255
	0.24

	630
	0.16
	0.175
	0.252
	0.237

	631
	0.159
	0.173
	0.249
	0.234

	632
	0.157
	0.17
	0.245
	0.23

	633
	0.156
	0.168
	0.243
	0.227

	634
	0.154
	0.166
	0.239
	0.225

	635
	0.153
	0.163
	0.236
	0.222

	636
	0.151
	0.161
	0.233
	0.218

	637
	0.15
	0.159
	0.23
	0.216

	638
	0.149
	0.157
	0.227
	0.213

	639
	0.147
	0.154
	0.224
	0.21

	640
	0.146
	0.152
	0.221
	0.207

	641
	0.144
	0.15
	0.219
	0.205

	642
	0.143
	0.148
	0.216
	0.202

	643
	0.142
	0.147
	0.214
	0.2

	644
	0.14
	0.145
	0.211
	0.197

	645
	0.139
	0.143
	0.209
	0.195

	646
	0.138
	0.141
	0.206
	0.192

	647
	0.137
	0.139
	0.204
	0.19

	648
	0.136
	0.137
	0.201
	0.188

	649
	0.134
	0.135
	0.199
	0.185

	650
	0.133
	0.134
	0.196
	0.183

	651
	0.131
	0.132
	0.194
	0.181

	652
	0.13
	0.13
	0.191
	0.178

	653
	0.129
	0.128
	0.189
	0.176

	654
	0.128
	0.127
	0.187
	0.174

	655
	0.127
	0.125
	0.185
	0.172

	656
	0.126
	0.124
	0.182
	0.17

	657
	0.124
	0.122
	0.18
	0.167

	658
	0.123
	0.121
	0.178
	0.165

	659
	0.122
	0.119
	0.176
	0.164

	660
	0.121
	0.118
	0.174
	0.162

	661
	0.12
	0.116
	0.172
	0.16

	662
	0.119
	0.115
	0.17
	0.158

	663
	0.118
	0.114
	0.169
	0.156

	664
	0.117
	0.112
	0.167
	0.154

	665
	0.116
	0.111
	0.165
	0.153

	666
	0.115
	0.11
	0.163
	0.151

	667
	0.114
	0.108
	0.16
	0.148

	668
	0.112
	0.106
	0.156
	0.145

	669
	0.11
	0.103
	0.153
	0.142

	670
	0.109
	0.101
	0.15
	0.139

	671
	0.108
	0.1
	0.147
	0.136

	672
	0.107
	0.098
	0.144
	0.134

	673
	0.105
	0.096
	0.142
	0.132

	674
	0.105
	0.095
	0.14
	0.13

	675
	0.103
	0.094
	0.139
	0.128

	676
	0.103
	0.093
	0.138
	0.127

	677
	0.102
	0.093
	0.137
	0.127

	678
	0.102
	0.093
	0.137
	0.127

	679
	0.102
	0.092
	0.136
	0.126

	680
	0.101
	0.092
	0.136
	0.126

	681
	0.101
	0.092
	0.136
	0.125

	682
	0.1
	0.091
	0.135
	0.125

	683
	0.1
	0.091
	0.135
	0.124

	684
	0.099
	0.09
	0.134
	0.123

	685
	0.098
	0.089
	0.133
	0.122

	686
	0.098
	0.088
	0.132
	0.121

	687
	0.097
	0.087
	0.13
	0.12

	688
	0.096
	0.087
	0.129
	0.119

	689
	0.095
	0.086
	0.128
	0.117

	690
	0.094
	0.085
	0.126
	0.116

	691
	0.094
	0.084
	0.125
	0.115

	692
	0.093
	0.083
	0.124
	0.113

	693
	0.092
	0.082
	0.122
	0.112

	694
	0.091
	0.081
	0.121
	0.111

	695
	0.09
	0.08
	0.12
	0.11

	696
	0.09
	0.079
	0.119
	0.109

	697
	0.089
	0.079
	0.117
	0.107

	698
	0.088
	0.078
	0.116
	0.106

	699
	0.087
	0.077
	0.115
	0.105

	700
	0.087
	0.076
	0.113
	0.104

	701
	0.086
	0.075
	0.112
	0.103

	702
	0.085
	0.074
	0.111
	0.101

	703
	0.084
	0.073
	0.11
	0.1

	704
	0.084
	0.073
	0.109
	0.099

	705
	0.083
	0.072
	0.108
	0.098

	706
	0.082
	0.071
	0.107
	0.097

	707
	0.082
	0.071
	0.106
	0.096

	708
	0.081
	0.07
	0.104
	0.095

	709
	0.081
	0.069
	0.104
	0.095

	710
	0.08
	0.069
	0.103
	0.094

	711
	0.079
	0.068
	0.102
	0.093

	712
	0.079
	0.067
	0.101
	0.092

	713
	0.078
	0.067
	0.1
	0.091

	714
	0.077
	0.066
	0.099
	0.091

	715
	0.077
	0.066
	0.099
	0.09

	716
	0.077
	0.065
	0.098
	0.089

	717
	0.076
	0.065
	0.097
	0.088

	718
	0.075
	0.064
	0.096
	0.087

	719
	0.075
	0.063
	0.095
	0.086

	720
	0.074
	0.063
	0.094
	0.085

	721
	0.074
	0.062
	0.093
	0.085

	722
	0.073
	0.062
	0.092
	0.084

	723
	0.073
	0.061
	0.091
	0.083

	724
	0.072
	0.061
	0.091
	0.082

	725
	0.072
	0.06
	0.09
	0.082

	726
	0.071
	0.06
	0.089
	0.081

	727
	0.071
	0.059
	0.088
	0.08

	728
	0.07
	0.059
	0.088
	0.079

	729
	0.07
	0.058
	0.087
	0.079

	730
	0.069
	0.058
	0.087
	0.078

	731
	0.069
	0.058
	0.086
	0.078

	732
	0.068
	0.057
	0.085
	0.077

	733
	0.068
	0.057
	0.085
	0.077

	734
	0.067
	0.056
	0.084
	0.076

	735
	0.067
	0.056
	0.083
	0.075

	736
	0.066
	0.055
	0.083
	0.075

	737
	0.066
	0.055
	0.082
	0.074

	738
	0.066
	0.055
	0.081
	0.073

	739
	0.065
	0.054
	0.081
	0.073

	740
	0.065
	0.054
	0.08
	0.072

	741
	0.064
	0.053
	0.079
	0.072

	742
	0.064
	0.053
	0.079
	0.071

	743
	0.064
	0.053
	0.078
	0.07

	744
	0.063
	0.052
	0.077
	0.07

	745
	0.063
	0.052
	0.077
	0.069

	746
	0.062
	0.051
	0.076
	0.069

	747
	0.062
	0.051
	0.076
	0.068

	748
	0.062
	0.05
	0.075
	0.068

	749
	0.061
	0.05
	0.074
	0.067

	750
	0.061
	0.05
	0.074
	0.067

	751
	0.06
	0.049
	0.074
	0.066

	752
	0.06
	0.049
	0.073
	0.065

	753
	0.06
	0.049
	0.073
	0.065

	754
	0.059
	0.049
	0.072
	0.065

	755
	0.059
	0.048
	0.072
	0.064

	756
	0.058
	0.048
	0.071
	0.064

	757
	0.058
	0.047
	0.071
	0.064

	758
	0.058
	0.047
	0.07
	0.063

	759
	0.057
	0.047
	0.07
	0.063

	760
	0.057
	0.046
	0.069
	0.062

	761
	0.057
	0.046
	0.069
	0.062

	762
	0.056
	0.046
	0.068
	0.061

	763
	0.056
	0.045
	0.068
	0.061

	764
	0.056
	0.045
	0.067
	0.06

	765
	0.055
	0.045
	0.067
	0.06

	766
	0.055
	0.044
	0.066
	0.059

	767
	0.055
	0.044
	0.066
	0.059

	768
	0.054
	0.044
	0.065
	0.058

	769
	0.054
	0.044
	0.065
	0.058

	770
	0.053
	0.043
	0.064
	0.057

	771
	0.053
	0.043
	0.064
	0.057

	772
	0.053
	0.043
	0.063
	0.057

	773
	0.053
	0.042
	0.063
	0.056

	774
	0.052
	0.042
	0.063
	0.056

	775
	0.052
	0.042
	0.062
	0.056

	776
	0.052
	0.042
	0.062
	0.055

	777
	0.051
	0.042
	0.062
	0.055

	778
	0.051
	0.041
	0.062
	0.055

	779
	0.051
	0.041
	0.061
	0.054

	780
	0.051
	0.041
	0.061
	0.054

	781
	0.05
	0.041
	0.06
	0.054

	782
	0.05
	0.04
	0.06
	0.053

	783
	0.05
	0.04
	0.059
	0.053

	784
	0.049
	0.04
	0.059
	0.052

	785
	0.049
	0.04
	0.059
	0.052

	786
	0.049
	0.039
	0.058
	0.052

	787
	0.048
	0.039
	0.058
	0.051

	788
	0.048
	0.039
	0.058
	0.051

	789
	0.048
	0.039
	0.057
	0.051

	790
	0.048
	0.038
	0.057
	0.05

	791
	0.047
	0.038
	0.056
	0.05

	792
	0.047
	0.038
	0.056
	0.05

	793
	0.047
	0.037
	0.056
	0.049

	794
	0.046
	0.037
	0.055
	0.049

	795
	0.047
	0.038
	0.055
	0.049

	796
	0.046
	0.037
	0.055
	0.049

	797
	0.046
	0.037
	0.055
	0.048

	798
	0.046
	0.037
	0.054
	0.048

	799
	0.045
	0.037
	0.054
	0.048

	800
	0.045
	0.036
	0.054
	0.048

	801
	0.045
	0.036
	0.053
	0.048

	802
	0.045
	0.036
	0.053
	0.047

	803
	0.045
	0.036
	0.053
	0.047

	804
	0.044
	0.035
	0.053
	0.047

	805
	0.044
	0.035
	0.052
	0.046

	806
	0.044
	0.035
	0.052
	0.046

	807
	0.043
	0.035
	0.052
	0.046

	808
	0.043
	0.035
	0.052
	0.046

	809
	0.043
	0.035
	0.051
	0.045

	810
	0.043
	0.034
	0.051
	0.045

	811
	0.043
	0.034
	0.051
	0.045

	812
	0.042
	0.034
	0.05
	0.044

	813
	0.042
	0.034
	0.05
	0.044

	814
	0.042
	0.034
	0.049
	0.044

	815
	0.042
	0.033
	0.049
	0.043

	816
	0.041
	0.033
	0.049
	0.043

	817
	0.041
	0.033
	0.049
	0.043

	818
	0.041
	0.033
	0.048
	0.043

	819
	0.041
	0.033
	0.048
	0.042

	820
	0.041
	0.033
	0.048
	0.042

	821
	0.04
	0.033
	0.048
	0.042

	822
	0.04
	0.033
	0.048
	0.042

	823
	0.04
	0.032
	0.047
	0.042

	824
	0.04
	0.032
	0.047
	0.041

	825
	0.04
	0.032
	0.047
	0.041

	826
	0.039
	0.032
	0.047
	0.041

	827
	0.039
	0.032
	0.047
	0.041

	828
	0.039
	0.031
	0.046
	0.041

	829
	0.039
	0.031
	0.046
	0.04

	830
	0.039
	0.031
	0.046
	0.04

	831
	0.038
	0.031
	0.046
	0.04

	832
	0.038
	0.031
	0.046
	0.04

	833
	0.038
	0.031
	0.045
	0.04

	834
	0.038
	0.031
	0.045
	0.04

	835
	0.038
	0.031
	0.045
	0.039

	836
	0.038
	0.03
	0.045
	0.039

	837
	0.038
	0.03
	0.044
	0.039

	838
	0.037
	0.03
	0.044
	0.039

	839
	0.037
	0.03
	0.044
	0.039

	840
	0.037
	0.03
	0.044
	0.038

	841
	0.037
	0.03
	0.044
	0.038

	842
	0.037
	0.03
	0.043
	0.038

	843
	0.036
	0.029
	0.043
	0.038

	844
	0.036
	0.029
	0.043
	0.038

	845
	0.036
	0.029
	0.043
	0.037

	846
	0.036
	0.029
	0.042
	0.037

	847
	0.036
	0.029
	0.042
	0.037

	848
	0.036
	0.029
	0.042
	0.037

	849
	0.036
	0.029
	0.042
	0.037

	850
	0.036
	0.029
	0.042
	0.036

	851
	0.035
	0.029
	0.042
	0.036

	852
	0.035
	0.028
	0.042
	0.036

	853
	0.035
	0.028
	0.041
	0.036

	854
	0.035
	0.028
	0.041
	0.036

	855
	0.035
	0.028
	0.041
	0.036

	856
	0.035
	0.028
	0.041
	0.036

	857
	0.035
	0.028
	0.041
	0.036

	858
	0.034
	0.028
	0.041
	0.036

	859
	0.034
	0.028
	0.04
	0.036

	860
	0.034
	0.028
	0.041
	0.036

	861
	0.034
	0.028
	0.04
	0.036

	862
	0.034
	0.028
	0.04
	0.035

	863
	0.034
	0.028
	0.04
	0.035

	864
	0.034
	0.028
	0.04
	0.035

	865
	0.033
	0.027
	0.04
	0.035

	866
	0.033
	0.027
	0.04
	0.035

	867
	0.033
	0.027
	0.04
	0.035

	868
	0.033
	0.027
	0.039
	0.034

	869
	0.033
	0.027
	0.039
	0.034

	870
	0.033
	0.027
	0.039
	0.034

	871
	0.033
	0.027
	0.039
	0.034

	872
	0.032
	0.027
	0.039
	0.034

	873
	0.032
	0.027
	0.039
	0.034

	874
	0.032
	0.026
	0.038
	0.033

	875
	0.032
	0.026
	0.038
	0.033

	876
	0.032
	0.026
	0.038
	0.033

	877
	0.032
	0.026
	0.038
	0.033

	878
	0.032
	0.026
	0.038
	0.033

	879
	0.032
	0.026
	0.037
	0.033

	880
	0.032
	0.026
	0.037
	0.033

	881
	0.032
	0.026
	0.037
	0.033

	882
	0.031
	0.026
	0.037
	0.033

	883
	0.031
	0.026
	0.037
	0.032

	884
	0.031
	0.026
	0.037
	0.032

	885
	0.031
	0.025
	0.037
	0.032

	886
	0.031
	0.026
	0.037
	0.032

	887
	0.031
	0.026
	0.037
	0.032

	888
	0.031
	0.026
	0.037
	0.032

	889
	0.031
	0.025
	0.037
	0.032

	890
	0.031
	0.025
	0.037
	0.032

	891
	0.031
	0.025
	0.037
	0.032

	892
	0.03
	0.025
	0.036
	0.032

	893
	0.03
	0.025
	0.036
	0.032

	894
	0.03
	0.025
	0.036
	0.032

	895
	0.03
	0.025
	0.036
	0.032

	896
	0.03
	0.025
	0.036
	0.031

	897
	0.03
	0.025
	0.036
	0.031

	898
	0.03
	0.025
	0.036
	0.032

	899
	0.03
	0.025
	0.036
	0.031

	900
	0.029
	0.025
	0.035
	0.031

	901
	0.029
	0.024
	0.035
	0.031

	902
	0.029
	0.024
	0.035
	0.031

	903
	0.029
	0.024
	0.035
	0.03

	904
	0.029
	0.024
	0.035
	0.03

	905
	0.029
	0.024
	0.035
	0.03

	906
	0.029
	0.024
	0.035
	0.03

	907
	0.029
	0.024
	0.035
	0.03

	908
	0.028
	0.024
	0.034
	0.03

	909
	0.028
	0.024
	0.034
	0.03

	910
	0.028
	0.024
	0.034
	0.03

	911
	0.028
	0.024
	0.034
	0.03

	912
	0.028
	0.024
	0.034
	0.03

	913
	0.028
	0.023
	0.034
	0.029

	914
	0.028
	0.024
	0.034
	0.029

	915
	0.028
	0.023
	0.034
	0.029

	916
	0.028
	0.024
	0.034
	0.03

	917
	0.028
	0.024
	0.034
	0.029

	918
	0.028
	0.024
	0.033
	0.029

	919
	0.028
	0.024
	0.034
	0.029

	920
	0.027
	0.024
	0.033
	0.029

	921
	0.027
	0.024
	0.033
	0.029

	922
	0.027
	0.024
	0.033
	0.029

	923
	0.027
	0.024
	0.033
	0.029

	924
	0.027
	0.023
	0.033
	0.029

	925
	0.027
	0.023
	0.033
	0.029

	926
	0.027
	0.023
	0.033
	0.029

	927
	0.027
	0.023
	0.033
	0.029

	928
	0.027
	0.023
	0.033
	0.029

	929
	0.027
	0.023
	0.033
	0.029

	930
	0.027
	0.023
	0.033
	0.029

	931
	0.027
	0.023
	0.033
	0.029

	932
	0.027
	0.023
	0.033
	0.029

	933
	0.027
	0.023
	0.033
	0.029

	934
	0.027
	0.023
	0.033
	0.029

	935
	0.027
	0.023
	0.033
	0.029

	936
	0.026
	0.023
	0.033
	0.028

	937
	0.026
	0.023
	0.032
	0.028

	938
	0.026
	0.023
	0.032
	0.028

	939
	0.026
	0.023
	0.032
	0.028

	940
	0.027
	0.023
	0.033
	0.029

	941
	0.026
	0.023
	0.033
	0.029

	942
	0.026
	0.023
	0.033
	0.029

	943
	0.026
	0.023
	0.032
	0.028

	944
	0.026
	0.023
	0.032
	0.028

	945
	0.026
	0.023
	0.032
	0.028

	946
	0.026
	0.023
	0.033
	0.028

	947
	0.026
	0.023
	0.033
	0.028

	948
	0.026
	0.023
	0.033
	0.029

	949
	0.026
	0.023
	0.033
	0.029

	950
	0.026
	0.023
	0.033
	0.028

	951
	0.026
	0.023
	0.033
	0.029

	952
	0.026
	0.023
	0.033
	0.029

	953
	0.026
	0.023
	0.033
	0.029

	954
	0.026
	0.023
	0.033
	0.028

	955
	0.026
	0.023
	0.032
	0.028

	956
	0.026
	0.023
	0.032
	0.028

	957
	0.026
	0.023
	0.032
	0.028

	958
	0.025
	0.023
	0.032
	0.028

	959
	0.025
	0.022
	0.031
	0.027

	960
	0.025
	0.022
	0.031
	0.027

	961
	0.025
	0.022
	0.031
	0.027

	962
	0.025
	0.022
	0.031
	0.027

	963
	0.025
	0.022
	0.031
	0.027

	964
	0.025
	0.022
	0.03
	0.027

	965
	0.025
	0.022
	0.03
	0.026

	966
	0.025
	0.021
	0.03
	0.026

	967
	0.025
	0.021
	0.03
	0.026

	968
	0.024
	0.021
	0.03
	0.026

	969
	0.024
	0.021
	0.03
	0.026

	970
	0.024
	0.021
	0.029
	0.026

	971
	0.024
	0.021
	0.029
	0.025

	972
	0.024
	0.021
	0.029
	0.025

	973
	0.024
	0.021
	0.029
	0.025

	974
	0.024
	0.021
	0.029
	0.025

	975
	0.024
	0.021
	0.029
	0.025

	976
	0.024
	0.021
	0.029
	0.025

	977
	0.024
	0.021
	0.029
	0.025

	978
	0.023
	0.02
	0.028
	0.025

	979
	0.024
	0.02
	0.028
	0.025

	980
	0.023
	0.02
	0.028
	0.025

	981
	0.023
	0.02
	0.028
	0.024

	982
	0.023
	0.02
	0.028
	0.024

	983
	0.023
	0.02
	0.028
	0.024

	984
	0.023
	0.02
	0.028
	0.024

	985
	0.023
	0.02
	0.028
	0.024

	986
	0.023
	0.02
	0.028
	0.024

	987
	0.023
	0.02
	0.027
	0.024

	988
	0.023
	0.02
	0.027
	0.024

	989
	0.023
	0.02
	0.027
	0.024

	990
	0.022
	0.019
	0.027
	0.024

	991
	0.022
	0.019
	0.027
	0.024

	992
	0.022
	0.02
	0.027
	0.024

	993
	0.022
	0.019
	0.027
	0.024

	994
	0.022
	0.019
	0.027
	0.023

	995
	0.022
	0.019
	0.027
	0.023

	996
	0.022
	0.019
	0.026
	0.023

	997
	0.022
	0.019
	0.026
	0.023

	998
	0.022
	0.019
	0.026
	0.023

	999
	0.022
	0.019
	0.026
	0.023

	1000
	0.022
	0.019
	0.027
	0.023

	1001
	0.022
	0.019
	0.026
	0.023

	1002
	0.021
	0.019
	0.026
	0.023

	1003
	0.022
	0.019
	0.026
	0.023

	1004
	0.021
	0.019
	0.026
	0.023

	1005
	0.021
	0.019
	0.026
	0.023

	1006
	0.021
	0.019
	0.026
	0.023

	1007
	0.021
	0.019
	0.026
	0.023

	1008
	0.021
	0.019
	0.026
	0.023

	1009
	0.021
	0.019
	0.025
	0.023

	1010
	0.021
	0.019
	0.025
	0.022

	1011
	0.021
	0.018
	0.025
	0.022

	1012
	0.021
	0.018
	0.025
	0.022

	1013
	0.021
	0.018
	0.025
	0.022

	1014
	0.021
	0.018
	0.025
	0.022

	1015
	0.021
	0.018
	0.025
	0.022

	1016
	0.021
	0.018
	0.025
	0.022

	1017
	0.021
	0.018
	0.024
	0.022

	1018
	0.02
	0.018
	0.024
	0.022

	1019
	0.02
	0.018
	0.024
	0.022

	1020
	0.021
	0.018
	0.025
	0.022

	1021
	0.021
	0.018
	0.024
	0.022

	1022
	0.02
	0.018
	0.024
	0.021

	1023
	0.02
	0.018
	0.024
	0.021

	1024
	0.02
	0.018
	0.024
	0.021

	1025
	0.02
	0.018
	0.024
	0.021

	1026
	0.02
	0.018
	0.024
	0.021

	1027
	0.02
	0.018
	0.024
	0.021

	1028
	0.02
	0.018
	0.024
	0.021

	1029
	0.02
	0.018
	0.024
	0.021

	1030
	0.02
	0.018
	0.023
	0.021

	1031
	0.02
	0.017
	0.023
	0.021

	1032
	0.02
	0.018
	0.023
	0.021

	1033
	0.02
	0.018
	0.023
	0.021

	1034
	0.02
	0.017
	0.023
	0.021

	1035
	0.02
	0.017
	0.023
	0.02

	1036
	0.02
	0.017
	0.023
	0.02

	1037
	0.02
	0.017
	0.023
	0.02

	1038
	0.02
	0.017
	0.023
	0.02

	1039
	0.019
	0.017
	0.022
	0.02

	1040
	0.019
	0.017
	0.022
	0.02

	1041
	0.019
	0.017
	0.022
	0.02

	1042
	0.019
	0.017
	0.022
	0.02

	1043
	0.019
	0.017
	0.022
	0.02

	1044
	0.019
	0.017
	0.022
	0.02

	1045
	0.019
	0.017
	0.022
	0.02

	1046
	0.019
	0.017
	0.022
	0.02

	1047
	0.019
	0.017
	0.022
	0.02

	1048
	0.019
	0.017
	0.022
	0.02

	1049
	0.019
	0.017
	0.022
	0.02

	1050
	0.019
	0.017
	0.022
	0.019

	1051
	0.019
	0.017
	0.022
	0.02

	1052
	0.018
	0.016
	0.021
	0.019

	1053
	0.019
	0.016
	0.021
	0.019

	1054
	0.019
	0.016
	0.021
	0.019

	1055
	0.019
	0.016
	0.021
	0.019

	1056
	0.018
	0.016
	0.021
	0.018

	1057
	0.019
	0.016
	0.021
	0.019

	1058
	0.018
	0.016
	0.021
	0.019

	1059
	0.019
	0.016
	0.02
	0.018

	1060
	0.018
	0.016
	0.02
	0.018

	1061
	0.018
	0.016
	0.02
	0.018

	1062
	0.018
	0.016
	0.02
	0.018

	1063
	0.018
	0.016
	0.02
	0.018

	1064
	0.018
	0.016
	0.02
	0.018

	1065
	0.018
	0.016
	0.02
	0.018

	1066
	0.018
	0.016
	0.02
	0.018

	1067
	0.018
	0.016
	0.02
	0.018

	1068
	0.018
	0.016
	0.02
	0.018

	1069
	0.018
	0.016
	0.02
	0.018

	1070
	0.018
	0.016
	0.019
	0.017

	1071
	0.018
	0.015
	0.019
	0.018

	1072
	0.018
	0.015
	0.02
	0.018

	1073
	0.018
	0.016
	0.019
	0.018

	1074
	0.018
	0.015
	0.019
	0.017

	1075
	0.018
	0.015
	0.019
	0.017

	1076
	0.018
	0.015
	0.019
	0.017

	1077
	0.018
	0.015
	0.019
	0.017

	1078
	0.018
	0.015
	0.019
	0.017

	1079
	0.018
	0.015
	0.019
	0.017

	1080
	0.018
	0.015
	0.019
	0.017

	1081
	0.017
	0.015
	0.019
	0.017

	1082
	0.018
	0.015
	0.019
	0.017

	1083
	0.017
	0.015
	0.019
	0.017

	1084
	0.018
	0.015
	0.019
	0.017

	1085
	0.017
	0.015
	0.019
	0.017

	1086
	0.018
	0.015
	0.019
	0.017

	1087
	0.017
	0.015
	0.019
	0.017

	1088
	0.017
	0.015
	0.018
	0.017

	1089
	0.018
	0.015
	0.019
	0.017

	1090
	0.017
	0.015
	0.019
	0.017

	1091
	0.017
	0.015
	0.019
	0.017

	1092
	0.017
	0.015
	0.019
	0.017

	1093
	0.017
	0.015
	0.019
	0.017

	1094
	0.017
	0.015
	0.018
	0.017

	1095
	0.017
	0.015
	0.018
	0.017

	1096
	0.017
	0.015
	0.018
	0.016

	1097
	0.017
	0.015
	0.018
	0.017

	1098
	0.017
	0.015
	0.018
	0.016

	1099
	0.017
	0.015
	0.018
	0.017

	1100
	0.017
	0.015
	0.018
	0.017


*SPR represents Surface Plasmon Resonance.



Table S2: UV-vis spectra of the synthesized silver nanoparticle sample at 1:2, 1:4, 1:6, and 1:10 ratios at 60 min. Here, 1:2 ratios produce the highest concentration and size of Ag NPs, represents raw data of Table 4B.
	SPR Wavelength (nm)
	Absorption at 1:2 (60 min)
	Absorption at 1:4 (60 min)
	Absorption at 1:6 (60 min)
	Absorption at 1:10 (60 min)

	325
	0.41
	0.342
	0.176
	0.096

	326
	0.434
	0.354
	0.161
	0.085

	327
	0.462
	0.368
	0.155
	0.088

	328
	0.495
	0.386
	0.163
	0.101

	329
	0.535
	0.409
	0.186
	0.13

	330
	0.572
	0.416
	0.218
	0.162

	331
	0.607
	0.442
	0.239
	0.178

	332
	0.637
	0.451
	0.266
	0.192

	333
	0.662
	0.469
	0.288
	0.202

	334
	0.681
	0.477
	0.309
	0.209

	335
	0.703
	0.491
	0.322
	0.221

	336
	0.714
	0.5
	0.337
	0.228

	337
	0.732
	0.511
	0.35
	0.24

	338
	0.742
	0.519
	0.36
	0.25

	339
	0.74
	0.533
	0.369
	0.257

	340
	0.757
	0.537
	0.382
	0.271

	341
	0.751
	0.55
	0.393
	0.28

	342
	0.764
	0.554
	0.408
	0.296

	343
	0.763
	0.563
	0.419
	0.306

	344
	0.766
	0.564
	0.429
	0.317

	345
	0.758
	0.579
	0.441
	0.328

	346
	0.768
	0.576
	0.449
	0.338

	347
	0.768
	0.581
	0.461
	0.349

	348
	0.768
	0.589
	0.472
	0.358

	349
	0.772
	0.589
	0.48
	0.368

	350
	0.771
	0.6
	0.49
	0.377

	351
	0.777
	0.597
	0.499
	0.386

	352
	0.779
	0.605
	0.507
	0.392

	353
	0.784
	0.605
	0.516
	0.402

	354
	0.786
	0.609
	0.524
	0.41

	355
	0.79
	0.615
	0.533
	0.418

	356
	0.795
	0.616
	0.54
	0.425

	357
	0.796
	0.621
	0.547
	0.43

	358
	0.8
	0.624
	0.556
	0.441

	359
	0.806
	0.628
	0.564
	0.446

	360
	1.035
	0.668
	0.594
	0.485

	361
	1.04
	0.673
	0.603
	0.493

	362
	1.045
	0.678
	0.611
	0.5

	363
	1.051
	0.685
	0.619
	0.508

	364
	1.058
	0.691
	0.627
	0.515

	365
	1.067
	0.699
	0.637
	0.524

	366
	1.076
	0.706
	0.646
	0.532

	367
	1.085
	0.714
	0.655
	0.54

	368
	1.094
	0.722
	0.664
	0.548

	369
	1.104
	0.731
	0.674
	0.556

	370
	1.114
	0.74
	0.683
	0.564

	371
	1.125
	0.749
	0.692
	0.572

	372
	1.136
	0.757
	0.701
	0.579

	373
	1.147
	0.766
	0.71
	0.587

	374
	1.158
	0.775
	0.719
	0.594

	375
	1.17
	0.784
	0.728
	0.602

	376
	1.181
	0.792
	0.736
	0.609

	377
	1.192
	0.801
	0.745
	0.616

	378
	1.204
	0.809
	0.754
	0.623

	379
	1.215
	0.818
	0.762
	0.63

	380
	1.225
	0.825
	0.769
	0.636

	381
	1.236
	0.833
	0.777
	0.642

	382
	1.246
	0.84
	0.784
	0.648

	383
	1.256
	0.846
	0.791
	0.654

	384
	1.266
	0.853
	0.798
	0.66

	385
	1.275
	0.86
	0.804
	0.665

	386
	1.284
	0.865
	0.81
	0.67

	387
	1.293
	0.871
	0.816
	0.675

	388
	1.302
	0.877
	0.822
	0.681

	389
	1.311
	0.882
	0.828
	0.685

	390
	1.319
	0.887
	0.833
	0.69

	391
	1.328
	0.892
	0.838
	0.695

	392
	1.335
	0.896
	0.843
	0.699

	393
	1.343
	0.901
	0.848
	0.703

	394
	1.35
	0.905
	0.852
	0.707

	395
	1.357
	0.909
	0.857
	0.711

	396
	1.364
	0.912
	0.861
	0.715

	397
	1.371
	0.916
	0.865
	0.719

	398
	1.377
	0.919
	0.869
	0.723

	399
	1.383
	0.923
	0.873
	0.726

	400
	1.39
	0.926
	0.877
	0.73

	401
	1.396
	0.929
	0.881
	0.733

	402
	1.402
	0.932
	0.885
	0.737

	403
	1.408
	0.935
	0.889
	0.74

	404
	1.414
	0.938
	0.892
	0.743

	405
	1.419
	0.941
	0.896
	0.747

	406
	1.425
	0.944
	0.9
	0.75

	407
	1.43
	0.946
	0.904
	0.753

	408
	1.435
	0.949
	0.907
	0.756

	409
	1.44
	0.951
	0.91
	0.759

	410
	1.445
	0.954
	0.914
	0.762

	411
	1.451
	0.957
	0.918
	0.765

	412
	1.456
	0.959
	0.921
	0.768

	413
	1.46
	0.961
	0.925
	0.771

	414
	1.465
	0.964
	0.929
	0.774

	415
	1.47
	0.966
	0.932
	0.777

	416
	1.475
	0.969
	0.936
	0.78

	417
	1.479
	0.971
	0.94
	0.783

	418
	1.483
	0.973
	0.944
	0.786

	419
	1.488
	0.975
	0.948
	0.789

	420
	1.519
	0.991
	1.008
	0.835

	421
	1.522
	0.993
	1.012
	0.838

	422
	1.527
	0.995
	1.016
	0.841

	423
	1.531
	0.997
	1.02
	0.844

	424
	1.535
	0.999
	1.025
	0.848

	425
	1.539
	1.001
	1.029
	0.851

	426
	1.542
	1.003
	1.032
	0.853

	427
	1.546
	1.005
	1.037
	0.856

	428
	1.548
	1.006
	1.04
	0.859

	429
	1.551
	1.008
	1.044
	0.861

	430
	1.554
	1.009
	1.048
	0.864

	431
	1.557
	1.011
	1.052
	0.866

	432
	1.559
	1.013
	1.055
	0.869

	433
	1.561
	1.014
	1.059
	0.871

	434
	1.563
	1.016
	1.063
	0.874

	435
	1.565
	1.017
	1.067
	0.876

	436
	1.566
	1.018
	1.07
	0.878

	437
	1.567
	1.019
	1.073
	0.88

	438
	1.568
	1.021
	1.076
	0.881

	439
	1.569
	1.022
	1.079
	0.883

	440
	1.57
	1.023
	1.082
	0.884

	441
	1.57
	1.023
	1.084
	0.886

	442
	1.571
	1.024
	1.087
	0.887

	443
	1.571
	1.025
	1.09
	0.888

	444
	1.571
	1.026
	1.092
	0.889

	445
	1.57
	1.026
	1.095
	0.89

	446
	1.569
	1.027
	1.098
	0.891

	447
	1.568
	1.028
	1.1
	0.892

	448
	1.567
	1.028
	1.103
	0.893

	449
	1.565
	1.029
	1.105
	0.893

	450
	1.564
	1.029
	1.106
	0.894

	451
	1.562
	1.029
	1.109
	0.894

	452
	1.561
	1.029
	1.111
	0.894

	453
	1.559
	1.029
	1.112
	0.895

	454
	1.557
	1.029
	1.114
	0.895

	455
	1.555
	1.029
	1.116
	0.895

	456
	1.553
	1.029
	1.117
	0.895

	457
	1.551
	1.029
	1.119
	0.895

	458
	1.549
	1.028
	1.121
	0.895

	459
	1.546
	1.028
	1.122
	0.895

	460
	1.543
	1.028
	1.124
	0.895

	461
	1.54
	1.027
	1.125
	0.895

	462
	1.537
	1.026
	1.126
	0.894

	463
	1.534
	1.026
	1.128
	0.894

	464
	1.53
	1.025
	1.129
	0.894

	465
	1.527
	1.024
	1.13
	0.893

	466
	1.524
	1.024
	1.131
	0.893

	467
	1.521
	1.023
	1.132
	0.893

	468
	1.516
	1.021
	1.133
	0.892

	469
	1.512
	1.02
	1.134
	0.891

	470
	1.508
	1.019
	1.135
	0.891

	471
	1.503
	1.017
	1.135
	0.89

	472
	1.499
	1.016
	1.135
	0.889

	473
	1.494
	1.014
	1.136
	0.888

	474
	1.489
	1.013
	1.136
	0.888

	475
	1.485
	1.011
	1.136
	0.886

	476
	1.48
	1.009
	1.136
	0.886

	477
	1.475
	1.007
	1.136
	0.884

	478
	1.469
	1.004
	1.136
	0.883

	479
	1.464
	1.002
	1.136
	0.882

	480
	1.458
	1
	1.136
	0.881

	481
	1.452
	0.997
	1.135
	0.88

	482
	1.446
	0.995
	1.135
	0.878

	483
	1.44
	0.992
	1.134
	0.877

	484
	1.434
	0.989
	1.134
	0.876

	485
	1.428
	0.986
	1.133
	0.874

	486
	1.421
	0.983
	1.132
	0.872

	487
	1.415
	0.98
	1.131
	0.871

	488
	1.408
	0.977
	1.13
	0.869

	489
	1.401
	0.974
	1.129
	0.868

	490
	1.394
	0.97
	1.128
	0.866

	491
	1.386
	0.966
	1.126
	0.864

	492
	1.379
	0.963
	1.125
	0.862

	493
	1.371
	0.959
	1.123
	0.86

	494
	1.364
	0.955
	1.122
	0.858

	495
	1.355
	0.951
	1.12
	0.856

	496
	1.347
	0.948
	1.118
	0.854

	497
	1.339
	0.943
	1.116
	0.852

	498
	1.331
	0.939
	1.115
	0.85

	499
	1.323
	0.935
	1.113
	0.848

	500
	1.28
	0.92
	1.052
	0.803

	501
	1.272
	0.916
	1.049
	0.801

	502
	1.263
	0.911
	1.047
	0.798

	503
	1.254
	0.906
	1.045
	0.796

	504
	1.245
	0.902
	1.043
	0.794

	505
	1.235
	0.897
	1.04
	0.791

	506
	1.226
	0.892
	1.037
	0.789

	507
	1.217
	0.887
	1.035
	0.786

	508
	1.208
	0.883
	1.032
	0.783

	509
	1.198
	0.877
	1.029
	0.781

	510
	1.189
	0.872
	1.026
	0.778

	511
	1.179
	0.867
	1.023
	0.775

	512
	1.169
	0.862
	1.02
	0.773

	513
	1.159
	0.856
	1.016
	0.77

	514
	1.148
	0.851
	1.013
	0.767

	515
	1.138
	0.845
	1.009
	0.764

	516
	1.127
	0.839
	1.005
	0.76

	517
	1.116
	0.833
	1.001
	0.757

	518
	1.106
	0.828
	0.997
	0.754

	519
	1.095
	0.822
	0.993
	0.75

	520
	1.084
	0.816
	0.989
	0.747

	521
	1.073
	0.81
	0.984
	0.744

	522
	1.062
	0.803
	0.98
	0.74

	523
	1.051
	0.797
	0.976
	0.737

	524
	1.04
	0.792
	0.972
	0.734

	525
	1.029
	0.785
	0.967
	0.73

	526
	1.017
	0.778
	0.962
	0.727

	527
	1.006
	0.772
	0.957
	0.723

	528
	0.994
	0.766
	0.952
	0.719

	529
	0.983
	0.759
	0.947
	0.716

	530
	0.971
	0.752
	0.941
	0.712

	531
	0.96
	0.746
	0.936
	0.708

	532
	0.948
	0.739
	0.93
	0.704

	533
	0.936
	0.732
	0.925
	0.7

	534
	0.924
	0.725
	0.919
	0.696

	535
	0.912
	0.718
	0.913
	0.691

	536
	0.9
	0.711
	0.906
	0.687

	537
	0.888
	0.703
	0.9
	0.683

	538
	0.876
	0.696
	0.894
	0.679

	539
	0.864
	0.689
	0.888
	0.674

	540
	0.853
	0.682
	0.882
	0.67

	541
	0.841
	0.676
	0.876
	0.666

	542
	0.83
	0.669
	0.87
	0.662

	543
	0.819
	0.662
	0.864
	0.658

	544
	0.807
	0.655
	0.858
	0.654

	545
	0.797
	0.648
	0.852
	0.65

	546
	0.786
	0.641
	0.846
	0.645

	547
	0.774
	0.634
	0.84
	0.641

	548
	0.763
	0.627
	0.833
	0.637

	549
	0.752
	0.62
	0.827
	0.632

	550
	0.741
	0.613
	0.82
	0.627

	551
	0.73
	0.606
	0.814
	0.623

	552
	0.72
	0.599
	0.807
	0.619

	553
	0.709
	0.592
	0.801
	0.614

	554
	0.698
	0.585
	0.794
	0.61

	555
	0.688
	0.578
	0.787
	0.605

	556
	0.678
	0.571
	0.781
	0.601

	557
	0.667
	0.565
	0.774
	0.596

	558
	0.657
	0.558
	0.767
	0.591

	559
	0.646
	0.551
	0.76
	0.587

	560
	0.636
	0.544
	0.754
	0.582

	561
	0.626
	0.537
	0.747
	0.577

	562
	0.616
	0.531
	0.741
	0.573

	563
	0.607
	0.524
	0.734
	0.568

	564
	0.597
	0.518
	0.727
	0.564

	565
	0.587
	0.511
	0.72
	0.559

	566
	0.579
	0.505
	0.714
	0.554

	567
	0.57
	0.499
	0.708
	0.55

	568
	0.561
	0.493
	0.701
	0.546

	569
	0.551
	0.486
	0.694
	0.54

	570
	0.543
	0.48
	0.688
	0.536

	571
	0.534
	0.473
	0.681
	0.531

	572
	0.525
	0.467
	0.674
	0.526

	573
	0.516
	0.461
	0.667
	0.521

	574
	0.508
	0.455
	0.66
	0.516

	575
	0.499
	0.448
	0.654
	0.511

	576
	0.491
	0.443
	0.647
	0.507

	577
	0.483
	0.437
	0.64
	0.502

	578
	0.475
	0.431
	0.634
	0.497

	579
	0.468
	0.426
	0.627
	0.493

	580
	0.46
	0.42
	0.62
	0.487

	581
	0.452
	0.414
	0.614
	0.483

	582
	0.445
	0.409
	0.607
	0.478

	583
	0.437
	0.403
	0.601
	0.473

	584
	0.431
	0.398
	0.594
	0.468

	585
	0.424
	0.393
	0.588
	0.464

	586
	0.417
	0.387
	0.582
	0.459

	587
	0.41
	0.382
	0.576
	0.455

	588
	0.404
	0.377
	0.57
	0.45

	589
	0.398
	0.372
	0.564
	0.446

	590
	0.391
	0.368
	0.558
	0.441

	591
	0.385
	0.363
	0.552
	0.437

	592
	0.379
	0.358
	0.546
	0.432

	593
	0.373
	0.353
	0.54
	0.427

	594
	0.367
	0.348
	0.533
	0.423

	595
	0.362
	0.344
	0.528
	0.418

	596
	0.356
	0.339
	0.521
	0.414

	597
	0.35
	0.334
	0.515
	0.409

	598
	0.345
	0.33
	0.509
	0.405

	599
	0.339
	0.326
	0.503
	0.4

	600
	0.334
	0.321
	0.498
	0.396

	601
	0.329
	0.317
	0.492
	0.391

	602
	0.324
	0.313
	0.486
	0.387

	603
	0.319
	0.309
	0.48
	0.383

	604
	0.314
	0.304
	0.475
	0.378

	605
	0.309
	0.3
	0.469
	0.374

	606
	0.305
	0.296
	0.463
	0.37

	607
	0.3
	0.292
	0.458
	0.365

	608
	0.296
	0.288
	0.452
	0.361

	609
	0.291
	0.285
	0.447
	0.357

	610
	0.287
	0.281
	0.442
	0.353

	611
	0.283
	0.277
	0.436
	0.349

	612
	0.279
	0.274
	0.431
	0.345

	613
	0.275
	0.27
	0.426
	0.341

	614
	0.27
	0.267
	0.421
	0.337

	615
	0.267
	0.263
	0.416
	0.333

	616
	0.263
	0.259
	0.41
	0.329

	617
	0.259
	0.256
	0.405
	0.325

	618
	0.255
	0.252
	0.4
	0.321

	619
	0.251
	0.249
	0.395
	0.317

	620
	0.248
	0.246
	0.391
	0.313

	621
	0.245
	0.243
	0.386
	0.309

	622
	0.241
	0.24
	0.381
	0.305

	623
	0.238
	0.236
	0.376
	0.302

	624
	0.234
	0.233
	0.371
	0.298

	625
	0.231
	0.23
	0.366
	0.294

	626
	0.228
	0.227
	0.362
	0.291

	627
	0.225
	0.224
	0.357
	0.287

	628
	0.221
	0.221
	0.353
	0.283

	629
	0.218
	0.219
	0.348
	0.28

	630
	0.216
	0.216
	0.344
	0.277

	631
	0.213
	0.213
	0.34
	0.273

	632
	0.21
	0.211
	0.336
	0.27

	633
	0.207
	0.208
	0.332
	0.267

	634
	0.205
	0.206
	0.328
	0.263

	635
	0.202
	0.203
	0.323
	0.26

	636
	0.199
	0.2
	0.319
	0.257

	637
	0.197
	0.198
	0.315
	0.253

	638
	0.194
	0.196
	0.311
	0.25

	639
	0.192
	0.193
	0.307
	0.247

	640
	0.189
	0.191
	0.303
	0.244

	641
	0.187
	0.189
	0.299
	0.241

	642
	0.184
	0.186
	0.296
	0.238

	643
	0.182
	0.184
	0.292
	0.235

	644
	0.18
	0.182
	0.289
	0.232

	645
	0.178
	0.18
	0.286
	0.23

	646
	0.176
	0.178
	0.282
	0.227

	647
	0.173
	0.176
	0.278
	0.224

	648
	0.171
	0.174
	0.275
	0.221

	649
	0.169
	0.172
	0.272
	0.218

	650
	0.167
	0.169
	0.268
	0.216

	651
	0.165
	0.168
	0.265
	0.213

	652
	0.163
	0.166
	0.262
	0.21

	653
	0.161
	0.164
	0.258
	0.208

	654
	0.159
	0.162
	0.255
	0.205

	655
	0.158
	0.16
	0.252
	0.203

	656
	0.156
	0.158
	0.249
	0.2

	657
	0.154
	0.156
	0.246
	0.198

	658
	0.152
	0.154
	0.243
	0.195

	659
	0.15
	0.153
	0.24
	0.193

	660
	0.149
	0.151
	0.238
	0.191

	661
	0.147
	0.149
	0.235
	0.189

	662
	0.145
	0.148
	0.232
	0.186

	663
	0.144
	0.146
	0.23
	0.185

	664
	0.142
	0.145
	0.228
	0.182

	665
	0.141
	0.143
	0.225
	0.18

	666
	0.139
	0.142
	0.222
	0.178

	667
	0.137
	0.14
	0.218
	0.175

	668
	0.135
	0.138
	0.214
	0.172

	669
	0.133
	0.136
	0.209
	0.168

	670
	0.131
	0.135
	0.205
	0.166

	671
	0.129
	0.133
	0.201
	0.163

	672
	0.127
	0.132
	0.198
	0.16

	673
	0.125
	0.13
	0.195
	0.158

	674
	0.124
	0.129
	0.193
	0.156

	675
	0.123
	0.128
	0.191
	0.154

	676
	0.121
	0.126
	0.19
	0.153

	677
	0.121
	0.125
	0.188
	0.151

	678
	0.12
	0.125
	0.188
	0.151

	679
	0.119
	0.123
	0.187
	0.15

	680
	0.119
	0.123
	0.186
	0.149

	681
	0.118
	0.122
	0.185
	0.148

	682
	0.117
	0.121
	0.185
	0.147

	683
	0.116
	0.12
	0.183
	0.146

	684
	0.115
	0.118
	0.182
	0.145

	685
	0.115
	0.117
	0.18
	0.144

	686
	0.113
	0.116
	0.179
	0.142

	687
	0.112
	0.115
	0.177
	0.141

	688
	0.111
	0.114
	0.175
	0.139

	689
	0.11
	0.113
	0.173
	0.138

	690
	0.109
	0.112
	0.172
	0.136

	691
	0.108
	0.11
	0.17
	0.135

	692
	0.107
	0.109
	0.168
	0.133

	693
	0.106
	0.108
	0.166
	0.132

	694
	0.105
	0.107
	0.165
	0.13

	695
	0.103
	0.106
	0.163
	0.129

	696
	0.102
	0.105
	0.161
	0.127

	697
	0.101
	0.104
	0.159
	0.126

	698
	0.1
	0.103
	0.158
	0.124

	699
	0.099
	0.102
	0.156
	0.123

	700
	0.098
	0.101
	0.155
	0.122

	701
	0.097
	0.1
	0.153
	0.121

	702
	0.096
	0.099
	0.151
	0.119

	703
	0.095
	0.098
	0.15
	0.118

	704
	0.094
	0.097
	0.148
	0.117

	705
	0.093
	0.096
	0.147
	0.115

	706
	0.092
	0.095
	0.145
	0.114

	707
	0.092
	0.095
	0.144
	0.113

	708
	0.091
	0.094
	0.143
	0.112

	709
	0.09
	0.093
	0.141
	0.111

	710
	0.089
	0.092
	0.14
	0.11

	711
	0.088
	0.091
	0.139
	0.109

	712
	0.088
	0.091
	0.138
	0.108

	713
	0.087
	0.09
	0.136
	0.107

	714
	0.086
	0.089
	0.135
	0.106

	715
	0.086
	0.089
	0.134
	0.105

	716
	0.085
	0.088
	0.133
	0.104

	717
	0.084
	0.087
	0.132
	0.103

	718
	0.083
	0.086
	0.13
	0.102

	719
	0.082
	0.085
	0.129
	0.101

	720
	0.082
	0.085
	0.128
	0.1

	721
	0.081
	0.084
	0.127
	0.099

	722
	0.08
	0.083
	0.126
	0.098

	723
	0.08
	0.083
	0.125
	0.097

	724
	0.079
	0.082
	0.123
	0.096

	725
	0.078
	0.081
	0.122
	0.095

	726
	0.078
	0.081
	0.121
	0.095

	727
	0.077
	0.08
	0.12
	0.094

	728
	0.076
	0.079
	0.119
	0.093

	729
	0.076
	0.079
	0.118
	0.092

	730
	0.075
	0.078
	0.117
	0.091

	731
	0.074
	0.078
	0.117
	0.091

	732
	0.074
	0.077
	0.116
	0.09

	733
	0.073
	0.076
	0.115
	0.089

	734
	0.073
	0.075
	0.114
	0.088

	735
	0.072
	0.075
	0.113
	0.088

	736
	0.072
	0.075
	0.112
	0.087

	737
	0.071
	0.074
	0.111
	0.086

	738
	0.071
	0.073
	0.11
	0.085

	739
	0.07
	0.073
	0.109
	0.085

	740
	0.07
	0.072
	0.109
	0.084

	741
	0.069
	0.072
	0.108
	0.083

	742
	0.068
	0.071
	0.107
	0.083

	743
	0.068
	0.071
	0.106
	0.082

	744
	0.067
	0.07
	0.105
	0.081

	745
	0.066
	0.07
	0.104
	0.081

	746
	0.066
	0.069
	0.104
	0.08

	747
	0.065
	0.068
	0.103
	0.079

	748
	0.065
	0.068
	0.102
	0.079

	749
	0.064
	0.067
	0.101
	0.078

	750
	0.064
	0.067
	0.1
	0.078

	751
	0.064
	0.066
	0.1
	0.077

	752
	0.063
	0.066
	0.099
	0.076

	753
	0.063
	0.065
	0.099
	0.076

	754
	0.062
	0.065
	0.098
	0.075

	755
	0.062
	0.065
	0.097
	0.075

	756
	0.061
	0.064
	0.097
	0.074

	757
	0.061
	0.064
	0.096
	0.074

	758
	0.06
	0.063
	0.095
	0.073

	759
	0.06
	0.063
	0.095
	0.073

	760
	0.059
	0.062
	0.094
	0.072

	761
	0.059
	0.062
	0.093
	0.071

	762
	0.058
	0.061
	0.092
	0.071

	763
	0.058
	0.061
	0.092
	0.07

	764
	0.058
	0.06
	0.091
	0.07

	765
	0.057
	0.06
	0.09
	0.069

	766
	0.057
	0.06
	0.09
	0.069

	767
	0.056
	0.059
	0.089
	0.068

	768
	0.056
	0.058
	0.088
	0.067

	769
	0.055
	0.058
	0.088
	0.067

	770
	0.055
	0.058
	0.087
	0.067

	771
	0.055
	0.057
	0.087
	0.066

	772
	0.054
	0.057
	0.086
	0.066

	773
	0.054
	0.056
	0.086
	0.065

	774
	0.053
	0.056
	0.085
	0.065

	775
	0.053
	0.056
	0.085
	0.064

	776
	0.053
	0.055
	0.084
	0.064

	777
	0.052
	0.055
	0.084
	0.064

	778
	0.052
	0.055
	0.083
	0.063

	779
	0.052
	0.054
	0.083
	0.063

	780
	0.051
	0.054
	0.082
	0.062

	781
	0.051
	0.053
	0.082
	0.062

	782
	0.051
	0.053
	0.081
	0.062

	783
	0.05
	0.053
	0.081
	0.061

	784
	0.05
	0.052
	0.08
	0.061

	785
	0.05
	0.052
	0.08
	0.06

	786
	0.049
	0.052
	0.079
	0.06

	787
	0.048
	0.051
	0.078
	0.059

	788
	0.048
	0.051
	0.078
	0.059

	789
	0.048
	0.051
	0.078
	0.059

	790
	0.048
	0.05
	0.077
	0.058

	791
	0.047
	0.05
	0.076
	0.058

	792
	0.047
	0.05
	0.076
	0.057

	793
	0.047
	0.049
	0.076
	0.057

	794
	0.046
	0.049
	0.075
	0.057

	795
	0.047
	0.049
	0.075
	0.057

	796
	0.046
	0.048
	0.074
	0.056

	797
	0.046
	0.048
	0.074
	0.056

	798
	0.045
	0.048
	0.073
	0.055

	799
	0.045
	0.048
	0.073
	0.055

	800
	0.045
	0.047
	0.073
	0.055

	801
	0.044
	0.047
	0.073
	0.055

	802
	0.044
	0.047
	0.072
	0.054

	803
	0.044
	0.046
	0.072
	0.054

	804
	0.044
	0.046
	0.071
	0.054

	805
	0.043
	0.046
	0.071
	0.053

	806
	0.043
	0.045
	0.071
	0.053

	807
	0.043
	0.045
	0.07
	0.053

	808
	0.043
	0.045
	0.07
	0.052

	809
	0.042
	0.045
	0.07
	0.052

	810
	0.042
	0.044
	0.069
	0.052

	811
	0.042
	0.044
	0.069
	0.051

	812
	0.041
	0.044
	0.068
	0.051

	813
	0.041
	0.043
	0.068
	0.051

	814
	0.041
	0.043
	0.067
	0.05

	815
	0.041
	0.043
	0.067
	0.05

	816
	0.04
	0.043
	0.066
	0.05

	817
	0.04
	0.042
	0.066
	0.05

	818
	0.04
	0.042
	0.065
	0.049

	819
	0.04
	0.042
	0.065
	0.049

	820
	0.039
	0.042
	0.065
	0.049

	821
	0.039
	0.042
	0.065
	0.049

	822
	0.039
	0.041
	0.064
	0.048

	823
	0.039
	0.041
	0.064
	0.048

	824
	0.039
	0.041
	0.064
	0.048

	825
	0.038
	0.041
	0.064
	0.047

	826
	0.038
	0.04
	0.063
	0.047

	827
	0.038
	0.04
	0.063
	0.047

	828
	0.038
	0.04
	0.063
	0.047

	829
	0.038
	0.04
	0.062
	0.047

	830
	0.037
	0.039
	0.062
	0.046

	831
	0.037
	0.039
	0.062
	0.046

	832
	0.037
	0.039
	0.062
	0.046

	833
	0.037
	0.039
	0.061
	0.046

	834
	0.037
	0.039
	0.061
	0.045

	835
	0.036
	0.038
	0.061
	0.045

	836
	0.036
	0.038
	0.06
	0.045

	837
	0.036
	0.038
	0.06
	0.045

	838
	0.036
	0.038
	0.06
	0.045

	839
	0.036
	0.037
	0.06
	0.044

	840
	0.035
	0.037
	0.059
	0.044

	841
	0.035
	0.037
	0.059
	0.044

	842
	0.035
	0.037
	0.058
	0.044

	843
	0.035
	0.037
	0.058
	0.043

	844
	0.035
	0.036
	0.058
	0.043

	845
	0.035
	0.036
	0.058
	0.043

	846
	0.034
	0.036
	0.057
	0.043

	847
	0.034
	0.036
	0.057
	0.043

	848
	0.034
	0.036
	0.057
	0.043

	849
	0.034
	0.035
	0.057
	0.042

	850
	0.034
	0.035
	0.056
	0.042

	851
	0.033
	0.035
	0.056
	0.042

	852
	0.033
	0.035
	0.056
	0.042

	853
	0.033
	0.035
	0.056
	0.041

	854
	0.033
	0.035
	0.056
	0.041

	855
	0.033
	0.034
	0.055
	0.041

	856
	0.033
	0.034
	0.055
	0.041

	857
	0.032
	0.034
	0.055
	0.041

	858
	0.032
	0.034
	0.055
	0.041

	859
	0.032
	0.034
	0.055
	0.041

	860
	0.032
	0.034
	0.055
	0.041

	861
	0.032
	0.034
	0.054
	0.041

	862
	0.032
	0.033
	0.054
	0.04

	863
	0.032
	0.033
	0.054
	0.04

	864
	0.032
	0.033
	0.054
	0.04

	865
	0.031
	0.033
	0.053
	0.04

	866
	0.031
	0.032
	0.053
	0.04

	867
	0.031
	0.032
	0.053
	0.04

	868
	0.031
	0.032
	0.053
	0.039

	869
	0.031
	0.032
	0.053
	0.039

	870
	0.031
	0.032
	0.052
	0.039

	871
	0.031
	0.032
	0.053
	0.039

	872
	0.03
	0.031
	0.052
	0.039

	873
	0.03
	0.032
	0.052
	0.039

	874
	0.03
	0.031
	0.051
	0.038

	875
	0.03
	0.031
	0.051
	0.038

	876
	0.03
	0.031
	0.051
	0.038

	877
	0.029
	0.031
	0.051
	0.038

	878
	0.029
	0.031
	0.051
	0.038

	879
	0.029
	0.031
	0.05
	0.037

	880
	0.029
	0.03
	0.05
	0.037

	881
	0.029
	0.03
	0.05
	0.037

	882
	0.029
	0.03
	0.05
	0.037

	883
	0.029
	0.03
	0.05
	0.037

	884
	0.029
	0.03
	0.05
	0.037

	885
	0.029
	0.03
	0.05
	0.037

	886
	0.029
	0.03
	0.05
	0.037

	887
	0.029
	0.029
	0.049
	0.036

	888
	0.028
	0.029
	0.049
	0.036

	889
	0.028
	0.029
	0.049
	0.036

	890
	0.028
	0.029
	0.049
	0.036

	891
	0.028
	0.029
	0.049
	0.036

	892
	0.028
	0.029
	0.049
	0.036

	893
	0.028
	0.029
	0.049
	0.036

	894
	0.028
	0.029
	0.049
	0.036

	895
	0.028
	0.029
	0.048
	0.036

	896
	0.028
	0.028
	0.048
	0.036

	897
	0.028
	0.028
	0.048
	0.036

	898
	0.028
	0.028
	0.048
	0.036

	899
	0.027
	0.028
	0.047
	0.035

	900
	0.027
	0.028
	0.047
	0.035

	901
	0.027
	0.027
	0.047
	0.035

	902
	0.027
	0.027
	0.047
	0.035

	903
	0.027
	0.027
	0.047
	0.035

	904
	0.026
	0.027
	0.046
	0.034

	905
	0.026
	0.027
	0.046
	0.034

	906
	0.026
	0.027
	0.046
	0.034

	907
	0.026
	0.027
	0.046
	0.034

	908
	0.026
	0.027
	0.046
	0.034

	909
	0.026
	0.026
	0.046
	0.034

	910
	0.026
	0.026
	0.045
	0.034

	911
	0.026
	0.026
	0.046
	0.034

	912
	0.026
	0.026
	0.045
	0.033

	913
	0.025
	0.026
	0.045
	0.033

	914
	0.025
	0.026
	0.045
	0.033

	915
	0.025
	0.026
	0.045
	0.033

	916
	0.025
	0.026
	0.045
	0.033

	917
	0.025
	0.026
	0.045
	0.033

	918
	0.025
	0.026
	0.045
	0.033

	919
	0.025
	0.026
	0.045
	0.033

	920
	0.025
	0.026
	0.044
	0.033

	921
	0.025
	0.025
	0.044
	0.033

	922
	0.025
	0.025
	0.044
	0.033

	923
	0.025
	0.025
	0.044
	0.033

	924
	0.025
	0.025
	0.044
	0.033

	925
	0.025
	0.025
	0.044
	0.032

	926
	0.025
	0.025
	0.044
	0.032

	927
	0.025
	0.025
	0.044
	0.033

	928
	0.025
	0.025
	0.044
	0.033

	929
	0.024
	0.024
	0.044
	0.032

	930
	0.024
	0.025
	0.044
	0.032

	931
	0.025
	0.025
	0.044
	0.032

	932
	0.025
	0.025
	0.044
	0.032

	933
	0.024
	0.024
	0.043
	0.032

	934
	0.024
	0.024
	0.043
	0.032

	935
	0.024
	0.024
	0.043
	0.032

	936
	0.024
	0.024
	0.043
	0.032

	937
	0.024
	0.024
	0.043
	0.032

	938
	0.024
	0.024
	0.043
	0.032

	939
	0.024
	0.024
	0.043
	0.032

	940
	0.024
	0.024
	0.043
	0.032

	941
	0.024
	0.024
	0.043
	0.032

	942
	0.024
	0.024
	0.043
	0.032

	943
	0.024
	0.024
	0.043
	0.032

	944
	0.024
	0.024
	0.042
	0.031

	945
	0.024
	0.024
	0.042
	0.032

	946
	0.024
	0.024
	0.043
	0.032

	947
	0.024
	0.024
	0.043
	0.032

	948
	0.024
	0.023
	0.042
	0.032

	949
	0.023
	0.023
	0.042
	0.032

	950
	0.023
	0.023
	0.042
	0.032

	951
	0.023
	0.023
	0.042
	0.032

	952
	0.024
	0.023
	0.043
	0.032

	953
	0.023
	0.023
	0.043
	0.032

	954
	0.023
	0.023
	0.042
	0.031

	955
	0.023
	0.023
	0.042
	0.031

	956
	0.023
	0.023
	0.042
	0.031

	957
	0.023
	0.023
	0.041
	0.031

	958
	0.023
	0.023
	0.041
	0.031

	959
	0.023
	0.023
	0.041
	0.031

	960
	0.022
	0.023
	0.041
	0.031

	961
	0.022
	0.023
	0.04
	0.03

	962
	0.022
	0.023
	0.04
	0.03

	963
	0.022
	0.022
	0.04
	0.03

	964
	0.022
	0.022
	0.04
	0.03

	965
	0.022
	0.022
	0.039
	0.03

	966
	0.022
	0.022
	0.039
	0.029

	967
	0.022
	0.022
	0.039
	0.029

	968
	0.022
	0.022
	0.039
	0.029

	969
	0.021
	0.022
	0.039
	0.029

	970
	0.021
	0.021
	0.038
	0.029

	971
	0.021
	0.021
	0.038
	0.029

	972
	0.021
	0.021
	0.038
	0.029

	973
	0.021
	0.021
	0.038
	0.029

	974
	0.021
	0.021
	0.038
	0.028

	975
	0.021
	0.021
	0.037
	0.028

	976
	0.021
	0.021
	0.037
	0.028

	977
	0.021
	0.021
	0.037
	0.028

	978
	0.021
	0.021
	0.037
	0.028

	979
	0.021
	0.021
	0.037
	0.028

	980
	0.021
	0.021
	0.037
	0.028

	981
	0.021
	0.021
	0.036
	0.028

	982
	0.02
	0.021
	0.036
	0.027

	983
	0.02
	0.021
	0.036
	0.027

	984
	0.02
	0.021
	0.036
	0.027

	985
	0.02
	0.02
	0.036
	0.027

	986
	0.02
	0.02
	0.036
	0.027

	987
	0.02
	0.02
	0.036
	0.027

	988
	0.02
	0.02
	0.036
	0.027

	989
	0.02
	0.02
	0.036
	0.027

	990
	0.02
	0.02
	0.035
	0.026

	991
	0.02
	0.02
	0.035
	0.026

	992
	0.02
	0.02
	0.035
	0.026

	993
	0.02
	0.02
	0.035
	0.026

	994
	0.02
	0.019
	0.035
	0.026

	995
	0.02
	0.019
	0.035
	0.026

	996
	0.019
	0.019
	0.035
	0.026

	997
	0.019
	0.019
	0.035
	0.026

	998
	0.019
	0.019
	0.034
	0.026

	999
	0.019
	0.019
	0.034
	0.026

	1000
	0.02
	0.019
	0.035
	0.026

	1001
	0.019
	0.019
	0.034
	0.026

	1002
	0.019
	0.019
	0.034
	0.026

	1003
	0.019
	0.019
	0.034
	0.026

	1004
	0.019
	0.019
	0.034
	0.025

	1005
	0.019
	0.019
	0.034
	0.025

	1006
	0.019
	0.018
	0.034
	0.025

	1007
	0.019
	0.018
	0.034
	0.025

	1008
	0.019
	0.018
	0.033
	0.025

	1009
	0.019
	0.018
	0.033
	0.025

	1010
	0.019
	0.018
	0.033
	0.025

	1011
	0.019
	0.018
	0.033
	0.025

	1012
	0.019
	0.018
	0.033
	0.024

	1013
	0.019
	0.018
	0.033
	0.025

	1014
	0.018
	0.018
	0.033
	0.025

	1015
	0.018
	0.018
	0.033
	0.024

	1016
	0.018
	0.018
	0.033
	0.024

	1017
	0.018
	0.018
	0.032
	0.024

	1018
	0.018
	0.018
	0.032
	0.024

	1019
	0.018
	0.018
	0.032
	0.024

	1020
	0.018
	0.018
	0.032
	0.024

	1021
	0.018
	0.018
	0.032
	0.024

	1022
	0.018
	0.018
	0.032
	0.024

	1023
	0.018
	0.017
	0.031
	0.024

	1024
	0.018
	0.017
	0.031
	0.024

	1025
	0.018
	0.017
	0.031
	0.024

	1026
	0.018
	0.017
	0.031
	0.024

	1027
	0.018
	0.017
	0.031
	0.024

	1028
	0.018
	0.017
	0.031
	0.024

	1029
	0.018
	0.017
	0.031
	0.023

	1030
	0.018
	0.017
	0.031
	0.023

	1031
	0.018
	0.017
	0.03
	0.023

	1032
	0.018
	0.017
	0.03
	0.023

	1033
	0.018
	0.017
	0.03
	0.023

	1034
	0.017
	0.017
	0.03
	0.023

	1035
	0.017
	0.017
	0.03
	0.023

	1036
	0.017
	0.017
	0.03
	0.023

	1037
	0.017
	0.017
	0.03
	0.023

	1038
	0.017
	0.017
	0.029
	0.023

	1039
	0.017
	0.016
	0.029
	0.023

	1040
	0.017
	0.016
	0.029
	0.022

	1041
	0.017
	0.016
	0.029
	0.022

	1042
	0.017
	0.016
	0.029
	0.022

	1043
	0.017
	0.017
	0.029
	0.023

	1044
	0.017
	0.016
	0.029
	0.022

	1045
	0.017
	0.016
	0.029
	0.022

	1046
	0.017
	0.016
	0.029
	0.022

	1047
	0.017
	0.016
	0.029
	0.022

	1048
	0.017
	0.016
	0.028
	0.022

	1049
	0.017
	0.016
	0.028
	0.022

	1050
	0.017
	0.016
	0.028
	0.022

	1051
	0.017
	0.016
	0.028
	0.022

	1052
	0.016
	0.016
	0.028
	0.022

	1053
	0.017
	0.016
	0.028
	0.022

	1054
	0.017
	0.016
	0.028
	0.022

	1055
	0.017
	0.016
	0.027
	0.021

	1056
	0.016
	0.016
	0.027
	0.021

	1057
	0.016
	0.016
	0.027
	0.021

	1058
	0.016
	0.016
	0.027
	0.021

	1059
	0.016
	0.016
	0.027
	0.021

	1060
	0.016
	0.016
	0.026
	0.021

	1061
	0.016
	0.016
	0.026
	0.021

	1062
	0.016
	0.016
	0.026
	0.021

	1063
	0.016
	0.016
	0.026
	0.021

	1064
	0.016
	0.016
	0.026
	0.021

	1065
	0.016
	0.015
	0.026
	0.021

	1066
	0.016
	0.015
	0.026
	0.02

	1067
	0.016
	0.015
	0.026
	0.02

	1068
	0.016
	0.015
	0.026
	0.02

	1069
	0.016
	0.015
	0.026
	0.02

	1070
	0.016
	0.015
	0.025
	0.02

	1071
	0.016
	0.015
	0.025
	0.02

	1072
	0.016
	0.015
	0.025
	0.02

	1073
	0.016
	0.015
	0.025
	0.02

	1074
	0.016
	0.015
	0.025
	0.02

	1075
	0.015
	0.015
	0.025
	0.02

	1076
	0.015
	0.015
	0.025
	0.02

	1077
	0.015
	0.015
	0.025
	0.02

	1078
	0.016
	0.015
	0.025
	0.02

	1079
	0.015
	0.015
	0.025
	0.02

	1080
	0.015
	0.015
	0.025
	0.02

	1081
	0.015
	0.015
	0.025
	0.02

	1082
	0.015
	0.015
	0.025
	0.02

	1083
	0.015
	0.015
	0.025
	0.02

	1084
	0.015
	0.015
	0.025
	0.02

	1085
	0.015
	0.015
	0.025
	0.02

	1086
	0.015
	0.015
	0.025
	0.02

	1087
	0.015
	0.015
	0.024
	0.02

	1088
	0.015
	0.015
	0.024
	0.02

	1089
	0.015
	0.015
	0.024
	0.02

	1090
	0.015
	0.015
	0.024
	0.02

	1091
	0.015
	0.015
	0.024
	0.02

	1092
	0.015
	0.015
	0.024
	0.02

	1093
	0.015
	0.015
	0.024
	0.019

	1094
	0.015
	0.015
	0.024
	0.019

	1095
	0.015
	0.015
	0.024
	0.019

	1096
	0.015
	0.015
	0.024
	0.019

	1097
	0.015
	0.015
	0.024
	0.019

	1098
	0.015
	0.014
	0.024
	0.019

	1099
	0.015
	0.014
	0.024
	0.019

	1100
	0.015
	0.015
	0.024
	0.019


*SPR represents Surface Plasmon Resonance.


Table S3: FTIR Peaks Position as cm-1 and Transmittance as T%, represents raw data of Table 5.
	Peak Position (cm-1)
	Transmittance (T%)

	4000
	99.4

	3999
	99.4

	3998
	99.4

	3997
	99.39

	3996
	99.39

	3995
	99.39

	3994
	99.39

	3993
	99.38

	3992
	99.37

	3991
	99.36

	3990
	99.36

	3989
	99.35

	3988
	99.35

	3987
	99.35

	3986
	99.36

	3985
	99.36

	3984
	99.37

	3983
	99.36

	3982
	99.36

	3981
	99.35

	3980
	99.34

	3979
	99.33

	3978
	99.33

	3977
	99.33

	3976
	99.34

	3975
	99.35

	3974
	99.35

	3973
	99.35

	3972
	99.35

	3971
	99.33

	3970
	99.31

	3969
	99.29

	3968
	99.27

	3967
	99.27

	3966
	99.27

	3965
	99.27

	3964
	99.28

	3963
	99.29

	3962
	99.29

	3961
	99.29

	3960
	99.28

	3959
	99.28

	3958
	99.28

	3957
	99.28

	3956
	99.29

	3955
	99.29

	3954
	99.3

	3953
	99.29

	3952
	99.29

	3951
	99.28

	3950
	99.28

	3949
	99.27

	3948
	99.26

	3947
	99.25

	3946
	99.25

	3945
	99.25

	3944
	99.26

	3943
	99.26

	3942
	99.25

	3941
	99.25

	3940
	99.26

	3939
	99.27

	3938
	99.28

	3937
	99.3

	3936
	99.31

	3935
	99.32

	3934
	99.31

	3933
	99.3

	3932
	99.28

	3931
	99.26

	3930
	99.25

	3929
	99.24

	3928
	99.24

	3927
	99.25

	3926
	99.25

	3925
	99.25

	3924
	99.25

	3923
	99.24

	3922
	99.23

	3921
	99.23

	3920
	99.24

	3919
	99.25

	3918
	99.25

	3917
	99.26

	3916
	99.26

	3915
	99.27

	3914
	99.28

	3913
	99.29

	3912
	99.29

	3911
	99.3

	3910
	99.31

	3909
	99.32

	3908
	99.32

	3907
	99.31

	3906
	99.3

	3905
	99.27

	3904
	99.25

	3903
	99.22

	3902
	99.19

	3901
	99.17

	3900
	99.15

	3899
	99.15

	3898
	99.15

	3897
	99.16

	3896
	99.16

	3895
	99.16

	3894
	99.16

	3893
	99.18

	3892
	99.2

	3891
	99.23

	3890
	99.25

	3889
	99.26

	3888
	99.25

	3887
	99.23

	3886
	99.22

	3885
	99.21

	3884
	99.2

	3883
	99.2

	3882
	99.2

	3881
	99.2

	3880
	99.21

	3879
	99.22

	3878
	99.24

	3877
	99.24

	3876
	99.24

	3875
	99.24

	3874
	99.23

	3873
	99.22

	3872
	99.21

	3871
	99.2

	3870
	99.2

	3869
	99.2

	3868
	99.2

	3867
	99.2

	3866
	99.2

	3865
	99.19

	3864
	99.19

	3863
	99.19

	3862
	99.19

	3861
	99.19

	3860
	99.2

	3859
	99.21

	3858
	99.21

	3857
	99.21

	3856
	99.2

	3855
	99.19

	3854
	99.19

	3853
	99.19

	3852
	99.19

	3851
	99.19

	3850
	99.2

	3849
	99.2

	3848
	99.2

	3847
	99.21

	3846
	99.21

	3845
	99.22

	3844
	99.21

	3843
	99.21

	3842
	99.2

	3841
	99.2

	3840
	99.19

	3839
	99.19

	3838
	99.19

	3837
	99.19

	3836
	99.19

	3835
	99.19

	3834
	99.2

	3833
	99.21

	3832
	99.23

	3831
	99.24

	3830
	99.24

	3829
	99.23

	3828
	99.22

	3827
	99.21

	3826
	99.21

	3825
	99.22

	3824
	99.23

	3823
	99.24

	3822
	99.23

	3821
	99.22

	3820
	99.21

	3819
	99.19

	3818
	99.17

	3817
	99.14

	3816
	99.13

	3815
	99.12

	3814
	99.13

	3813
	99.13

	3812
	99.12

	3811
	99.12

	3810
	99.13

	3809
	99.13

	3808
	99.13

	3807
	99.12

	3806
	99.11

	3805
	99.11

	3804
	99.1

	3803
	99.09

	3802
	99.08

	3801
	99.08

	3800
	99.09

	3799
	99.1

	3798
	99.11

	3797
	99.12

	3796
	99.15

	3795
	99.17

	3794
	99.18

	3793
	99.17

	3792
	99.15

	3791
	99.12

	3790
	99.1

	3789
	99.08

	3788
	99.07

	3787
	99.06

	3786
	99.06

	3785
	99.05

	3784
	99.04

	3783
	99.03

	3782
	99.02

	3781
	99.01

	3780
	99

	3779
	98.99

	3778
	98.99

	3777
	99

	3776
	99.02

	3775
	99.02

	3774
	99.02

	3773
	99.01

	3772
	99

	3771
	98.98

	3770
	98.96

	3769
	98.96

	3768
	98.95

	3767
	98.95

	3766
	98.94

	3765
	98.93

	3764
	98.92

	3763
	98.91

	3762
	98.91

	3761
	98.9

	3760
	98.9

	3759
	98.88

	3758
	98.87

	3757
	98.84

	3756
	98.82

	3755
	98.8

	3754
	98.78

	3753
	98.76

	3752
	98.76

	3751
	98.76

	3750
	98.77

	3749
	98.79

	3748
	98.8

	3747
	98.8

	3746
	98.78

	3745
	98.75

	3744
	98.73

	3743
	98.72

	3742
	98.7

	3741
	98.68

	3740
	98.66

	3739
	98.66

	3738
	98.68

	3737
	98.68

	3736
	98.66

	3735
	98.62

	3734
	98.58

	3733
	98.53

	3732
	98.51

	3731
	98.5

	3730
	98.5

	3729
	98.48

	3728
	98.43

	3727
	98.38

	3726
	98.34

	3725
	98.32

	3724
	98.31

	3723
	98.31

	3722
	98.32

	3721
	98.32

	3720
	98.32

	3719
	98.3

	3718
	98.28

	3717
	98.27

	3716
	98.24

	3715
	98.2

	3714
	98.15

	3713
	98.11

	3712
	98.08

	3711
	98.02

	3710
	97.93

	3709
	97.84

	3708
	97.78

	3707
	97.77

	3706
	97.78

	3705
	97.77

	3704
	97.74

	3703
	97.69

	3702
	97.64

	3701
	97.59

	3700
	97.52

	3699
	97.44

	3698
	97.34

	3697
	97.25

	3696
	97.2

	3695
	97.16

	3694
	97.11

	3693
	97.03

	3692
	96.92

	3691
	96.81

	3690
	96.7

	3689
	96.61

	3688
	96.53

	3687
	96.45

	3686
	96.35

	3685
	96.24

	3684
	96.12

	3683
	96.01

	3682
	95.92

	3681
	95.81

	3680
	95.7

	3679
	95.58

	3678
	95.47

	3677
	95.35

	3676
	95.23

	3675
	95.1

	3674
	94.96

	3673
	94.79

	3672
	94.59

	3671
	94.37

	3670
	94.17

	3669
	93.99

	3668
	93.84

	3667
	93.7

	3666
	93.57

	3665
	93.45

	3664
	93.34

	3663
	93.22

	3662
	93.09

	3661
	92.96

	3660
	92.82

	3659
	92.65

	3658
	92.47

	3657
	92.29

	3656
	92.11

	3655
	91.94

	3654
	91.77

	3653
	91.59

	3652
	91.43

	3651
	91.28

	3650
	91.15

	3649
	91

	3648
	90.83

	3647
	90.62

	3646
	90.4

	3645
	90.18

	3644
	89.98

	3643
	89.8

	3642
	89.64

	3641
	89.5

	3640
	89.37

	3639
	89.24

	3638
	89.1

	3637
	88.96

	3636
	88.81

	3635
	88.65

	3634
	88.5

	3633
	88.35

	3632
	88.22

	3631
	88.1

	3630
	87.98

	3629
	87.85

	3628
	87.71

	3627
	87.54

	3626
	87.34

	3625
	87.13

	3624
	86.94

	3623
	86.77

	3622
	86.62

	3621
	86.5

	3620
	86.39

	3619
	86.28

	3618
	86.17

	3617
	86.03

	3616
	85.88

	3615
	85.71

	3614
	85.55

	3613
	85.39

	3612
	85.24

	3611
	85.1

	3610
	84.95

	3609
	84.8

	3608
	84.66

	3607
	84.52

	3606
	84.38

	3605
	84.25

	3604
	84.12

	3603
	83.98

	3602
	83.84

	3601
	83.7

	3600
	83.56

	3599
	83.43

	3598
	83.29

	3597
	83.14

	3596
	82.99

	3595
	82.84

	3594
	82.69

	3593
	82.55

	3592
	82.42

	3591
	82.29

	3590
	82.15

	3589
	82.02

	3588
	81.89

	3587
	81.76

	3586
	81.63

	3585
	81.48

	3584
	81.32

	3583
	81.15

	3582
	80.99

	3581
	80.84

	3580
	80.69

	3579
	80.55

	3578
	80.41

	3577
	80.27

	3576
	80.13

	3575
	80

	3574
	79.86

	3573
	79.72

	3572
	79.57

	3571
	79.42

	3570
	79.27

	3569
	79.12

	3568
	78.98

	3567
	78.84

	3566
	78.69

	3565
	78.53

	3564
	78.36

	3563
	78.18

	3562
	78.01

	3561
	77.85

	3560
	77.7

	3559
	77.56

	3558
	77.43

	3557
	77.3

	3556
	77.17

	3555
	77.03

	3554
	76.89

	3553
	76.74

	3552
	76.58

	3551
	76.42

	3550
	76.24

	3549
	76.07

	3548
	75.89

	3547
	75.72

	3546
	75.56

	3545
	75.42

	3544
	75.27

	3543
	75.11

	3542
	74.95

	3541
	74.79

	3540
	74.62

	3539
	74.46

	3538
	74.3

	3537
	74.15

	3536
	74.01

	3535
	73.86

	3534
	73.71

	3533
	73.56

	3532
	73.41

	3531
	73.26

	3530
	73.11

	3529
	72.96

	3528
	72.81

	3527
	72.65

	3526
	72.49

	3525
	72.32

	3524
	72.16

	3523
	71.99

	3522
	71.82

	3521
	71.65

	3520
	71.48

	3519
	71.32

	3518
	71.17

	3517
	71.03

	3516
	70.89

	3515
	70.75

	3514
	70.6

	3513
	70.44

	3512
	70.27

	3511
	70.1

	3510
	69.95

	3509
	69.8

	3508
	69.65

	3507
	69.5

	3506
	69.35

	3505
	69.2

	3504
	69.04

	3503
	68.88

	3502
	68.73

	3501
	68.57

	3500
	68.41

	3499
	68.24

	3498
	68.08

	3497
	67.92

	3496
	67.76

	3495
	67.61

	3494
	67.46

	3493
	67.31

	3492
	67.15

	3491
	67

	3490
	66.86

	3489
	66.72

	3488
	66.58

	3487
	66.43

	3486
	66.28

	3485
	66.11

	3484
	65.95

	3483
	65.79

	3482
	65.63

	3481
	65.48

	3480
	65.33

	3479
	65.18

	3478
	65.02

	3477
	64.86

	3476
	64.7

	3475
	64.54

	3474
	64.39

	3473
	64.24

	3472
	64.09

	3471
	63.95

	3470
	63.8

	3469
	63.65

	3468
	63.5

	3467
	63.34

	3466
	63.17

	3465
	63.01

	3464
	62.85

	3463
	62.69

	3462
	62.54

	3461
	62.38

	3460
	62.24

	3459
	62.09

	3458
	61.95

	3457
	61.8

	3456
	61.64

	3455
	61.48

	3454
	61.32

	3453
	61.17

	3452
	61.03

	3451
	60.89

	3450
	60.74

	3449
	60.6

	3448
	60.46

	3447
	60.32

	3446
	60.17

	3445
	60

	3444
	59.84

	3443
	59.68

	3442
	59.53

	3441
	59.4

	3440
	59.28

	3439
	59.16

	3438
	59.03

	3437
	58.89

	3436
	58.75

	3435
	58.61

	3434
	58.47

	3433
	58.32

	3432
	58.18

	3431
	58.03

	3430
	57.87

	3429
	57.71

	3428
	57.55

	3427
	57.4

	3426
	57.26

	3425
	57.12

	3424
	56.98

	3423
	56.85

	3422
	56.73

	3421
	56.6

	3420
	56.48

	3419
	56.36

	3418
	56.24

	3417
	56.11

	3416
	55.99

	3415
	55.87

	3414
	55.75

	3413
	55.63

	3412
	55.52

	3411
	55.42

	3410
	55.33

	3409
	55.22

	3408
	55.1

	3407
	54.97

	3406
	54.85

	3405
	54.73

	3404
	54.6

	3403
	54.48

	3402
	54.36

	3401
	54.26

	3400
	54.16

	3399
	54.06

	3398
	53.95

	3397
	53.84

	3396
	53.74

	3395
	53.64

	3394
	53.55

	3393
	53.45

	3392
	53.35

	3391
	53.27

	3390
	53.19

	3389
	53.11

	3388
	53.04

	3387
	52.96

	3386
	52.87

	3385
	52.79

	3384
	52.7

	3383
	52.61

	3382
	52.51

	3381
	52.41

	3380
	52.33

	3379
	52.27

	3378
	52.23

	3377
	52.21

	3376
	52.19

	3375
	52.15

	3374
	52.09

	3373
	52.01

	3372
	51.93

	3371
	51.87

	3370
	51.84

	3369
	51.82

	3368
	51.79

	3367
	51.76

	3366
	51.72

	3365
	51.68

	3364
	51.64

	3363
	51.6

	3362
	51.57

	3361
	51.53

	3360
	51.48

	3359
	51.43

	3358
	51.38

	3357
	51.33

	3356
	51.29

	3355
	51.26

	3354
	51.24

	3353
	51.21

	3352
	51.19

	3351
	51.18

	3350
	51.19

	3349
	51.2

	3348
	51.22

	3347
	51.23

	3346
	51.21

	3345
	51.17

	3344
	51.13

	3343
	51.09

	3342
	51.08

	3341
	51.1

	3340
	51.13

	3339
	51.15

	3338
	51.15

	3337
	51.13

	3336
	51.11

	3335
	51.08

	3334
	51.07

	3333
	51.06

	3332
	51.07

	3331
	51.09

	3330
	51.11

	3329
	51.12

	3328
	51.11

	3327
	51.1

	3326
	51.09

	3325
	51.09

	3324
	51.1

	3323
	51.11

	3322
	51.12

	3321
	51.13

	3320
	51.13

	3319
	51.14

	3318
	51.15

	3317
	51.16

	3316
	51.16

	3315
	51.16

	3314
	51.16

	3313
	51.17

	3312
	51.18

	3311
	51.2

	3310
	51.2

	3309
	51.21

	3308
	51.2

	3307
	51.2

	3306
	51.21

	3305
	51.23

	3304
	51.26

	3303
	51.28

	3302
	51.29

	3301
	51.3

	3300
	51.31

	3299
	51.31

	3298
	51.32

	3297
	51.33

	3296
	51.34

	3295
	51.35

	3294
	51.37

	3293
	51.38

	3292
	51.39

	3291
	51.39

	3290
	51.39

	3289
	51.38

	3288
	51.38

	3287
	51.4

	3286
	51.42

	3285
	51.45

	3284
	51.47

	3283
	51.48

	3282
	51.51

	3281
	51.54

	3280
	51.57

	3279
	51.61

	3278
	51.64

	3277
	51.64

	3276
	51.64

	3275
	51.63

	3274
	51.63

	3273
	51.64

	3272
	51.65

	3271
	51.65

	3270
	51.66

	3269
	51.67

	3268
	51.7

	3267
	51.74

	3266
	51.78

	3265
	51.81

	3264
	51.84

	3263
	51.86

	3262
	51.88

	3261
	51.9

	3260
	51.93

	3259
	51.95

	3258
	51.97

	3257
	52

	3256
	52.03

	3255
	52.07

	3254
	52.11

	3253
	52.13

	3252
	52.14

	3251
	52.16

	3250
	52.16

	3249
	52.17

	3248
	52.17

	3247
	52.2

	3246
	52.24

	3245
	52.31

	3244
	52.38

	3243
	52.45

	3242
	52.51

	3241
	52.56

	3240
	52.61

	3239
	52.65

	3238
	52.69

	3237
	52.73

	3236
	52.77

	3235
	52.82

	3234
	52.88

	3233
	52.94

	3232
	52.99

	3231
	53.06

	3230
	53.13

	3229
	53.2

	3228
	53.26

	3227
	53.3

	3226
	53.34

	3225
	53.38

	3224
	53.44

	3223
	53.52

	3222
	53.64

	3221
	53.76

	3220
	53.87

	3219
	53.96

	3218
	54.04

	3217
	54.12

	3216
	54.22

	3215
	54.34

	3214
	54.45

	3213
	54.56

	3212
	54.66

	3211
	54.77

	3210
	54.88

	3209
	55.02

	3208
	55.15

	3207
	55.29

	3206
	55.41

	3205
	55.53

	3204
	55.64

	3203
	55.75

	3202
	55.86

	3201
	55.96

	3200
	56.08

	3199
	56.21

	3198
	56.36

	3197
	56.51

	3196
	56.67

	3195
	56.81

	3194
	56.95

	3193
	57.08

	3192
	57.22

	3191
	57.37

	3190
	57.52

	3189
	57.69

	3188
	57.86

	3187
	58.04

	3186
	58.21

	3185
	58.38

	3184
	58.55

	3183
	58.7

	3182
	58.85

	3181
	59

	3180
	59.17

	3179
	59.35

	3178
	59.55

	3177
	59.74

	3176
	59.93

	3175
	60.1

	3174
	60.27

	3173
	60.45

	3172
	60.64

	3171
	60.82

	3170
	61

	3169
	61.16

	3168
	61.32

	3167
	61.49

	3166
	61.67

	3165
	61.86

	3164
	62.06

	3163
	62.28

	3162
	62.49

	3161
	62.71

	3160
	62.93

	3159
	63.13

	3158
	63.32

	3157
	63.5

	3156
	63.67

	3155
	63.85

	3154
	64.04

	3153
	64.23

	3152
	64.43

	3151
	64.65

	3150
	64.87

	3149
	65.1

	3148
	65.31

	3147
	65.51

	3146
	65.71

	3145
	65.9

	3144
	66.09

	3143
	66.28

	3142
	66.48

	3141
	66.69

	3140
	66.9

	3139
	67.11

	3138
	67.32

	3137
	67.53

	3136
	67.76

	3135
	67.99

	3134
	68.22

	3133
	68.44

	3132
	68.64

	3131
	68.83

	3130
	69.02

	3129
	69.23

	3128
	69.43

	3127
	69.63

	3126
	69.83

	3125
	70.01

	3124
	70.2

	3123
	70.4

	3122
	70.61

	3121
	70.83

	3120
	71.05

	3119
	71.26

	3118
	71.45

	3117
	71.63

	3116
	71.82

	3115
	72.01

	3114
	72.22

	3113
	72.44

	3112
	72.65

	3111
	72.84

	3110
	73.03

	3109
	73.21

	3108
	73.39

	3107
	73.58

	3106
	73.79

	3105
	74.01

	3104
	74.23

	3103
	74.45

	3102
	74.66

	3101
	74.85

	3100
	75.03

	3099
	75.22

	3098
	75.42

	3097
	75.62

	3096
	75.81

	3095
	76

	3094
	76.19

	3093
	76.37

	3092
	76.54

	3091
	76.71

	3090
	76.87

	3089
	77.03

	3088
	77.19

	3087
	77.36

	3086
	77.55

	3085
	77.74

	3084
	77.93

	3083
	78.11

	3082
	78.27

	3081
	78.43

	3080
	78.59

	3079
	78.77

	3078
	78.96

	3077
	79.17

	3076
	79.38

	3075
	79.58

	3074
	79.77

	3073
	79.94

	3072
	80.11

	3071
	80.28

	3070
	80.43

	3069
	80.57

	3068
	80.71

	3067
	80.87

	3066
	81.02

	3065
	81.18

	3064
	81.34

	3063
	81.49

	3062
	81.64

	3061
	81.8

	3060
	81.97

	3059
	82.14

	3058
	82.33

	3057
	82.52

	3056
	82.69

	3055
	82.83

	3054
	82.95

	3053
	83.08

	3052
	83.21

	3051
	83.36

	3050
	83.5

	3049
	83.63

	3048
	83.75

	3047
	83.85

	3046
	83.96

	3045
	84.09

	3044
	84.23

	3043
	84.38

	3042
	84.53

	3041
	84.7

	3040
	84.85

	3039
	84.99

	3038
	85.09

	3037
	85.2

	3036
	85.31

	3035
	85.44

	3034
	85.58

	3033
	85.71

	3032
	85.83

	3031
	85.93

	3030
	86.02

	3029
	86.13

	3028
	86.24

	3027
	86.35

	3026
	86.45

	3025
	86.55

	3024
	86.67

	3023
	86.79

	3022
	86.91

	3021
	87.04

	3020
	87.16

	3019
	87.26

	3018
	87.36

	3017
	87.44

	3016
	87.51

	3015
	87.59

	3014
	87.68

	3013
	87.79

	3012
	87.91

	3011
	88.03

	3010
	88.15

	3009
	88.24

	3008
	88.32

	3007
	88.4

	3006
	88.47

	3005
	88.53

	3004
	88.58

	3003
	88.62

	3002
	88.68

	3001
	88.75

	3000
	88.83

	2999
	88.93

	2998
	89.01

	2997
	89.09

	2996
	89.16

	2995
	89.23

	2994
	89.31

	2993
	89.4

	2992
	89.5

	2991
	89.58

	2990
	89.65

	2989
	89.71

	2988
	89.77

	2987
	89.82

	2986
	89.89

	2985
	89.98

	2984
	90.07

	2983
	90.14

	2982
	90.21

	2981
	90.26

	2980
	90.33

	2979
	90.41

	2978
	90.5

	2977
	90.58

	2976
	90.67

	2975
	90.75

	2974
	90.84

	2973
	90.93

	2972
	91.02

	2971
	91.1

	2970
	91.16

	2969
	91.22

	2968
	91.28

	2967
	91.35

	2966
	91.43

	2965
	91.51

	2964
	91.6

	2963
	91.67

	2962
	91.74

	2961
	91.79

	2960
	91.85

	2959
	91.91

	2958
	91.98

	2957
	92.06

	2956
	92.15

	2955
	92.24

	2954
	92.32

	2953
	92.38

	2952
	92.43

	2951
	92.48

	2950
	92.55

	2949
	92.63

	2948
	92.72

	2947
	92.81

	2946
	92.89

	2945
	92.96

	2944
	93.03

	2943
	93.08

	2942
	93.13

	2941
	93.18

	2940
	93.23

	2939
	93.28

	2938
	93.34

	2937
	93.4

	2936
	93.45

	2935
	93.49

	2934
	93.52

	2933
	93.56

	2932
	93.6

	2931
	93.66

	2930
	93.72

	2929
	93.78

	2928
	93.84

	2927
	93.89

	2926
	93.93

	2925
	93.98

	2924
	94.03

	2923
	94.1

	2922
	94.16

	2921
	94.21

	2920
	94.26

	2919
	94.29

	2918
	94.34

	2917
	94.38

	2916
	94.44

	2915
	94.51

	2914
	94.58

	2913
	94.64

	2912
	94.68

	2911
	94.72

	2910
	94.75

	2909
	94.78

	2908
	94.81

	2907
	94.83

	2906
	94.85

	2905
	94.87

	2904
	94.91

	2903
	94.95

	2902
	95

	2901
	95.04

	2900
	95.08

	2899
	95.12

	2898
	95.16

	2897
	95.2

	2896
	95.26

	2895
	95.32

	2894
	95.38

	2893
	95.43

	2892
	95.47

	2891
	95.5

	2890
	95.54

	2889
	95.58

	2888
	95.62

	2887
	95.67

	2886
	95.71

	2885
	95.74

	2884
	95.77

	2883
	95.79

	2882
	95.83

	2881
	95.87

	2880
	95.93

	2879
	95.98

	2878
	96.02

	2877
	96.05

	2876
	96.08

	2875
	96.11

	2874
	96.14

	2873
	96.17

	2872
	96.21

	2871
	96.24

	2870
	96.28

	2869
	96.32

	2868
	96.36

	2867
	96.39

	2866
	96.43

	2865
	96.46

	2864
	96.5

	2863
	96.52

	2862
	96.55

	2861
	96.58

	2860
	96.61

	2859
	96.65

	2858
	96.69

	2857
	96.73

	2856
	96.78

	2855
	96.82

	2854
	96.86

	2853
	96.89

	2852
	96.92

	2851
	96.95

	2850
	96.99

	2849
	97.02

	2848
	97.06

	2847
	97.08

	2846
	97.11

	2845
	97.15

	2844
	97.19

	2843
	97.22

	2842
	97.24

	2841
	97.26

	2840
	97.28

	2839
	97.32

	2838
	97.35

	2837
	97.38

	2836
	97.41

	2835
	97.43

	2834
	97.45

	2833
	97.47

	2832
	97.49

	2831
	97.51

	2830
	97.55

	2829
	97.58

	2828
	97.6

	2827
	97.62

	2826
	97.63

	2825
	97.65

	2824
	97.66

	2823
	97.66

	2822
	97.67

	2821
	97.69

	2820
	97.71

	2819
	97.75

	2818
	97.78

	2817
	97.8

	2816
	97.82

	2815
	97.83

	2814
	97.84

	2813
	97.86

	2812
	97.88

	2811
	97.9

	2810
	97.91

	2809
	97.93

	2808
	97.94

	2807
	97.97

	2806
	97.99

	2805
	98.01

	2804
	98.03

	2803
	98.04

	2802
	98.05

	2801
	98.07

	2800
	98.09

	2799
	98.11

	2798
	98.13

	2797
	98.15

	2796
	98.16

	2795
	98.17

	2794
	98.18

	2793
	98.19

	2792
	98.2

	2791
	98.22

	2790
	98.23

	2789
	98.25

	2788
	98.27

	2787
	98.28

	2786
	98.3

	2785
	98.31

	2784
	98.33

	2783
	98.34

	2782
	98.35

	2781
	98.36

	2780
	98.37

	2779
	98.39

	2778
	98.4

	2777
	98.42

	2776
	98.43

	2775
	98.45

	2774
	98.45

	2773
	98.46

	2772
	98.47
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	99.36

	1877
	99.39

	1876
	99.41

	1875
	99.42

	1874
	99.41

	1873
	99.41

	1872
	99.41

	1871
	99.4

	1870
	99.39

	1869
	99.38

	1868
	99.37

	1867
	99.36

	1866
	99.37

	1865
	99.38

	1864
	99.39

	1863
	99.39

	1862
	99.38

	1861
	99.39

	1860
	99.39

	1859
	99.39

	1858
	99.4

	1857
	99.4

	1856
	99.39

	1855
	99.39

	1854
	99.39

	1853
	99.39

	1852
	99.39

	1851
	99.4

	1850
	99.4

	1849
	99.4

	1848
	99.4

	1847
	99.4

	1846
	99.4

	1845
	99.4

	1844
	99.4

	1843
	99.4

	1842
	99.4

	1841
	99.4

	1840
	99.4

	1839
	99.4

	1838
	99.4

	1837
	99.4

	1836
	99.4

	1835
	99.4

	1834
	99.4

	1833
	99.4

	1832
	99.4

	1831
	99.4

	1830
	99.4

	1829
	99.4

	1828
	99.4

	1827
	99.4

	1826
	99.4

	1825
	99.4

	1824
	99.4

	1823
	99.4

	1822
	99.39

	1821
	99.39

	1820
	99.39

	1819
	99.39

	1818
	99.39

	1817
	99.38

	1816
	99.38

	1815
	99.38

	1814
	99.37

	1813
	99.37

	1812
	99.36

	1811
	99.36

	1810
	99.35

	1809
	99.35

	1808
	99.33

	1807
	99.32

	1806
	99.31

	1805
	99.3

	1804
	99.29

	1803
	99.28

	1802
	99.27

	1801
	99.27

	1800
	99.27

	1799
	99.27

	1798
	99.27

	1797
	99.27

	1796
	99.25

	1795
	99.23

	1794
	99.2

	1793
	99.17

	1792
	99.14

	1791
	99.12

	1790
	99.12

	1789
	99.12

	1788
	99.12

	1787
	99.11

	1786
	99.1

	1785
	99.08

	1784
	99.06

	1783
	99.04

	1782
	99.01

	1781
	98.98

	1780
	98.95

	1779
	98.93

	1778
	98.92

	1777
	98.9

	1776
	98.87

	1775
	98.83

	1774
	98.79

	1773
	98.76

	1772
	98.77

	1771
	98.79

	1770
	98.8

	1769
	98.77

	1768
	98.71

	1767
	98.66

	1766
	98.63

	1765
	98.63

	1764
	98.62

	1763
	98.59

	1762
	98.53

	1761
	98.47

	1760
	98.43

	1759
	98.39

	1758
	98.34

	1757
	98.3

	1756
	98.27

	1755
	98.25

	1754
	98.21

	1753
	98.12

	1752
	98.02

	1751
	97.93

	1750
	97.88

	1749
	97.86

	1748
	97.85

	1747
	97.83

	1746
	97.78

	1745
	97.7

	1744
	97.62

	1743
	97.55

	1742
	97.51

	1741
	97.5

	1740
	97.5

	1739
	97.47

	1738
	97.39

	1737
	97.27

	1736
	97.11

	1735
	96.92

	1734
	96.76

	1733
	96.67

	1732
	96.62

	1731
	96.54

	1730
	96.45

	1729
	96.38

	1728
	96.33

	1727
	96.26

	1726
	96.16

	1725
	96.06

	1724
	95.94

	1723
	95.81

	1722
	95.65

	1721
	95.5

	1720
	95.37

	1719
	95.25

	1718
	95.12

	1717
	94.95

	1716
	94.74

	1715
	94.5

	1714
	94.31

	1713
	94.19

	1712
	94.09

	1711
	93.97

	1710
	93.81

	1709
	93.63

	1708
	93.45

	1707
	93.25

	1706
	93.06

	1705
	92.87

	1704
	92.68

	1703
	92.47

	1702
	92.27

	1701
	92.06

	1700
	91.82

	1699
	91.53

	1698
	91.19

	1697
	90.86

	1696
	90.58

	1695
	90.29

	1694
	90.01

	1693
	89.74

	1692
	89.48

	1691
	89.24

	1690
	88.99

	1689
	88.72

	1688
	88.45

	1687
	88.19

	1686
	87.94

	1685
	87.68

	1684
	87.39

	1683
	87.01

	1682
	86.59

	1681
	86.22

	1680
	85.9

	1679
	85.61

	1678
	85.33

	1677
	85.07

	1676
	84.83

	1675
	84.56

	1674
	84.24

	1673
	83.88

	1672
	83.53

	1671
	83.21

	1670
	82.91

	1669
	82.58

	1668
	82.22

	1667
	81.84

	1666
	81.51

	1665
	81.23

	1664
	81

	1663
	80.76

	1662
	80.46

	1661
	80.12

	1660
	79.78

	1659
	79.47

	1658
	79.21

	1657
	78.98

	1656
	78.81

	1655
	78.69

	1654
	78.57

	1653
	78.32

	1652
	77.79

	1651
	77.11

	1650
	76.68

	1649
	76.56

	1648
	76.57

	1647
	76.52

	1646
	76.29

	1645
	75.92

	1644
	75.57

	1643
	75.34

	1642
	75.22

	1641
	75.18

	1640
	75.18

	1639
	75.18

	1638
	75.2

	1637
	75.23

	1636
	75.25

	1635
	75.17

	1634
	75.02

	1633
	74.9

	1632
	74.91

	1631
	75.02

	1630
	75.19

	1629
	75.39

	1628
	75.61

	1627
	75.82

	1626
	76.01

	1625
	76.21

	1624
	76.45

	1623
	76.71

	1622
	76.97

	1621
	77.21

	1620
	77.48

	1619
	77.82

	1618
	78.19

	1617
	78.56

	1616
	78.9

	1615
	79.22

	1614
	79.54

	1613
	79.91

	1612
	80.32

	1611
	80.75

	1610
	81.14

	1609
	81.49

	1608
	81.81

	1607
	82.14

	1606
	82.47

	1605
	82.81

	1604
	83.14

	1603
	83.48

	1602
	83.84

	1601
	84.2

	1600
	84.55

	1599
	84.89

	1598
	85.23

	1597
	85.56

	1596
	85.87

	1595
	86.15

	1594
	86.41

	1593
	86.67

	1592
	86.95

	1591
	87.25

	1590
	87.54

	1589
	87.82

	1588
	88.07

	1587
	88.29

	1586
	88.49

	1585
	88.68

	1584
	88.87

	1583
	89.09

	1582
	89.32

	1581
	89.55

	1580
	89.76

	1579
	89.96

	1578
	90.13

	1577
	90.25

	1576
	90.33

	1575
	90.42

	1574
	90.57

	1573
	90.75

	1572
	90.92

	1571
	91.09

	1570
	91.26

	1569
	91.43

	1568
	91.59

	1567
	91.7

	1566
	91.79

	1565
	91.89

	1564
	92.02

	1563
	92.18

	1562
	92.32

	1561
	92.43

	1560
	92.53

	1559
	92.67

	1558
	92.79

	1557
	92.86

	1556
	92.92

	1555
	92.98

	1554
	93.05

	1553
	93.13

	1552
	93.22

	1551
	93.33

	1550
	93.41

	1549
	93.48

	1548
	93.54

	1547
	93.63

	1546
	93.72

	1545
	93.8

	1544
	93.86

	1543
	93.89

	1542
	93.9

	1541
	93.91

	1540
	93.9

	1539
	93.9

	1538
	93.95

	1537
	94.04

	1536
	94.14

	1535
	94.26

	1534
	94.39

	1533
	94.52

	1532
	94.64

	1531
	94.71

	1530
	94.73

	1529
	94.72

	1528
	94.73

	1527
	94.75

	1526
	94.79

	1525
	94.84

	1524
	94.89

	1523
	94.95

	1522
	95

	1521
	95.05

	1520
	95.11

	1519
	95.16

	1518
	95.2

	1517
	95.22

	1516
	95.24

	1515
	95.26

	1514
	95.29

	1513
	95.33

	1512
	95.36

	1511
	95.4

	1510
	95.43

	1509
	95.46

	1508
	95.5

	1507
	95.55

	1506
	95.59

	1505
	95.62

	1504
	95.64

	1503
	95.66

	1502
	95.7

	1501
	95.73

	1500
	95.77

	1499
	95.82

	1498
	95.87

	1497
	95.9

	1496
	95.92

	1495
	95.94

	1494
	95.97

	1493
	96

	1492
	96.03

	1491
	96.06

	1490
	96.09

	1489
	96.12

	1488
	96.14

	1487
	96.16

	1486
	96.19

	1485
	96.23

	1484
	96.26

	1483
	96.28

	1482
	96.3

	1481
	96.32

	1480
	96.34

	1479
	96.36

	1478
	96.39

	1477
	96.41

	1476
	96.44

	1475
	96.46

	1474
	96.48

	1473
	96.51

	1472
	96.54

	1471
	96.57

	1470
	96.59

	1469
	96.61

	1468
	96.62

	1467
	96.63

	1466
	96.65

	1465
	96.67

	1464
	96.69

	1463
	96.7

	1462
	96.72

	1461
	96.75

	1460
	96.77

	1459
	96.8

	1458
	96.82

	1457
	96.84

	1456
	96.84

	1455
	96.85

	1454
	96.86

	1453
	96.87

	1452
	96.9

	1451
	96.92

	1450
	96.94

	1449
	96.96

	1448
	96.97

	1447
	97

	1446
	97.02

	1445
	97.05

	1444
	97.06

	1443
	97.08

	1442
	97.09

	1441
	97.1

	1440
	97.11

	1439
	97.12

	1438
	97.13

	1437
	97.15

	1436
	97.17

	1435
	97.18

	1434
	97.18

	1433
	97.19

	1432
	97.2

	1431
	97.21

	1430
	97.23

	1429
	97.25

	1428
	97.27

	1427
	97.29

	1426
	97.3

	1425
	97.31

	1424
	97.31

	1423
	97.32

	1422
	97.33

	1421
	97.33

	1420
	97.33

	1419
	97.33

	1418
	97.34

	1417
	97.36

	1416
	97.38

	1415
	97.39

	1414
	97.4

	1413
	97.41

	1412
	97.41

	1411
	97.42

	1410
	97.42

	1409
	97.43

	1408
	97.44

	1407
	97.46

	1406
	97.47

	1405
	97.48

	1404
	97.49

	1403
	97.5

	1402
	97.5

	1401
	97.51

	1400
	97.52

	1399
	97.54

	1398
	97.55

	1397
	97.55

	1396
	97.56

	1395
	97.56

	1394
	97.56

	1393
	97.57

	1392
	97.6

	1391
	97.62

	1390
	97.64

	1389
	97.65

	1388
	97.67

	1387
	97.68

	1386
	97.7

	1385
	97.71

	1384
	97.73

	1383
	97.74

	1382
	97.74

	1381
	97.75

	1380
	97.75

	1379
	97.76

	1378
	97.77

	1377
	97.79

	1376
	97.81

	1375
	97.83

	1374
	97.85

	1373
	97.87

	1372
	97.88

	1371
	97.89

	1370
	97.91

	1369
	97.93

	1368
	97.95

	1367
	97.97

	1366
	97.98

	1365
	97.99

	1364
	98

	1363
	98.01

	1362
	98.02

	1361
	98.04

	1360
	98.06

	1359
	98.07

	1358
	98.09

	1357
	98.1

	1356
	98.11

	1355
	98.12

	1354
	98.14

	1353
	98.15

	1352
	98.17

	1351
	98.18

	1350
	98.19

	1349
	98.21

	1348
	98.22

	1347
	98.23

	1346
	98.24

	1345
	98.25

	1344
	98.26

	1343
	98.28

	1342
	98.29

	1341
	98.3

	1340
	98.31

	1339
	98.33

	1338
	98.34

	1337
	98.35

	1336
	98.36

	1335
	98.37

	1334
	98.39

	1333
	98.4

	1332
	98.41

	1331
	98.42

	1330
	98.43

	1329
	98.44

	1328
	98.45

	1327
	98.47

	1326
	98.48

	1325
	98.49

	1324
	98.5

	1323
	98.51

	1322
	98.52

	1321
	98.53

	1320
	98.54

	1319
	98.55

	1318
	98.55

	1317
	98.56

	1316
	98.57

	1315
	98.58

	1314
	98.59

	1313
	98.61

	1312
	98.63

	1311
	98.64

	1310
	98.66

	1309
	98.66

	1308
	98.67

	1307
	98.68

	1306
	98.69

	1305
	98.7

	1304
	98.71

	1303
	98.71

	1302
	98.73

	1301
	98.74

	1300
	98.75

	1299
	98.76

	1298
	98.77

	1297
	98.77

	1296
	98.77

	1295
	98.77

	1294
	98.78

	1293
	98.78

	1292
	98.78

	1291
	98.79

	1290
	98.79

	1289
	98.8

	1288
	98.8

	1287
	98.81

	1286
	98.82

	1285
	98.83

	1284
	98.83

	1283
	98.84

	1282
	98.85

	1281
	98.87

	1280
	98.88

	1279
	98.89

	1278
	98.9

	1277
	98.9

	1276
	98.9

	1275
	98.9

	1274
	98.91

	1273
	98.91

	1272
	98.91

	1271
	98.92

	1270
	98.93

	1269
	98.94

	1268
	98.94

	1267
	98.95

	1266
	98.95

	1265
	98.95

	1264
	98.96

	1263
	98.96

	1262
	98.97

	1261
	98.97

	1260
	98.98

	1259
	98.98

	1258
	98.98

	1257
	98.99

	1256
	98.99

	1255
	99

	1254
	99

	1253
	99.01

	1252
	99.01

	1251
	99.01

	1250
	99.02

	1249
	99.02

	1248
	99.03

	1247
	99.04

	1246
	99.05

	1245
	99.06

	1244
	99.07

	1243
	99.07

	1242
	99.07

	1241
	99.07

	1240
	99.08

	1239
	99.08

	1238
	99.09

	1237
	99.09

	1236
	99.09

	1235
	99.1

	1234
	99.11

	1233
	99.12

	1232
	99.12

	1231
	99.13

	1230
	99.12

	1229
	99.12

	1228
	99.11

	1227
	99.11

	1226
	99.12

	1225
	99.12

	1224
	99.13

	1223
	99.14

	1222
	99.13

	1221
	99.13

	1220
	99.13

	1219
	99.13

	1218
	99.13

	1217
	99.15

	1216
	99.17

	1215
	99.19

	1214
	99.2

	1213
	99.21

	1212
	99.21

	1211
	99.21

	1210
	99.21

	1209
	99.21

	1208
	99.21

	1207
	99.21

	1206
	99.21

	1205
	99.21

	1204
	99.21

	1203
	99.21

	1202
	99.2

	1201
	99.19

	1200
	99.2

	1199
	99.21

	1198
	99.22

	1197
	99.23

	1196
	99.24

	1195
	99.24

	1194
	99.24

	1193
	99.24

	1192
	99.24

	1191
	99.24

	1190
	99.25

	1189
	99.26

	1188
	99.26

	1187
	99.27

	1186
	99.27

	1185
	99.27

	1184
	99.26

	1183
	99.24

	1182
	99.22

	1181
	99.21

	1180
	99.21

	1179
	99.21

	1178
	99.22

	1177
	99.24

	1176
	99.25

	1175
	99.26

	1174
	99.28

	1173
	99.29

	1172
	99.3

	1171
	99.29

	1170
	99.29

	1169
	99.3

	1168
	99.31

	1167
	99.32

	1166
	99.33

	1165
	99.32

	1164
	99.31

	1163
	99.3

	1162
	99.29

	1161
	99.3

	1160
	99.33

	1159
	99.36

	1158
	99.39

	1157
	99.42

	1156
	99.43

	1155
	99.42

	1154
	99.41

	1153
	99.39

	1152
	99.38

	1151
	99.38

	1150
	99.38

	1149
	99.38

	1148
	99.4

	1147
	99.42

	1146
	99.42

	1145
	99.41

	1144
	99.39

	1143
	99.37

	1142
	99.36

	1141
	99.34

	1140
	99.33

	1139
	99.33

	1138
	99.35

	1137
	99.36

	1136
	99.36

	1135
	99.36

	1134
	99.36

	1133
	99.37

	1132
	99.37

	1131
	99.37

	1130
	99.35

	1129
	99.33

	1128
	99.32

	1127
	99.32

	1126
	99.31

	1125
	99.31

	1124
	99.3

	1123
	99.29

	1122
	99.27

	1121
	99.24

	1120
	99.22

	1119
	99.2

	1118
	99.18

	1117
	99.17

	1116
	99.17

	1115
	99.15

	1114
	99.13

	1113
	99.1

	1112
	99.08

	1111
	99.07

	1110
	99.06

	1109
	99.05

	1108
	99.04

	1107
	99.02

	1106
	99

	1105
	98.99

	1104
	98.96

	1103
	98.94

	1102
	98.92

	1101
	98.91

	1100
	98.91

	1099
	98.9

	1098
	98.89

	1097
	98.87

	1096
	98.85

	1095
	98.81

	1094
	98.77

	1093
	98.73

	1092
	98.71

	1091
	98.7

	1090
	98.7

	1089
	98.69

	1088
	98.66

	1087
	98.62

	1086
	98.58

	1085
	98.55

	1084
	98.55

	1083
	98.55

	1082
	98.52

	1081
	98.46

	1080
	98.4

	1079
	98.36

	1078
	98.36

	1077
	98.36

	1076
	98.35

	1075
	98.34

	1074
	98.32

	1073
	98.31

	1072
	98.31

	1071
	98.31

	1070
	98.31

	1069
	98.3

	1068
	98.27

	1067
	98.23

	1066
	98.19

	1065
	98.18

	1064
	98.19

	1063
	98.2

	1062
	98.2

	1061
	98.18

	1060
	98.15

	1059
	98.13

	1058
	98.11

	1057
	98.09

	1056
	98.1

	1055
	98.14

	1054
	98.2

	1053
	98.25

	1052
	98.29

	1051
	98.31

	1050
	98.31

	1049
	98.32

	1048
	98.35

	1047
	98.39

	1046
	98.43

	1045
	98.46

	1044
	98.49

	1043
	98.53

	1042
	98.59

	1041
	98.65

	1040
	98.69

	1039
	98.72

	1038
	98.73

	1037
	98.74

	1036
	98.73

	1035
	98.71

	1034
	98.66

	1033
	98.61

	1032
	98.62

	1031
	98.69

	1030
	98.79

	1029
	98.87

	1028
	98.92

	1027
	98.95

	1026
	98.99

	1025
	99.03

	1024
	99.05

	1023
	99.06

	1022
	99.04

	1021
	99.04

	1020
	99.05

	1019
	99.07

	1018
	99.09

	1017
	99.09

	1016
	99.09

	1015
	99.1

	1014
	99.11

	1013
	99.12

	1012
	99.13

	1011
	99.13

	1010
	99.15

	1009
	99.16

	1008
	99.16

	1007
	99.16

	1006
	99.16

	1005
	99.17

	1004
	99.18

	1003
	99.17

	1002
	99.15

	1001
	99.14

	1000
	99.14

	999
	99.17

	998
	99.21

	997
	99.24

	996
	99.26

	995
	99.27

	994
	99.29

	993
	99.31

	992
	99.34
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