Supplementary Material

Statistical optimization for removal of basic dyes from aqueous solutions using chitosan-assembled zinc oxide nanocomposite

Tables captions

Table S1. The removal of BB41 and BR46.

Table S2. Optimum conditions of variables.

Figures captions

Fig. S1. a) FTIR, b) SEM, c) pHpzc, d) XRD, and e) BET of CTS/ZnO.

Fig. S2. Normal probability for a) BB41 and b) BR46; Correlation between experimental and predicted values for c) BB41 and d) BR46.

Table S1. The removal of BB41 and BR46.

|  | Variables |  |  |  | %R of BB41 |  | %R of BR46 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Run | CTS/ZnO dosage (g) | Solution pH | Initial concentration (mg L-1) | Ultrasound contact time (min) | Experimental | Predicted | Experimental | Predicted |  |
| 1 | 0.15 | 7 | 30 | 30 | 86.10 | 87.85 | 81.37 | 83.01 |  |
| 2 | 0.2 | 5 | 40 | 40 | 60.67 | 62.46 | 52.51 | 51.14 |  |
| 3 | 0.05 | 7 | 30 | 30 | 40.05 | 38.26 | 35.83 | 35.33 |  |
| 4 | 0.25 | 7 | 30 | 30 | 82.90 | 81.18 | 71.65 | 70.43 |  |
| 5 | 0.2 | 5 | 40 | 20 | 42.59 | 42.81 | 38.79 | 40.49 |  |
| 6 | 0.1 | 9 | 40 | 20 | 36.94 | 39.35 | 45.06 | 47.43 |  |
| 7 | 0.1 | 5 | 40 | 20 | 33.00 | 31.19 | 29.63 | 27.85 |  |
| 8 | 0.15 | 7 | 30 | 30 | 87.48 | 87.85 | 81.73 | 83.01 |  |
| 9 | 0.15 | 7 | 30 | 30 | 85.86 | 87.85 | 85.55 | 83.01 |  |
| 10 | 0.15 | 11 | 30 | 30 | 70.49 | 68.13 | 68.52 | 67.62 |  |
| 11 | 0.1 | 5 | 20 | 40 | 56.93 | 56.18 | 55.69 | 55.82 |  |
| 12 | 0.15 | 7 | 30 | 10 | 54.55 | 53.71 | 55.97 | 54.12 |  |
| 13 | 0.2 | 9 | 40 | 20 | 59.29 | 60.32 | 62.27 | 62.43 |  |
| 14 | 0.1 | 9 | 40 | 40 | 47.74 | 47.98 | 52.34 | 49.99 |  |
| 15 | 0.1 | 9 | 20 | 40 | 62.46 | 65.47 | 66.76 | 66.49 |  |
| 16 | 0.2 | 9 | 20 | 40 | 94.67 | 96.76 | 86.88 | 88.95 |  |
| 17 | 0.1 | 5 | 20 | 20 | 51.14 | 54.68 | 44.60 | 44.70 |  |
| 18 | 0.2 | 5 | 20 | 40 | 77.31 | 78.13 | 76.84 | 75.90 |  |
| 19 | 0.1 | 9 | 20 | 20 | 65.13 | 63.62 | 58.04 | 59.70 |  |
| 20 | 0.15 | 7 | 30 | 30 | 87.76 | 87.85 | 81.92 | 83.01 |  |
| 21 | 0.15 | 7 | 50 | 30 | 44.01 | 43.00 | 43.52 | 42.91 |  |
| 22 | 0.15 | 7 | 30 | 30 | 91.10 | 87.85 | 82.31 | 83.01 |  |
| 23 | 0.15 | 7 | 30 | 50 | 77.89 | 75.22 | 71.44 | 71.57 |  |
| 24 | 0.15 | 7 | 30 | 30 | 88.78 | 87.85 | 85.19 | 83.01 |  |
| 25 | 0.2 | 9 | 20 | 20 | 82.25 | 83.52 | 79.83 | 78.39 |  |
| 26 | 0.1 | 5 | 40 | 40 | 37.50 | 39.46 | 31.88 | 34.75 |  |
| 27 | 0.15 | 7 | 10 | 30 | 85.43 | 82.93 | 81.05 | 79.94 |  |
| 28 | 0.2 | 5 | 20 | 20 | 65.21 | 65.25 | 58.39 | 61.03 |  |
| 29 | 0.2 | 9 | 40 | 40 | 80.63 | 80.32 | 67.43 | 68.76 |  |
| 30 | 0.15 | 3 | 30 | 30 | 42.49 | 41.34 | 35.82 | 35.00 |  |

| a) | b) |
| --- | --- |
|  | d) |
| e) |  |
| Fig. S1. a) FTIR, b) SEM, c) pHpzc, d) XRD, and e) BET of CTS/ZnO. |  |

c)

| a) b) |  |
| --- | --- |
| c) | d) |
| Fig. S2. Normal probability for a) BB41 and b) BR46; Correlation between experimental and predicted values for c) BB41 and d) BR46. |  |

Table S2. Optimum conditions of variables.

| Optimal conditions |  |  |  | %R of BB41 ± RSD (n= 3) |  |  | %R of BR46 ± RSD (n= 3) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CTS/ZnO dosage (g) | Solution pH | Initial concentration (mg L-1) | Ultrasound contact time (min) |  | Experimental | Predicted |  | Experimental | Predicted |
| 0.18 | 7 | 16 | 36 |  | 96.19 ± 2.4 | 94.75 |  | 91.87 ± 2.3 | 91.01 |