# Tailoring Copper Content in High-Entropy Oxides for Enhanced Water Oxidation Catalysis

Seyedsaeed Mehrabi-Kalajahi*1, Seyed Amir Hossein Vasigh1, Hassan Yousefi Bavili2, Behrouz Shaabani*1, Maryam Badri1, Shadab Akbarpour1, Sama Maghoul1, Alexei Vagov3, Ahmad Ostovari Moghaddam3, Mikhail A. Varfolomeev4

1Faculty of Chemistry, Department of Inorganic Chemistry, University of Tabriz, Tabriz, Iran

2Department of Chemical & Biomolecular Engineering, University of Houston, Houston, TX, 77204, USA

3HSE University, 101000 Moscow, Russia

4Department of Petroleum Engineering, Kazan Federal University, Kazan 420008, Russia

*Corresponding authors

*(S.Mehrabi-Kalajahi) E-mail:ss.mehrabikalajahi@gmail.com

*(B. Shaabani) E-mail: shaabani.b@gmail.com, shaabani@tabrizu.ac.ir

AFM Instrumentation

Surface topography measurements were performed using a BIRISK model Atomic Force Microscope, developed by Ara Pajouhesh Company (Iran).

AFM Analysis of HEO‒Cu 40%

Atomic Force Microscopy (AFM) was employed to analyze the surface topography of HEO‒Cu 40%. The AFM data, collected in tapping mode over a 5 µm × 5 µm scan area, revealed a heterogeneous surface with notable roughness and dispersed nanoscale features. The 2D and 3D topographic images show numerous protrusions distributed across the surface, with a maximum height variation of approximately 38.1 nm, as indicated by the polynomial fit. These surface features are likely associated with crystalline domains, secondary phases, or copper-rich agglomerates formed during synthesis. A cross-sectional profile along the X-direction indicates height fluctuations exceeding 160 nm, suggesting the presence of localized asperities. This surface morphology shows a relatively high surface roughness, which is evidenced by the surface roughness and increased surface area that results from electrocatalytic activity.

Figure S1. 3D surface topography by AFM, and AFM thickness profile of HEO‒Cu 40% nanocomposite.

Table S1. Co, Ni, Fe, Mn, and Cu ratios in HEOs as obtained by ICP-MS.

| Sample(s) | Percentage (Atom, %) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Fe | Mn | Cu |
| HEO‒Cu 20% | 19.23 | 20.12 | 19.85 | 20.47 | 20.33 |
| HEO‒Cu 30% | 17.84 | 17.79 | 17.25 | 17.54 | 29.58 |
| HEO‒Cu 40% | 15.29 | 15.69 | 14.72 | 14.89 | 39.41 |
| HEO‒Cu 50% | 12.73 | 12.64 | 12.67 | 12.58 | 49.38 |
| HEO‒Cu 60% | 10.14 | 10.09 | 9.99 | 10.04 | 59.74 |

Table S2. Comparison of Electrocatalytic Activity for Oxygen Evolution Reaction (OER).

| Catalyst | Tafel slope mV/dec | Electrolyte | Reference |
| --- | --- | --- | --- |
| Ir nanoparticles | 64 | - | 1 |
| Cobalt Polyoxometalate | 148 | NaPi/NaNO3 | 2 |
| α‑MnO2/FeCo-LDH | 70.4 | KOH | 3 |
| La(CrMnFeCoNi)O3 | 78.6 | KOH | 4 |
| CoFerrite | 72.7 | KOH | 5 |
| Co0.9Ni0.1Ferrite | 81.1 | KOH | 5 |
| NiFeOH/CoSx | 121.3 | KOH | 6 |
| NiFeOH | 134.6 | KOH | 6 |
| CoSx | 132.1 | KOH | 6 |
| La(FeCoCuTiNiMnMgSnZn)O3−rGO | 81.9 | KOH | 7 |
| (CoFeMnCuNiCr)3O4−rGO | 86 | KOH | 8 |
| HEO–Cu 40%/NF | 64.5 | KOH | This work |

Table S3. Calculated fitting values of the equivalent circuit elements for the different catalysts.

| Sample Name | Charge transfer resistance (Rct (Ω)) | Ohmic Resistance (Rs (Ω)) | Constant Phase Element (CPEdl-T) | Constant Phase Element (CPEdl-P) |
| --- | --- | --- | --- | --- |
| NF | 212.83 | 7.98 | 2.13 ×10-7 | 0.61 |
| HEO_Cu 20%/NF | 177.25 | 7.11 | 1.76 ×10-6 | 0.70 |
| HEO_Cu 30%/NF | 158.40 | 5.30 | 1.57 ×10-6 | 0.79 |
| HEO_Cu 40%/NF | 82.81 | 4.31 | 2.73 ×10-6 | 0.93 |
| HEO_Cu 50%/NF | 114.81 | 4.42 | 1.14 ×10-6 | 0.88 |
| HEO_Cu 60%/NF | 119.91 | 4.65 | 1.18 ×10-6 | 0.87 |

References:

- Reier, T. et al. Electrocatalytic Oxygen Evolution Reaction (OER) on Ru, Ir, and Pt Catalysts: A Comparative Study of Nanoparticles and Bulk Materials. ACS Catalysis 2, 1765–1772 (2012).

- Soriano-López, J. et al. Cobalt Polyoxometalates as Heterogeneous Water Oxidation Catalysts. Inorganic Chemistry 52, 4753–4755 (2013).

- Shahparast, S. et al. α-MnO2/FeCo-LDH on Nickel Foam as an Efficient Electrocatalyst for Water Oxidation. ACS Omega 8, 1702–1709 (2023).

- Nguyen, T. X. et al. Advanced High Entropy Perovskite Oxide Electrocatalyst for Oxygen Evolution Reaction. Adv. Funct. Mater. 31, 2101632 (2021).

- Chamani, S. et al. Microwave-Assisted Auto-Combustion Synthesis of Binary/Ternary CoₓNi₁₋ₓFe₂O₄ for Electrochemical Hydrogen and Oxygen Evolution. ACS Omega 6, 33024–33032 (2021).

- Bose, R. et al. High performance multicomponent bifunctional catalysts for overall water splitting. J. Mater. Chem. A 8, 13795–13805 (2020).

- Moghaddam A.O. et al. Synergistic Multimetal Effects in a High-Entropy Perovskite Oxide Anchored on Reduced Graphene Oxide for Accelerated Water Oxidation. The Journal of Physical Chemistry Letters, (2026).

- Mehrabi-Kalajahi, S. et al. High Entropy (CoFeMnCuNiCr)3O4 Nanoparticles Anchored on Graphene-Based Supports for High-Performance Oxygen Evolution Electrocatalysis. ACS Appl. Energy Mater. 8, 8524–8531 (2025).