Examining the Immunomodulatory Role of Nanoparticles on Mast Cell Activation

Jessica Perez Pineda1 and Lisa A. DeLouise1,2

1Department of Biomedical Engineering, University of Rochester, Rochester, NY

2Department of Dermatology, University of Rochester Medical Center, Rochester, NY

Supplemental Information

Created in Biorender

| Nanoparticle | Surface charge (mV) | Size (TEM) | Hydrodynamic Size | PDI |
| --- | --- | --- | --- | --- |
| SiO2 (20 nm) 10 µg/mL | -26.6 3.89 | 21.42 2.37 | 31.8 1.67 | 0.217 |
| mTiO2 (<100 nm) 1 µg/mL | -9.1 2.26 | 56.02 17.3 | 530.7 45.5 | 0.296 |

Table S1 Nanoparticle characterization via DLS (pH=6.5) and TEM

Fig. S1 Mast Cells Surface Marker expression. Before activation (left) and after being exposed to antigen (right).  This  image was created in BioRender. Perez, J. (2025) https://BioRender.com/ospqk4j

Fig. S2 TEM of SiO2 NPs. Scale bar 100 nm

Fig. S3 TEM of mTiO2 NPs. Scale bar 100 nm

Fig. S4 BMMC Gating strategy performed through FlowJo. A) Cell population excluding the debris was selected. B-C) Single cells were gated through FSC and SSC. D) Cells were gated under FcεRI+CD117+ (Q2) which are defined as the BMMC. E) Fixable Viability Dye eFluor™780 was used to stain dead cells, then live cell population was separated. F) After live cells were separated, cells were gated for the evaluation of each marker

Fig. S5 FMO Controls Gating. Positive identification of each marker was done using single staining and compared to non-stained cells to identify the positive population. Comparison between non-stained cells (left) and single-stained cells (right) for each marker. A) FcεRI, B) CD117, C) CD63, D) LAMP-1.

Fig. S10 Release of proinflammatory cytokine IL-13 as a function of time after NP exposure.