### Supplementary material

### Research Design

#### 1 Research Approach

This study used a laboratory-based experimental research approach to (i) synthesis and analyze nitrogen-doped activated carbon (AC600) from sawdust, and (ii) assess its efficacy in adsorbing and removing hexavalent chromium [Cr(VI)] from aqueous solutions.

The research integrates:

- Material synthesis and physicochemical characterization,

- Controlled batch adsorption experiments,

- Isotherm and kinetic modeling, and

- Process optimization and predictive modeling using Response Surface Methodology (RSM) and Artificial Neural Network (ANN).

The design is quantified, regulated, and reproduced to assure statistical dependability.

#### 2 Adsorbent Synthesis

A preliminary experimental approach was employed to synthesis nitrogen-doped activated carbon (AC600) from sawdust through:

- Pre-treatment

  - Drying at 105 °C to constant weight

  - Particle size standardization (1–2 mm)

- Hydrothermal activation

  - Impregnation with ZnCl₂

  - Hydrothermal treatment at 180 °C for 5 h

- Carbonization and Nitrogen Doping

  - Carbonization at 600 °C under NH₃ flow (100 mL/min) for 1 h

  - Tube furnace system with controlled gas flow

- Post-treatment and purification

  - Acid washing (2N HCl)

  - Sonication

  - Ethanol washing and drying

The final product was labeled as AC600. This stage uses a controlled synthesis design in which temperature, activation duration, gas flow rate, and chemical impregnation ratio are fixed variables to produce a repeatable adsorbent.

#### 3 Characterization Design

This characterization phase intended to correlate material attributes with adsorption performance. A descriptive analytical design was employed to determine the physicochemical properties of AC600 using:

- Surface morphology & elemental composition: SEM–EDX

- Surface functional groups: FTIR

- Surface area & pore structure: BET and BJH (N2 adsorption at 77 K)

- Crystallinity: XRD

- Thermal stability: TGA (25–1000 °C, N2 atmosphere)

- Surface chemical states: XPS

#### 4 Batch Adsorption Design

A controlled batch adsorption experimental approach was employed to investigate Cr(VI) removal performance.

##### Independent Variables:

- Adsorbent dose (0.5–2.5 g/L)

- Initial Cr(VI) concentration (100–400 mg/L)

- Contact time (10–120 min)

- Solution pH (1.5–11.3)

##### Dependent Variables:

- Removal efficiency (RE%)

- Adsorption capacity (qₑ, mg/g)

##### Controlled Variables:

- Temperature (25 ± 2 °C)

- Shaking speed (200 rpm)

- Solution volume (100 mL)

- Synthetic Cr(VI) solution in deionized water

Experiments were conducted in triplicate to ensure reproducibility (standard deviation ≤ 2.2). Cr(VI) concentrations were measured spectrophotometrically at λ545 nm using 1,5-diphenylcarbazide. A control sample (without adsorbent) was used to confirm Cr(VI) stability and eliminate experimental bias.

#### 5 Adsorption Modeling Design

A comparative mathematical modeling design was employed to interpret adsorption mechanisms.

##### Isotherm Models Applied: These theories explain adsorption equilibrium and surface heterogeneity.

- Langmuir

- Freundlich

- Temkin

- Halsey

##### Kinetic Models Applied: Model fitting was tested using statistical parameters and the standard error of estimations.

- Pseudo-first-order

- Pseudo-second-order

- Elovich

- Power function

- Intraparticle diffusion

#### 6 Response Surface Methodology (RSM)

A multivariate optimization design utilizing Response Surface Methodology (RSM) was implemented.

- Software: Design-Expert v13

- Number of experiments: 20

- Design type: D-Optimal Design (DOD)

##### Factors:

- A: Adsorbent dose (0.5–2.5 g/L)

- B: Contact time (15–120 min)

- C: Initial Cr(VI) ions concentration (100–400 mg/L)

##### Response:

- Cr(VI) ions removal efficiency (%)

RSM was used to:

- Determine interaction effects

- Develop a predictive polynomial model

- Identify optimal operating conditions

#### 7. Artificial Neural Network (ANN)

A computational predictive modeling architecture was utilized to simulate and predict Cr(VI) ions removal performance.

- Software: MATLAB R2015b

- Algorithm: Levenberg–Marquardt (LM)

- Data division:

  - Training: 70%

  - Validation: 15%

  - Testing: 15%

##### ANN Structure:

- Input layer:

  - Adsorbent dose

  - Contact time

  - Initial Cr(VI) concentration

- Two hidden layers (7 neurons each)

- Output layer: Cr(VI) removal efficiency (%)

ANN modeling was used to:

- Capture nonlinear relationships

- Improve prediction accuracy

- Compare performance with RSM

The combination of experimental inquiry with statistical and machine learning methodologies enables both mechanistic understanding and predictive capability for Cr(VI) removal utilizing nitrogen-doped activated carbon (AC600).