Supplementary Information

Dose-dependent effects of zinc oxide nanoparticles on pre-osteoblast cellular response

Jeong-Hyun Ryu1,2, Utkarsh Mangal3, Jae-Hyung Kim1, Jae-Sung Kwon4,5, Ki Woo Kim4,6, Sung-Hwan Choi1,4,7,*

1Department of Orthodontics, Institute of Craniofacial Deformity, Yonsei University College of Dentistry, Seoul, Republic of Korea

2Department of Biomedical Engineering, Daelim University, Anyang, Republic of Korea

3Department of Oral Biology, Yonsei University College of Dentistry, Republic of Korea

4BK21 FOUR Project, Yonsei University College of Dentistry, Seoul, Republic of Korea

5Department and Research Institute of Dental Biomaterials and Bioengineering, Yonsei University College of Dentistry, Seoul, Republic of Korea

6Division of Physiology, Department of Oral Biology, Yonsei University College of Dentistry, Seoul, Korea

7Center for Systems Biology, Massachusetts General Hospital, Boston, MA, USA.

*Correspondence and reprints, materials should be addressed to:

Sung-Hwan Choi (selfexam@yuhs.ac)

Tel: +82-2-2228-3102, Fax: +82-2-364-3404

Methods

Cytotoxicity assay

MC3T3-E1 cells were seeded at 1 × 104 cells per well in 96-well plates and cultured for 24 h. Then, the old medium was discarded, and each extraction was changed. After 24 h, cytotoxicity was determined using the water-soluble tetrazolium salt assay (WST-1, EZ−cytox, DoGenBio, Seoul, Republic of Korea) according to the manufacturer’s instructions. The Optical density was measured at 450 nm using a microplate reader (BioTek, Winooski, VT, USA).

Results

Cytotoxicity assay

Fig.S1 Cytotoxicity assay for each extraction of ZnO-NPs (n = 3; *p < 0.05; ***p < 0.001). Control, growth medium; Zn0.01, 0.01 mg/mL ZnO-NPs extraction; Zn0.1, 0.1 mg/mL ZnO-NPs; Zn1, 1 mg/mL ZnO-NPs; Zn10, 10 mg/mL ZnO-NPs; ZnO-NPs, zinc oxide nanoparticles.

Table S1. Post hoc multiple comparisons of cytotoxicity among ZnO-NPs concentration groups

p-value

|  | Control | Zn0.01 | Zn0.1 | Zn1 | Zn10 |
| --- | --- | --- | --- | --- | --- |
| Control | - | 0.022 | 0.000 | 0.000 | 0.000 |
| Zn0.01 | 0.022 | - | 0.086 | 0.029 | 0.000 |
| Zn0.1 | 0.000 | 0.086 | - | 0.951 | 0.000 |
| Zn1 | 0.000 | 0.029 | 0.951 | - | 0.000 |
| Zn10 | 0.000 | 0.000 | 0.000 | 0.000 | - |

Statistical analysis was performed using one-way analysis of variance, followed by Tukey’s post hoc test.

Table S2. Post hoc multiple comparisons of mitochondrial metabolic activity among ZnO-NPs concentration groups

p-value

| Day 1 | Control | Zn0.01 | Zn0.1 | Zn1 |
| --- | --- | --- | --- | --- |
| Control | - | 0.649 | 0.886 | 0.196 |
| Zn0.01 | 0.649 | - | 0.964 | 0.736 |
| Zn0.1 | 0.886 | 0.964 | - | 0.478 |
| Zn1 | 0.196 | 0.736 | 0.478 | - |
| Day 2 | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.000 | 0.002 | 0.017 |
| Zn0.01 | 0.000 | - | 0.061 | 0.005 |
| Zn0.1 | 0.002 | 0.061 | - | 0.305 |
| Zn1 | 0.017 | 0.05 | 0.305 | - |
| Day 3 | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.232 | 0.858 | 0.032 |
| Zn0.01 | 0.232 | - | 0.078 | 0.002 |
| Zn0.1 | 0.858 | 0.078 | - | 0.096 |
| Zn1 | 0.032 | 0.002 | 0.096 | - |

Statistical analysis was performed using one-way analysis of variance, followed by Tukey’s post hoc test.

Table S3. Post hoc multiple comparisons of osteogenic gene expression for 7 days among ZnO-NPs concentration groups

p-value

| RUNX2 | Control | Zn0.01 | Zn0.1 | Zn1 |
| --- | --- | --- | --- | --- |
| Control | - | 0.000 | 0.010 | 0.000 |
| Zn0.01 | 0.000 | - | 0.000 | 0.001 |
| Zn0.1 | 0.010 | 0.000 | - | 0.106 |
| Zn1 | 0.000 | 0.001 | 0.106 | - |
| OSX | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.001 | 0.019 | 0.001 |
| Zn0.01 | 0.001 | - | 0.220 | 1.000 |
| Zn0.1 | 0.019 | 0.220 | - | 0.205 |
| Zn1 | 0.001 | 1.000 | 0.205 | - |
| OPN | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.000 | 0.393 | 0.001 |
| Zn0.01 | 0.000 | - | 0.000 | 0.297 |
| Zn0.1 | 0.393 | 0.000 | - | 0.003 |
| Zn1 | 0.001 | 0.297 | 0.003 | - |
| SPARC | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.000 | 0.261 | 0.038 |
| Zn0.01 | 0.000 | - | 0.000 | 0.005 |
| Zn0.1 | 0.261 | 0.000 | - | 0.003 |
| Zn1 | 0.038 | 0.005 | 0.003 | - |
| OCN | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.000 | 0.001 | 0.394 |
| Zn0.01 | 0.000 | - | 0.000 | 0.000 |
| Zn0.1 | 0.001 | 0.000 | - | 0.000 |
| Zn1 | 0.394 | 0.000 | 0.000 | - |
| BSP | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.000 | 0.112 | 0.903 |
| Zn0.01 | 0.000 | - | 0.000 | 0.297 |
| Zn0.1 | 0.393 | 0.000 | - | 0.003 |
| Zn1 | 0.001 | 0.297 | 0.003 | - |

Statistical analysis was performed using one-way analysis of variance, followed by Tukey’s post hoc test.

Table S4. Post hoc multiple comparisons of alkaline phosphatase activity for 7 days and 14 days among ZnO-NPs concentration groups

p-value

| Day 7 | Control | Zn0.01 | Zn0.1 | Zn1 |
| --- | --- | --- | --- | --- |
| Control | - | 0.000 | 0.000 | 0.000 |
| Zn0.01 | 0.000 | - | 0.000 | 0.000 |
| Zn0.1 | 0.000 | 0.000 | - | 0.000 |
| Zn1 | 0.000 | 0.000 | 0.000 | - |
| Day 14 | Control | Zn0.01 | Zn0.1 | Zn1 |
| Control | - | 0.000 | 0.990 | 0.745 |
| Zn0.01 | 0.000 | - | 0.000 | 0.000 |
| Zn0.1 | 0.990 | 0.000 | - | 0.889 |
| Zn1 | 0.745 | 0.000 | 0.889 | - |

Statistical analysis was performed using one-way analysis of variance, followed by Tukey’s post hoc test.

Table S5. Post hoc multiple comparisons of biomineralization for 21 days among ZnO-NPs concentration groups

p-value

| Day 21 | Control | Zn0.01 | Zn0.1 | Zn1 |
| --- | --- | --- | --- | --- |
| Control | - | 0.000 | 0.000 | 0.000 |
| Zn0.01 | 0.000 | - | 0.000 | 0.000 |
| Zn0.1 | 0.000 | 0.000 | - | 0.000 |
| Zn1 | 0.000 | 0.000 | 0.000 | - |

Statistical analysis was performed using one-way analysis of variance, followed by Tukey’s post hoc test.