Supplementary Table S1. Active ingredient contents and physical characteristics of long-lasting insecticidal net (LLINs) samples used in the experimental hut trial at M’be, Côte d’Ivoire.

| Net sample |  | Composition |  | Unit |  | Before trial |  |  |  | After trial |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Mean |  | RSD (%) |  | Mean |  | RSD (%) |
| Untreated net |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Deltamethrin |  | g/kg |  | <0.01 |  | - |  | <0.01 |  | - |
|  |  | Fabric weight |  | g/m2 |  | 43.8 |  | 1.4 |  | 43.1 |  | 2.3 |
|  |  | Deltamethrin |  | mg/m2 |  | <0.4 |  | - |  | <0.4 |  | - |
|  |  | Alpha-cypermethrin |  | g/kg |  | < 0.05 |  | - |  | < 0.05 |  |  |
|  |  | Fabric weight |  | g/m2 |  | 43.8 |  | 1.4 |  | 43.1 |  | 2.3 |
|  |  | Alpha-cypermethrin |  | mg/m2 |  | < 2 |  | - |  | < 2 |  | - |
| MAGNet |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Alpha-cypermethrin |  | g/kg |  | 5.80 |  | 0.6 |  | 5.80 |  | 0.9 |
|  |  | Fabric weight |  | g/m2 |  | 47.5 |  | 4.1 |  | 56.3 |  | 3.3 |
|  |  | Alpha-cypermethrin |  | mg/m2 |  | 276 |  | 4.2 |  | 326 |  | 3.1 |
| Veeralin |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Alpha-cypermethrin |  | g/kg |  | 7.06 |  | 1.8 |  | 7.05 |  | 0.8 |
|  |  | Fabric weight |  | g/m2 |  | 40.1 |  | 3.4 |  | 47.6 |  | 3.6 |
|  |  | Alpha-cypermethrin |  | mg/m2 |  | 283 |  | 3.3 |  | 336 |  | 3.9 |
|  |  | Piperonyl butoxide |  | g/kg |  | 2.55 |  | 2.6 |  | 2.30 |  | 0.7 |
|  |  | Fabric weight |  | g/m2 |  | 40.1 |  | 3.4 |  | 47.6 |  | 3.6 |
|  |  | Piperonyl butoxide |  | mg/m2 |  | 102 |  | 4.9 |  | 109 |  | 3.5 |
| PermaNet 3.0 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Deltamethrin (side) |  | g/kg |  | 1.98 |  | 6.2 |  | 2.16 |  | 6.9 |
|  |  | Fabric weight (side) |  | g/m2 |  | 42.6 |  | 3.5 |  | 41.8 |  | 0.8 |
|  |  | Deltamethrin (side) |  | mg/m2 |  | 84 |  | 4.8 |  | 90 |  | 7.7 |
|  |  | Deltamethrin (roof) |  | g/kg |  | 3.69 |  | - |  | 3.71 |  | - |
|  |  | Fabric weight (roof) |  | g/m2 |  | 30.4 |  | - |  | 32.1 |  | - |
|  |  | Deltamethrin (roof) |  | mg/m2 |  | 112 |  | - |  | 119 |  | - |
|  |  | Piperonyl butoxide (side) |  | g/kg |  | 25.2 |  | 16.5 |  | 16.8 |  | 16.5 |
|  |  | Fabric weight (side) |  | g/m2 |  | 30.4 |  | 4.0 |  | 32.1 |  | 4.0 |
|  |  | Piperonyl butoxide (side) |  | mg/m2 |  | 766 |  | 13.9 |  | 539 |  | 13.9 |
| Olyset Plus |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Permethrin |  | g/kg |  | 19.1 |  | 3.4 |  | 17.1 |  | 2.4 |
|  |  | Fabric weight |  | g/m2 |  | 36.0 |  | 6.7 |  | 40.3 |  | 7.1 |
|  |  | Permethrin |  | mg/m2 |  | 689 |  | 6.4 |  | 689 |  | 9.2 |
|  |  | Piperonyl butoxide |  | g/kg |  | 8.61 |  | 3.1 |  | 7.83 |  | 2.7 |
|  |  | Fabric weight |  | g/m2 |  | 36.0 |  | 6.7 |  | 40.3 |  | 7.1 |
|  |  | Piperonyl butoxide |  | mg/m2 |  | 310 |  | 6.4 |  | 316 |  | 9.2 |
| Interceptor G2 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Alpha-cypermethrin |  | g/kg |  | 2.52 |  | 4.3 |  | 2.44 |  | 4.5 |
|  |  | Chorfenapyr |  | g/kg |  | 4.81 |  | 3.1 |  | 4.60 |  | 2.7 |
|  |  | Fabric weight |  | g/m2 |  | 47.4 |  | 2.4 |  | 45.3 |  | 4.0 |
|  |  | Alpha-cypermethrin |  | g/m2 |  | 119 |  | 5.5 |  | 110 |  | 6.5 |
|  |  | Chorfenapyr |  | g/m2 |  | 228 |  | 4.3 |  | 209 |  | 5.6 |

RSD: relative standard deviations