Supplementary Table S1. Active ingredient contents and physical characteristics of long-lasting insecticidal net (LLINs) samples used in the experimental hut trial at M’be, Côte d’Ivoire.
	Net sample
	 
	Composition
	 
	Unit
	 
	Before trial
	 
	After trial

	 
	 
	 
	 
	 
	 
	Mean
	 
	RSD (%)
	 
	Mean
	 
	RSD (%)

	Untreated net
	
	
	
	
	
	
	
	
	
	
	
	

	
	
	Deltamethrin 
	
	g/kg
	
	<0.01
	
	 - 
	
	<0.01
	
	 - 

	
	
	Fabric weight 
	
	g/m2
	
	43.8
	
	1.4
	
	43.1
	
	2.3

	
	
	[bookmark: _GoBack]Deltamethrin 
	
	mg/m2
	
	<0.4
	
	 - 
	
	<0.4
	
	 - 

	
	
	Alpha-cypermethrin 
	
	g/kg
	
	< 0.05
	
	 - 
	
	< 0.05
	
	

	
	
	Fabric weight 
	
	g/m2
	
	43.8
	
	1.4
	
	43.1
	
	2.3

	
	
	Alpha-cypermethrin 
	
	mg/m2
	
	< 2
	
	 - 
	
	< 2
	
	 - 

	MAGNet
	
	
	
	
	
	
	
	
	
	
	
	

	
	
	Alpha-cypermethrin 
	
	g/kg
	
	5.80
	
	0.6
	
	5.80
	
	0.9

	
	
	Fabric weight 
	
	g/m2
	
	47.5
	
	4.1
	
	56.3
	
	3.3

	
	
	Alpha-cypermethrin 
	
	mg/m2
	
	276
	
	4.2
	
	326
	
	3.1

	Veeralin
	
	
	
	
	
	
	
	
	
	
	
	

	
	
	Alpha-cypermethrin 
	
	g/kg
	
	7.06
	
	1.8
	
	7.05
	
	0.8

	
	
	Fabric weight 
	
	g/m2
	
	40.1
	
	3.4
	
	47.6
	
	3.6

	
	
	Alpha-cypermethrin 
	
	mg/m2
	
	283
	
	3.3
	
	336
	
	3.9

	
	
	Piperonyl butoxide 
	
	g/kg
	
	2.55
	
	2.6
	
	2.30
	
	0.7

	
	
	Fabric weight 
	
	g/m2
	
	40.1
	
	3.4
	
	47.6
	
	3.6

	
	
	Piperonyl butoxide 
	
	mg/m2
	
	102
	
	4.9
	
	109
	
	3.5

	PermaNet 3.0
	
	
	
	
	
	
	
	
	
	
	
	

	
	
	Deltamethrin (side)
	
	g/kg
	
	1.98
	
	6.2
	
	2.16
	
	6.9

	
	
	Fabric weight (side)
	
	g/m2
	
	42.6
	
	3.5
	
	41.8
	
	0.8

	
	
	Deltamethrin (side)
	
	mg/m2
	
	84
	
	4.8
	
	90
	
	7.7

	
	
	Deltamethrin (roof)
	
	g/kg
	
	3.69
	
	 - 
	
	3.71
	
	 - 

	
	
	Fabric weight (roof)
	
	g/m2
	
	30.4
	
	 - 
	
	32.1
	
	 - 

	
	
	Deltamethrin (roof)
	
	mg/m2
	
	112
	
	 - 
	
	119
	
	 - 

	
	
	Piperonyl butoxide (side)
	
	g/kg
	
	25.2
	
	16.5
	
	16.8
	
	16.5

	
	
	Fabric weight (side)
	
	g/m2
	
	30.4
	
	4.0
	
	32.1
	
	4.0

	
	
	Piperonyl butoxide (side)
	
	mg/m2
	
	766
	
	13.9
	
	539
	
	13.9

	Olyset Plus
	
	
	
	
	
	
	
	
	
	
	
	

	
	
	Permethrin 
	
	g/kg
	
	19.1
	
	3.4
	
	17.1
	
	2.4

	
	
	Fabric weight 
	
	g/m2
	
	36.0
	
	6.7
	
	40.3
	
	7.1

	
	
	Permethrin 
	
	mg/m2
	
	689
	
	6.4
	
	689
	
	9.2

	
	
	Piperonyl butoxide 
	
	g/kg
	
	8.61
	
	3.1
	
	7.83
	
	2.7

	
	
	Fabric weight 
	
	g/m2
	
	36.0
	
	6.7
	
	40.3
	
	7.1

	
	
	Piperonyl butoxide 
	
	mg/m2
	
	310
	
	6.4
	
	316
	
	9.2

	Interceptor G2
	
	
	
	
	
	
	
	
	
	
	
	

	
	
	Alpha-cypermethrin 
	
	g/kg
	
	2.52
	
	4.3
	
	2.44
	
	4.5

	
	
	Chorfenapyr 
	
	g/kg
	
	4.81
	
	3.1
	
	4.60
	
	2.7

	
	
	Fabric weight
	
	g/m2
	
	47.4
	
	2.4
	
	45.3
	
	4.0

	
	
	Alpha-cypermethrin 
	
	g/m2
	
	119
	
	5.5
	
	110
	
	6.5

	 
	 
	Chorfenapyr 
	 
	g/m2
	 
	228
	 
	4.3
	 
	209
	 
	5.6


RSD: relative standard deviations


