Supplementary Information

Supplementary Table 1. Mass loss of hydrothermally modified Douglas fir wood

| Temperature | Time (h) | Mass loss (%) |
| --- | --- | --- |
| Control | - | - |
| 140°C | 0.5 | 0.86±0.10 |
|  | 1 | 1.21±0.05 |
|  | 2 | 1.60±0.05 |
| 160°C | 0.5 | 2.26±0.18 |
|  | 1 | 2.45±0.13 |
|  | 2 | 5.33±0.51 |
| 180°C | 0.5 | 10.20±0.44 |
|  | 1 | 11.53±0.78 |
|  | 2 | 19.61±0.31 |

Mass loss of hydrothermally modified Douglas fir wood

Supplementary Table 2. Volumetric swelling (%) of control and hydrothermally modified Douglas fir wood

| Temperature | Time (h) | Volumetric swelling (%) |
| --- | --- | --- |
| Control | - | 14.46±0.24 |
| 140°C | 0.5 | 12.20±0.47 |
|  | 1 | 11.86±0.83 |
|  | 2 | 11.68±0.61 |
| 160°C | 0.5 | 10.80±0.29 |
|  | 1 | 10.29±1.12 |
|  | 2 | 10.20±0.33 |
| 180°C | 0.5 | 10.49±0.39 |
|  | 1 | 9.89±0.47 |
|  | 2 | 9.63±0.43 |

Volumetric swelling (%) of control and hydrothermally modified Douglas fir wood

Supplementary Table 3. MOE and MOR of control and hydrothermally modified Douglas fir wood

| Temperature | Time (h) | MOE (GPa) | MOR (MPa) |
| --- | --- | --- | --- |
| Control | - | 9.5667±0.95 | 86.4733±6.56 |
| 140°C | 0.5 | 8.77±0.69 | 81.92±2.67 |
|  | 1 | 8.20±0.63 | 76.44±10.25 |
|  | 2 | 7.75±0.50 | 71.12±8.27 |
| 160°C | 0.5 | 7.08±1.30 | 62.10±4.58 |
|  | 1 | 6.55±1.24 | 54.03±6.41 |
|  | 2 | 5.07±0.77 | 47.78±5.58 |
| 180°C | 0.5 | 5.22±0.30 | 30.14±3.33 |
|  | 1 | 5.01±1.64 | 24.95±5.04 |
|  | 2 | 3.65±0.62 | 15.70±1.65 |

MOE and MOR of control and hydrothermally modified Douglas fir wood

Supplementary Table 4. DMOE of control and hydrothermally modified Douglas fir wood

| Temperature | Time (h) | DMOE (GPa) |
| --- | --- | --- |
| Control | - | 18.30±1.61 |
| 140°C | 0.5 | 18.00±1.72 |
|  | 1 | 17.51±1.94 |
|  | 2 | 17.65±1.77 |
| 160°C | 0.5 | 14.07±3.53 |
|  | 1 | 13.84±4.84 |
|  | 2 | 10.88±1.29 |
| 180°C | 0.5 | 13.86±2.78 |
|  | 1 | 12.16±3.55 |
|  | 2 | 7.49±1.51 |

DMOE of control and hydrothermally modified Douglas fir wood

Supplementary Table 5. Surface hardness of control and hydrothermally modified Douglas fir wood

| Temperature | Time (h) | Hardness (N) |
| --- | --- | --- |
| Control | - | 2650.50±235.31 |
| 140°C | 0.5 | 2454.04±199.71 |
|  | 1 | 2304.59±274.07 |
|  | 2 | 2093.90±89.17 |
| 160°C | 0.5 | 1957.70±236.70 |
|  | 1 | 1897.58±320.31 |
|  | 2 | 1669.43±221.16 |
| 180°C | 0.5 | 1308.98±115.62 |
|  | 1 | 986.13±86.43 |
|  | 2 | 826.76±136.87 |

Surface hardness of control and hydrothermally modified Douglas fir wood