Supplementary Data for

Plant-Mediated Formation of Zinc Oxide and Silver Nanoparticles Using Garuga pinnata Bark: Characterization and Bioactivity Assessment

Table S1: Total phenolic content (TPC) of crude extracts of bark of Garuga pinnata)

| Solvent extract | Absorbance at 765 nm |  |  | TPC (mg GAE/g) |  |  | Average TPC | SD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Abs1 | Abs2 | Abs3 | TPC1 | TPC2 | TPC3 |  |  |
| Aqueous | 0.295 | 0.325 | 0.417 | 25.31 | 27.92 | 35.92 | 29.71 | 5.52 |
| Methanol | 0.801 | 0.977 | 0.985 | 69.31 | 84.61 | 85.31 | 79.75 | 9.043 |
| Ethanol | 1.271 | 1.37 | 1.292 | 110.18 | 118.79 | 112.0 | 113.66 | 4.53 |
| Ethyl acetate | 0.488 | 0.541 | 0.598 | 42.09 | 46.70 | 51.66 | 46.82 | 4.78 |
| Dichloromethane | 0.53 | 0.452 | 0.427 | 45.74 | 38.96 | 36.79 | 40.50 | 4.67 |
| Hexane | 0.283 | 0.341 | 0.404 | 24.26 | 29.31 | 34.79 | 29.46 | 5.26 |

(Linear regression equation from gallic acid calibration curve, y = 0.0115x + 0.0039)

Table S2: Total flavonoid content (TFC) of crude extracts of bark of Garuga pinnata

| Solvent extract | Absorbance at 415 nm |  |  | TFC (mg QE/g) |  |  | Average TFC | SD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Abs1 | Abs2 | Abs3 | TFC1 | TFC2 | TFC3 |  |  |
| Aqueous | 0.046 | 0.045 | 0.034 | 16.9 | 16.45 | 11.45 | 14.93 | 3.02 |
| Methanol | 0.023 | 0.04 | 0.042 | 6.45 | 14.18 | 15.09 | 11.91 | 4.74 |
| Ethanol | 0.038 | 0.042 | 0.035 | 13.27 | 15.09 | 11.9 | 13.42 | 1.6 |
| Ethyl acetate | 0.08 | 0.103 | 0.11 | 32.36 | 42.81 | 46 | 40.39 | 7.13 |
| Dichloromethane | 0.035 | 0.023 | 0.019 | 11.9 | 6.45 | 4.63 | 7.67 | 3.78 |
| Hexane | 0.027 | 0.034 | 0.038 | 8.27 | 11.45 | 13.27 | 11 | 2.53 |

(Linear regression equation from quercetin calibration curve, y = 0.0022x + 0.0088)

Table S3: DPPH radical scavenging activity (RSA) of crude extracts and nanoparticles

| Sample | Conc. (µg/mL) | Absorbance at 517 nm |  |  |  | Percentage radical scavenging activity (RSA) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Control | Abs1 | Abs2 | Abs3 | RSA1 | RSA2 | RSA3 |
| Aqueous | 500 | 0.349 | 0.082 | 0.08 | 0.07 | 76.5043 | 77.07736 | 79.94269 |
|  | 250 |  | 0.099 | 0.101 | 0.081 | 71.63324 | 71.06017 | 76.79083 |
|  | 125 |  | 0.13 | 0.147 | 0.15 | 62.75072 | 57.87966 | 57.02006 |
|  | 62.5 |  | 0.222 | 0.211 | 0.211 | 36.38968 | 39.54155 | 39.54155 |
|  | 31.25 |  | 0.25 | 0.254 | 0.265 | 28.36676 | 27.22063 | 24.06877 |
|  | 15.62 |  | 0.275 | 0.271 | 0.27 | 21.20344 | 22.34957 | 22.6361 |
| Methanol | 500 | 0.464 | 0.002 | 0.013 | 0.007 | 99.5689 | 97.1982 | 98.4913 |
|  | 250 |  | 0.015 | 0.017 | 0.017 | 96.7672 | 96.3362 | 96.3362 |
|  | 125 |  | 0.025 | 0.029 | 0.022 | 94.6120 | 93.75 | 95.2586 |
|  | 62.5 |  | 0.089 | 0.097 | 0.093 | 80.8189 | 79.0948 | 79.9569 |
|  | 31.25 |  | 0.094 | 0.1 | 0.106 | 79.7413 | 78.4482 | 77.1551 |
|  | 15.62 |  | 0.157 | 0.19 | 0.19 | 66.1637 | 59.0517 | 59.0517 |
| Ethanol | 500 | 0.464 | 0.112 | 0.11 | 0.105 | 75.862069 | 76.293103 | 77.37069 |
|  | 250 |  | 0.133 | 0.145 | 0.159 | 71.336207 | 68.75 | 65.732759 |
|  | 125 |  | 0.159 | 0.174 | 0.189 | 65.732759 | 62.5 | 59.267241 |
|  | 62.5 |  | 0.206 | 0.225 | 0.213 | 55.603448 | 51.508621 | 54.094828 |
|  | 31.25 |  | 0.24 | 0.254 | 0.241 | 48.275862 | 45.258621 | 48.060345 |
|  | 15.62 |  | 0.313 | 0.311 | 0.317 | 32.543103 | 32.974138 | 31.681034 |
| Ethyl acetate | 500 | 0.464 | 0.104 | 0.124 | 0.112 | 77.58621 | 73.27586 | 75.86207 |
|  | 250 |  | 0.138 | 0.158 | 0.164 | 70.25862 | 65.94828 | 64.65517 |
|  | 125 |  | 0.191 | 0.2 | 0.224 | 58.83621 | 56.89655 | 51.72414 |
|  | 62.5 |  | 0.217 | 0.254 | 0.219 | 53.23276 | 45.25862 | 52.80172 |
|  | 31.25 |  | 0.303 | 0.284 | 0.306 | 34.69828 | 38.7931 | 34.05172 |
|  | 15.62 |  | 0.368 | 0.366 | 0.349 | 20.68966 | 21.12069 | 24.78448 |
| DCM | 500 | 0.409 | 0.292 | 0.305 | 0.248 | 28.6063 | 25.4278 | 39.3643 |
|  | 250 |  | 0.314 | 0.291 | 0.28 | 23.2273 | 28.8508 | 31.5403 |
|  | 125 |  | 0.291 | 0.316 | 0.264 | 28.8508 | 22.7383 | 35.4523 |
|  | 62.5 |  | 0.323 | 0.316 | 0.327 | 21.0268 | 22.7383 | 20.0489 |
|  | 31.25 |  | 0.326 | 0.336 | 0.332 | 20.2934 | 17.8484 | 18.8264 |
|  | 15.62 |  | 0.351 | 0.352 | 0.362 | 14.1809 | 13.9364 | 11.4914 |
| Hexane | 500 | 0.409 | 0.225 | 0.198 | 0.227 | 44.98778 | 51.58924 | 44.49878 |
|  | 250 |  | 0.234 | 0.24 | 0.237 | 42.78729 | 41.32029 | 42.05379 |
|  | 125 |  | 0.273 | 0.266 | 0.254 | 33.25183 | 34.96333 | 37.89731 |
|  | 62.5 |  | 0.284 | 0.279 | 0.265 | 30.56235 | 31.78484 | 35.20782 |
|  | 31.25 |  | 0.32 | 0.312 | 0.315 | 21.76039 | 23.71638 | 22.98289 |
|  | 15.62 |  | 0.353 | 0.341 | 0.332 | 13.69193 | 16.62592 | 18.82641 |
| Ag NPs | 500 | 0.349 | 0.098 | 0.088 | 0.117 | 71.91977 | 74.7851 | 66.47564 |
|  | 250 |  | 0.12 | 0.124 | 0.112 | 65.61605 | 64.46991 | 67.90831 |
|  | 125 |  | 0.127 | 0.127 | 0.165 | 63.61032 | 63.61032 | 52.72206 |
|  | 62.5 |  | 0.191 | 0.196 | 0.181 | 45.27221 | 43.83954 | 48.13754 |
|  | 31.25 |  | 0.217 | 0.216 | 0.191 | 37.82235 | 38.10888 | 45.27221 |
|  | 15.62 |  | 0.232 | 0.226 | 0.246 | 33.52436 | 35.24355 | 29.51289 |
| ZnO NPs | 500 | 0.349 | 0.118 | 0.1 | 0.105 | 66.18911 | 71.3467 | 69.91404 |
|  | 250 |  | 0.135 | 0.125 | 0.109 | 61.31805 | 64.18338 | 68.76791 |
|  | 125 |  | 0.177 | 0.154 | 0.199 | 49.28367 | 55.87393 | 42.97994 |
|  | 62.5 |  | 0.233 | 0.195 | 0.194 | 33.23782 | 44.12607 | 44.41261 |
|  | 31.25 |  | 0.283 | 0.28 | 0.284 | 18.91117 | 19.77077 | 18.62464 |
|  | 15.62 |  | 0.266 | 0.283 | 0.277 | 23.78223 | 18.91117 | 20.63037 |

Table S4: DPPH radical scavenging activity (RSA) of standard quercetin

| Concentration (µg/mL) | Percentage radical scavenging activity (RSA) |  |  |
| --- | --- | --- | --- |
|  | RSA1 | RSA2 | RSA3 |
| 20 | 92.44754 | 97.90209 | 96.64335 |
| 10 | 89.51047 | 94.54545 | 94.12587 |
| 5 | 68.53142 | 68.95101 | 73.5664 |
| 2.5 | 34.96494 | 38.74117 | 42.93698 |
| 1.25 | 23.63626 | 14.40547 | 25.31458 |
| 0.625 | 13.98589 | 13.56631 | 11.04883 |

Table S5: IC50 values of the crude extracts and nanoparticles for radical scavenging activity

| Sample | IC50 (µg/mL) |
| --- | --- |
| Aqueous extract | 96.24 ± 1.784 |
| Methanol extract | 17.57 ± 2.371 |
| Ethanol extract | 40.09 ± 0.972 |
| Ethyl acetate extract | 45.32 ± 1.484 |
| DCM extract | 29.92 ± 0.710 |
| Hexane extract | 50.84 ± 1.39 |
| Ag NPs | 76.27 ± 1.263 |
| ZnO NPs | 92.05 ± 3.722 |
| Quercetin | 3.43 ± 1.613 |

Table S6: Percentage cytotoxicity of nanoparticles on cancer and normal cells (MTT assay)

| Sample and cell | Conc. (µg/mL) | Absorbance at 570 nm |  |  |  | Percentage cytotoxicity |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Abs1 | Abs2 | Abs3 | Control | PC1 | PC2 | PC3 |
| ZnO NPs, A549 | 100 | 0.404 | 0.391 | 0.382 | 0.452 | 10.619 | 13.496 | 15.487 |
|  | 50 | 0.407 | 0.42 | 0.419 |  | 9.9558 | 7.0796 | 7.3009 |
|  | 25 | 0.435 | 0.404 | 0.386 |  | 3.7611 | 10.619 | 14.602 |
|  | 12.5 | 0.444 | 0.423 | 0.403 |  | 1.7699 | 6.4159 | 10.841 |
| Ag NPs, A549 | 100 | 0.371 | 0.361 | 0.368 | 0.452 | 17.92 | 20.133 | 18.584 |
|  | 50 | 0.374 | 0.372 | 0.379 |  | 17.257 | 17.699 | 16.15 |
|  | 25 | 0.371 | 0.374 | 0.389 |  | 17.92 | 17.257 | 13.938 |
|  | 12.5 | 0.415 | 0.39 | 0.38 |  | 8.1858 | 13.717 | 15.929 |
| ZnO NPs, HeLa | 100 | 0.29 | 0.299 | 0.294 | 0.519 | 44.123 | 42.389 | 43.353 |
|  | 50 | 0.32 | 0.358 | 0.358 |  | 38.343 | 31.021 | 31.021 |
|  | 25 | 0.459 | 0.466 | 0.438 |  | 15.561 | 10.212 | 15.607 |
|  | 12.5 | 0.505 | 0.494 | 0.499 |  | 2.6975 | 4.817 | 3.8536 |
| Ag NPs, HeLa | 100 | 0.306 | 0.31 | 0.319 | 0.519 | 41.04 | 40.27 | 38.536 |
|  | 50 | 0.321 | 0.33 | 0.34 |  | 38.15 | 36.416 | 34.48 |
|  | 25 | 0.376 | 0.382 | 0.372 |  | 27.553 | 26.397 | 28.324 |
|  | 12.5 | 0.463 | 0.477 | 0.448 |  | 10.79 | 8.0925 | 13.68 |
| ZnO NPs, normal epithelial cells | 12.5 | 0.925 | 0.957 | 0.882 | 0.833 | -11.0444 | -14.8859 | -5.8823 |
|  | 25 | 0.87 | 0.856 | 0.815 |  | -4.4418 | -2.7611 | 2.1609 |
|  | 50 | 0.803 | 0.827 | 0.795 |  | 3.6014 | 0.7202 | 4.5618 |
|  | 100 | 0.79 | 0.861 | 0.791 |  | 5.1621 | -3.3613 | 5.0420 |
| Ag NPs, normal epithelial cells | 12.5 | outlier | 0.592 | 0.464 | 0.513 | Outlier | -15.3996 | 9.5517 |
|  | 25 |  | 0.463 | 0.441 |  |  | 9.7466 | 14.0351 |
|  | 50 |  | 0.489 | 0.487 |  |  | 4.6784 | 5.0682 |
|  | 100 |  | 0.473 | 0.433 |  |  | 7.7973 | 15.5945 |

Table S7: IC50 values cytotoxicity of nanoparticles on cancer and normal cells (MTT assay)

| Sample and cell | Anticancer activity, IC50 (µg/mL) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | IC50 1 | IC50 2 | IC50 3 | Mean IC50 | SD |
| ZnO NPs against A549 | 479.0358 | 683.9925 | 1157.155 | 773.3946 | 347.7874 |
| Ag NPs against A549 | 515.3316 | 581.0129 | 867.3939 | 654.5795 | 187.2058 |
| ZnO NPs HeLa | 101.7673 | 110.7976 | 108.771 | 107.112 | 4.7382 |
| Ag NPs HeLa | 116.7401 | 118.2578 | 136.4825 | 123.8268 | 10.9864 |
| ZnO NPs normal epithelial cell | 351.4143 | 671.9101 | 545.6881 | 523.0042 | 161.4476 |
| Ag NPs against normal epithelial cell | The value was removed as an outlier. | 338.1665 | 884.0679 | 611.1172 | 386.0106 |

IC50 values were calculated by non-linear regression analysis of percentage cytotoxicity versus concentration curve. Calculations were performed on GraphPad Prism and MS Excel 2019 software.