Linking Molecular Antioxidant Activity to Polyurethane Foam Stability - The Case of Abies marocana Essential Oil

Mohamed El Bakkali1, Dalal K. Thbayh2,3, Dóra Mentes3,4, László Farkas3, 
Dávid Salamon3,4, Anikó Csábrádiné Jordán3,4, Béla Viskolcz3,4, Amin Bouchfara1, 
Badredine Souhail1, Mounir Nechar1, Rehana Bano3, Béla Fiser3,4,5,*

1 Laboratory of Water, studies and Environmental Analysis, Faculty of Sciences, Tétouan, Abdelmalek Essaâdi University, Morocco

2 Polymer Research Center, University of Basrah, Basrah, Iraq

3 Higher Education and Industrial Cooperation Centre, University of Miskolc, 3515 Miskolc-Egyetemváros, Hungary

4 Institute of Chemistry, University of Miskolc, 3515 Miskolc-Egyetemváros, Hungary

5 Department of Physical Chemistry, Faculty of Chemistry, University of Lodz, 90-236 Lodz, Poland

* Corresponding author: Béla Fiser, bela.fiser@uni-miskolc.hu

Supplementary Information

Figure S1. Experimental force values measured at 50% compression before  (F50½,0) and after (F50%,1) dry heat ageing, and the corresponding calculated percentage force loss (ΔF50%) as a function of AMEO concentration.

Figure S1. Raw FTIR spectra of the reference FPUF and FPUF/AMEO containing 0.15 g (AMEO1), 0.30 g (AMEO2), 0.45 g (AMEO3), and 0.60 g (AMEO4) of AMEO. For each formulation, Rep 1, Rep 2, and Rep 3 represent three independent replicate measurements.

Table S1. Raw replicate mechanical force (F₅₀%) values measured at 50% compression before and after dry heat ageing and the corresponding percentage change (ΔF₅₀%(%)).

| Sample ID | Weight of oil (g) | Before dry heat ageing (N) |  |  | Mean ± SD | After dry heat ageing (N) |  |  | Mean ± SD | ∆F50% (%) ± SD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Rep1 | Rep2 | Rep3 |  | Rep1 | Rep2 | Rep3 |  |  |
| Reference | 0.00 | 4.59 | 5.59 | 6.2 | 5.46 ± 0.81 | 3.45 | 4.08 | 4.68 | 4.07 ± 0.62 | 25.46 ± 1.36 |
| AMEO1 | 0.15 | 4.76 | 5.62 | 6.27 | 5.55 ± 0.76 | 3.72 | 4.23 | 4.92 | 4.29 ± 0.60 | 22.70 ± 1.76 |
| AMEO2 | 0.30 | 5.60 | 4.70 | 6.95 | 5.75 ± 1.13 | 4.23 | 3.72 | 5.24 | 4.39 ± 0.77 | 23.65 ± 2.02 |
| AMEO3 | 0.45 | 6.50 | 6.26 | 5.58 | 6.11 ± 0.48 | 4.91 | 4.75 | 4.16 | 4.60 ± 0.39 | 24.70 ± 0.69 |
| AMEO4 | 0.60 | 4.92 | 6.38 | 7.47 | 6.26 ± 1.28 | 3.92 | 4.95 | 5.8 | 4.89 ± 0.84 | 21.88 ± 1.28 |

Table S2. Raw replicate sample height measurements before and after dry heat ageing and the corresponding decrease in height (∆h (%)).

| Sample ID | Weight of oil (g) | Initial height before compression (mm) |  |  | Mean ± SD | Height after dry heat ageing (mm) |  |  | Mean ± SD | ∆h (%) ± SD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Rep1 | Rep2 | Rep3 |  | Rep1 | Rep2 | Rep3 |  |  |
| Reference | 0.00 | 28.97 | 29.39 | 30.23 | 29.53 ± 0.64 | 29.27 | 29.73 | 30.52 | 29.84 ± 0.63 | -1.05 ± 0.11 |
| AMEO1 | 0.15 | 31.06 | 29.97 | 29.97 | 30.33 ± 0.63 | 31.29 | 30.11 | 30.11 | 30.5 ± 0.68 | -0.56 ± 0.15 |
| AMEO2 | 0.30 | 29.40 | 29.40 | 29.93 | 29.58 ± 0.30 | 29.33 | 29.33 | 29.90 | 29.52 ± 0.33 | 0.20 ± 0.08 |
| AMEO3 | 0.45 | 29.37 | 30.17 | 29.71 | 29.75 ± 0.40 | 28.93 | 29.71 | 29.32 | 29.32 ± 0.39 | 1.45 ± 0.12 |
| AMEO4 | 0.60 | 30.89 | 29.23 | 29.23 | 29.78 ± 0.96 | 30.63 | 28.97 | 28.97 | 29.52 ± 0.96 | 0.87 ± 0.04 |

Cartesian coordinates of the optimized AMEO compounds calculated at the M06-2X/6-311+G(d,p) level of theory

β-pinene

C                  1.07453100   -0.32762600    0.20743400

C                  0.87245500    1.15313200   -0.24767200

C                 -0.12355400   -0.64111900   -0.75574400

C                  0.31881100    0.59752600   -1.58432800

C                 -0.28082300    1.80916200    0.52348000

C                 -1.43689800   -0.27788600   -0.08919200

C                  0.95024100   -0.66447100    1.68757300

C                  2.39030100   -0.91154900   -0.30883200

C                 -1.50210300    0.91736800    0.49958600

C                 -2.56087800   -1.26724100   -0.13456100

H                  1.75908200    1.79185900   -0.27551600

H                 -0.14877800   -1.62252800   -1.23561700

H                  1.09935200    0.37805700   -2.30916100

H                 -0.48089700    1.16443100   -2.06259200

H                 -0.51403700    2.78423500    0.08037700

H                  0.01813600    2.00679800    1.56048300

H                  0.99735200   -1.74844700    1.83181400

H                  0.02065800   -0.30748800    2.12860000

H                  1.78540500   -0.22306900    2.24080000

H                  2.56521100   -0.71353100   -1.36646300

H                  2.40234200   -1.99604400   -0.16527300

H                  3.23104000   -0.49266900    0.25235800

H                 -2.41192600    1.25611000    0.98690100

H                 -3.45339800   -0.88234600    0.36100200

H                 -2.26605300   -2.20141000    0.35502600

H                 -2.81599800   -1.51772200   -1.16920400

α-pinene

C                  1.07453100   -0.32762600    0.20743400

C                  0.87245500    1.15313200   -0.24767200

C                 -0.12355400   -0.64111900   -0.75574400

C                  0.31881100    0.59752600   -1.58432800

C                 -0.28082300    1.80916200    0.52348000

C                 -1.43689800   -0.27788600   -0.08919200

C                  0.95024100   -0.66447100    1.68757300

C                  2.39030100   -0.91154900   -0.30883200

C                 -1.50210300    0.91736800    0.49958600

C                 -2.56087800   -1.26724100   -0.13456100

H                  1.75908200    1.79185900   -0.27551600

H                 -0.14877800   -1.62252800   -1.23561700

H                  1.09935200    0.37805700   -2.30916100

H                 -0.48089700    1.16443100   -2.06259200

H                 -0.51403700    2.78423500    0.08037700

H                  0.01813600    2.00679800    1.56048300

H                  0.99735200   -1.74844700    1.83181400

H                  0.02065800   -0.30748800    2.12860000

H                  1.78540500   -0.22306900    2.24080000

H                  2.56521100   -0.71353100   -1.36646300

H                  2.40234200   -1.99604400   -0.16527300

H                  3.23104000   -0.49266900    0.25235800

H                 -2.41192600    1.25611000    0.98690100

H                 -3.45339800   -0.88234600    0.36100200

H                 -2.26605300   -2.20141000    0.35502600

H                 -2.81599800   -1.51772200   -1.16920400

Limonene

C                 -0.70647500    0.03719200   -0.27692100

C                 -0.04425100   -1.05524300    0.57808900

C                  0.01848300    1.35909000   -0.02861800

C                  1.41371000   -1.25614800    0.16573000

C                  2.15723900    0.04240700   -0.03163500

C                  1.51520400    1.20828500   -0.10744200

C                 -2.20710400    0.09662400   -0.07827200

C                  3.65137500   -0.06858100   -0.14587800

C                 -2.95665000   -1.17595900   -0.38716900

C                 -2.85792400    1.18952400    0.31857700

H                 -0.54179300   -0.23952600   -1.32978700

H                 -0.58014000   -2.00253700    0.49111400

H                 -0.09718600   -0.74711500    1.62878800

H                 -0.25207600    1.74597700    0.96214400

H                 -0.31493600    2.10988800   -0.75186400

H                  1.46331500   -1.83409900   -0.76700700

H                  1.93781800   -1.85834200    0.91626400

H                  2.09459100    2.11976900   -0.23369100

H                  3.92546300   -0.74670600   -0.96063800

H                  4.08048400   -0.48410300    0.77130700

H                  4.11335100    0.90114600   -0.33539900

H                 -2.60974800   -1.61321200   -1.32836000

H                 -2.80201800   -1.92639800    0.39270200

H                 -4.02807500   -0.99038500   -0.46547900

H                 -3.93738200    1.18308900    0.42340800

H                 -2.35331200    2.11940700    0.54771400

Camphene

C                  0.48489900   -1.11488600    0.47124800

C                 -0.83584600   -0.43909300   -0.00427700

C                  1.03571200    1.07576200    0.39597400

C                  1.05975700   -0.06008900    1.43840900

C                  1.54671600   -1.06857600   -0.64315300

C                  1.87074000    0.45075900   -0.75275500

C                 -0.41188900    1.03554500   -0.03170600

C                 -1.32594200   -0.91640800   -1.37559500

C                 -1.95586500   -0.67590600    1.01887000

C                 -1.17611200    2.06865200   -0.36569900

H                  0.32038000   -2.11158600    0.88521800

H                  1.37951300    2.05828200    0.71747000

H                  2.07022900   -0.30598000    1.77403700

H                  0.43305100    0.14348300    2.30711100

H                  1.20803500   -1.50462000   -1.58233600

H                  2.42959900   -1.62902100   -0.32788600

H                  2.93457100    0.64101200   -0.59516300

H                  1.59427400    0.87443100   -1.71979900

H                 -0.64957500   -0.62001300   -2.17853900

H                 -1.43164500   -2.00589900   -1.38962900

H                 -2.30406900   -0.48079000   -1.59447900

H                 -1.65522500   -0.39655300    2.02974700

H                 -2.83730000   -0.08470600    0.75925900

H                 -2.24217200   -1.73204000    1.02393100

H                 -2.20978600    1.93639700   -0.66976500

H                 -0.79290200    3.08304600   -0.34706400