Supporting Information

A Non-enzymatic Ag/CuS-MWCNT-Chitosan/SPCE Sensor for Simultaneous Detection of Paraoxon-ethyl and Carbaryl

Orapan Pechtesa, Chiravoot Pechyena,d,*, Natthapon Nakpathomkunb,d, Itsarapong Chuasontiac, Benchamaporn Tangnorawichb,d,*

aDepartment of Material and Textile Technology, Faculty of Science and Technology, Thammasat University, Pathum Thani, 12120, Thailand

bDepartment of Physics, Faculty of Science and Technology, Thammasat University, Pathum Thani, 12120, Thailand

cFaculty of Learning Sciences and Education, Thammasat University, Pathum Thani, 12120, Thailand

dThammasat University Center of Excellence in Modern Technology and Advanced Manufacturing for Medical innovation, Thammasat University, Pathum Thani, 12120, Thailand

*Corresponding author. Department of Material and Textile Technology, Faculty of Science and Technology, Thammasat University, Pathum Thani, 12120, Thailand

E-mail address: chiravoot.p@gmail.com (C.Pechyen)

Table S1 Results of the Ag/CuS-modified electrode at different Ag concentrations

| Concentrations of Ag (M) | Ipa (µA) | Ipc (µA) | Ipa/Ipc | ΔEp (V) |
| --- | --- | --- | --- | --- |
| 0.10 | 821.047 | -726.856 | 1.130 | 0.369 |
| 0.25 | 854.670 | -786.155 | 1.087 | 0.343 |
| 0.50 | 893.366 | -829.467 | 1.077 | 0.382 |
| 0.75 | 957.036 | -831.553 | 1.151 | 0.395 |
| 1.00 | 908.287 | -773.430 | 1.174 | 0.401 |

Table S2 Results of nano-ink-modified SPCE recorded at different scan rates

| Scan rate (V/s) | Ipa (µA) | Ipc(µA) | Ipa/Ipc | ΔEp (V) |
| --- | --- | --- | --- | --- |
| 0.025 | 510.210 | -355.295 | 1.436 | 0.247 |
| 0.050 | 733.853 | -506.897 | 1.448 | 0.333 |
| 0.100 | 1014.549 | -726.578 | 1.396 | 0.438 |
| 0.200 | 1408.930 | -1135.720 | 1.241 | 0.605 |
| 0.300 | 1530.221 | -1298.666 | 1.178 | 0.715 |

Table S3 Results of the nano-ink SPCE in phosphate-buffered saline (PBS) at different pH values

| pH | Ipa (µA) | Ipc(µA) | Ipa/Ipc | ΔEp (V) |
| --- | --- | --- | --- | --- |
| 5 | 153.306 | -57.036 | 1.436 | 0.251 |
| 7 | 203.015 | -131.261 | 1.448 | 0.247 |
| 8 | 90.308 | -15.341 | 1.396 | 0.237 |
| 9 | 55.619 | -10.028 | 1.241 | 0.251 |

| Concentration of Pesticides (ppm) | Paraoxon-ethyl |  | Carbaryl |  |
| --- | --- | --- | --- | --- |
|  | Ipa (µA) | Epa (V) | Ipa (µA) | Epa (V) |
| 5 | 74.313 | 0.078 | 42.806 | 0.068 |
| 10 | 76.937 | 0.078 | 47.934 | 0.068 |
| 15 | 84.869 | 0.078 | 49.743 | 0.068 |
| 20 | 85.985 | 0.078 | 51.413 | 0.068 |
| 25 | 88.880 | 0.078 | 59.494 | 0.073 |
| 30 | 90.145 | 0.078 | 61.646 | 0.073 |

Table S4 Results of nano-ink-modified SPCE for the detection of paraoxon-ethyl and carbaryl (5–30 ppm)

Table S5 Results of Ag with ICP technique Ag/CuS Nanocomposite and nano-ink

| Sample name | Ag Quant Average (mg/L) | Ag RSD |
| --- | --- | --- |
| Ag/CuS | 1740 | 2.53 |
| Nano-ink | 1570 | 0.85 |

S1. Calibration curve of Ag Standard by ICP technique

Table S6 Fitting results of the Nyquist plots obtained for the nano-ink-modified SPCEs.

| Element | Fitted Value | Min Value | Max Value | Unit |
| --- | --- | --- | --- | --- |
| Rs | 109.2 | 1.00×10-6 | 1.00×1012 | Ω |
| Rct | 0.002 | 1.00×10-6 | 1.00×1012 | Ω |
| W1 | 294.2 | 1.00×10-6 | 1.00×1012 | σ |
| C1 | 2.994×10-4 | 1.00×10-12 | 1.00×10-3 | F |
| Chi-Squared (χ²): | 0.0003 |

S2.  Nyquist plots of the nano-ink-modified SPCE were obtained from a repeated experiment, showing results comparable to the previous measurement.

S3.  Nyquist plot of the nano-ink-modified SPCE from the previous experiment.

S4.  linear relation plot of logarithm of Ipa versus logarithm of scan rate (v)