Enhanced Hydrogen Generation from NaBH₄ Hydrolysis over Green-Synthesized Co₃O₄ Catalysts through Control of Parsley Ratio and Calcination Temperature

Simon W. Samouel1, Hatem A. Mahmoud 1,*, Bahaa M. Abu-Zied 2, Tarek T. Ali 1

1Chemistry Department, Sohag University, 82524 Sohag, Egypt

2Chemistry Department, Assiut University, 71516 Assiut, Egypt

Corresponding author: Hatem A. Mahmoud

Email address: hatem.elnakeeb@science.sohag.edu.eg

Fig. S1. X-ray diffraction patterns of PWB600 before and after hydrolysis of NaBH4.

Fig. S2. N2 adsorption isotherms (a) and distribution particle sizes (b) for green-synthesized catalysts.

Fig. S3. HGR values versus different parameters effect during NaBH4 hydrolysis over Co3O4 NPs: catalyst weight (a), concentration of NaBH4 (b), concentration of base (c), and cycles number (d).

Fig. S4. The linear relationship plots of PWB400-100 between ln (k) and ln (mcat) (a) and  ln (k) and ln (NaBH4 weight) (b).

Table S1. XPS binding energy and atomic percentage of Co2p, O1s, and C1s for the prepared catalysts PWB400-15, PWB400-100, and PWB400-150.

| Catalyst | PWB400-15 |  | PWB400-100 |  | PWB400-150 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | BE (eV) | Atomic (%) | BE (eV) | Atomic (%) | BE (eV) | Atomic (%) |
| Co3+ (2p3/2) (2p1/2) | 779.95 794.93 | 22.22 7.44 | 781.38 796.62 | 29.79 13.37 | 780.88 796.14 | 30.78 14.8 |
| Co2+ (2p3/2) (2p1/2) | 781.45 796.53 | 32.35 16.63 | 783.31 798.73 | 27.82 10.53 | 782.95 798.46 | 24.07 9.39 |
| Ratio of Co2+/Co3+ (2p3/2) | 1.46 |  | 0.93 |  | 0.78 |  |
| O 1s (lattice oxygen) | 529.92 | 35.61 | 531.01 | 32.78 | 530.68 | 52.34 |
| O 1s (oxygen defect) | 531.19 | 64.39 | 532.46 | 59.82 | 532.36 | 47.66 |
| O 1s (surface oxygen (H2O)) | ------- | ------- | 534.37 | 7.39 | ------- | ------- |
| Ratio of Olattice / Odefect | 0.553 |  | 0.548 |  | 1.098 |  |
| C 1s (C-C/C-H) | 284.57 | 50.73 | 285.63 | 56.89 | 284.82 | 38.19 |
| C 1s (C-O/C=O) | 286.1 | 32.08 | 287.36 | 30.73 | 286.18 | 39.05 |
| C 1s (O-C=O) | 288.38 | 17.18 | 289.92 | 12.39 | 288.75 | 22.76 |

Table S2. XPS binding energy and atomic percentage of Co2p, O1s, and C1s for the pre-treatment catalysts PWB300, PWB600, and PWB900.

| Catalyst | PWB300 |  | PWB600 |  | PWB900 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | BE (eV) | Atomic (%) | BE (eV) | Atomic (%) | BE (eV) | Atomic (%) |
| Co3+ (2p3/2) (2p1/2) | 780.29 795.37 | 23.93 9.01 | 780.14 795.17 | 16.14 6.36 | 779.74 794.91 | 11.44 5.11 |
| Co2+ (2p3/2) (2p1/2) | 781.85 797.08 | 31.18 14.71 | 781.55 797.04 | 39.05 16.76 | 781.05 796.83 | 39 17.33 |
| Ratio of Co2+/Co3+ (2p3/2) | 1.3 |  | 2.42 |  | 3.41 |  |
| O 1s (lattice oxygen) | 530.25 | 35.2 | 530.34 | 39.76 | 530.2 | 37.33 |
| O 1s (oxygen defect) | 531.55 | 64.8 | 531.7 | 60.24 | 531.74 | 62.67 |
| Ratio of Olattice / Odefect | 0.54 |  | 0.66 |  | 0.60 |  |
| C 1s (C-C/C-H) | 284.86 | 50.87 | 284.81 | 74.41 | 284.83 | 64.12 |
| C 1s (C-O/C=O) | 286.35 | 26.13 | 286.25 | 12.4 | 286.18 | 29.16 |
| C 1s (O-C=O) | 288.23 | 22.99 | 287.72 | 13.19 | 288.64 | 6.71 |