Facile synthesis of NiCo2O4/Fe-MOF and its use as a renewable electroactive material in a symmetrical supercapacitor and detection of non-Steroidal anti-inflammatory drug

Zena Abdul-Ameer Mahdia , Farqad A. Albaidhanib ,Hajar Altemeemic, Mohammad Bigdelood, Atefeh Omidid, Hasan Zandid, Ali Ehsani*d

aDepartment of Medical physics, College of Applied Medical Sciences, University of Kerbala, Karbala, Iraq, Postal code 56001, Zena.a.mahdy@uokerbala.edu.iq

bDepartment of Engineering, College of Engineering, Prosthetics and Orthotics University of Kerbala, Karbala, Iraq, Postal code 56001, farqad.abduljawad@uokerbala.edu.iq

cDepartment of Biochemistry, College of medicine, University of Kerbala, Karbala, Iraq

Postal code 56001, hajar.s@uokerbala.edu.iq.

dDepartment of Chemistry, Faculty of Science, University of Qom, Qom, Iran

*E-mail addresses: a.ehsani@qom.ac.ir

Table S1. Comparative study for detecting naproxen by newly fabricated NiCo2O4/Fe-MOF/ GCE with reported studies.

| LOD | Linear Range | Technique | Electrode / Modifier | Reference |
| --- | --- | --- | --- | --- |
| 0.222 nM | 0.05-3.0 μM | DPV | Gr/ZnFe2O4/ CPE | 1 |
| 0.23 μM | 1-200 μM | CV | ZnO/MWCNT/ CPE | 2 |
| 12.0 nM | 0.05-5.0μM | Amperometric | Alumina-modified GCE | 3 |
| 14.0 nM | 0.1-15.60μM | Amperometric | Au@f-CNT/GO/ GCE | 4 |
| 0.69 μM | 4.3-65.0μM | LSV | PLS/GCEc | 5 |
| 0.90 μM | 2.0-50.0μM | Amperometric | 3D-printed CB/ PLA | 6 |
| 0.23 μM | 4.3-87μM | CV | PLS/ rGO- Nafion/ GCE | 7 |
| 3.20 nM | 0.05-80.0μM | SWV | NiCo2O4/Fe-MOF | This Work |

[1] N. Soltani, N. Tavakkoli, E. Eslami, L.S. Mirmohammadi,  Electrochemical measurement of naproxen in the presence of diclofenac and ascorbic acid using Gr/ZnFe2O4/CPE, Diamond & Related Materials 141 (2024) 110569.

[2] J. Tashkhourian, B. Hemmateenejad, H. Beigizadeh, M. Hosseini-Sarvari, Z. Razmi, ZnO nanoparticles and multiwalled carbon nanotubes modified carbon paste electrode for determination of naproxen using electrochemical techniques, J. Electroanal. Chem. 714–715 (2014) 103–108.

[3] A.P. Lima, G.L. Nunes, R.G. Franco, R. Mariano-Neto, G.S. Oliveira, E.M. Richter, E. Nossol, R.A.A. Munoz, Al2O3 microparticles immobilized on glassy-carbon electrode as catalytic sites for the electrochemical oxidation and high detectability of naproxen: experimental and simulation insights, J. Electroanal. Chem. 882 (2021), 114988.

[4] K. Alagumalai, S. Musuvadhi Babulal, S.-M. Chen, R. Shanmugam, J. Yesuraj, Electrochemical evaluation of naproxen through Au@f-CNT/GO nanocomposite in environmental water and biological samples, J. Ind. Eng. Chem. 104 (2021) 32–42.

[5] C.-M. Hung, C.P. Huang, S.-K. Chen, C.-W. Chen, C.-D. Dong, Electrochemical analysis of naproxen in water using poly(l-serine)-modified glassy carbon electrode, Chemosphere 254 (2020), 126686.

[6] A.F. Jo˜ao, L.V. de Faria, D.L.O. Ramos, R.G. Rocha, E.M. Richter, R.A.A. Mu˜noz, 3D-printed carbon black/polylactic acid electrochemical sensor combined with batch injection analysis: a cost-effective and portable tool for naproxen sensing, Microchem. J. 180 (2022), 107565.

[7] C.-M. Hung, C.-P. Huang, C.-W. Chen, C.-D. Dong, A poly-(L-serine)/reduced graphene oxide–Nafion supported on glassy carbon (PLS/rGO􀀀 Nafion/GCE) electrode for the detection of naproxen in aqueous solutions, Environ. Sci. Pollut. Res. 29 (2022) 12450–12461.