Supplementary Figure

Figure S1. 13C NMR chemical shifts in [N(C2H5)4]2ZnCl4 measured at spinning speeds of 6 and 10 kHz.

Figure S2. Apparent 14N resonance positions in [N(C2H5)4]2ZnCl4 at spinning speeds of 5 and 7 kHz. The symbols x and o denote the spinning sidebands of the main peaks indicated by the arrows.

Figure S3. 14N NMR spectra of [N(C2H5)4]2ZnCl4 recorded at a spinning speed of 5 kHz as a function of temperature.

Figure S4. 1H spin-lattice relaxation time T1 in [N(C2H5)4]2ZnCl4 as a function of inverse temperature. Dot lines represent the activation energies.

Supplementary Table

Table S1. Atomic coordinates (×104) and equivalent isotropic displacement parameters (Å2×103) for [N(C2H5)4]2ZnCl4 at 300 K. U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

|  | x | y | z | U(eq) |  |
| --- | --- | --- | --- | --- | --- |
| Zn(1) Cl(1) | 2500 2500 | 7500 5478(3) | 7500 6611(2) |  | 66(1) 125(2) |
| N(1) | 2500 | 2500 | 4149(5) |  | 82(3) |
| C(1) | 4047(4) | 2500 | 4196(12) |  | 490(40) |
| C(2) | 4703(18) | 2500 | 5153(10) |  | 143(5) |
| C(3) | 2500 | 4047(6) | 4096(17) |  | 950(100) |
| C(4) H(1A) H(1B) H(2A) H(2B) H(2C) H(3A) H(3B) H(4A) H(4B) H(4C) | 2500 4413 4413 5764 4376 4376 3364 1636 2500 3367 1633 | 4740(30) 3365 1635 2500 3367 1633 4409 4409 5801 4427 4427 | 3149(13) 3883 3883 5119 5466 5466 4412 4412 3198 2831 2831 |  | 190(8) 583 583 214 214 214 1137 1137 286 286 286 |

Table S2. The bond-lengths (Å) and bond-angles (°) for [N(C2H5)4]2ZnCl4 at 300 K.

| Zn(1)-Cl(1)#1 | 2.260(3) | C(3)#4-C(1)-C(3) | 89.7(3) |
| --- | --- | --- | --- |
| Zn(1)-Cl(1)#2 | 2.260(3) | N(1)-C(1)-H(1A) | 108.4 |
| Zn(1)-Cl(1)#3 Zn(1)-Cl(1) | 2.260(2) 2.260(2) | C(2)-C(1)-H(1A) C(3)#4-C(1)-H(1A) | 108.4 140.6 |
| N(1)-C(1) | 1.400(4) | C(3)-C(1)-H(1A) | 68.6 |
| N(1)-C(1)#4 | 1.400(4) | N(1)-C(1)-H(1B) | 108.4 |
| N(1)-C(3)#4 | 1.400(5) | C(2)-C(1)-H(1B) | 108.4 |
| N(1)-C(3) | 1.400(5) | C(3)#4-C(1)-H(1B) | 68.6 |
| C(1)-C(2) | 1.550(4) | C(3)-C(1)-H(1B) | 140.6 |
| C(1)-H(1A) | 0.9700 | H(1A)-C(1)-H(1B) | 107.5 |
| C(1)-H(1B) | 0.9700 | C(1)-C(2)-H(2A) | 109.5 |
| C(2)-H(2A) | 0.9600 | C(1)-C(2)-H(2B) | 109.5 |
| C(2)-H(2B) | 0.9600 | H(2A)-C(2)-H(2B) | 109.5 |
| C(2)-H(2C) | 0.9600 | C(1)-C(2)-H(2C) | 109.5 |
| C(3)-C(4) | 1.550(4) | H(2A)-C(2)-H(2C) | 109.5 |
| C(3)-H(3A) | 0.9700 | H(2B)-C(2)-H(2C) | 109.5 |
| C(3)-H(3B) | 0.9700 | N(1)-C(3)-C(4) | 117.1(19) |
| C(4)-H(4A) | 0.9600 | N(1)-C(3)-C(1) | 44.91(13) |
| C(4)-H(4B) | 0.9600 | C(4)-C(3)-C(1) | 110.8(14) |
| C(4)-H(4C) | 0.9600 | N(1)-C(3)-C(1)#4 | 44.91(13) |
| Cl(1)#1-Zn(1)-Cl(1)#2 | 107.92(17) | C(4)-C(3)-C(1)#4 | 110.8(14) |
| Cl(1)#1-Zn(1)-Cl(1)#3 | 110.25(9) | C(1)-C(3)-C(1)#4 | 89.7(3) |
| Cl(1)#2-Zn(1)-Cl(1)#3 | 110.25(9) | N(1)-C(3)-H(3A) | 108.0 |
| Cl(1)#1-Zn(1)-Cl(1) | 110.25(9) | C(4)-C(3)-H(3A) | 108.0 |
| Cl(1)#2-Zn(1)-Cl(1) | 110.25(9) | C(1)-C(3)-H(3A) | 68.5 |
| Cl(1)#3-Zn(1)-Cl(1) | 107.92(17) | C(1)#4-C(3)-H(3A) | 140.2 |
| C(1)-N(1)-C(1)#4 | 174.2(15) | N(1)-C(3)-H(3B) | 108.0 |
| C(1)-N(1)-C(3)#4 | 90.16(7) | C(4)-C(3)-H(3B) | 108.0 |
| C(1)#4-N(1)-C(3)#4 | 90.16(7) | C(1)-C(3)-H(3B) | 140.2 |
| C(1)-N(1)-C(3) | 90.16(7) | C(1)#4-C(3)-H(3B) | 68.5 |
| C(1)#4-N(1)-C(3) | 90.16(7) | H(3A)-C(3)-H(3B) | 107.3 |
| C(3)#4-N(1)-C(3) | 174(2) | C(3)-C(4)-H(4A) | 109.5 |
| N(1)-C(1)-C(2) | 115.4(12) | C(3)-C(4)-H(4B) | 109.5 |
| N(1)-C(1)-C(3)#4 | 44.92(13) | H(4A)-C(4)-H(4B) | 109.5 |
| C(2)-C(1)-C(3)#4 | 109.9(11) | C(3)-C(4)-H(4C) | 109.5 |
| N(1)-C(1)-C(3) | 44.92(13) | H(4A)-C(4)-H(4C) | 109.5 |
| C(2)-C(1)-C(3) | 109.9(11) | H(4B)-C(4)-H(4C) | 109.5 |

Symmetry transformations used to generate equivalent atoms:

#1 -y+1,x+1/2,-z+3/2   #2 y-1/2,-x+1,-z+3/2   #3 -x+1/2,-y+3/2,z   #4 -x+1/2,-y+1/2,z