Description of Additional Supplementary Files

File Name: Supplementary Movie 1

Description: The movie shows the structural

phase changes upon the post-deposition annealing of a Sn on the Au(111) surface with an initial

coverage of 0.6ML (The energy of the electrons in the diffraction experiment is 40 eV). At room

temperature (start of the movie), the diffraction pattern of the X-phase can be observed (#1 to #60).

When the post-deposition annealing temperature increases, a gradual change from the X-phase to

an intermediate structures takes place (#300 to #420). At higher temperatures, the series of

diffraction patterns passes through the phase, around #570 and finally stabilizes at the diffraction

pattern of the √3-phase (above #990).