Three-dimensional bulk electronic structure of the Kondo lattice CeIn3 revealed by photoemission

Yun Zhang1,2*, Haiyan Lu1, Xiegang Zhu1, Shiyong Tan1, Qin Liu1, Qiuyun Chen1, Wei Feng1,

Donghua Xie1, Lizhu Luo1, Yu Liu4,5, Haifeng Song4,5, Zhengjun Zhang3, Xinchun Lai1*

1Science and Technology on Surface Physics and Chemistry Laboratory, Mianyang 621907, China

2Department of Engineering Physics, Tsinghua University, Beijing 100084, China

3School of Materials Science and Engineering, Advanced Materials Laboratory, Tsinghua University, Beijing 100084, China

4Laboratory of Computational Physics, Institute of Applied Physics and Computational Mathematics, Beijing 100088, China

5CAEP Software Center for High Performance Numerical Simulation, Beijing 100088, China

Supplementary Information

Figure S1. Valence band structure of CeIn3. (a) and (b) Photoemission intensity plots taken using 542 eV s-polarised light along the Γ-M and Γ-X directions, respectively.
    Figure S1 shows the ARPES spectra along the Γ-M and Γ-X directions. Two nearly non-dispersive f bands are observed around EF. If we change the relative intersection angle between the surface of the sample and the light source, the two flat f bands seem constant over all angles and over different photon energies. Namely, the two flat bands are apparently momentum and photon-energy independent. In fact, if hybridization between f electrons and conduction electrons occurs, then the f bands should not be visible in some of the momentum space around EF. The region where hybridization occurs should have an energy gap, and the f band should only be partially observed, as is shown in Fig. 4(c) in the main text. We propose that the f electrons in CeIn3 primarily remain nearly localized at ambient pressure and low temperature.