Additional Table 4: cell viability after 24 hours incubation on A549 cells, measured with MTT assay.
	Particle Name
	
	IC50 (µg/ml)
	IC75 (µg/ml)
	IC25 (µg/ml)

	Copper
	Lab. B
	13.49 (11.1-15.6)
	12.13
	15

	
	Lab. C
	17.04 (11.51-25.24)
	11.69
	24.84

	Copper (commercial source)
	Lab. A
	48.13 (28.13-82.36)
	34.65
	66.86

	
	Lab. C
	33.74 (28.8-42.48)
	15.54
	68.83

	Copper oxide (cuprous)
	Lab. A
	45 (38.6-52.45)
	26.86
	75.39

	
	Lab. C
	52.52 (42.23-65.3)
	36.33
	75.91

	Copper oxide (cupric)
	Lab. A
	47.41 (29.65-75.83)
	34.78
	64.62

	
	Lab. B
	35.61 (33.2-39.1)
	32.45
	39.08

	Copper oxide (cupric commercial source)
	Lab. B
	10.07 (5.71-17.73)
	6.72
	15.08

	
	Lab. C
	10.82 (8.08-14.49)
	6.89
	17

	Copper-Zinc mixed oxide variants
	Lab. B
	14.41 (8.14-25.5)
	9.21
	22.56

	
	Lab. C
	158.6 (69.72-360.8)
	29.43
	854.57

	Zinc oxide stoechiometric
	Lab. A
	66.17 (44.46-98.48)
	13.71
	319.24

	
	Lab. B
	34.31 (32.7-36.5)
	31.99
	36.79

	Zinc-Titania mixed oxide variants 50-50 mix
	Lab. A
	86.73 (73.89-101.8)
	49.95
	171.17

	
	Lab. C
	275.9 (203.1-374.6)
	131.53
	578.73

	Titania stoechiometric
	Lab. B
	NT
	
	

	
	Lab. C
	NT
	
	

	Titania non-stoechiometric
	Lab. A
	NT
	
	

	
	Lab. C
	NT
	
	

	Silver
	Lab. A
	42.67 (20.19-90.16)
	9.86
	187.73

	
	Lab. B
	NA
	
	

	Silver (commercial source)
	Lab. A
	NT
	
	

	
	Lab. C
	NT
	
	

	Cobalt
	Lab. A
	NT
	
	

	
	Lab. C
	NT
	
	

	Cobalt (commercial source)
	Lab. A
	1142 (405.2-3220)
	225.21
	>3300

	
	Lab. B
	3039 (81.72-112980)
	803.97
	>3300

	Nickel-Cobalt-Manganese mixed variants
	Lab. A
	NT
	
	

	
	Lab. C
	NT
	
	

	Nickel
	Lab. B
	NT
	
	

	
	Lab. C
	NT
	
	

	Nickel oxide
	Lab. B
	994.9 (937.3-1007.9)
	935.77
	1057.77

	
	Lab. C
	NT
	
	

	Zirconia
	Lab. A
	911.2 (613.4-1354)
	667.02
	1244.75

	
	Lab. C
	82.88 (39.99-171.8)
	34.68
	198.07

	Yttria doped Zirconia
	Lab. B
	NT
	
	

	
	Lab. C
	NT
	
	

	Stainless steel
	Lab. B
	NT
	
	

	
	Lab. C
	NT
	
	

	Alumina
	Lab. A
	NT
	
	

	
	Lab. B
	NT
	
	

	Tin oxide
	Lab. A
	NT
	
	

	
	Lab. B
	NT
	
	

	Tungsten carbide
	Lab. A
	NT
	
	

	
	Lab. B
	NT
	
	

	Ceria
	Lab. A
	NT
	
	

	
	Lab. B
	NT
	
	



TC50, TC25 and TC75 values (µg/ml) obtained with MTT assay, after 24 hours exposure of A549 cells, for each laboratory. 95% confidence interval is given in brackets for TC50. NT stands for Non Toxic (no TC50 could be calculated), and NA for Not Available (experiment not performed).





