Effects of artificial cell walls on syringyl-lignin growth reaction using recombinant cationic cell wall peroxidase

Naofumi Matsuhisa1,3, Go Tamura1, Natsumi Kawaguchi1, Koki Fujita2, Kengo Shigetomi4 and Yuji Tsutsumi2*

1, Department of Agro-Environmental Sciences, Graduate School of Agriculture, Kyushu University, 744 Motooka Nishi-Ku, Fukuoka, 819-0395, Japan

2, Faculty of Agriculture, Kyushu University, 744 Motooka Nishi-Ku, Fukuoka, 819-0395, Japan

3, Graduate School of Agriculture, Hokkaido University, Kita-9, Nishi-9, Kita-ku, Sapporo 060-8589, Japan

4, Research Faculty of Agriculture, Hokkaido University,Kita-9, Nishi-9, Kita-ku Sapporo 060-8589, Japan

*Corresponding author : y-tsutsu@agr.kyushu-u.ac.jp Tel: ＋81-092-802-4664

Fig. S1 FT-IR spectra of esterification compounds. orange line: LFXG, blue line: HFXG, gray line: XG, yellow line: FA

Fig. S2 confocal laser scanning microscopy images of the surface of various films. [A]: NOC, [B]: LFXG-film, [C]: HFXG-film, [D]: SLCF12, [E]: GLCF12.

Table S1 amount of FA monomers on films

| sample | Amount of FA (％) |
| --- | --- |
| LFXG-film | 0.036 |
| HFXG-film | 0.22 |

Fig. S3 Molecular weight distribution diagrams of DHPs. Red line: S-DHP at 270 nm, green dotted line: DHPs of SLCF-ZT at 270 nm, orange dotted line: DHPs of SLCF-AD at 270 nm, blue dotted line: DHPs of SLCF-LFXG at 270 nm, purple dotted line: DHPs of SLCF12 at 270 nm.

Fig. S4 SEM images of the surface of various films. [A]: LFXG-NOC, [B]: SLCF-LFXG, [C]:  SL-NOC, [D]: SL-XG-NOC, [E]: illustrated SLCF-non-ordered cellulose film. The blue arrow indicated the orientation of cellulose.

Fig. S5 Br-mapping images by EDXA [A]: HFXG-film, [A1]: HFXG-film, [B] HFXG-non-ordered cellulose film, [B1]: illustrated HFXG non-ordered cellulose film. The blue arrow indicated the orientation of cellulose.