Supporting Information

Graphene Oxide-Polymer Composite Langmuir Films Constructed by Interfacial Thiol-Ene Photopolymerization

Xiaona Luo1,2#, Kai Ma2,#, Tifeng Jiao1,2,3*, Ruirui Xing2,3, Lexin Zhang2, Jingxin Zhou2, Bingbing Li4,*

1State Key Laboratory of Metastable Materials Science and Technology, Yanshan University, Qinhuangdao 066004, P. R. China

2Hebei Key Laboratory of Applied Chemistry, School of Environmental and Chemical Engineering, Yanshan University, Qinhuangdao 066004, P. R. China

3State Key Laboratory of Biochemical Engineering, Institute of Process Engineering, Chinese Academy of Sciences, Beijing 100190, P. R. China

4Department of Chemistry and Biochemistry, Central Michigan University, Mount Pleasant, MI 48859, USA

Table S1. Elemental analysis data of as-prepared GO-based materials.

| Sample | C [wt.%] | H [wt.%] | N [wt.%] | S [wt.%] |
| --- | --- | --- | --- | --- |
| GO | 44.30 0.02 | 2.01 0.08 | -- | -- |
| GO-COOH | 44.70 0.06 | 2.10 0.07 | -- | -- |
| GO-SH | 49.87 0.07 | 4.33 0.04 | 9.74 0.03 | 10.10 0.07 |

Table S2. Comparison of XPS data and elemental analysis data of as-prepared GO-based materials.

| Sample | C [at. %] | C [wt. %] | N [at. %] | N [wt. %] | S [at. %] | S [wt. %] | N/C ratio [at./at.]% | S/C ratio [at./at.]% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| GO-SHa | 68.13 | -- | 9.66 | -- | 5.99 | -- | 14.2 | 8.79 |
| GO-SHb | 37.39b | 49.87 | 6.26b | 9.74 | 2.84b | 10.10 | 16.7 | 7.61 |

a, values calculated from integrated area in XPS data in Fig. S3; b, values calculated from elemental analysis data in Table S1.

Figure S1. XRD curves of as-prepared materials: graphite, GO, GO-COOH, and GO-SH, respectively.

Figure S2. Raman spectra (a) and D/G ratio analysis (b) of as-prepared materials: GO, GO-COOH, and GO-SH, respectively.

Figure S3. Survey XPS spectra (A) of present as-prepared lyophilized materials. Deconvolution of XPS C(1s) peaks of GO (B), GO-COOH (C), and GO-SH (D), respectively.

Figure S4. IR spectra of as-prepared materials: graphite, GO, GO-COOH, and GO-SH, respectively.

Figure S5. IR spectra of transferred 40-layered LB films of GO-SH from pure water surface and DA subphase by interfacial thiol-ene photopolymerization.

Figure S6. XRD curves of transferred 40-layered LB films of GO-SH from pure water surface and DA subphase by interfacial thiol-ene photopolymerization.