Supplementary material

Fig. S1 Overview of conductivity and stretchability with other works: rPET, PGW-1, PGW-2, PGW-3, PGW-4, PGW-5, graphite nanoplatelet welded carbon nanotube (GNP-w-CNT) [1], graphene/carboxymethylcellulose-2 (CE/CMC-2) [2], graphene aerogels-2 (GA-2) [3].

After an overall literature research (Fig. S1), the conductivity and stretchability properties of composite fabric were compared with those of previous researched materials, revealing that PGW-5 exhibited excellent electrical conductivity with 592 S/m, an outstanding property that could allow it to be used as a sensor for signal capture to monitor the full range of human movement or for applications in thermal therapy.

[1]	Zhang F, Ren D, Huang L, Zhang Y, Sun Y, Liu D, Zhang Q, Feng W, Zheng Q (2021) Advanced Functional Materials 31: 2107082.https://doi.org:https://doi.org/10.1002/adfm.202107082

[2]	Huang Z-M, Liu X-Y, Wu W-G, Li Y-Q, Wang H (2017) Journal of Materials Science 52: 12540-12552.https://doi.org:10.1007/s10853-017-1374-1

[3]	Afroze J D, Abden M J, Yuan Z, Wang C, Wei L, Chen Y, Tong L (2020) Carbon 162: 365-374.https://doi.org:10.1016/j.carbon.2020.02.057

Fig. S2 (R–R0)/R0 of PGW-5 from 0 to 5% at different temperatures (30 °C, 40 °C, 50 °C, 60 °C)

(R–R0)/R0 of PGW-5 at different temperatures (30 °C, 40 °C, 50 °C, 60 °C), as shown in Fig. S2 above. It had been found that the (R–R0)/R0 of PGW-5 was minimally affected by temperatures ranging from 30 °C to 60 °C, indicating that PGW-5 can maintain excellent sensing monitoring during thermotherapy and demonstrate the integration of both thermal therapy and sensing capabilities.