Additional file

1) DLS measurements

The system used a backscattering angle of 173° at a wavelength of 632.8 nm.

For batch-DLS measurements, the temperature of the measurement cell was set to 25 °C. All measurements were performed in automatic mode, which optimizes attenuation and cell position automatically. The directly obtained intensity-weighted size distribution is converted to a number-weighted distribution by the MALVERN Zetasizer software (version 7.11) according to a refractive index of 1.59.

For the flow-DLS measurements (AF4-UV-MALS-DLS) the cell position was set to 4.2 and the attenuation to 11, which means no attenuation. The measurement time was 3 seconds.

2) Sample preparation

Dilution with ultrapure water, no sonication, thorough mixing for 30 seconds.

3) AF4-UV-MALS-DLS Fractionation System (Postnova Analytics GmbH, Landsberg, Germany) consisting of:

AF2000 MT

PN7520 Solvent Degasser

PN1130 isocratic pump

PN 5300 Autosampler

PN4020 Channel oven

PN3211 UV Detector at a wavelength of 254 nm, R=0.0005

PN3621 MALS

DLS Zetasizer Nano S MALVERN

Injection volume 125 µL at a concentration of 20 mg/L.

4) AF4 separation method and fractogram

The measurements were carried out in triplicate. Further fractionation conditions were as follows: injection volume was adjusted to 125 µl, detector flow with 0.5 mL min-1, cross flow 1 mL min-1 with a power gradient of 0.2, injection flow 0.2 mL min-1 with an injection time of 7 min and a fractionation time of 50 min (see figure 1). A rinse step of 10 min at the end of the fractionation process was used between injections.

Figure S1: Separation program for AF4-measurements.

5) Data evaluation by AF4-MALS

Gyration diameters were calculated with the sphere model based on the Rayleigh-Debye-Gans Theory within the Postnova AF2000 control software. Detection angles from 12° till 156° (19 of 21 angles applied).
R(ϑ)c K=MP(ϑ)

with K: contrast factor; ϑ: Scattering angle; Rϑ: Rayleigh ratio; c: Concentration of the analyte; λ0 the wavelength; M: Molar mass.

K=4π2λ04NA(n0dndc)2

with: n0: refractive index of the solvent; dn/dc: refractive index increment of the analyte in solvent: λ0: wavelength of the light; NA: Avogadro’s number; r: radius of gyration.

q=sinϑ2

h=rq=r4πn0λ0sinϑ2

Sphere model: Pϑ=3h3sinh-hcosh2

1P(ϑ)=1+16π2n02r23λ02sin2(ϑ2)

5) Obtained results

- Batch-DLS

Figure S2: Intensity-weighted size distribution by batch-DLS.

Figure S3: Number-weighted size distribution by batch-DLS.

- AF4-UV-MALS-DLS

Figure S4: AF4-UV-MALS-DLS measurements corrected by a blank run with radius of gyration and hydrodynamic radius.

Table 1: Results of AF4-UV-MALS-DLS measurements of PS-F Nanoparticles.

|  | Peak maximum (22.8 min) |  |
| --- | --- | --- |
|  | Gyration diameter [nm] | Hydrodynamic diameter [nm] |
| run 1 | 46.2 | 73.4 |
| run 2 | 46.5 | 71.2 |  |  |  |
| run 3 | 46.7 | 72.4 |  |  |  |
| average | 46.4 | 72.3 |  |  |  |  |
|  | 0.3 | 1.2 |  |  |  |  |
| Gyration diameter [nm] | 46.4 ± 0.3 |  |  |  |  |  |  |
| Hydrodynamic diameter [nm] | 72.3 ± 1.2 |  |  |  |  |  |  |

Figure S5: Number-weighted size distribution obtained from AF4-DLS (n=3).

Figure S6: Mass-weighted size distribution obtained from AF4-UV-MALS (n=3).