Additional file for

Pyrolysis kinetic modelling of abundant plastic waste (PET) and in-situ emissions monitoring

Ahmed I. Osman a,b*, Charlie Farrell c,d, Ala'a H. Al-Muhtasebe, Ahmed S. Al-Fateshf, John Harrison c,  David W. Rooney a

a School of Chemistry and Chemical Engineering, Queen’s University Belfast, Belfast BT9 5AG, Northern Ireland, UK.

b Chemistry Department, Faculty of Science - Qena, South Valley University, Qena 83523 – Egypt.

c South West College, Cookstown, Co. Tyrone, BT80 8DN, Northern Ireland, UK.

d School of Mechanical and Aerospace Engineering, Queen’s University Belfast, Belfast BT9 5AH, Northern Ireland, UK.

e Department of Petroleum and Chemical Engineering, College of Engineering, Sultan Qaboos University, Muscat, Oman.

f Chemical Engineering Department, College of Engineering, King Saud University, P.O. Box 800, Riyadh 11421, Saudi Arabia.

Corresponding Author: Ahmed Osman

Email:  aosmanahmed01@qub.ac.uk

Address: School of Chemistry and Chemical Engineering, Queen's University Belfast, David Keir Building, Stranmillis Road, Belfast BT9 5AG, Northern Ireland, United Kingdom

Fax: +44 2890 97 4687

Tel.: +44 2890 97 4412

Figure S1: The PET sample used herein.

Temperature (°C)

Temperature (°C)

Temperature (°C)

(8 °C.min-1)

(4 °C.min-1)

(2 °C.min-1)

Temperature (°C)

dm/dt(%/min)

Figure S2: The % integrated mass derived from TGA results of PET pyrolysis at heating rates of 0.5, 1, 2, 4 and 8 °C.min-1. The integration of the DTG curve is shown in yellow and simulation results are shown by black lines.

Temperature (°C)

(1 °C.min-1)

(0.5 °C.min-1)

TG (%)

dm/dt(%/min)

dm/dt(%/min)

dm/dt(%/min)

TG (%)

TG (%)

dm/dt(%/min)

TG (%)

TG (%)

b)

Carbon graphitization

PET pyrolysis

a)

Carbon graphitization

PET pyrolysis

PET melting

Figure S3: The DSC-TGA thermogram of the PET pyrolysis at heating rate of 0.5 °C.min-1 (a) and 1°C.min-1 (b) under nitrogen atmosphere.

Figure S4: Benzene evolution during the PET pyrolysis.