Supplementary Information

Additional file 1

Title: Analysis of microbial populations in plastic–soil systems after exposure to high poly(butylene succinateco-adipate) load using high-resolution molecular technique

Benjawan Tanunchai1, Kantida Juncheed2,1, Sara Fareed Mohamed Wahdan1,3,4, Vusal Guliyev1,5, Maria Udovenko1, Ann-Sophie Lehnert6, Eliane Gomes Alves6, Bruno Glaser7, Matthias Noll8, François Buscot1,9*, Evgenia Blagodatskaya1,10*, Witoon Purahong1*¶

Affiliations:

1UFZ-Helmholtz Centre for Environmental Research, Department of Soil Ecology, Theodor-Lieser-Str. 4, 06120 Halle (Saale), Germany

2Department of Biomedical Science and Biomedical Engineering, Faculty of Medicine, Prince of Songkla University, Songkhla, 90110 Thailand

3Department of Biology, Leipzig University, Leipzig, Germany

4Botany Department, Faculty of Science, Suez Canal University, 41522 Ismailia, Egypt

5Institute of Soil Science and Agrochemistry, Azerbaijan National Academy of Sciences, 5 M.Rahim, AZ1073 Baku, Azerbaijan

6Max Planck Institute for Biogeochemistry, Biogeochemical Processes Department, Hans-Knöll-Str. 10,

07745 Jena, Germany.

7Soil Biogeochemistry, Martin Luther University Halle-Wittenberg, Von-Seckendorff-Platz 3, 06120 Halle (Saale), Germany

8Institute of Bioanalysis, Coburg University of Applied Sciences and Arts, Coburg, Germany

9German Centre for Integrative Biodiversity Research (iDiv) Halle-Jena-Leipzig, Deutscher Platz 5e, 04103 Leipzig, Germany

10Agro-Technological Institute, RUDN University, Miklukho-Maklaya 6, Moscow, 117198, Russia

¶ Correspondence

*Senior authors

Appendix 1. PBSA chemical and physical properties

Total C, H and N concentrations were determined with an Elementar Vario EL III elemental analyzer (Elementar Analysensysteme GmbH, Hanau, Germany). Physical properties are provided in BioPBS™ FD92PM / FD92PB Technical Data Sheet, PTT MCC Biochem Company Limited.

| Sample type | Total C (%) | H (%) | Total N (%) |
| --- | --- | --- | --- |
| PBSA | 56.940 | 7.371 | 0.000 |
| Properties Test |  | Test method | Unit | FD92PM / FD92PB |
| Density |  | ISO 1183 | g/cm3 | 1.24 |
| Melt index flow rate (190°C, 2.16 kg) |  | ISO 1133 | g/ 10 min | 4 |
| Melting point |  | ISO 3146 | °C | 84 |
| Tensile modulus | MD | ISO 527-3 | MPa | 280 |
|  | TD |  |  | 320 |
| Yield stress | MD | ISO 527-3 | MPa | 18 |
|  | TD |  |  | 17 |
| Stress at break | MD | ISO 527-3 | MPa | 32 |
|  | TD |  |  | 27 |
| Strain at break | MD | ISO 527-3 | % | 600 |
|  | TD |  |  | 580 |
| Elmendorf tear strength | MD | ISO 6383-2 | N/mm | 2 |
|  | TD |  |  | 5 |
| Puncture impact |  | PTTMCC method | kJ/m | 6 |

Figure S1. Rarefaction curves of archaea (a), bacteria (b), and fungi (c).

Figure S2. Links between soil pH and microbial richness: a) soil pH values of initial soil, control S, control SN, initial-N soil, and soils in PS, and PSN treatment on 90 days. Correlations between soil pH and richness of archaea (b), bacteria (c) and fungi (d).

Figure S3. Factors explain variations in microbial community composition: percent explainable variations of archaeal (a), bacterial (b), and fungal (c) communities explained by PBSA addition, N fertilization, soil pH, and combinations of these factors. Total variations of archaeal, bacterial, and fungal communities explained by PBSA addition, N fertilization, soil pH, and combinations of these factors are 13, 23 and 28%, respectively.

Table S1. Information on relative abundance (%) of archaeal ASVs detected in poly(butylene succinate-co-adipate) (PBSA) and soils of all treatments. Please see in another excel file.

Table S2. Information on relative abundance (%) of bacterial ASVs detected in poly(butylene succinate-co-adipate) (PBSA) and soils of all treatments. Please see in another excel file.

Table S3. Information on relative abundance (%) of fungal ASVs detected in poly(butylene succinate-co-adipate) (PBSA) and soils of all treatments. Please see in another excel file.

Table S4. Comparisons between microbial community compositions of (i) PBSA and soil counterparts and (ii) soils of different treatments and (iii) control soils (Control S and Control SN) and PBSA (PS and PSN treatments) using analysis of similarities (ANOSIM) and non-parametric multivariate analysis of variance (NPMANOVA).

(i)

| Comparison | Archaea |  | Bacteria |  | Fungi |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ANOSIM | NPMANOVA | ANOSIM | NPMANOVA | ANOSIM | NPMANOVA |
| PBSA-soil: PBSA vs. soil community composition | R = 0.91, P = 0.010 | F = 12.22, P = 0.008 | R = 1.00, P = 0.010 | F = 4.26, P = 0.008 | R = 0.70, P = 0.010 | F = 3.07, P = 0.008 |
| PBSA-soil-N: PBSA vs. soil community composition | R = 0.37, P = 0.007 | F = 5.01, P = 0.008 | R = 0.96, P = 0.007 | F = 3.74, P = 0.008 | R = 0.39, P = 0.040 | F = 2.38, P = 0.031 |

(ii)

| Comparison | Archaea |  | Bacteria |  | Fungi |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ANOSIM | NPMANOVA | ANOSIM | NPMANOVA | ANOSIM | NPMANOVA |
| Control S vs. Control SN | R = 0.03, P = 0.31 | F = 1.04, P = 0.374 | R = 1.00, P = 0.007 | F = 4.67, P = 0.008 | R = 1.00, P = 0.008 | F = 2.99, P = 0.009 |
| Control S vs. Soil-PS | R = 0.12, P = 0.24 | F = 1.39, P = 0.275 | R = 0.64, P = 0.008 | F = 2.09, P = 0.007 | R = 0.88, P = 0.008 | F = 3.44, P = 0.011 |
| Control S vs. Soil-PSN | R = 0.67, P = 0.008 | F = 4.67, P = 0.008 | R = 1.00, P = 0.007 | F = 4.97, P = 0.006 | R = 0.59, P = 0.008 | F = 4.62, P = 0.007 |
| Control SN vs. Soil-PS | R = 0, P = 0.696 | F = 0.80, P = 0.679 | R = 0.87, P = 0.009 | F = 3.91, P = 0.006 | R = 0.94, P = 0.008 | F = 3.92, P = 0.010 |
| Control SN vs. Soil-PSN | R = 0.53, P = 0.008 | F = 4.60, P = 0.006 | R = 0.94, P = 0.008 | F = 4.88, P = 0.009 | R = 0.59, P = 0.007 | F = 4.43, P = 0.008 |
| Soil-PS vs. Soil-PSN | R = 0.47, P = 0.015 | F = 3.47, P = 0.024 | R = 0.98, P = 0.009 | F = 3.84, P = 0.007 | R = 0.48, P = 0.008 | F = 3.14, P = 0.007 |

(iii)

| Comparison | Archaea |  | Bacteria |  | Fungi |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ANOSIM | NPMANOVA | ANOSIM | NPMANOVA | ANOSIM | NPMANOVA |
| Control S vs. PBSA-PS | R = 0.92, P = 0.008 | F = 12.16, P = 0.008 | R = 1.00, P = 0.008 | F = 5.82, P = 0.009 | R = 0.96, P = 0.008 | F = 5.20, P = 0.009 |
| Control S vs. PBSA-PSN | R = 0.37, P = 0.007 | F = 5.41, P = 0.009 | R = 1.00, P = 0.009 | F = 6.59, P = 0.007 | R = 1.00, P = 0.008 | F = 9.12, P = 0.007 |
| Control SN vs. PBSA-PS | R = 0.92, P = 0.008 | F = 12.98, P = 0.008 | R = 1.00, P = 0.008 | F = 6.36, P = 0.007 | R = 0.97, P = 0.009 | F = 5.16, P = 0.008 |
| Control SN vs. PBSA-PSN | R = 0.37, P = 0.008 | F = 5.71, P = 0.009 | R = 1.00, P = 0.009 | F = 7.15, P = 0.008 | R = 1.00, P = 0.008 | F = 8.87, P = 0.008 |
| PBSA-PS vs. PBSA-PSN | R = 0.22, P = 0.033 | F = 2.18, P = 0.031 | R = 1.00, P = 0.008 | F = 3.99, P = 0.008 | R = 0.96, P = 0.007 | F = 4.03, P = 0.007 |