Release of substances from joint grouts based on various binder types and their ecotoxic effects

Ute Schoknecht1*, Ute Kalbe1, Ines Heisterkamp2, Martina Kretzschmar2, Stefan Gartiser2, Oliver Happel3, Outi Ilvonen4

1BAM Federal Institute for Materials Research and Testing, Unter den Eichen 87 12205 Berlin, Germany

2Hydrotox GmbH, Freiburg, Germany

3TZW: DVGW-Technologiezentrum Wasser (German Water Center), Karlsruhe, Germany

4 German Environment Agency, Dessau, Germany

* Corresponding author: ute.schoknecht@bam.de, phone: +49 (0)30 / 8104 1413

Supporting Information

SI 1: Limits of quantification (LOQs) for anions and cations

LOQs for anions

| Anion | LOQ for experiments 1 and 2a in mg L-1 | LOQ for experiments 2b, 3a and 3b in mg L-1 |
| --- | --- | --- |
| F- | 0.014 | 0.27 |
| Cl- | 0.54 | 0.095 |
| Br- | 0.010 | 0.076 |
| NO2- | 0.015 | 0.10 |
| NO3- | 0.11 | 0.27 |
| PO43- | 0.032 | 0.27 |
| SO42- | 0.81 | 0.19 |

LOQs for elements

| Cation | LOQ ICP-OES Experiments 1 and 2a in µg L-1 | LOQ ICP-OES Experiments 2b, 3a and 3b in µg L-1 | LOQ ICP-MS Experiments 1 and 2a in µg L-1 | LOQ ICP-MS Experiments 2b, 3a and 3b in µg L-1 |
| --- | --- | --- | --- | --- |
| As |  |  | 0.03 | 1.50 |
| Ba | 2.0 | 0.36 |  | 0.05 |
| Cd | 2.5 |  | 0.026 |  |
| Cr | 3.5 | 0.77 | 0.031 |  |
| Cu |  |  | 0.77 | 2.54 |
| Hg |  |  | 0.050 | 0.34 |
| Mn | 2.4 | 0.30 |  | 0.05 |
| Mo | 2.0 | 0.49 | 0.12 |  |
| Ni |  |  | 0.15 |  |
| Pb |  |  | 0.050 |  |
| Sb |  |  | 0.034 | 7.7 |
| Sn | 4.1 | 1.0 |  | 0.020 |
| Sr | 2.3 | 0.3 |  |  |
| V | 1.4 | 1.4 |  |  |
| Zn |  |  | 0.022 |  |
| Co | 2.5 |  | 0.019 |  |
| Al | 470 | 34 |  |  |
| Ca | 80 | 67 |  |  |
| Fe | 62 | 86 |  |  |
| K | 77 | 170 |  |  |
| Mg | 95 | 51 |  |  |
| Na | 170 | 4100 |  | 0.46 |
| B | 93 | 11 |  |  |
| P | 19 | 13 |  |  |
| S | 23 | 13 |  | 0.014 |
| Se |  |  | 0.18 | 1.50 |
| Si | 250 | 4900 |  | 0.05 |
| Ti | 8400 | 2500 |  |  |
| Tl |  |  | 0.022 |  |

SI 2: Analytical methods on organic substances applied at BAM

Sample preparation for quantitative analysis and GC-MS screening of eluates at BAM

100 ml of the sample were transferred to a separating funnel of 250 ml capacity. Extraction was performed first under acidic conditions and then repeated under alkaline conditions. The pH of the samples was adjusted to pH 2 by 1 ml HCl (1 mol L-1) and controlled by means of pH paper. Subsequently, the samples were extracted twice for 3 min using 30 ml dichlormethane for each step. The dichlormethane extracts were dried on sodium sulfate and transferred to a 100 ml pear shaped flask and combined. The remaining aqueous samples were adjusted to pH 10 by addition of 4 ml NaOH (1 mol L-1). Again, the pH was controlled by means of pH paper. The procedure was continued as described for extraction under acidic conditions. The combined extracts were reduced to a volume of 1 ml using a rotary evaporator, completely transferred to 2 ml vials and analyzed.

GC-MS methods

GC-MS-System:			Agilent 6890N GC-System equipped with an Agilent 7683B 					autosampler

Detector:			Agilent 5973Network Mass Selective Detector

Column:			HP-5MS, 30 m x 0.25 mm ID, 0.25 µm

Carrier gas:			Helium

Flow rate:			He, 1.0 ml min-1

Split-Mode:			Pulsed splitless

Injection volume:		1.0 µl

Injector temperature:		280 °C

Oven program:			60 °C (2 min), 30 ° min-1 to 120°C, 5 ° min-1 to 320 °C (5 min)

MS-Parameters for Screening

Mode: 				EI-SCAN

Tune: 				Autotune (Atune)

Transfer line temperature:	280 °C

MS Source temperature:	230 °C

MS Quad temperature:		150 °C

Ionization Energy: 		70 eV

Scan Mass Range: 		m/z 30 to m/z 650

MS-Parameters for quantitative analysis of benzyl alcohol, 4-tert-butylphenol, 1,3-benzenedimethanamine, N,N-dimethyl-1-dodecanamine, 2-ethylhexanoic acid

Mode: 				EI-SIM

Tune: 				Autotune (Atune)

Transfer line temperature:	280 °C

MS Source temperature:	230 °C

MS Quad temperature:		150 °C

Ionization Energy: 		70 eV

Calibration standards

| Substance | CAS | Supplier | Purity in % |
| --- | --- | --- | --- |
| Benzyl alcohol | 100-51-6 | Chemsolut | 99.8 |
| 2-Ethylhexanoic acid | 149-57-5 | Sigma-Aldrich | >99.0 |
| 4-tert-Butylphenol | 98-54-4 | HPC Standards GmbH | 99.9 |
| 1,3-Benzenedimethanamine | 1477-55-0 | Sigma-Aldrich | 99.0 |
| N,N-Dimethyl-1-dodecanamine | 112-18-5 | HPC Standards GmbH | 98.3 |

Signals for quantification by external calibration

| Substance | CAS | Signal | Retention time | Calibration range |
| --- | --- | --- | --- | --- |
|  |  | In m/z | In min | In mg l-1 |
| Benzyl alcohol | 100-51-6 | 108 | 5.13 | 1 - 20 |
| 2-Ethylhexanoic acid | 149-57-5 | 88 | 5.89 | 1 - 20 |
| 4-tert-Butylphenol | 98-54-4 | 135 | 8.14 | 1 - 20 |
| 1,3-Benzenedimethanamine | 1477-55-0 | 106 | 9.45 | 1 - 20 |
| N,N-Dimethyl-1-dodecanamine | 112-18-5 | 58 | 11.75 | 1 - 20 |

Identification of substances

Substances were tentatively identified by comparing observed mass spectra with the spectra libraries NIST 14 and RTLPest 2. Selected spectra were also compared with the spectra library NIST 17.

The structures of the quantified substances were confirmed by reference standards.

SI 3: Analytical methods on organic substances applied at TZW

Sample preparation for GC-MS screening at TZW

200 ml of the sample were extracted first under acidic conditions and then repeated under alkaline conditions. Before extraction approx. 5 mg ascorbic acid and the mixture of labelled internal standards (100 µl) were added to the sample. The pH of the samples was adjusted to pH 2 by HCl (10 %). The samples were extracted twice using 50 ml dichlormethane for each step. The dichlormethane extracts were dried on sodium sulfate and transferred to a 100 ml pear shaped flask and combined. The remaining aqueous samples were adjusted to pH 10 by NaOH (0.5 mol L-1). The procedure was continued as described for extraction under acidic conditions (2x extraction by 50 mL dichlormethane and drying on sodium sulfate). The combined extracts were reduced in a first step to a volume of approx. 5 ml using a rotary evaporator (30 °C, approx. 580 mbar) and in a second step evaporated to 0.5 ml by using a TurboVap.

Internal standards for semiquantitative measurements (in acetone)

d21-BHT 80 ng µL-1 
d5-Chlorbenzol 20 ng µL-1

d34-Hexadecan 10 ng µL-1
 d8-Naphthalin 10 ng µL-1
 d10-Phenanthren 20 ng µL-1
 d5-Phenol 80 ng µL-1
 d62-Squalan 80 ng µL-1

GC-MS method

GC-MS-System:                             Agilent GC/MS-system 6890N

Detector:			Agilent MSD 5973 Network Mass Selective Detector

Column:			Rtx-5MS, 60 m x 0.25 mm ID, 0.25 µm

Carrier gas:                                    Helium

Flow rate:			He, 1.5 ml He min-1

Split-Mode:                                    Splitless

Injection volume:                         1.0 µl

Injector temperature:		280 °C

Oven program:                              38 °C (7 min), 8 ° min-1 to 200°C, (4 min), 10 ° min-1 to 280 °C (16 min)
 				runtime approx. 55 min

MS-Parameters for Screening

Mode: 				EI-SCAN

Tune: 				Autotune (Atune)

Transfer line temperature:	280 °C

MS Source temperature:	200 °C

MS Quad temperature:		150 °C

Ionization Energy: 		70 eV

Scan Mass Range: 		m/z 30 to m/z 650

The working range is approx. 1 µg L-1 to 500 µg L-1. In contrast to DIN EN 15768, the measurement must be made at a starting temperature of 38 °C instead of 30 °C, as the measurement instrument reaches the low value only very slowly at normal ambient temperature. For the measurement it is necessary to carry a laboratory blank value. Signals that clearly differ from the laboratory blank value are evaluated. The NIST spectrum database is used to search for matches. The evaluation and integration of the areas of internal standards and signals in the sample is done via the TIC.

LC-ESI-QTOF method

LC system	 	Agilent 1200 Series

Column			Zorbax Eclipse Plus C18 (150 mm x 2.1 mm, 3 µm, Agilent)

Injection volume	100 µL (direct injection)

Flow 			0.30 mL min-1

Temperature 		30 °C

Mobile phase A		0.1% formic acid in water

Mobile phase B 	0.1% formic acid in acetonitrile

Elution profile

| time |  | mobile phase A | mobile phase B |
| --- | --- | --- | --- |
| 1 | min | 98 % | 2 % |
| 2 | min | 80 % | 20 % |
| 16.5 | min | 0 % | 100 % |
| 22 | min | 0 % | 100 % |
| 22.1 | min | 98% | 2 % |
| 30 | min | 98 % | 2 % |

Detection

ESI-QTOF	 	TripleTOF 6600, Sciex

Ionization 		positive and negative (ESI+ and ESI-)

Mass Range 		m/z 100 to m/z 1200

Data evaluation

The LC screening was matched with a list of potential substances from roofing films and lack as [M+H+]+ or [M-H+]- and with MS2 spectra from the manufacturer Sciex. In addition, a screening for signals with clearly positive hits (significant spectra, not just a fragment) was carried out at the MS2 spectra database (Sciex) (list: LC(NIST)).

Conditions for a positive hit:

a) The difference of the measured mass from the exact mass is < 5 ppm (calculated from sum formula).

b) The signal-to-noise (S/N) > 10 and the signal in the blank is 10 times lower to the measured signal.

c) The MS2 spectrum match and a reference spectrum are present (dot in the LC(NIST) column). In addition, a score of > 70 was found.

LC-DAD method

LC system	 	Agilent 1100 Series

Column			Nucleodur C18 Gravity

(150 mm x 2 mm, 3 µm, Macherey Nagel)

Injection volume	20 µl (direct injection)

Flow 			0.45 ml/min

Temperature 		30 °C

Mobile phase A		phosphoric acid in water (10 mmol L-1)

Mobile phase B 	phosphoric acid in acetonitrile (10 mmol L-1)

Elution profile

| time |  | mobile phase A | mobile phase B |
| --- | --- | --- | --- |
| 0 | min | 90 % | 10 % |
| 1 | min | 90 % | 10 % |
| 10 | min | 0 % | 100 % |
| 15 | min | 0 % | 100 % |
| 15,5 | min | 90 % | 10 % |
| 22 | min | 90 % | 10 % |

Detection

diode array detector 	Agilent 1100er series (G1315B)

range 			200 nm to 360 nm

SI 4: Data on test assemblies

1*: percolation test, all other experiments: DSLT

DSLT: Total water volume from two eluation periods: 4.8 L, percolation test: Water volume at L/S 2: 4.8 L

28**: test specimens were covered by cling film during storage

| Code | Experiment | Duration of storage | Mass of test specimen or test material at the beginning of the test in g | Mass of test specimen or test material at the beginning of the test in g | Total water uptake in g | Water uptake in % |
| --- | --- | --- | --- | --- | --- | --- |
| MOE1 | 1 | 12 | 532 | 589 | 57 | 11 |
| MOE1 | 1* | 46 | 2400 | not determined |  |  |
| MOE1 | 3a | 7 | 589 | 667 | 78 | 13 |
| MOE1 | 3a | 14 | 550 | 620 | 70 | 13 |
| MOE1 | 3b | 28 | 462 | 530 | 68 | 15 |
| MOE1 | 3b | 28** | 508 | 578 | 70 | 14 |
| MOE2 | 2a | 8 | 658 | 727 | 69 | 10 |
| MOE2 | 2b | 7 | 540 | 550 | 10 | 2 |
| MOE3 | 2a | 8 | 806 | 874 | 68 | 8 |
| MOE3 | 2b | 7 | 654 | 737 | 83 | 13 |
| MOE4 | 2a | 7 | 777 | 858 | 81 | 10 |
| MOE4 | 2b | 7 | 624 | 696 | 72 | 12 |
| MOE5 | 2a | 10 | 612 | 627 | 15 | 2 |
| MOE5 | 2b | 7 | 546 | 551 | 5 | 1 |
| MOE6 | 2a | 11 | 577 | 676 | 99 | 17 |
| MOE6 | 2b | 7 | 536 | 558 | 22 | 4 |
| MOE7 | 2a | 7 | 596 | 637 | 41 | 7 |
| MOE7 | 3a | 7 | 555 | 600 | 45 | 8 |
| MOE7 | 3a | 14 | 517 | 557 | 40 | 8 |
| MOE7 | 3b | 28 | 472 | 492 | 20 | 4 |
| MOE7 | 3b | 28** | 479 | 503 | 23 | 5 |
| MOE8 | 2a | 12 | 683 | 697 | 14 | 2 |
| MOE8 | 2b | 7 | 550 | 558 | 8 | 1 |

Comment:  formation of foam in eluate samples of MOE1, MOE2, MOE6, MOE7

SI 5: Results for TOC, TN, pH, conductivity and turbidity of eluates

Eluates 1 + 2 originate from DSLT, L/S 2 fraction originates from percolation tests

28*: test specimens were covered by cling film during storage

| Experiment | Code | Storage in d | Sample | TOC in mg L-1 | TN in mg L-1 | pH | Conductivity in µS cm-1 | Turbidity in FNU |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Blank | - | Eluate 1 + 2 | 0.24 | < 0.05 | 7.3 | 3.5 | n.d. |
| 1 | MOE1 | 12 | Eluate 1 + 2 | 427 | 81.0 | 9.1 | 240 | n.d. |
| 1 | MOE1 | 46 | L/S 2 fraction | 1280 | 270 | 9.0 | 600 | 7.03 |
| 3a | Blank | - | Eluate 1 + 2 | 0.27 | < 0.05 | 7.1 | 2.8 | n.d. |
| 3b | Blank | - | Eluate 1 + 2 | 1.33 | < 0.05 | 6.9 | 1.7 | n.d. |
| 3a | MOE1 | 7 | Eluate 1 + 2 | 401 | 70.1 | 9.1 | 236 | n.d. |
| 3a | MOE1 | 14 | Eluate 1 + 2 | 410 | 77.2 | 9.2 | 262 | n.d. |
| 3b | MOE1 | 28 | Eluate 1 + 2 | 324 | 63.5 | 9.2 | 240 | n.d. |
| 3b | MOE1 | 28* | Eluate 1 + 2 | 379 | 74.7 | 9.3 | 238 | n.d. |
| 2a | Blank | - | Eluate 1 + 2 | 0.9 | < 0.05 | 7.0 | 2.0 | n.d. |
| 2b | Blank | - | Eluate 1 + 2 | 0.14 | < 0.05 | 7.1 | 1.8 | n.d. |
| 2a | MOE2 | 8 | Eluate 1 + 2 | 72.8 | < 0.05 | 3.9 | 64 | n.d. |
| 2b | MOE2 | 7 | Eluate 1 + 2 | 43.1 | < 0.05 | 4.0 | 55 | n.d. |
| 2a | MOE3 | 8 | Eluate 1 + 2 | 59.2 | 0.22 | 11.8 | 2310 | n.d. |
| 2b | MOE3 | 7 | Eluate 1 + 2 | 105 | 0.50 | 12.0 | 3050 | n.d. |
| 2a | MOE4 | 7 | Eluate 1 + 2 | 5.53 | < 0.05 | 11.5 | 1170 | n.d. |
| 2b | MOE4 | 7 | Eluate 1 + 2 | 1.50 | < 0.05 | 11.9 | 1780 | n.d. |
| 2a | MOE5 | 10 | Eluate 1 + 2 | 1.16 | < 0.05 | 8.3 | 3.3 | n.d. |
| 2b | MOE5 | 7 | Eluate 1 + 2 | 0.59 | < 0.05 | 8.0 | 3.5 | n.d. |
| 2a | MOE6 | 11 | Eluate 1 + 2 | 556 | 36.2 | 9.5 | 103 | n.d. |
| 2b | MOE6 | 7 | Eluate 1 + 2 | 355 | 29.9 | 9.5 | 133 | n.d. |
| 2a | MOE7 | 7 | Eluate 1 + 2 | 42.8 | < 0.05 | 4.1 | 43.6 | n.d. |
| 3a | MOE7 | 7 | Eluate 1 + 2 | 36.4 | 0.13 | 4.1 | 54.2 | n.d |
| 3a | MOE7 | 14 | Eluate 1 + 2 | 36.4 | 0.25 | 4.4 | 36.7 | n.d. |
| 3b | MOE7 | 28 | Eluate 1 + 2 | 38.6 | 0.40 | 4.4 | 45.0 | n.d. |
| 3b | MOE7 | 28* | Eluate 1 + 2 | 44.0 | 0.31 | 4.0 | 63.4 | n.d. |
| 2a | MOE8 | 12 | Eluate 1 + 2 | 4.55 | 0.19 | 8.8 | 7.1 | 4.55 |
| 2b | MOE8 | 7 | Eluate 1 + 2 | 3.48 | 0.21 | 7.4 | 9.0 | 3.48 |

SI 6: Concentration of anions in eluates from DSLT and percolation test

Eluates 1 + 2 originate from DSLT, L/S 2 fraction originates from percolation test, 28*: test specimens were covered by cling film during storage

| Experiment | Code | Storage period in d | Sample | F- in mg L-1 | Cl- in mg L-1 | Br- in mg L-1 | NO2- in mg L-1 | NO3- in mg L-1 | PO43- in mg L-1 | SO42- in mg L-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Blank | - | Eluate 1 + 2 | 0.02 | < 0.54 | 0.08 | < 0.015 | 0.37 | 0.55 | 0.90 |
| 1 | MOE1 | 12 | Eluate 1 + 2 | 0.87 | 2.99 | 0.61 | 0.45 | 0.39 | 0.48 | 1.76 |
| 1 | Blank | - | Blind column | 0.05 | < 0.54 | 0.08 | 0.29 | 0.39 | 0.47 | 0.42 |
| 1 | MOE1 | 46 | L/S 2 fraction | 0.11 | 9.83 | 1.38 | 0.70 | 0.47 | 0.60 | 5.38 |
| 3a | Blank | - | Eluate 1 + 2 | <0.267 | <0.095 | <0.105 | <0.076 | <0.271 | <0.266 | 0.37 |
| 3b | Blank | - | Eluate 1 + 2 | <0.267 | <0.095 | <0.105 | <0.076 | <0.271 | 0.847 | <0.19 |
| 3a | MOE1 | 7 | Eluate 1 + 2 | <0.267 | 3.27 | 0.241 | <0.076 | 0.31 | 0.89 | 59.5 |
| 3a | MOE1 | 14 | Eluate 1 + 2 | <0.267 | 3.27 | 0.239 | 0.087 | 0.30 | 0.89 | 57.4 |
| 3b | MOE1 | 28 | Eluate 1 + 2 | <0.267 | 2.70 | 0.189 | 0.15 | <0.271 | 0.87 | 45.8 |
| 3b | MOE1 | 28* | Eluate 1 + 2 | <0.267 | 3.17 | 0.216 | <0.076 | <0.271 | 0.88 | 52.7 |
| 2a | Blank | - | Eluate 1 + 2 | 0.021 | 0.025 | <0.017 | <0.016 | <0.078 | 1.52 | <0.28 |
| 2b | Blank | - | Eluate 1 + 2 | <0.267 | 0.14 | <0.105 | <0.076 | <0.271 | <0.266 | 0.27 |
| 2a | MOE2 | 8 | Eluate 1 + 2 | 0.33 | 0.11 | <0.017 | 0.035 | <0.078 | 1.43 | 0.326 |
| 2b | MOE2 | 7 | Eluate 1 + 2 | <0.267 | 0.10 | <0.105 | 0.084 | <0.271 | <0.266 | 0.283 |
| 2a | MOE3 | 8 | Eluate 1 + 2 | 0.066 | 0.06 | <0.017 | 0.15 | <0.078 | 2.99 | 0.354 |
| 2b | MOE3 | 7 | Eluate 1 + 2 | <0.267 | 0.45 | <0.105 | 0.20 | <0.271 | <0.266 | 3.62 |
| 2a | MOE4 | 7 | Eluate 1 + 2 | 0.13 | 3.51 | <0.017 | <0.016 | 0.093 | 1.45 | 47.6 |
| 2b | MOE4 | 7 | Eluate 1 + 2 | <0.267 | 3.21 | <0.105 | <0.076 | <0.271 | 1.31 | 34.6 |
| 2a | MOE5 | 10 | Eluate 1 + 2 | 0.022 | 0.04 | <0.017 | <0.016 | 0.092 | 1.54 | <0.28 |
| 2b | MOE5 | 7 | Eluate 1 + 2 | <0.267 | 0.10 | <0.105 | <0.076 | <0.271 | <0.266 | 0.182 |
| 2a | MOE6 | 11 | Eluate 1 + 2 | 0.048 | 1.68 | <0.017 | 0.028 | 0.23 | 1.64 | 2.21 |
| 2b | MOE6 | 7 | Eluate 1 + 2 | <0.267 | 0.87 | <0.105 | 0.11 | <0.271 | 0.86 | 2.41 |
| 2a | MOE7 | 7 | Eluate 1 + 2 | 0.15 | 0.09 | <0.017 | 0.024 | <0.078 | 1.46 | 0.369 |
| 3a | MOE7 | 7 | Eluate 1 + 2 | <0.267 | <0.095 | <0.105 | 0.15 | <0.271 | <0.266 | 0.286 |
| 3a | MOE7 | 14 | Eluate 1 + 2 | <0.267 | <0.095 | <0.105 | 0.11 | <0.271 | <0.266 | 0.310 |
| 3b | MOE7 | 28 | Eluate 1 + 2 | <0.267 | <0.095 | <0.105 | 0.13 | <0.271 | <0.266 | <0.19 |
| 3b | MOE7 | 28* | Eluate 1 + 2 | <0.267 | <0.095 | <0.105 | 0.12 | <0.271 | <0.266 | <0.19 |
| 2a | MOE8 | 12 | Eluate 1 + 2 | 0.02 | 0.05 | <0.017 | 0.20 | <0.078 | 1.57 | <0.28 |
| 2b | MOE8 | 7 | Eluate 1 + 2 | <0.267 | 0.101 | <0.105 | <0.076 | <0.271 | 0.861 | 0.309 |

SI 7: Concentration of cations in eluates from DSLT and percolation test

Results from ICP-OES analysis (part 1)

Eluates 1 + 2 originate from DSLT, Fractions L/S 2 originate from percolation tests, 28*: test specimens were covered by cling film during storage

| Experi-ment | Code | Storage period in d | Sample | Ba in µg L-1 | Cd in µg L-1 | Cr in µg L-1 | Mn in µg L-1 | Mo in µg L-1 | Sn in µg L-1 | Sr in µg L-1 | V in µg L-1 | Co in µg L-1 | Al in µg L-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Blank | - | Eluate 1 + 2 | <2.0 | <2.5 | <3.5 | <2.4 | <2.0 | <4.1 | <2.3 | <1.4 | <2.5 | <474 |
| 1 | MOE1 | 12 | Eluate 1 + 2 | 2.01 | <2.5 | <3.5 | 3.21 | <2.0 | <4.1 | 47.1 | <1.4 | <2.5 | <474 |
| 1 | Blank | - | Blind column | <2.0 | <2.5 | <3.5 | <2.4 | <2.0 | <4.1 | <2.3 | <1.4 | <2.5 | <474 |
| 1 | MOE1 | 46 | L/S 2 fraction | 25.8 | <2.5 | <3.5 | 41.3 | 4.85 | <4.1 | 104 | 2.85 | 2.52 | 1470 |
| 3a | Blank | - | Eluate 1 + 2 | <0.36 | <0.031 | <0.77 | <0.30 | <0.49 | <1.0 | <0.32 | <1.3 | <0.020 | <34 |
| 3b | Blank | - | Eluate 1 + 2 | <0.36 | <0.031 | <0.77 | <0.30 | <0.49 | <1.0 | <0.32 | <1.3 | <0.020 | <34 |
| 3a | MOE1 | 7 | Eluate 1 + 2 | 1.51 | <0.031 | <0.77 | 6.89 | 13.6 | <1.0 | 48.4 | <1.3 | 0.91 | <34 |
| 3a | MOE1 | 14 | Eluate 1 + 2 | 1.95 | <0.031 | <0.77 | 5.76 | 13.4 | <1.0 | 51.3 | <1.3 | 0.98 | <34 |
| 3b | MOE1 | 28 | Eluate 1 + 2 | 2.13 | <0.031 | <0.77 | 5.76 | 10.9 | <1.0 | 47.1 | <1.3 | 0.82 | <34 |
| 3b | MOE1 | 28* | Eluate 1 + 2 | 1.06 | <0.031 | <0.77 | 6.11 | 12.8 | <1.0 | 53.7 | <1.3 | 1.03 | <34 |
| 2a | Blank | - | Eluate 1 + 2 | <0.51 | <0.84 | <1.6 | <0.30 | <0.80 | 11.2 | 11.2 | <1.6 | <2.7 | <21 |
| 2b | Blank | - | Eluate 1 + 2 | <0.36 | <0.036 | <0.77 | <0.30 | <0.49 | <0.10 | <0.32 | <1.3 | <0.02 | <34 |
| 2a | MOE2 | 8 | Eluate 1 + 2 | 8.39 | <0.84 | <1.6 | 21.3 | <0.80 | 12.0 | 2.07 | <1.6 | 1600 | 135 |
| 2b | MOE2 | 7 | Eluate 1 + 2 | 4.37 | <0.031 | <0.77 | 522 | <0.49 | <0.10 | 1.51 | <1.3 | 1190 | <34 |
| 2a | MOE3 | 8 | Eluate 1 + 2 | 674 | <0.84 | <1.6 | <0.30 | <0.80 | 9.03 | 693 | <1.6 | <2.7 | 535 |
| 2b | MOE3 | 7 | Eluate 1 + 2 | 1910 | <0.031 | 1.01 | <0.30 | <0.49 | 1.02 | 1480 | <1.3 | 0.56 | 494 |
| 2a | MOE4 | 7 | Eluate 1 + 2 | 29.5 | <0.84 | 5.47 | <0.30 | 7.28 | 10.5 | 231 | <1.6 | <2.7 | 31900 |
| 2b | MOE4 | 7 | Eluate 1 + 2 | 33.5 | <0.031 | 3.76 | <0.30 | 5.52 | 0.36 | 349 | <1.3 | 0.13 | 16900 |
| 2a | MOE5 | 10 | Eluate 1 + 2 | 1.45 | <0.84 | <1.6 | <0.30 | <0.80 | 976 | <0.54 | <1.6 | <2.7 | <21 |
| 2b | MOE5 | 7 | Eluate 1 + 2 | 1.52 | <0.031 | <0.77 | <0.30 | <0.49 | 725 | <0.32 | <1.3 | <0.02 | <34 |
| 2a | MOE6 | 11 | Eluate 1 + 2 | 17.8 | <0.84 | <1.6 | 0.38 | <0.80 | 80.3 | 5.51 | <1.6 | <2.7 | 33.8 |
| 2b | MOE6 | 7 | Eluate 1 + 2 | 11.6 | <0.031 | <0.77 | <0.30 | <0.49 | 31.4 | 2.41 | <1.3 | <0.02 | <34 |
| 2a | MOE7 | 7 | Eluate 1 + 2 | 6.74 | <0.84 | <0.77 | 1320 | <0.80 | 10.4 | 1.00 | <1.6 | <2.7 | 74.9 |
| 3a | MOE7 | 7 | Eluate 1 + 2 | 3.03 | <0.031 | <0.77 | 599 | <0.49 | <1.0 | <0.32 | <1.3 | <1.3 | 45.4 |
| 3a | MOE7 | 14 | Eluate 1 + 2 | 5.28 | <0.031 | <0.77 | 655 | <0.49 | <1.0 | 1.89 | <1.3 | <1.3 | 37.6 |
| 3b | MOE7 | 28 | Eluate 1 + 2 | 1.59 | <0.031 | <0.77 | 722 | <0.49 | <1.0 | <0.32 | <1.3 | <1.3 | <34 |
| 3b | MOE7 | 28* | Eluate 1 + 2 | 1.60 | <0.031 | <0.77 | 850 | <0.49 | <1.0 | <0.32 | <1.3 | <1.3 | <34 |
| 2a | MOE8 | 12 | Eluate 1 + 2 | 1.18 | <0.84 | <1.6 | 0.32 | <0.80 | 18.4 | 2.25 | <1.6 | <2.7 | <21 |
| 2b | MOE8 | 7 | Eluate 1 + 2 | 1.62 | <0.031 | <0.77 | <0.30 | <0.49 | 1.20 | <0.32 | <1.3 | <0.02 | <34 |

Results from ICP-OES analysis (part 2)

Eluates 1 + 2 originate from DSLT, Fractions L/S 2 originate from percolation tests, 28* test specimens were covered by cling film during storage

| Experi-ment | Code | Storage period in d | Sample | Ca in µg L-1 | Fe in µg L-1 | K in µg L-1 | Mg in µg L-1 | Na in µg L-1 | B in µg L-1 | P in µg L-1 | S in µg L-1 | Si in µg L-1 | Ti in µg L-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Blank | - | Eluate 1 + 2 | <80 | <62 | <77 | <95 | <171 | <93 | <19 | <23 | <250 | <8400 |
| 1 | MOE1 | 12 | Eluate 1 + 2 | 2190 | <62 | 630 | 1190 | 6300 | <93 | <19 | 35900 | 812 | <8400 |
| 1 | Blank | - | Blind column | 190 | <62 | <77 | <95 | 650 | <93 | <19 | 43.4 | 366 | <8400 |
| 1 | MOE1 | 46 | L/S 2 fraction | 5060 | <62 | 3080 | 2250 | 19200 | <93 | 45.7 | 91800 | 1690 | <8400 |
| 3a | Blank | - | Eluate 1 + 2 | <67 | <86 | <167 | <51 | <2950 | <11 | <13 | <13 | <4930 | <2460 |
| 3b | Blank | - | Eluate 1 + 2 | <67 | <86 | <167 | <51 | <2950 | <11 | <13 | 24.3 | <4930 | <2460 |
| 3a | MOE1 | 7 | Eluate 1 + 2 | 1960 | <86 | 776 | 468 | 11100 | <11 | 24.5 | 46300 | <4930 | <2460 |
| 3a | MOE1 | 14 | Eluate 1 + 2 | 1980 | <86 | 713 | 485 | 10200 | <11 | 22.2 | 43200 | <4930 | <2460 |
| 3b | MOE1 | 28 | Eluate 1 + 2 | 2250 | <86 | <167 | 501 | 9200 | <11 | 20.0 | 38700 | <4930 | <2460 |
| 3b | MOE1 | 28* | Eluate 1 + 2 | 1749 | <86 | <167 | 301 | 7857 | <11 | 30.8 | 44300 | <4930 | <2460 |
| 2a | Blank | - | Eluate 1 + 2 | <31 | <43 | <155 | <24 | <4050 | <14 | <67 | <16 | <50 | <3990 |
| 2b | Blank | - | Eluate 1 + 2 | <67 | <86 | <167 | <51 | 4120 | <11 | <13 | <13 | <4930 | <2460 |
| 2a | MOE2 | 8 | Eluate 1 + 2 | 624 | <43 | 377 | 81.8 | <3990 | <14 | <67 | 40.5 | 299 | <3990 |
| 2b | MOE2 | 7 | Eluate 1 + 2 | 618 | <86 | 352 | 57.2 | 3974 | <11 | <13 | 22.1 | <4930 | <2460 |
| 2a | MOE3 | 8 | Eluate 1 + 2 | 189000 | <43 | 106000 | 29.8 | 8490 | <14 | <67 | 1310 | 1870 | <3990 |
| 2b | MOE3 | 7 | Eluate 1 + 2 | 308000 | <86 | 106000 | 52.6 | 4820 | <11 | <13 | 1399 | <4930 | <2460 |
| 2a | MOE4 | 7 | Eluate 1 + 2 | 45700 | <43 | 10600 | <24 | 25300 | <14 | <67 | 17700 | 823 | <3990 |
| 2b | MOE4 | 7 | Eluate 1 + 2 | 66700 | <86 | 96000 | <51 | 27700 | <11 | <13 | 12800 | <4930 | <2460 |
| 2a | MOE5 | 10 | Eluate 1 + 2 | 170 | <43 | <155 | <24 | <3990 | <14 | <67 | 82.6 | <50 | <3990 |
| 2b | MOE5 | 7 | Eluate 1 + 2 | 101 | <86 | <167 | <51 | 4042 | <11 | <13 | 19.2 | <4930 | <2460 |
| 2a | MOE6 | 11 | Eluate 1 + 2 | 919 | <43 | 210 | 91.8 | <3990 | <14 | <67 | 1082 | 139 | <3990 |
| 2b | MOE6 | 7 | Eluate 1 + 2 | 214 | <86 | <167 | 61.5 | 4370 | <11 | 20 | 194 | <4930 | <2460 |
| 2a | MOE7 | 7 | Eluate 1 + 2 | 282 | <43 | <155 | 60.8 | <3990 | <14 | <67 | 48 | 92 | <3990 |
| 3a | MOE7 | 7 | Eluate 1 + 2 | 147 | <86 | <167 | <51 | 4540 | <11 | 30.6 | 28.3 | <4930 | <2460 |
| 3a | MOE7 | 14 | Eluate 1 + 2 | 2240 | <86 | <167 | <51 | 4720 | <11 | 29.9 | 22.0 | <4930 | <2460 |
| 3b | MOE7 | 28 | Eluate 1 + 2 | 163 | <86 | <167 | <51 | <2960 | <11 | 30.7 | 24.2 | <4930 | <2460 |
| 3b | MOE7 | 28* | Eluate 1 + 2 | 133 | <86 | <167 | <51 | <2960 | <11 | 30.0 | 20.6 | <4930 | <2460 |
| 2a | MOE8 | 12 | Eluate 1 + 2 | 1520 | <43 | <155 | <24 | <3990 | <14 | <67 | 38.9 | <50 | <3990 |
| 2b | MOE8 | 7 | Eluate 1 + 2 | <67 | <86 | <167 | <51 | 5060 | <11 | <13 | 6.98 | <4930 | <2460 |

Results from ICP-MS analysis

Eluates 1 + 2 originate from DSLT, Fractions L/S 2 originate from percolation tests, 28*: test specimens were covered by cling film during storage

| Experiment | Code | Storage period in d | Sample | As in µg L-1 | Cu in µg L-1 | Hg in µg L-1 | Ni in µg L-1 | Pb in µg L-1 | Sb in µg L-1 | Zn in µg L-1 | Se in µg L-1 | Tl in µg L-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Blank | - | Eluate 1 + 2 | <0.03 | <0.77 | 0.084 | 64.3 | 0.12 | 0.78 | 10.6 | <0.18 | <0.022 |
| 1 | MOE1 | 12 | Eluate 1 + 2 | 0.148 | 7.89 | <0.05 | 5.42 | 3.89 | 0.43 | 105 | 1.88 | <0.022 |
| 1 | Blank | - | Blind column | 0.31 | 13.6 | 0.42 | 29.0 | 0.72 | 0.36 | 14.8 | 0.40 | <0.022 |
| 1 | MOE1 | 46 | L/S 2 fraction | 0.78 | 38.6 | <0.05 | 8.72 | 6.74 | 0.28 | 236 | <0.18 | <0.022 |
| 3a | Blank | - | Eluate 1 + 2 | <0.084 | 5.60 | <0.048 | <2.5 | <0.34 | <0.050 | <7.7 | <0.46 | <0.014 |
| 3b | Blank | - | Eluate 1 + 2 | <0.084 | <1.56 | <0.048 | <2.5 | <0.34 | <0.050 | 19.0 | <0.46 | <0.014 |
| 3a | MOE1 | 7 | Eluate 1 + 2 | 0.52 | 5.85 | <0.048 | <2.5 | 2.31 | 0.42 | <7.7 | <0.46 | <0.014 |
| 3a | MOE1 | 14 | Eluate 1 + 2 | 0.45 | 5.68 | <0.048 | <2.5 | 2.74 | 0.39 | 10.6 | <0.46 | <0.014 |
| 3b | MOE1 | 28 | Eluate 1 + 2 | 0.38 | 11.4 | <0.048 | <2.5 | 2.86 | <0.050 | <7.7 | <0.46 | <0.014 |
| 3b | MOE1 | 28* | Eluate 1 + 2 | 0.40 | 9.88 | <0.048 | <2.5 | 2.84 | <0.050 | <7.7 | <0.46 | <0.014 |
| 2a | Blank | - | Eluate 1 + 2 | <0.030 | <0.084 | <0.050 | <0.15 | 0.01 | <0.034 | 0.63 | <0.18 | <0.022 |
| 2b | Blank | - | Eluate 1 + 2 | <0.084 | <1.5 | <0.048 | <2.5 | <0.34 | <0.050 | <7.7 | <0.46 | <0.014 |
| 2a | MOE2 | 8 | Eluate 1 + 2 | 0.22 | 11.7 | <0.050 | 1.72 | 1.11 | <0.034 | 5.99 | <0.18 | <0.022 |
| 2b | MOE2 | 7 | Eluate 1 + 2 | 0.16 | 39 | <0.048 | <2.5 | 54.3 | 0.10 | 60.0 | <0.46 | <0.014 |
| 2a | MOE3 | 8 | Eluate 1 + 2 | <0.030 | 3.76 | <0.050 | 30.68 | 0.15 | <0.034 | 8.76 | <0.18 | <0.022 |
| 2b | MOE3 | 7 | Eluate 1 + 2 | 0.10 | 5.14 | 0.11 | <2.5 | <0.34 | 1.56 | 8.76 | <0.46 | <0.014 |
| 2a | MOE4 | 7 | Eluate 1 + 2 | <0.030 | 2.34 | <0.050 | 5.03 | 0.02 | 0.26 | 5.33 | <0.18 | <0.022 |
| 2b | MOE4 | 7 | Eluate 1 + 2 | <0.084 | 1.84 | 0.11 | <2.5 | <0.34 | 1.20 | <7.7 | <0.46 | <0.014 |
| 2a | MOE5 | 10 | Eluate 1 + 2 | <0.030 | 1.68 | <0.050 | 5.84 | 0.03 | <0.034 | 1.71 | <0.18 | <0.022 |
| 2b | MOE5 | 7 | Eluate 1 + 2 | <0.084 | 2.62 | <0.048 | <2.5 | 1.61 | 0.12 | <7.7 | <0.46 | <0.014 |
| 2a | MOE6 | 11 | Eluate 1 + 2 | 0.55 | 16.2 | <0.050 | 10.0 | 0.23 | <0.034 | 5.90 | <0.18 | <0.022 |
| 2b | MOE6 | 7 | Eluate 1 + 2 | 0.23 | 10.3 | <0.048 | <2.5 | <0.34 | <0.050 | <7.7 | <0.46 | <0.014 |
| 2a | MOE7 | 7 | Eluate 1 + 2 | <0.030 | 3.77 | <0.050 | 4.49 | 0.52 | 0.27 | 5.65 | <0.18 | <0.022 |
| 3a | MOE7 | 7 | Eluate 1 + 2 | <0.084 | 3.75 | <0.048 | <2.5 | 1.66 | 0.40 | <7.7 | <0.46 | <0.014 |
| 3a | MOE7 | 14 | Eluate 1 + 2 | <0.084 | 8.81 | <0.048 | <2.5 | 1.73 | 0.18 | <7.7 | <0.46 | <0.014 |
| 3b | MOE7 | 28 | Eluate 1 + 2 | 0.09 | 15.38 | <0.048 | 5.54 | 4.41 | <0.050 | <7.7 | <0.46 | <0.014 |
| 3b | MOE7 | 28* | Eluate 1 + 2 | <0.084 | <1.496 | <0.048 | 3.25 | 1.81 | <0.050 | <7.7 | <0.46 | <0.014 |
| 2a | MOE8 | 12 | Eluate 1 + 2 | <0.030 | 4.42 | <0.050 | 2.51 | 0.03 | <0.034 | 1.16 | <0.18 | <0.022 |
| 2b | MOE8 | 7 | Eluate 1 + 2 | <0.084 | 1.80 | <0.048 | <2.5 | <0.34 | <0.050 | <7.7 | <0.46 | <0.014 |

SI 8: Comparison of emissions from MOE1 in DSLT and percolation test

Data for 5 independent DSLT experiments are summarized. The complete sets of data are given under SI 5, 6, 7 and 11.

| Component | Concentration in mg L-1 |  | Emission in mg m-2 | Emission in mg kg-2 |  |
| --- | --- | --- | --- | --- | --- |
|  | DSLT (mean) | Percolation | DSLT (mean) | DSLT (mean) | Percolation |
| TOC | 390 | 1300 | 19400 | 3500 | 2600 |
| TN | 73 | 270 | 3700 | 670 | 540 |
| Cl- | 3,1 | 9.8 | 150 | 28 | 20 |
| Br- | 0,3 | 1.4 | 15 | 3 | 3 |
| SO42- | 43 | 5.4 | 2200 | 400 | 11 |
| 4-tert-Butylphenol | 6.1 | 22 | 300 | 56 | 44 |
| 1,3-Benzene-dimethanamine | 27 | 200 | 1350 | 240 | 400 |
| N,N-Dimethyl-1-dodecanamine | 0.3 | 1.2 | 13 | 2 | 2 |
|  | Concentration in µg L-1 |  | Emission in µg m-2 | Emission in µg kg-2 |  |
| As | 0.38 | 0.78 | 19 | 3.4 | 1.6 |
| Ba | 1.7 | 26 | 87 | 16 | 52 |
| Cu | 8.2 | 39 | 410 | 76 | 77 |
| Mn | 5.6 | 41 | 280 | 51 | 83 |
| Mo | 10 | 4.8 | 520 | 95 | 10 |
| Pb | 2.9 | 6.4 | 150 | 27 | 14 |

n = 5 for DSLT and n = 1 for percolation test

SI 9: Results from ecotoxicity test on eluates from joint grouts

Eluates 1 + 2 originate from DSLTs, fraction L/S 2 originates from a percolation test, 28*: test specimens were covered by cling film during storage,

Comments: 1) Data from repeated tests are given in brackets. During the first experiments on MOE1 only a limited number of dilutions was tested to estimate the ranges of toxicity while the repeated tests were performed with complete sets of dilutions. This can explain differences between both tests. LIDs could be estimated more precisely from the results of the second test.

2) Ames test: can also indicate cytotoxicity

3) Algae tests for MOE2 to MOE 8 were performed using eluates from a repeated DSLT (experiments 2b and 3a) since effects on algae (LID > 6) were observed for the blank sample from experiment 2a.

| Experiment | Code | Storage period in d | Sample | Algae LIDA | Daphnia LIDD 48 h | Fish egg LIDEgg | Luminescent bacteria LIDlb | Umu LIDEU | Ames |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Blank | - | Eluate 1 + 2 | ≤2 | ≤2 | ≤2 | ≤2 | ≤1,5 | 1 |
| 1 | MOE1 | 12 | Eluate 1 + 2 | 384 (1536) | 96 (64) | 12 (8) | 3072 (2048) | 3 (3) | 1 |
| 1 | Blank | - | Blind column | ≤2 | ≤2 | ≤2 | ≤2 | ≤1,5 | 1 |
| 1 | MOE1 | 46 | L/S 2 fraction | 3072 (3072) | 512 (256) | 32 (24) | 16384 (12288) | 6 (6) | 1 |
| 3a | Blank | - | Eluate 1 + 2 | ≤2 | ≤2 | n.d. | ≤2 | n.d. | n.d. |
| 3b | Blank | - | Eluate 1 + 2 | ≤2 | ≤2 | n.d. | ≤2 | n.d. | n.d. |
| 3a | MOE1 | 7 | Eluate 1 + 2 | 384 | 64 | n.d. | 1536 | n.d. | n.d. |
| 3a | MOE1 | 14 | Eluate 1 + 2 | 384 | 64 | n.d. | 2048 | n.d. | n.d. |
| 3b | MOE1 | 28 | Eluate 1 + 2 | 384 | 192 | n.d. | 2048 | n.d. | n.d. |
| 3b | MOE1 | 28* | Eluate 1 + 2 | 384 | 128 | n.d. | 2048 | n.d. | n.d. |
| 2a | Blank | - | Eluate 1 + 2 | n.d. | ≤2 | ≤2 | ≤2 | ≤1,5 | 1 |
| 2b | Blank | - | Eluate 1 + 2 | ≤2 | n.d. | n.d. | n.d. | n.d. | n.d. |
| 2a | MOE2 | 8 | Eluate 1 + 2 | n.d. | ≤2 | ≤2 | 16 | ≤1,5 | 1 |
| 2b | MOE2 | 7 | Eluate 1 + 2 | 32 | n.d. | n.d. | n.d. | n.d. | n.d. |
| 2a | MOE3 | 8 | Eluate 1 + 2 | n.d. | ≤2 | ≤2 | ≤2 | ≤1,5 | ≥2 |
| 2b | MOE3 | 7 | Eluate 1 + 2 | 3 | n.d. | n.d. | n.d. | n.d. | n.d. |
| 2a | MOE4 | 7 | Eluate 1 + 2 | n.d. | 4 | ≤2 | ≤2 | ≤1,5 | 2 |
| 2b | MOE4 | 7 | Eluate 1 + 2 | inconsistent | n.d. | n.d. | n.d. | n.d. | n.d. |
| 2a | MOE5 | 10 | Eluate 1 + 2 | n.d. | 3 | ≤2 | ≤2 | ≤1,5 | 1 |
| 2b | MOE5 | 7 | Eluate 1 + 2 | 4 | n.d. | n.d. | n.d. | n.d. | n.d. |
| 2a | MOE6 | 11 | Eluate 1 + 2 | n.d. | 192 | 16 | 96 | ≤6 | 1 |
| 2b | MOE6 | 7 | Eluate 1 + 2 | 3072 | n.d. | n.d. | n.d. | n.d. | n.d. |
| 2a | MOE7 | 7 | Eluate 1 + 2 | n.d. | 3 | ≤2 | 24 | ≤1,5 | 1 |
| 3a | MOE7 | 7 | Eluate 1 + 2 | 8 | ≤2 | n.d. | 24 | n.d. | n.d. |
| 3a | MOE7 | 14 | Eluate 1 + 2 | 8 | ≤2 | n.d. | 24 | n.d. | n.d. |
| 3b | MOE7 | 28 | Eluate 1 + 2 | 12 | ≤2 | n.d. | 24 | n.d. | n.d. |
| 3b | MOE7 | 28* | Eluate 1 + 2 | 8 | ≤2 | n.d. | 24 | n.d. | n.d. |
| 2a | MOE8 | 12 | Eluate 1 + 2 | n.d. | ≤2 | ≤2 | ≤2 | ≤1,5 | 1 |
| 2b | MOE8 | 7 | Eluate 1 + 2 | ≤2 | n.d. | n.d. | n.d. | n.d. | n.d. |

SI 10: Results from GC-MS Screening at BAM

Substances that were tentatively identified in dichlormethane extracts (extracted at pH 2 and pH 10) from eluates of grouts (MOE1 and MOE6: epoxy resin-based, MOE2 and MOE7: polybutadiene-based). Selection criteria: compliance of observed and library mass at least 85 %. Only benzyl alcohol was identified in eluates of MOE3 and MOE4 (modified cement) and MOE5 and MOE8 (polyurethane-based). Substances printed in bold types were confirmed by reference substances.

*Data from ECHA page on registered substances, https://echa.europe /de/information-on-chemicals/registered-substances, assessed on 2022-06-21

| Substance | CAS | MOE1 | MOE6 | MOE2 | MOE7 | H-phrases* Environmental hazards | H-phrases* Health hazards | Total tonnage band* in t per year |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1-Methyl-3-propylcyclohexane (or structural isomer) | 4291-80-9 |  |  | x |  |  |  | no entry |
| Benzaldehyde | 100-52-7 | x | x |  |  |  | H302 | 10.000 - 100.000 |
| 1-(2-Methoxy-1-methylenethoxy)-2-propanol | 20324-32-7 |  |  | x |  |  |  | no entry |
| Benzyl alcohol | 100-51-6 | x | x | x | x |  | H302, H332 | 10.000 - 100.000 |
| Methyl phenol | 95-48-7 | x |  |  |  | H412 | H301, H311, H314 | 10.000 - 100.000 |
| 2-Ethylhexanoi acid | 149-57-5 |  |  | x | x |  | H361 | 10.000 - 100.000 |
| 2,2,4-Trimethylhexane-1,6-diamine | 25513-64-8 | x |  |  |  |  | H302, H314, H317 | 1.000 - 10.000 |
| 4-tert-Butylphenol | 98-54-4 | x |  |  |  | H410 | H315, H318, H361 | 10.000 - 100.000 |
| 1,3-Cyclohexanedimethaneamine | 2579-20-6 |  | x |  |  | H412 | H302, H312, H314 | 1.000 - 10.000 |
| 3-Aminomethyl-3,5,5-trimethylcyclohexylamine | 2855-13-2 |  | x |  |  |  | H302, H314, H317 | 10.000 - 100.000 |
| 1,3-Benzenedimethanamine | 1477-55-0 | x | x |  |  | H412 | H302, H332, H314, H317 | 10.000 - 100.000 |
| Methyl 9-oxononanoate | 1931-63-1 |  |  |  | x |  |  | no entry |
| 2-(2-Butoxyethoxy)-ethanol | 112-34-5 | x |  |  |  |  | H319 | 10.000 - 100.000 |
| Nonyl-cyclopropan | 74663-85-7 |  | x |  |  |  |  | no entry |
| N,N-Dimethyl-1-dodecanamine | 112-18-5 | x |  |  |  | H410 | H302, H314 | 100 - 1.000 |
| p-Tolyl glycerol | 17131-24-7 | x |  |  |  |  |  | no entry |
| 5-(1-Hydroxyhexyl)-tetrahydrofuran-2-one | 1000131-83-9 |  |  | x |  |  |  | no entry |
| Isopropyl laurate | 10233-13-3 |  |  | x | x |  |  | 1.000 - 10.000 |
| 4-Dodecanol | 10203-32-4 |  |  |  | x |  |  | no entry |
| N,N-Dimethyl-1-tetradecanamine | 112-75-4 | x |  |  |  | H410 | H302, H314 | 100 - 1.000 |
| 2-[(Dodecyloxy)methyl]-oxiran | 2461-18-9 |  | x |  |  |  |  | no entry |

SI 11: Results for selected organic substances in eluates of MOE1 and MOE 7 after different duration of storage of test specimens before leaching tests

Eluates originate from DSLT (combined sample of eluate 1 and 2), 28*: test specimens were covered by cling film during storage, the substances were not detected in the blank samples

| Experiment | Code | Storage in d | Benzyl alcohol in mg l-1 | 4-tert-Butyl-phenol in mg l-1 | 1,3-Benzol-dimethanamin in mg l-1 | Dodecyldimethyl-amine in mg l-1 | 2-Ethyl-hexanoic acid in mg l-1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | MOE1 | 12 | 10.1 | 7.8 | 49.8 | 0.4 |  |
| 3a | MOE1 | 7 | 15.2 | 3.0 | 27.4 | 0.11 |  |
| 3a | MOE1 | 14 | 10.7 | 7.7 | 22.2 | 0.32 |  |
| 3b | MOE1 | 28 | 2.9 | 4.4 | 17.4 | 0.19 |  |
| 3b | MOE1 | 28* | 3.8 | 7.4 | 18.2 | 0.28 |  |
| 2a | MOE7 | 7 | n.d. |  |  |  | 4.2 |
| 3a | MOE7 | 7 | 7.74 |  |  |  | 7.0 |
| 3a | MOE7 | 14 | 0.06 |  |  |  | 4.5 |
| 3b | MOE7 | 28 | 0.05 |  |  |  | 2.7 |
| 3b | MOE7 | 28* | 0.05 |  |  |  | 4.2 |

SI 12: Data from TZW

Table SI 12-1:  Results for sample MOE1 in percolation test eluate (experiment 1*, see SI 4)

Green mark in the LC column: Identification level "probable substance". All conditions were fulfilled.

Yellow marking in LC column: Identification level "signal of a substance" means that no hit was found by MS2 spectral database comparison. Reason may be: missing reference spectrum or no measured MS2 spectrum).

| # | Substance | CAS- number | Molweight in g mol-1 | List | LCNIST | LC | GC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Benzaldehyd | 100-52-7 | 106 | GCNIST |  | 0 | 1 |
| 2 | Benzylalkohol | 100-51-6 | 108 | GCNIST |  | 0 | 1 |
| 3 | Methylphenol | 95-48-7 | 108 | GCNIST |  | 0 | 1 |
| 4 | 2-Butoxyethanol | 111-76-2 | 118 | GCNIST |  | 0 | 1 |
| 5 | 4-tert-Butylphenol | 98-54-4 | 150 | GCNIST |  | 0 | 1 |
| 6 | N,N-Dibutylformamid | 761-65-9 | 157 | Lacke | • | 2 | 0 |
| 7 | 2-(Benzyloxy)propanal | 53346-05-7 | 164 | Dachfolie | • | 2 | 0 |
| 8 | 2-Phenylbutyric acid | 90-27-7 | 164 | LCNIST | • | 1 | 0 |
| 9 | 3-Phenylbutyric acid | 4593-90-2 | 164 | LCNIST | • | 1 | 0 |
| 10 | Glycidyl-2-methylphenylether | 2210-79-9 | 164 | GCNIST |  | 0 | 1 |
| 11 | 2-Mercaptobenzothiazole | 149-30-4 | 167 | LCNIST | • | 1 | 0 |
| 12 | Benzylphosphonic acid | 6881-57-8 | 172 | LCNIST | • | 1 | 0 |
| 13 | p-Toluenesulfonic acid | 104-15-4 | 172 | LCNIST | • | 1 | 0 |
| 14 | 2-(Benzylmethylamino)ethanol N-oxide | 15831-63-7 | 181 | LCNIST | • | 1 | 0 |
| 15 | 3-(Octylamino)propionitril | 29504-89-0 | 182 | GCNIST |  | 0 | 1 |
| 16 | Tripropylene glycol (PPG-3) |  | 192 | Lacke | • | 2 | 0 |
| 17 | Tetraethylene glycol (PEG-4) | 112-60-7 | 194 | Lacke | • | 2 | 0 |
| 18 | Sebacic acid | 111-20-6 | 202 | LCNIST | • | 1 | 0 |
| 19 | N,N-Dimethyl-n-dodecylamin | 112-18-5 | 213 | GCNIST |  | 0 | 1 |
| 20 | Laurylguanidine | 112-65-2 | 227 | LCNIST | • | 1 | 0 |
| 21 | 3-Ethyl-5-methylphenyl trifluoracetate |  | 232 | Dachfolie |  | 2 | 0 |
| 22 | 4-Amino-7-diethylamino-chromen-2-one | 107995-76-6 | 232 | Dachfolie |  | 2 | 0 |
| 23 | Tetrapropylene glycol (PPG-4) |  | 250 | Lacke | • | 2 | 0 |
| 24 | 2,2,4-Trimethyl-1,3-pentanediol diisobutyrate | 6846-50-0 | 286 | Lacke | • | 2 | 0 |
| 25 | Benzyldodecyldimethylammonium cation | 7281-04-1 | 303 | LCNIST | • | 1 | 0 |
| 26 | Clomipramine | 303-49-1 | 314 | LCNIST | • | 1 | 0 |
| 27 | 2-Ethylhexyl maleate | 142-16-5 | 340 | Lacke |  | 2 | 0 |
| 28 | Bis(2-ethylhexyl)-(2E)-2-butendioat | 141-02-6 | 340 | Lacke |  | 2 | 0 |
| 29 | Hexapropylene glycol (PPG-6) | 74388-92-4 | 366 | Lacke | • | 1 | 0 |
| 30 | Heptapropylene glycol (PPG-7) | 14362-16-4 | 424 | Lacke | • | 2 | 0 |
| 31 | Octapropylene glycol (PPG-8) | 25322-69-4 | 482 | Lacke | • | 1 | 0 |
| 32 | Nonapropylene glycol (PPG-9) | 2172326-56-4 | 540 | Lacke | • | 1 | 0 |
| 33 | Decapropylene glycol (PPG-10) | 25322-69-4 | 598 | Lacke | • | 1 | 0 |

Table SI 12-2:  Results for sample MOE1 in DSLT eluate (experiment 1, see SI 4)

| # | Substance | CAS- number | Molweight in g mol-1 | List | LCNIST | LC | GC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Benzaldehyd | 100-52-7 | 106 | GCNIST |  | 0 | 1 |
| 2 | Benzylalkohol | 100-51-6 | 108 | GCNIST |  | 0 | 1 |
| 3 | Methylphenol | 95-48-7 | 108 | GCNIST |  | 0 | 1 |
| 4 | 2-Phenylacetamide | 103-81-1 | 135 | Dachfolie |  | 2 | 0 |
| 5 | 3-Propionylperazine | 1570-48-5 | 135 | LCNIST | • | 2 | 0 |
| 6 | Propylphenol | 644-35-9 | 136 | GCNIST |  | 0 | 1 |
| 7 | Octanic acid | 124-07-2 | 144 | Lacke | • | 2 | 0 |
| 8 | o-Propylanisol | 13629-73-7 | 150 | GCNIST |  | 0 | 1 |
| 9 | 4-tert-Butylphenol | 98-54-4 | 150 | GCNIST |  | 0 | 1 |
| 10 | N,N-Dibutylformamid | 761-65-9 | 157 | Lacke |  | 2 | 0 |
| 11 | 2-Phenylbutyric acid | 90-27-7 | 164 | LCNIST | • | 1 | 0 |
| 12 | 3-Phenylbutyric acid | 4593-90-2 | 164 | LCNIST | • | 1 | 0 |
| 13 | 2-(Benzyloxy)propanal | 53346-05-7 | 164 | Dachfolie |  | 2 | 0 |
| 14 | 2-Mercaptobenzothiazole | 149-30-4 | 167 | LCNIST | • | 1 | 0 |
| 15 | Benzylphosphonic acid | 6881-57-8 | 172 | LCNIST | • | 1 | 0 |
| 16 | p-Toluenesulfonic acid | 104-15-4 | 172 | LCNIST | • | 1 | 0 |
| 17 | 2-(Benzylmethylamino)ethanol N-oxide | 15831-63-7 | 181 | LCNIST | • | 1 | 0 |
| 18 | Tripropylene glycol (PPG-3) |  | 192 | Lacke | • | 2 | 0 |
| 19 | Tetraethylene glycol (PEG-4) | 112-60-7 | 194 | Lacke | • | 1 | 0 |
| 20 | 3,4-Dihydroxymandelic acid | 775-01-9 | 202 | LCNIST | • | 1 | 0 |
| 21 | Sebacic acid | 111-20-6 | 202 | LCNIST | • | 1 | 0 |
| 22 | Laurylguanidine | 112-65-2 | 227 | LCNIST | • | 1 | 0 |
| 23 | 7,9-Di-tert-butyl-1-oxaspiro[4.5]deca-6,9-diene-2,8-dione | 82304-66-3 | 276 | Dachfolie |  | 2 | 0 |
| 24 | 2,2,4-Trimethyl-1,3-pentanediol diisobutyrate | 6846-50-0 | 286 | Lacke | • | 2 | 0 |
| 25 | Benzyldodecyldimethylammonium cation | 7281-04-1 | 303 | LCNIST | • | 1 | 0 |
| 26 | Pentapropylene glycol (PPG-5) | 21482-12-2 | 308 | Lacke | • | 2 | 0 |
| 27 | Prostaglandin A1 methyl ester | 26771-94-8 | 310 | LCNIST | • | 1 | 0 |
| 28 | 2-Ethylhexyl maleate | 142-16-5 | 340 | Lacke |  | 2 | 0 |
| 29 | Bis(2-ethylhexyl)-(2E)-2-butendioat | 141-02-6 | 340 | Lacke |  | 2 | 0 |
| 30 | Decamethylcyclopentasiloxane | 541-02-6 | 370 | LCNIST | • | 1 | 0 |
| 31 | Decapropylene glycol (PPG-10) | 25322-69-4 | 598 | Lacke | • | 2 | 0 |

Table SI 12-3:  Results for inter-laboratory test sample MOE1 in percolation test (see Heisterkamp et al. 2021)

| # | Substance | CAS- | Molweight | List | LCNIST | LC | GC |  | H-phrases | REACH | Production quantity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | number | in g mol-1 |  |  |  |  |  |  |  | in t per a |
| 1 | 3-[N-[2-Diethylaminoethyl]-1-cyclohexenylamino]propylnitril | 959229-47-1 | 86 | GCNIST |  |  | 1 |  |  | no |  |
| 2 | Butoxyethanol | 111-76-2 | 87 | GCNIST |  |  | 1 |  | H302, H315, H319, H332 | yes | 100 000 - 1 000 000 |
| 3 | Phenol | 108-95-2 | 94 | GCNIST |  |  | 1 |  | H301, H311, H314, H331, H341, H373, H411 | yes | 1 000 000 - 10 000 000 |
| 4 | Benzaldehyd | 100-52-7 | 106 | GCNIST |  |  | 1 |  | H302, H332, H315, H319, H335, H412 | yes | 10 000 - 100 000 |
| 5 | Benzylalkohol | 100-51-6 | 108 | GCNIST |  |  | 1 |  | H303, H319, H332 | yes | 10 000 - 100 000 |
| 6 | Methylphenol | 95-48-7 | 108 | GCNIST |  |  | 1 |  | H301, H311, H314, H411 | yes | 10 000 - 100 000 |
| 7 | m-Xylylendiamin | 1477-55-0 | 117 | GCNIST |  |  | 1 |  | H302, H332, H314, H317, H412 | yes | 10 000 - 100 000 |
| 8 | Azabenzimidazol | 273-21-2 | 119 | GCNIST |  |  | 1 |  | H302 | yes | 1 - 10 |
| 9 | Benzaldehydoxim | 932-90-1 | 121 | GCNIST |  |  | 1 |  |  | yes | 1 - 10 |
| 10 | Benzylchlorid | 100-44-7 | 126 | GCNIST |  |  | 1 |  | H302, H315, H317, H318, H331, H335, H340, H350, H373 | yes | 10 - 100 |
| 11 | 2-(2-Hydroxypropoxy)-1-propanol | 106-62-7 | 134 | Lack |  | 2 |  |  |  | no |  |
| 12 | Dipropylene glycol | 25265-71-8 | 134 | Lack |  | 2 |  |  |  | yes | 100 000 - 1 000 000 |
| 13 | N-Methyl-N-benzyltetradecanamin | 83690-72-6 | 134 | GCNIST |  |  | 1 |  |  | no |  |
| 14 | 2-Phenylacetamide | 103-81-1 | 135 | Roof film | • | 1 |  |  | H302, H319 | no |  |
| 15 | 3-Propionylperazine | 1570-48-5 | 135 | LCNIST |  | 2 |  |  |  | no |  |
| 16 | 2-Phenoxyethanol | 122-99-6 | 138 | Lack | • | 2 |  |  | H302, H319 | yes | 10000-100000 |
| 17 | Isophorone | 78-59-1 | 138 | LCNIST | • | 1 |  |  | H312, H319, H335, H351, H302 | yes | 100 - 1 000 |
| 18 | Octanoic acid | 124-07-2 | 144 | Lack | • | 2 |  |  | H412, H314 | yes | 10 000 - 100 000 |
| 19 | Allyl o-tolyl ether | 936-72-1 | 148 | GCNIST |  |  | 1 |  | H302 | yes |  |
| 20 | 4-Hydroxy-3-methoxystyrene | 7786-61-0 | 150 | Roof film |  | 2 |  |  |  | no |  |
| 21 | 4-Hydroxy-2-methylacetophenone | 875-59-2 | 150 | Roof film |  | 2 |  |  |  | no |  |
| 22 | 4-tert-Butylphenol | 98-54-4 | 150 | GCNIST |  |  | 1 |  | H315, H318, H361f, H410 | yes | 10 000 - 100 000 |
| 23 | Benzylisothiazolinon | 2634-33-5 | 151 | Lack |  | 2 |  |  | H400, H411, H302, H315, H318, H317 | yes | 100 - 1 000 |
| 24 | N,N-Dibutylformamide | 761-65-9 | 157 | Lack |  | 2 |  |  | H412 | yes | 10 - 100 |
| 25 | Isobutyric acid anhydride | 97-72-3 | 158 | Lack |  | 2 |  |  | H311, H331, H314 | yes | 100 - 1 000 |
| 26 | 1-(2-Butoxyethoxy)ethanol | 54446-78-5 | 162 | Roof film, Lack |  | 2 |  |  |  | no |  |
| 27 | Butyldiglycol (PEG-2 Butyl Ether) | 112-34-5 | 162 | Roof film, Lack | • | 2 |  |  |  | yes | 10 000 - 100 000 |
| 28 | 2-Phenylbutyric acid | 90-27-7 | 164 | LCNIST | • | 1 |  |  | H302 | yes | Intermediate use only |
| 29 | 3-Phenylbutyric acid | 4593-90-2 | 164 | LCNIST | • | 1 |  |  |  | no |  |
| 30 | 2-(Benzyloxy)propanal | 53346-05-7 | 164 | Roof film |  | 2 |  |  |  | no |  |
| 31 | Glycidyl-2-methylphenylether | 2210-79-9 | 164 | GCNIST |  |  | 1 |  | H315, H317, H341, H411 | yes | 1000 - 10 000 |
| 32 | 2-Mercaptobenzothiazole | 149-30-4 | 167 | LCNIST | • | 1 |  |  | H410, H317 | yes | 1 000 - 10 000 |
| 33 | p-Toluenesulfonic acid | 104-15-4 | 172 | LCNIST | • | 1 |  |  |  | yes | 100 - 1 000 |
| 34 | 2-(2-Butoxyethoxy)acetic acid | 82941-26-2 | 176 | LCNIST | • | 1 |  |  |  | no |  |
| 35 | Diisopropylphenol | 2934-05-6 | 178 | GCNIST |  |  | 1 |  | H315, H319, H335 | yes |  |
| 36 | Diisopropylphenol | 26886-05-5 | 178 | GCNIST |  |  | 1 |  |  | yes |  |
| 37 | 3-(4-Methylphenoxy)-1,2-propandiol | 17131-24-7 | 182 | GCNIST |  |  | 1 |  |  | no |  |
| 38 | 3-(Octylamino)propionitril | 29504-89-0 | 182 | GCNIST |  |  | 1 |  |  | yes | 1 - 10 |
| 39 | Dimethyl-benzenesulfonic acid | 88-61-9 | 186 | LCNIST | • | 1 |  |  |  | no |  |
| 40 | Decyl formate | 5451-52-5 | 186 | Lack |  | 2 |  |  |  | no |  |
| 41 | 1-Acetylnaphthalen-8-ol | 18528-55-7 | 189 | GCNIST |  |  | 1 |  |  | no |  |
| 42 | Diethoxytetraethylenglycol | 4353-28-0 | 190 | GCNIST |  |  | 1 |  |  | yes |  |
| 43 | Tripropylene glycol (PPG-3) | 24800-44-0 | 192 | Lack | • | 2 |  |  |  | yes | 10 000 - 100 000 |
| 44 | 2-Isopropyl-6-tert-butylphenol | 22791-95-3 | 192 | GCNIST |  |  | 1 |  |  | no |  |
| 45 | Tetraethylene glycol (PEG-4) | 112-60-7 | 194 | Lack | • | 2 |  |  |  | yes | 100 - 1000 |
| 46 | Dimethyl-4-isopropylnaphthaIen | 483-78-3 | 198 | GCNIST |  |  | 1 |  |  | yes |  |
| 47 | 3,4-Dihydroxymandelic acid | 775-01-9 | 202 | LCNIST | • | 1 |  |  |  | no |  |
| 48 | Sebacic acid | 111-20-6 | 202 | LCNIST | • | 1 |  |  |  | yes | 10 000 - 100 000 |
| 49 | 1-Benzyl-3-methylpiperidin-4-one | 34737-89-8 | 203 | LCNIST | • | 1 |  |  |  | no |  |
| 50 | 3-Benzoylpiperazin-2,5-dion | 5037-75-2 | 204 | GCNIST |  |  | 1 |  |  | no |  |
| 51 | 2-(2-(2-Methoxypropoxy)propoxy)-1-propanol |  | 206 | Lack |  | 2 |  |  |  |  |  |
| 52 | N,N-Dimethyl-n-dodecylamin | 112-18-5 | 213 | GCNIST |  |  | 1 |  | H302, H314, H410 | yes | 1 - 10 |
| 53 | Diphenylmethylphosphine oxide | 2129-89-7 | 216 | LCNIST | • | 1 |  |  |  | no |  |
| 54 | Diethyl phthalate | 84-66-2 | 222 | LCNIST | • | 1 |  |  |  | yes | 1 000 - 10 000 |
| 55 | Laurylguanidine | 112-65-2 | 227 | LCNIST | • | 1 |  |  |  | no |  |
| 56 | Dodecanedioic acid | 693-23-2 | 230 | LCNIST | • | 1 |  |  | H319 | yes | 10 000 - 100 000 |
| 57 | 3-Ethyl-5-methylphenyl trifluoracetate |  | 232 | Roof film |  | 2 |  |  |  |  |  |
| 58 | Diphenoxypropanol | 622-04-8 | 244 | GCNIST |  |  |  | 1 | H302, H319 | yes | 1 - 10 |
| 59 | Tetrapropylene glycol (PPG-4) | 24800-25-7 | 250 | Lack | • | 2 |  |  |  | no |  |
| 60 | 7,9-Di-tert-butyl-1-oxaspiro[4.5]deca-6,9-diene-2,8-dione | 82304-66-3 | 276 | Roof film |  | 2 |  |  |  | no |  |
| 61 | 2,2,4-Trimethyl-1,3-pentanediol diisobutyrate | 6846-50-0 | 286 | Lack | • | 2 |  |  | H412, H361 | yes | 1 000 - 10 000 |
| 62 | Bis(phenoxyethoxy)methane | 13879-32-8 | 288 | Lack |  | 2 |  |  |  | no |  |
| 63 | Benzyldodecyldimethylammonium cation | 7281-04-1 | 303 | LCNIST | • | 1 |  |  | Component of biocides | no |  |
| 64 | 1-(1-Pentyl-1H-indol-3-yl)-2-phenyl-ethanone |  | 305 | LCNIST | • | 1 |  |  |  |  |  |

Table SI 12-4:  Results for inter-laboratory test sample MOE1 in DSLT (see Heisterkamp et al. 2021)

| # | Substance | CAS- | Molweight | List | LCNIST | LC | GC | H-phrases | REACH | Production quantity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | number | in g mol-1 |  |  |  |  |  |  | in t per a |
| 1 | Benzaldehyd | 100-52-7 | 106 | GCNIST |  |  | 1 | H302, H332, H315, H319, H335, H412 | yes | 10 000 - 100 000 |
| 2 | Benzylalkohol | 100-51-6 | 108 | GCNIST |  |  | 1 | H303, H319, H332 | yes | 10 000 - 100 000 |
| 3 | Methylphenol | 95-48-7 | 108 | GCNIST |  |  | 1 | H301, H311, H314, H411 | yes | 10 000 - 100 000 |
| 4 | Benzylchlorid | 100-44-7 | 126 | GCNIST |  |  | 1 | H302, H315, H317, H318, H331, H335, H340, H350, H373 | yes | 10 - 100 |
| 5 | N-Methyl-N-benzyltetradecanamin | 83690-72-6 | 134 | GCNIST |  |  | 1 |  | no |  |
| 6 | 2-Phenylacetamide | 103-81-1 | 135 | Roof film | • | 1 |  | H302, H319 | no |  |
| 7 | 3-Propionylperazine | 1570-48-5 | 135 | LCNIST |  | 2 |  | H302, H312, H332, H315, H319, H335 | no |  |
| 8 | Octanoic acid | 124-07-2 | 144 | Lack | • | 2 |  | H412, H314 | yes | 10 000 - 100 000 |
| 9 | 4-tert-Butylphenol | 98-54-4 | 150 | GCNIST |  |  | 1 | H315, H318, H361f, H410 | yes | 10 000 - 100 000 |
| 10 | N,N-Dibutylformamide | 761-65-9 | 157 | Lack |  | 2 |  | H412 | yes | 10 - 100 |
| 11 | 2-Phenylbutyric acid | 90-27-7 | 164 | LCNIST | • | 1 |  | H302 | yes |  |
| 12 | 3-Phenylbutyric acid | 4593-90-2 | 164 | LCNIST | • | 1 |  |  | no |  |
| 13 | 2-(Benzyloxy)propanal | 53346-05-7 | 164 | Roof film |  | 2 |  |  | no |  |
| 14 | Glycidyl-2-methylphenylether | 2210-79-9 | 164 | GCNIST |  |  | 1 | H315, H317, H341, H411 | yes | 1000 - 10 000 |
| 15 | 2-Mercaptobenzothiazole | 149-30-4 | 167 | LCNIST | • | 1 |  | H410, H317 | yes | 1 000 - 10 000 |
| 16 | p-Toluenesulfonic acid | 104-15-4 | 172 | LCNIST | • | 1 |  |  | yes | 100 - 1 000 |
| 17 | 3-(Octylamino)propionitril | 29504-89-0 | 182 | GCNIST |  |  | 1 |  |  |  |
| 18 | Tripropylene glycol (PPG-3) | 24800-44-0 | 192 | Lack | • | 2 |  |  | yes | 10 000 - 100 000 |
| 19 | Tetraethylene glycol (PEG-4) | 112-60-7 | 194 | Lack | • | 2 |  |  | yes | 100 - 1000 |
| 20 | Sebacic acid | 111-20-6 | 202 | LCNIST | • | 1 |  |  | yes | 10 000 - 100 000 |
| 21 | N,N-Dimethyl-n-dodecylamin | 112-18-5 | 213 | GCNIST |  |  | 1 | H302, H314, H410 | yes | 1 - 10 |
| 22 | Diphenoxypropanol | 622-04-8 | 244 | GCNIST |  |  | 1 | H302, H315, H319, H335 | yes |  |
| 23 | Tetrapropylene glycol (PPG-4) | 24800-25-7 | 250 | Lack | • | 2 |  |  | no |  |
| 24 | Octapropylene glycol (PPG-8) | 25322-69-4 | 482 | Lack | • | 2 |  |  | yes | 10 000 - 100 000 |

Figure SI 12-1: GC-MS chromatogram of the laboratory blank with spiked internal standards. Standards used for the evaluation of the semi-quantitative determinations are outlined in red.

Figure SI 12-2: LC-DAD measurement of the two eluates of sample MOE1 and the laboratory blank sample (20 µL injection volume). The perc eluate has significantly higher signals compared to the DSLT-eluate. The measurement serves only for the qualitative comparison of the samples. No standards were used for a possible elucidation of the signals.

Figure SI 12-3: Top: LC-DAD-chromatogram of the perc eluate of MOE1 at a detection wavelength of 254 nm. Bottom: Extracted spectra from selected signals.

References

Heisterkamp I, Ratte M, Schoknecht U, Gartiser S, Kalbe U, Ilvonen O (2021) Ecotoxicological evaluation of construction products: inter-laboratory test with DSLT and percolation test eluates in an aquatic biotest battery. Environ Sci Eur 33:75, 1-14. doi.org/10.1186/s12302-021-00514-x