Supplementary Information

Advancing Sustainability of Textiles: A Life Cycle and Microfiber Emission Assessment of Locally-Manufactured Circular Sportswear

Pellengahr, F., Ghannadzadeh, A. & van der Meer, Y.

Content

Supplementary note 1: Literature review of polyester textile case studies	2

Supplementary note 2: General approach for data acquisition and template used for textile value chain inventory data collection	4

Supplementary note 3: Life cycle inventory	7

Supplementary note 4: Life Cycle Assessment results	12

References	15

# Supplementary note 1: Literature review of polyester textile case studies

Table S1: LCA case studies of polyester textiles.

| Study | Object of study | Geogra-phical scope | Functional unit | Processing steps and characteristics | Additional notes |
| --- | --- | --- | --- | --- | --- |
| Moazzem, Crossin, et al., 2018 | Polyester knitted T-shirt | Australia | 50 days use of a polyester knitted T-shirt over one year life time | PET resin manufacturing, polyester filament spinning (22.23 kWh/kg, 15 % loss, fiber preparation: 5 % loss), knitting (8.08 kWh/kg, 1.5 % loss), wet processing (dyeing and pretreatment: 3 % loss, dyeing and finishing: 7.11 kWh/kg), apparel making (inspection, laying, cutting, sewing: 11 % material loss, 2.38 kWh/kg), importing agent, retailer, consumer, disposal |  |
| Walser et al., 2011 | Polyester T-shirt (conventional, nanoparticles triclosan) (1.56 m2 textile, 130 g) | Switzer-land | Being dressed with a biocidal polyester T-shirt for outdoor activities during one year in Switzerland (wearing it once a week) | PET spinning (3 kWh/kg, 5 % loss; incinerated), knitting (1.5 kWh/kg), finishing (24.8 kg water use, 0.82 kWh/kg), making up (0.3 kWh/kg), transport, polyester fabric manufacturing, use phase, disposal | 100 washes |
| Braun et al., 2021 | Polyester jacket (size L; PES 1.55 m2, 233+20+47 g; yarn 400 m PVA, 3.5 g) | Germany | Use of a three-layer-laminate jacket, repellent to water and permeable to heat and moisture, for a period of four years | PES fiber production (partly from PET bottles) (5 % loss), fabric production (10 % loss), garment production (37 % loss), use phase (3x washing), dismantling (5 % loss), shredding (5 % loss), regranulation (1 % loss) | Including auxiliary products, circular jacket; no data for individual production steps |
| Krishna Manda et al. 2015 | Antibacterial T-shirt |  | One T-shirt being worn for 100 days |  | Modal fibers |
| Moazzem, Daver, et al., 2018 | Polyester knit shirt | Australia | Use of one kilogram selected apparel over the life time | PES fiber production, yarn production (spinning and yarning 1.76 kWh/kg, 4 % loss), fabric production (knitting), wet processing (pre-treatment, dyeing, finishing; 3-10 % loss), textile make-up (cutting 13.57 % loss, inspection 6.91 %, sewing 4.31 % --> 13 % loss during make-up), distribution and transportation, use phase (washing, drying, ironing), consumer transport, end-of-life (landfill, reuse in Australia, reuse in overseas) |  |

Table S1 (continued): LCA case studies of polyester textiles.

| Study | Object of study | Geogra-phical scope | Functional unit | Processing steps and characteristics | Additional notes |
| --- | --- | --- | --- | --- | --- |
| Temizel-Sekeryan & Hicks, 2021 | Antibacterial T-shirt | USA | 145 g silver enabled PES textile (indicates men’s t-shirt with a large size) during its lifetime of 100 laundering cycles | PES textile manufacturing (adapted to 1 kg of PES: 24,83 kg/kg deionized water, 19.77 kWh/kg, 9.26 MJ/kg) | 100 laundry cycles, landfilling and incineration, using data from Walser et al. 2011 |
| Wu, 2020 | 100 % polyester sports shirt | China | Lifetime of 1 100 % polyester sports shirt | PET production (26.67 MJ/kg, 1.36 %), PES manufacturing (120 MJ/kg, 1.36 %), PES transportation (8 MJ/kg, 0.67 %), yarn manufacturing (40 MJ/kg, 2.67 %), weaving (7.33 MJ/kg, 8.67 %). pre-treatment (6 MJ/kg, 2 %), dyeing (12 MJ/kg, 6 %), finishing (6 MJ/kg, 2 %), transportation (0.14 MJ/kg, 1.33 %), washing and drying (480 MJ/kg, 142 %), disposal (landfill, 26.67 MJ/kg, 1.36 %) | Life span: 2 years, 52 times laundry (values scaled on 1 kg, assuming 150 g of T-shirt) |

# Supplementary note 2: General approach for data acquisition and template used for textile value chain inventory data collection

To collect inventory data for the case study, the following steps were conducted.

- Step 1: First meeting with the jersey brand to identify the supply chain partner and to map out the value chin and life cycle of the jersey.

- Step 2: Creation of LCI information sheets (as shown in Figure S1 and Figure S2 for the case of the supply chain partner that is responsible for texturizing and knitting), tailored to each supply chain partner.

- Step 3: Verification meeting with the brand to discuss the value chain map and LCI sheets.

- Step 4: LCI sheets are sent to supply chain partners through the brand.

- Step 5: Returned LCI sheets are screened. If information is missing or unclear, a meeting for an interview is scheduled.

- Step 6: Interviews are conducted together with a brand representative to complete the LCI data.

Figure S1: Life cycle inventory information sheet as sent to the supply chain partner responsible for texturizing and knitting (page 1).

Figure S2: Life cycle inventory information sheet as sent to the supply chain partner responsible for texturizing and knitting (page 2).

# Supplementary note 3: Life cycle inventory

The following LCI information are based on supplier information and, where applicable, literature data.

Table S2: LCI of the production phase.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Yarn production |  |  |  |
| Polyester yarn | 1.30E-01 | kg | Based on confidential supplier information |
| Elastane | 9.77E-03 | kg | Based on Sandin et al. (2019) |
| Knitting |  |  | See Table S3 |
| Garment preparation and assembly |  |  | See Table S4 |

Table S3: LCI of the knitting process for fabric for one jersey based on supplier information.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Electricity | 4.88E-02 | kWh |  |
| Oil | 2.09E-03 | L |  |
| Waste | 6.61E-03 | kg | See Table S4 |

Table S4: LCI of knitting waste treatment per 1 kg of waste based on supplier information.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transportation | 2.50E-01 | tkm |  |
| Shredding electricity demand | 9.00E-02 | kWh | Based on Witik et al. (2011) |
| Filling material avoided | -4.00E-01 | kg | Assuming a 50:50 mix of cotton and polyester fiber |

Table S5: LCI of the garment preparation and assembly processes, based on supplier information, Moazzem, Crossin, et al. (2018b) and Horn et al. (2023).

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Zipper | 1.2 | - | See Table S6, one large zipper in front, one small in the back (20% of front) |
| Sublimation printing |  |  | See Table S7 |
| Electricity | 3.16E-01 |  |  |
| Polyester thread | 4.07E-04 |  |  |
| Heat | 8.14E-03 |  |  |
| Water | 2.09E-02 |  |  |
| Wicking chemical | 1.57E-03 |  |  |
| Waste water | -2.09E-05 |  |  |
| Waste fabric to incineration | -1.99E-02 |  |  |
| Packaging | 1.20E-02 |  | Paper packaging, brand information |

Table S6: LCI of the zipper production per one zipper, based on supplier information.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Recycled polyester yarn | 7-71E-03. | kg |  |
| Recycled polyester chips | 6.43E-03 | kg |  |
| Recycled polyamide chips | 2.68E-03 | kg |  |
| Transport of raw materials | 7.57E-03 | tkm |  |
| Tape weaving | 7.71E-03 | kg | Modelled by adapting the ecoinvent process “weaving of synthetic fiber, for industrial use (GLO)” to polyester and CN electricity supply |
| Zipper teeth extrusion | 6.43E-03 | kg |  |
| Zipper slider injection | 2.68E-03 | kg |  |
| Treatment of waste | -4,02E-04 | kg |  |
| Transport by air to Nice | 1,67E-01 | tkm | Based on searates.com and airportdistancecalculator.com |
| Assembling packaging | 5,44E-03 | kg | Kraft paper |
| Transport by truck to CZ | 1,80E-02 | tkm |  |

Table S7: LCI of the sublimation printing per garment, adapted from Peters et al. (2018).

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Electricity | 1.30E-03 | kWh |  |
| Paper | 8.10E-02 | kg |  |
| Electricity for heat press | 3.91E-01 | kWh |  |
| Compressed air | 2.04E-01 | L |  |
| Dyestuff | 4.25E-03 | L |  |
| Paper waste | -8.10E-02 | kg |  |

Table S8: LCI of the transportation phase.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transport from Spain to the Czech Republic | 2.66E-01 | tkm | Based on Google Maps, 2000 km |
| Transport from the Czech Republic to the Netherlands | 1.07E-01 | tkm | Based on Google Maps, 800 km |

Table S9: LCI of the use phase.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Online purchase |  |  | See Table S10 |
| Washing | 5.88E+00 | kg | See Table S11 |
| Tumble drying | 2.06E+00 | kg | See Table S12 |

Table S10: LCI of the online purchase (Hischier, 2018).

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| “Delivery to me transport” – lorry | 2.33E-02 | tkm | 80% of 200 km |
| “Delivery to me transport” – van | 5.84E-03 | tkm | 20% of 200 km |
| Packaging waste management | -1.20E-02 | kg |  |

Table S11: LCI of the washing process for 1 kg of laundry (Sandin et al., 2019).

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Water | 6.20E+00 | kg |  |
| Detergent | 1.58E-02 | kg | LCI see Sandin et al. 2019 |
| Electricity | 2.25E-01 | kWh |  |
| Waste water treatment | -5.20E-03 | m3 |  |

Table S12: LCI of the tumble drying process for 1 kg of laundry (Sandin et al., 2019).

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Electricity | 6.70E-01 | kWh |  |
| Waste water treatment | -1.00E-03 | m3 |  |

Table S13: LCI of the end-of-life phase of one jersey.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Incineration with energy recovery in NL | 55.00 | % | See Table S14 |
| Incineration in open burning in PAK | 4.50 | % | See Table S15 |
| Open dump in PAK | 3.15 | % | See Table S16 |
| Reuse in PAK | 23.40 | % | See Table S17 |
| Mechanical recycling in PAK | 13.95 | % | See Table S18 |

Table S14: LCI of the incineration in the Netherlands of one jersey.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transport for collection | 1.34E-02 | tkm |  |
| Jersey incineration in municipal incineration plant | -1.34E-01 | kg |  |
| Electricity from polyester incineration, avoided impact | -2.27E-01 | kWh |  |
| Heat from polyester incineration, avoided impact | -7.77E-01 | MJ |  |

Table S15: LCI of the open burning in Pakistan of one jersey.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transportation from NL to PAK | 1.34E-01 | kg | See Table S19 |
| Open burning of jersey | -1.34E-01 | kg |  |

Table S16: LCI of the open dumping in Pakistan of one jersey.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transportation from NL to PAK | 1.34E-01 | kg | See Table S19 |
| Open dumping of jersey | -1.34E-01 | kg |  |

Table S17: LCI of the reuse in Pakistan of one jersey.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transportation from NL to PAK | 1.34E-01 | kg | See Table S19 |
| Jersey reuse |  |  | Cut off |

Table S18: LCI of the mechanical recycling in Pakistan of one jersey.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Transport to PAK | 1.34E-01 | kg | See Table S19 |
| Mechanical recycling of polyester textile | 1.34E-01 | kg | See Table S20 |

Table S19: LCI of the transport to Pakistan of one kilogram of textile.

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Truck transport within the Netherlands | 1.00E-01 | tkm |  |
| Sea freight transport to Pakistan | 1.39E+01 | tkm |  |

Table S20: LCI of the mechanical recycling of polyester textile per 1 kg of textile waste (Duhoux et al., 2021).

| Activity/process | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Electricity | 5.00E-01 | kWh |  |
| Water | 2.00E-02 | kg |  |
| Spinnable fibers | -2.50E-01 | kg |  |
| Fluff | -7.50E-02 | kg | PET assumed |
| Filling material, avoided | -3.00E-01 | kg | Polyurethane foam assumed |

Table S21: LCI for ethylene glycol based glycolysis of 1 kg of waste PET based on Selvam et al. (2023), using conventional heating and homogeneous catalysis.

| Material | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Input |  |  |  |
| PET | 1.000 | kg |  |
| Ethylene glycol | 0.328 | kg |  |
| Water | 0.247 | kg |  |
| Steam | 0.300 | MJ |  |
| Electricity | 0.074 | kWh |  |
| Zinc acetate | 0.100 | kg | See Table S22 |
| Output |  |  |  |
| BHET | 1.323 | kg |  |
| Waste treatment | 0.005 | kg |  |

Table S22: LCI for zinc acetate based on a stoichiometric approach and Huber et al. (2022).

| Material | Quantity | Unit | Comment |
| --- | --- | --- | --- |
| Input |  |  |  |
| Zinc oxide | 0.444 | kg |  |
| Acetic acid | 0.654 | kg |  |
| Heat | 4.000 | MJ | Conservative estimation, based on Huber et al. (2022) |
| Output |  |  |  |
| Zinc acetate | 1.000 | kg |  |
| Waste water | 0.098 | kg |  |

To model the polycondensation of BHET to PET, the ecoinvent activity to produce PET, amorphous, bottle-grade, was used. This approach serves as a conservative estimate.

# Supplementary note 4: Life Cycle Assessment results

Table S23: LCA results for the functional unit (see manuscript) in terrestrial acidification, global warming (GWP), ecotoxicity, freshwater (FETP), marine (METP), and terrestrial (TETP), fossil depletion (FDP), and freshwater eutrophication potential (FEP).

|  | TAP | GWP | FETP | METP | TETP | FDP | FEP |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Life cycle phase | kg SO2-eq. | kg CO2-eq. | kg 1,4-DCB-eq. | kg 1,4-DCB-eq. | kg 1,4-DCB-eq. | kg oil-eq. | kg P-eq. |
| Yarn production | 2.23E-03 | 5.69E-01 | 3.16E-03 | 5.17E-03 | 1.93E+00 | 1.72E-01 | 4.12E-05 |
| PES fiber production | 1.99E-03 | 4.98E-01 | 4.06E-04 | 1.54E-03 | 1.69E+00 | 1.47E-01 | 2.62E-05 |
| Elastane fiber production | 2.47E-04 | 7.06E-02 | 2.76E-03 | 3.62E-03 | 2.44E-01 | 2.51E-02 | 1.50E-05 |
| Knitting | -3.38E-05 | 5.19E-03 | -1.99E-04 | 4.11E-05 | 5.33E-03 | 3.58E-03 | -3.58E-06 |
| Garment preparation and assembly | 2.46E-03 | 1.01E+00 | 3.93E-02 | 5.34E-02 | 1.80E+00 | 2.03E-01 | 9.60E-04 |
| Zippers | 7.72E-04 | 2.83E-01 | 5.71E-03 | 8.03E-03 | 9.48E-01 | 8.12E-02 | 5.61E-05 |
| Sublimation printing | 1.06E-03 | 4.63E-01 | 1.97E-02 | 2.64E-02 | 5.56E-01 | 7.43E-02 | 5.70E-04 |
| Electricity | 5.97E-04 | 2.10E-01 | 1.03E-02 | 1.38E-02 | 1.69E-01 | 4.44E-02 | 3.32E-04 |
| Others | 3.41E-05 | 4.95E-02 | 3.63E-03 | 5.11E-03 | 1.24E-01 | 2.95E-03 | 2.58E-06 |
| Transport | 2.62E-04 | 8.85E-02 | 2.02E-03 | 3.53E-03 | 1.43E+00 | 2.83E-02 | 6.28E-06 |
| Transport for production | 1.87E-04 | 6.31E-02 | 1.44E-03 | 2.51E-03 | 1.02E+00 | 2.02E-02 | 4.47E-06 |
| Transport to NL | 7.52E-05 | 2.54E-02 | 5.81E-04 | 1.01E-03 | 4.12E-01 | 8.13E-03 | 1.80E-06 |
| Use phase | 2.73E-03 | 1.41E+00 | 1.28E-01 | 1.60E-01 | 6.87E+00 | 4.42E-01 | 6.25E-04 |
| Purchase delivery | 2.81E-05 | 1.03E-02 | 3.55E-04 | 5.48E-04 | 1.35E-01 | 2.92E-03 | 7.35E-07 |
| Washing | 1.62E-03 | 7.48E-01 | 6.62E-02 | 8.29E-02 | 3.59E+00 | 2.34E-01 | 3.48E-04 |
| Drying | 1.09E-03 | 6.54E-01 | 6.10E-02 | 7.70E-02 | 3.14E+00 | 2.05E-01 | 2.76E-04 |
| End-of-life | -5.58E-05 | 4.48E-02 | 8.74E-03 | 1.28E-02 | 3.23E-01 | -4.17E-02 | -3.45E-05 |
| Incineration NL | -8.90E-05 | 6.84E-02 | 1.07E-02 | 1.53E-02 | 3.20E-01 | -2.52E-02 | -2.28E-05 |
| Incineration PAK | 3.56E-05 | 1.40E-02 | 1.93E-04 | 2.75E-04 | 1.17E-01 | 2.86E-04 | 3.93E-08 |
| Landfill PAK | 1.47E-05 | 1.10E-03 | 2.78E-05 | 6.58E-05 | 5.49E-02 | 2.00E-04 | 2.75E-08 |
| Reuse PAK | 8.54E-05 | 5.18E-03 | 5.65E-05 | 8.87E-05 | 2.31E-02 | 1.49E-03 | 2.04E-07 |
| Recycling PAK | -1.03E-04 | -4.39E-02 | -2.25E-03 | -2.97E-03 | -1.93E-01 | -1.85E-02 | -1.20E-05 |

Table S24: LCA results for the functional unit (see manuscript) in marine eutrophication (MEP), human toxicity, carcinogenic (HTPc) and non-carcinogenic (HTPnc), ionizing radiation (IRP), Land use (LOP),  material resources, metals/minerals (SOP), and ozone depletion potential (ODP).

|  | MEP | HTPc | HTPnc | IRP | LOP | SOP | ODP |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Life cycle phase | kg N-eq. | kg 1,4-DCB-eq. | kg 1,4-DCB-eq. | kg Co-60-eq. | m2*a crop-eq. | kg Cu-eq. | kg CFC-11-eq. |
| Yarn production | 2.43E-05 | 6.93E-03 | 1.68E-01 | 1.55E-02 | 1.42E-01 | 1.67E-03 | 4.02E-07 |
| PES fiber production | 1.35E-05 | 3.30E-03 | 1.14E-01 | 1.36E-02 | 1.41E-01 | 1.04E-03 | 2.75E-07 |
| Elastane fiber production | 1.08E-05 | 3.64E-03 | 5.40E-02 | 1.83E-03 | 8.28E-04 | 6.21E-04 | 1.27E-07 |
| Knitting | -5.72E-05 | 2.56E-04 | -3.35E-03 | 1.02E-02 | -7.58E-03 | 5.98E-05 | -8.72E-08 |
| Garment preparation and assembly | 1.69E-04 | 5.63E-02 | 1.20E+00 | 2.17E-01 | 1.88E-01 | 1.01E-02 | 5.83E-07 |
| Zippers | 1.97E-05 | 7.69E-03 | 1.68E-01 | 5.59E-03 | 3.88E-02 | 2.69E-03 | 3.45E-07 |
| Sublimation printing | 1.26E-04 | 3.03E-02 | 6.41E-01 | 1.25E-01 | 1.45E-01 | 6.82E-03 | 1.54E-07 |
| Electricity | 2.25E-05 | 1.78E-02 | 3.64E-01 | 8.65E-02 | 3.23E-03 | 4.55E-04 | 4.98E-08 |
| Others | 1.08E-06 | 5.22E-04 | 2.38E-02 | 3.50E-04 | 3.91E-04 | 1.73E-04 | 3.43E-08 |
| Transport | 2.58E-06 | 4.45E-03 | 6.56E-02 | 1.76E-03 | 2.90E-03 | 9.22E-04 | 1.33E-08 |
| Transport for production | 1.84E-06 | 3.17E-03 | 4.67E-02 | 1.26E-03 | 2.07E-03 | 6.57E-04 | 9.51E-09 |
| Transport to NL | 7.41E-07 | 1.28E-03 | 1.88E-02 | 5.06E-04 | 8.33E-04 | 2.65E-04 | 3.83E-09 |
| Use phase | 3.15E-04 | 7.16E-02 | 1.83E+00 | 1.65E-01 | 9.17E-02 | 1.08E-02 | 9.52E-07 |
| Purchase delivery | 6.34E-07 | 6.30E-04 | 1.07E-02 | 1.98E-04 | 2.82E-04 | 1.13E-04 | 6.37E-09 |
| Washing | 2.81E-04 | 4.29E-02 | 1.02E+00 | 8.87E-02 | 7.22E-02 | 6.50E-03 | 6.02E-07 |
| Drying | 3.34E-05 | 2.81E-02 | 8.05E-01 | 7.57E-02 | 1.92E-02 | 4.18E-03 | 3.44E-07 |
| End-of-life | -9.17E-06 | -3.87E-03 | -1.60E-02 | -8.32E-03 | -2.19E-03 | -6.21E-04 | -1.19E-07 |
| Incineration NL | -1.56E-06 | -1.76E-03 | 2.40E-02 | -7.16E-03 | -1.68E-03 | -2.32E-04 | 3.42E-08 |
| Incineration PAK | 2.21E-08 | 2.92E-04 | 2.13E-03 | 6.82E-06 | 7.96E-06 | 7.80E-06 | 8.14E-09 |
| Landfill PAK | 1.55E-08 | 3.35E-05 | 1.21E-03 | 4.77E-06 | 1.66E-05 | 5.46E-06 | 3.06E-10 |
| Reuse PAK | 1.15E-07 | 2.36E-04 | 1.22E-03 | 3.54E-05 | 4.14E-05 | 4.06E-05 | 2.27E-09 |
| Recycling PAK | -7.76E-06 | -2.67E-03 | -4.45E-02 | -1.20E-03 | -5.77E-04 | -4.42E-04 | -1.64E-07 |

Table S25: LCA results for the functional unit (see manuscript) in particulate matter formation potential (PMFP), photochemical oxidant formation: humans (HOFP) and ecosystem (EOFP), water consumption (WCP), and water deprivation potential (WDP), and endpoint damage on ecosystem quality (DEQ).

|  | PMFP | HOFP | EOFP | WCP | WDP | DEQ |
| --- | --- | --- | --- | --- | --- | --- |
| Life cycle phase | kg PM2.5-eq. | kg NOx-eq. | kg NOx-eq. | cubic meter | cubic meter | species*year |
| Yarn production | 8.97E-04 | 1.32E-03 | 1.36E-03 | 1.40E-02 | 6.28E-02 | 2.20E-08 |
| PES fiber production | 7.89E-04 | 1.16E-03 | 1.19E-03 | 8.07E-03 | 8.07E-03 | 1.89E-08 |
| Elastane fiber production | 1.08E-04 | 1.65E-04 | 1.74E-04 | 5.90E-03 | 5.48E-02 | 3.05E-09 |
| Knitting | 2.12E-07 | 1.47E-05 | 2.05E-05 | 1.08E-02 | -2.50E-01 | 1.07E-10 |
| Garment preparation and assembly | 8.66E-04 | 2.30E-03 | 2.38E-03 | 1.33E-01 | 2.45E-01 | 6.64E-08 |
| Zippers | 2.96E-04 | 1.21E-03 | 1.26E-03 | 9.39E-03 | 3.88E-02 | 1.33E-08 |
| Sublimation printing | 3.57E-04 | 7.15E-04 | 7.38E-04 | 7.65E-02 | 1.37E-01 | 3.45E-08 |
| Electricity | 1.98E-04 | 3.44E-04 | 3.49E-04 | 4.58E-02 | 5.87E-02 | 1.56E-08 |
| Others | 1.49E-05 | 3.09E-05 | 3.21E-05 | 1.18E-03 | 1.03E-02 | 2.98E-09 |
| Transport | 1.11E-04 | 5.37E-04 | 5.57E-04 | 1.93E-03 | 6.11E-03 | 4.41E-09 |
| Transport for production | 7.88E-05 | 3.83E-04 | 3.97E-04 | 1.37E-03 | 4.36E-03 | 3.15E-09 |
| Transport to NL | 3.18E-05 | 1.54E-04 | 1.60E-04 | 5.53E-04 | 1.76E-03 | 1.27E-09 |
| Use phase | 1.02E-03 | 2.16E-03 | 2.27E-03 | 2.08E-01 | 5.25E-01 | 8.38E-08 |
| Purchase delivery | 1.17E-05 | 5.64E-05 | 5.85E-05 | 2.56E-04 | 1.47E-03 | 1.02E-09 |
| Washing | 5.97E-04 | 1.19E-03 | 1.27E-03 | 1.37E-01 | 3.86E-01 | 4.46E-08 |
| Drying | 4.08E-04 | 9.13E-04 | 9.48E-04 | 7.13E-02 | 1.37E-01 | 3.82E-08 |
| End-of-life | 4.34E-05 | 3.02E-05 | 1.85E-05 | -1.29E-02 | -4.53E-02 | 5.77E-09 |
| Incineration NL | -3.33E-05 | -9.74E-05 | -1.04E-04 | -8.37E-03 | -6.54E-03 | 6.42E-09 |
| Incineration PAK | 1.45E-05 | 7.15E-05 | 7.29E-05 | 9.84E-06 | 1.71E-04 | 1.21E-09 |
| Landfill PAK | 8.99E-05 | 2.11E-05 | 2.12E-05 | 6.89E-06 | 2.75E-05 | 2.22E-10 |
| Reuse PAK | 2.77E-05 | 9.03E-05 | 9.15E-05 | 5.12E-05 | 2.04E-04 | 1.91E-10 |
| Recycling PAK | -5.54E-05 | -5.52E-05 | -6.34E-05 | -4.65E-03 | -3.92E-02 | -2.27E-09 |

# References

Braun, G., Som, C., Schmutz, M., & Hischier, R. (2021). Environmental Consequences of Closing the Textile Loop—Life Cycle Assessment of a Circular Polyester Jacket. Applied Sciences, 11(7), 2964. https://doi.org/10.3390/app11072964

Duhoux, T., Maes, E., Hirschnitz-Garbers, M., Peeters, K., Asscherickx, L., Christis, M., Stubbe, B., Colignon, P., Hinzmann, M., & Sachdeva, A. (2021). Study on the technical, regulatory, economic and environmental effectiveness of textile fibres recycling. European Commission.

Hischier, R. (2018). Car vs. Packaging—A First, Simple (Environmental) Sustainability Assessment of Our Changing Shopping Behaviour. Sustainability, 10(9), 3061. https://doi.org/10.3390/su10093061

Horn, S., Mölsä, K. M., Sorvari, J., Tuovila, H., & Heikkilä, P. (2023). Environmental sustainability assessment of a polyester T-shirt - Comparison of circularity strategies. The Science of the Total Environment, 884, 163821. https://doi.org/10.1016/j.scitotenv.2023.163821

Huber, E., Bach, V., Holzapfel, P., Blizniukova, D., & Finkbeiner, M. (2022). An Approach to Determine Missing Life Cycle Inventory Data for Chemicals (RREM). Sustainability, 14(6), 3161. https://doi.org/10.3390/su14063161

Moazzem, S., Crossin, E., Daver, F., & Wang, L. (2018). Baseline Scenario of Carbon Footprint of Polyester T-Shirt. Journal of Fiber Bioengineering and Informatics, 11(1), 1–14. https://doi.org/10.3993/jfbim00262

Moazzem, S., Daver, F., Crossin, E., & Wang, L. (2018). Assessing environmental impact of textile supply chain using life cycle assessment methodology. The Journal of the Textile Institute, 109(12), 1574–1585. https://doi.org/10.1080/00405000.2018.1434113

Peters, G., Sandin, Spak, B., & Roos, S. (2018). LCA on fast and slow garment prototypes. Mistra Future Fashion Report.

Sandin, G., Roos, S., Spak, B., Zamani, B., & Peters, G. M. (2019). Environmental assessment of Swedish clothing consumption. https://doi.org/10.13140/RG.2.2.30502.27205

Selvam, E., Luo, Y., Ierapetritou, M., Lobo, R. F., & Vlachos, D. G. (2023). Microwave-assisted depolymerization of PET over heterogeneous catalysts. Catalysis Today, 418, 114124. https://doi.org/10.1016/j.cattod.2023.114124

Temizel-Sekeryan, S., & Hicks, A. L. (2021). Cradle-to-grave environmental impact assessment of silver enabled t-shirts: Do nano-specific impacts exceed non nano-specific emissions? NanoImpact, 22, 100319. https://doi.org/10.1016/j.impact.2021.100319

Walser, T., Demou, E., Lang, D. J., & Hellweg, S. (2011). Prospective environmental life cycle assessment of nanosilver T-shirts. Environmental Science & Technology, 45(10), 4570–4578. https://doi.org/10.1021/es2001248

Witik, R. A., Payet, J., Michaud, V., Ludwig, C., & Månson, J.‑A. E. (2011). Assessing the life cycle costs and environmental performance of lightweight materials in automobile applications. Composites Part a: Applied Science and Manufacturing, 42(11), 1694–1709. https://doi.org/10.1016/j.compositesa.2011.07.024

Wu, Z. (2020). Haode Evaluating the Life-cycle Environmental Impacts of Polyester Sports T-shirts. IOP Conference Series: Earth and Environmental Science, 474(2), 22017. https://doi.org/10.1088/1755-1315/474/2/022017