Supporting Information

Boosting immunogenic cell death via Hollow MnO2 based multiple stimuli-responsive drug delivery systems for improved cancer immunotherapy

Yueyao Wua,b#, Runtian Wanga#, Peiliang Shenb, Weijia Zhoub, Chao Chenb, Kaiyong Yangb, Jingjing Yangb,c, Yujun Songc*, Xin Hana,b* and Xiaoxiang Guana,d*

aDepartment of Oncology, The First Affiliated Hospital of Nanjing Medical University, Nanjing 210029, China.

bJiangsu Key Laboratory for Pharmacology and Safety Evaluation of Chinese Materia Medica, School of Medicine & Holistic Integrative Medicine, Nanjing University of Chinese Medicine, Nanjing 210023, China.

cCollege of Engineering and Applied Sciences, State Key Laboratory of Analytical Chemistry for Life Science, Nanjing University, Nanjing, 210023, China.

dJiangsu Key Lab of Cancer Biomarkers, Prevention and Treatment, Collaborative Innovation Center for Personalized Cancer Medicine, Nanjing Medical University, Nanjing 211166, China.

*Corresponding author(s). Xiaoxiang Guan, Xin Han, Yujun Song

E-mail address(es): xguan@njmu.edu.cn

xhan0220@njucm.edu.cn

ysong@nju.edu.cn

# These authors contribute equally to this work.

Supporting schemes

Figure S1. Synthesis process of hollow MnO2.

Figure S2. UV–vis-NIR spectra of MnO2-Ce6-HA and MnO2-MTZ-HA.

Figure S3. Physiological stability evaluation: Digital images of H-MnO2 and MnO2-C/M-HA dispersed in H2O, PBS and DMEM solution for 24 h.

Figure S4. TEM image of H-MnO2 at pH 7.4 and pH 5.5.

Figure S5. Fluorescence microscopic images of 4T1 cells incubated with Free Ce6 or MnO2-Ce6-HA at different time points. Scale bar: 50 μm.

Figure S6. Cell viability of 4T1 with different concentrations of MTZ with or without 660 nm (1.0 W·cm-2, 15 min) for 24 h.

Figure S7. Cell viability of 4T1 with different concentrations of MnO2-HA for 24 h.

Figure S8. Cell viability of 4T1 with different concentrations of MnO2-C/M-HA with or without 660 nm (1.0 W·cm-2, 15 min) for 24 h.

Figure S9. The cytotoxicity of 4T1 cells of varying formulations with or without 660 nm (1.0 W·cm-2, 15 min) for 24 h in hypoxia.

Figure S10. Fluorescence microscope images of ROS generation by DCFH-DA staining in cells in hypoxia. Scale bar: 100 μm.

Figure S11. Intracellular ATP level after various treatments.

Figure S12. Schematic diagram of co-culture by non-contact communication cell chip.

Figure S13. Local structure of non-contact communication cell chip.

Figure S14. Immunofluorescence of CD11c in 3D-cell cultures of BMDCs. Scale bar: 50 μm.

Figure S15. Immunofluorescence of CD80/CD86 in 3D-cell cultures of BMDCs. Scale bar: 50 μm.

Figure S16. Ex vivo fluorescence images (12 h post-injection) of 4T1 tumor-bearing mice organs or tissue treated with free Ce6 and MnO2-C/M-HA.

Figure S17. H&E staining of heart, liver, spleen, lung, and kidney at the end of antitumor study. Scale bar: 100 μm.

Figure S18. Hemolysis rate by incubating RBCs with MnO2-HA and MnO2-C/M-HA at different concentrations (25-100 µg/mL) for 4 h.

Figure S19. Blood biochemical indices of healthy mice at day 1, 4 and 7 after intravenous injection of MnO2-C/M-HA.

Figure S20. The whole tumor staining of TUNEL. Scale bar: 1000 μm.

Figure S21. Immunohistochemical assay of CRT and HMGB1 in the tumor tissues after various treatments. Scale bar: 200 µm.

Figure S22. Representative flow cytometry plots showing mature DCs (CD11c+CD80+CD86+) after various treatments.

Figure S23. Representative flow cytometry plots showing cytotoxic T lymphocytes (CD3+CD8+) after various treatments.

Table S1. Antibodies were used for WB, FC or IF/IHC in this study.

| Antibodies | Company | Catalog No. | Application |
| --- | --- | --- | --- |
| Calreticulin Rabbit Polyclonal antibody | Proteintech | 27298-1-AP | WB, IF, IHC |
| HMGB1 Rabbit Polyclonal antibody | Proteintech | 10829-1-AP | WB, IF, IHC |
| CoraLite 488-Goat anti-Rabbit IgG | Proteintech | SA00013-2 | IF |
| Cy3-Goat anti-Rabbit IgG | Proteintech | SA00009-2 | IF |
| Goat anti-Rabbit IgG | YIFEIXUE | YFSA02 | WB |
| Goat anti-Mouse IgG | YIFEIXUE | YISA01 | WB |
| GADPH Mouse Monoclonal antibody | Bioworld | AP0063 | WB |
| PE/Cyanine7 anti-mouse CD11c | Biolegend | 117317 | FC, IF |
| APC anti-mouse CD80 | Biolegend | 104713 | FC, IF |
| PE anti-mouse CD86 | Biolegend | 159203 | FC, IF |
| Brilliant Violet 421TM anti-mouse CD86 | Biolegend | 105031 | FC |
| APC anti-mouse CD3 | Biolegend | 100236 | FC |
| PE anti-mouse CD8a | Biolegend | 100708 | FC |

WB: Western Blot.  FC: Flow cytometry.

IF: Immunofluorescence.  IHC: Immunohistochemistry.