Supporting Information

Aptamer modified Ti3C2 nanosheets application in smart targeted photothermal therapy for cancer

Zhiqiang Bai12, Lu Zhao2, Haidi Feng2, Zhihui Xin12, Chaoyu Wang2, Zhixiong Liu2, Maozhong Tian2, Haifei Zhang4, Yunfeng Bai2,**, Feng Feng123,*

1 School of Chemistry and Material Science, Shanxi Normal University, Linfen 041004, P. R. China.

2 School of Chemistry and Chemical Engineering, Shanxi Provincial Key Laboratory of Chemical Biosensing, Shanxi Datong University, Datong 037009, P. R. China.

3 Department of Energy Chemistry and Material Engineering, Shanxi Institute of Energy, Taiyuan 030600, P. R. China.

4 Department of Chemistry, University of Liverpool, Crown Street, Liverpool, L69 7ZD, United Kingdom.

* Corresponding author.

** Corresponding author.

E-mail: feng-feng64@263.net (Feng Feng), baiyunfeng1130@126.com (Yunfeng Bai)

Mail address: School of Chemistry and Chemical Engineering, Shanxi Datong University, Datong 037009, P. R. China

Supplementary figures and tables

Figure S1. SEM images of (a) Ti3AlC2 ceramic bulks and (b) Ti3C2 bulks.

Figure S2. (a) AFM image and (b) the corresponding thickness of Ti3C2 nanosheets.

Figure S3. EDS spectra of Ti3C2 nanosheets.

Figure S4. XPS spectra of Ti3C2 nanosheets.

Figure S5. Digital images of Ti3C2 nanosheets and Ti3C2/Apt-M nanosheets dispersed in various solvents.

Figure S6. Digital images of hemolysis assay of Ti3C2, Ti3C2-PEG and Ti3C2/Apt-M nanosheets at different concentrations.

Figure S7. UV-vis spectra of Ti3C2, Ti3C2-PEG and Ti3C2/Apt-M nanosheets.

Figure S8. UV-vis spectra of (a) Ti3C2, (b) Ti3C2-PEG and (c) Ti3C2/Apt-C nanosheets at different concentrations. Mass extinction coefficient of (d) Ti3C2, (e) Ti3C2-PEG and (f) Ti3C2/Apt-C nanosheets at 808 nm. Normalized absorbance intensity at λ = 808 nm divided by the characteristic length of the cell (A/L) at varied concentrations (10, 20, 30, 40 and 50 µg mL-1).

Figure S9. Photothermal performance of (a) Ti3C2, (b) Ti3C2-PEG and (c) Ti3C2/Apt-C nanosheets dispersed in aqueous solution under 808 nm laser irradiation. Calculation of time constant and photothermal-conversion efficiency of (d) Ti3C2, (e) Ti3C2-PEG and (f) Ti3C2/Apt-C nanosheets at 808 nm laser irradiation.

Figure S10. (a) Infrared thermal images and (b) temperature changes of Ti3C2/Apt-M nanosheet aqueous solutions under different laser power irradiation at 808 nm.

Figure S11. Cell viabilities of (a-b) MCF-7 and (c-d) HepG2 cells after incubation with Ti3C2-PEG, Ti3C2/Apt-M and Ti3C2/Apt-C nanosheets of varied concentrations for 24 h and 48 h.

Figure S12. Cell viability of (a) MCF-7 and (b) HepG2 cells treated with different concentrations of Ti3C2-PEG, Ti3C2/Apt-C and Ti3C2/Apt-M nanosheets.

Figure S13. (a) The representative infrared thermal images and (b) temperature curves of tumor-bearing mice with different treatments at different time points.

Figure S14. Body weight curves of tumor-bearing mice after different treatments in 17 d.

Figure S15. H&E stained tissue sections of major organs (heart, liver, spleen, lung and kidney) from mice with different treatments. Scale bar: 100 μm.

Table S1. Aptamer sequences.

| Name | Sequences (5’-3’) |
| --- | --- |
| Apt-M | NH2-(CH2)6-GCA GTT GAT CCT TTG GAT ACC CTG GTT TTT TTT TT |
| Apt-C | NH2-(CH2)6-ATT GCA CTT ACT ATA TTG CAC TTA CTA TAT TGC AC |
| Apt-Mf | NH2-(CH2)6-GCA GTT GAT CCT TTG GAT ACC CTG GTT TTT TTT TT-FAM |
| Apt-Cf | NH2-(CH2)6-ATT GCA CTT ACT ATA TTG CAC TTA CTA TAT TGC AC-FAM |

Table S2. The photothermal performance parameters (mass extinction coefficient and photothermal conversion efficiency) of various nanoagents in the literatures.

| Nanomaterials | Mass Extinction Coefficient (ε, Lg-1cm-1) | Photothermal Conversion Efficiency (η, %) | Wavelength (λ, nm) |
| --- | --- | --- | --- |
| Ti3C2 nanosheets1 | 25.2 | 30.6 | 808 |
| Nb2C nanosheets2 | 37.6 or 35.4 | 36.5 or 46.65 | 808 or 1064 |
| Ta4C3 nanosheets3 | 8.67 | 34.9 | 808 |
| Mo2C nanosheets4 | 18.0 or 12.3 | 24.5 or 43.3 | 808 or 1064 |
| V2C nanosheets5 | 38.3 | 48.5 | 808 |
| Ti2N quantum dots6 | 41.25 or 34.92 | 48.62 or 45.51 | 808 or 1064 |
| W1.33C nanosheets7 | 8.54 or 4.94 | 32.5 or 49.3 | 808 or 1064 |
| Ti3CN nanosheets8 | 36.6 or 43.5 | 36.5 or 32.1 | 808 or 1064 |
| Au nanorods9 | 13.9 | 21.0 | 808 |
| BP quantum dots10 | 14.8 | 28.4 | 808 |
| SnS bulk11 | 8.2 | 24.0 | 808 |
| WS2 nanosheets12 | 23.8 | 44.3 | 808 |

References

1.	Lin, H.; Wang, X.; Yu, L.; Chen, Y.; Shi, J. Nano Lett. 2017, 17, (1), 384-391.

2.	Lin, H.; Gao, S.; Dai, C.; Chen, Y.; Shi, J. J. Am. Chem. Soc. 2017, 139, (45), 16235-16247.

3.	Dai, C.; Chen, Y.; Jing, X.; Xiang, L.; Yang, D.; Lin, H.; Liu, Z.; Han, X.; Wu, R. ACS Nano 2017, 11, (12), 12696-12712.

4.	Feng, W.; Wang, R.; Zhou, Y.; Ding, L.; Gao, X.; Zhou, B.; Hu, P.; Chen, Y. Adv. Funct. Mater. 2019, 29, (22), 1901942.

5.	Zada, S.; Dai, W.; Kai, Z.; Lu, H.; Meng, X.; Zhang, Y.; Cheng, Y.; Yan, F.; Fu, P.; Zhang, X.; Dong, H. Angew. Chem. Int. Ed. 2020, 59, (16), 6601-6606.

6.	Shao, J.; Zhang, J.; Jiang, C.; Lin, J.; Huang, P. Chem. Eng. J. 2020, 400, 126009.

7.	Zhou, B. G.; Yin, H. H.; Dong, C. H.; Sun, L. P.; Feng, W.; Pu, Y. Y.; Han, X. X.; Li, X. L.; Du, D.; Xu, H. X.; Chen, Y. Adv. Sci. 2021, 8, (24), 2101043.

8.	Zhu, Y. H.; Tang, X. F.; Liu, Q.; Xia, Y. J.; Zhai, X. W.; Zhang, H.; Duan, D. L.; Wang, H.; Zhan, W. Q.; Wu, L.; Zheng, N.; Lv, W. F.; Wang, Y. C.; Zhou, M. Small 2022, 18, (22), 2200646.

9.	Zeng, J.; Goldfeld, D.; Xia, Y. Angew. Chem. Int. Ed. 2013, 52, (15), 4169-4173.

10.	Sun, Z.; Xie, H.; Tang, S.; Yu, X. F.; Guo, Z.; Shao, J.; Zhang, H.; Huang, H.; Wang, H.; Chu, P. K. Angew. Chem. Int. Ed. 2015, 54, (39), 11526-11530.

11.	Ren, Q.; Li, B.; Peng, Z.; He, G.; Zhang, W.; Guan, G.; Huang, X.; Xiao, Z.; Liao, L.; Pan, Y.; Yang, X.; Zou, R.; Hu, J. New J. Chem. 2016, 40, (5), 4464-4467.

12.	Yong, Y.; Cheng, X.; Bao, T.; Zu, M.; Yan, L.; Yin, W.; Ge, C.; Wang, D.; Gu, Z.; Zhao, Y. ACS Nano 2015, 9, (12), 12451-12463.