[bookmark: _GoBack]S1 Table. Characteristics of the Precizon toric IOL and Tecnis toric IOL.
	Characteristics
	Precizon toric IOL
	Tecnis toric IOL

	Optic characteristics
	
	

	Powers (D)
	+10 to +30 D
	+5.00 to +34.00


	Cylinder powers (IOL plane) (D)
	1 to 10 D 
(0.5 D increments)
	1.50/2.25/3.00/4.00


	Cylinder powers (corneal plane) (D)
	0.69 to 6.85
	1.03/1.54/3.06/2.74


	Diameter (mm)
	6.0
	6.0


	Shape
	Biconvex, transitional conic toric aspheric surface
	Biconvex, anterior toric aspheric surface


	Material
	Acrylic - hydrophilic
	Acrylic - UV filtering hydrophobic


	Refractive Index
	1.46
	1.47


	Edge design
	Square edge
	Square edge

	Spherical aberration (㎛)
	0
	-0.27

	Biometry
	
	

	A-constant (mm)
	118.0 (US); 118.5 (optical)
	118.8 (US); 119.3 (optical)

	Theoretical ACD (mm)
	5.26
	5.4

	Haptic characteristics
	
	

	Overall length (mm)
	12.5
	13.0


	Configuration
	close-loop design
	modified C-loop design, integral with optic

	Material
	Same as optic
	Same as optic


 IOL: intralocular lens; ACD: anterior chamber depth; US: ultrasound.
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