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Supplementary Figure 1: Preoperative radiographs demonstrating septic loosening of a total knee arthroplasty in a 59-year-old male patient (left). Postoperative radiograph after prosthesis removal and implantation of an arthrodesis bone cement spacer, additionally using two carbon fiber rods and a connection clamp (right). Radiographic images were retrieved from the institutional picture archiving and communication system (PACS). The images were anonymized and used solely for illustrative purposes. 
Supplementary Table 1: CAD-derived surface characteristics of the cement specimens.
	Cement-structure
	Surface area [mm²]
	Volume [mm³]
	Surface area-to-volume ratio
	Surface area increase [%]

	Reference group
	2063,7
	2478,3
	0,83
	100%

	Surface group 1
	2348,7
	2478,3
	0,95
	114%

	Surface group 2
	2636,7
	2478,3
	1,06
	128%

	Surface group 3
	3221,3
	2478,3
	1,30
	156%



Supplementary Table 2: Vancomycin mass released per specimen in mg/specimen, for each interval.
	[bookmark: _Hlk233128875]Days
	0.208
	1
	2
	4
	7
	14
	21
	28
	35
	42

	Reference group (mg)
	1,25
	0,35
	0,15
	0,20
	0,16
	0,22
	0,13
	0,12
	0,12
	0,12

	Mean ± SD
	0,03
	0,02
	0,01
	0,01
	0,01
	0,02
	0,01
	0,00
	0,00
	0,00

	

	Surface group 1 (mg)
	2,46
	0,68
	0,37
	0,52
	0,39
	0,46
	0,25
	0,19
	0,13
	0,12

	Mean ± SD
	0,14
	0,09
	0,04
	0,09
	0,04
	0,22
	0,01
	0,03
	0,01
	0,01

	

	Surface group 2 (mg)
	2,44
	0,84
	0,47
	0,45
	0,43
	0,52
	0,38
	0,28
	0,17
	0,15

	Mean ± SD
	0,13
	0,04
	0,07
	0,05
	0,06
	0,04
	0,04
	0,04
	0,02
	0,05

	

	Surface group 3 (mg)
	2,85
	1,41
	0,57
	0,56
	0,56
	0,56
	0,42
	0,30
	0,20
	0,15

	Mean ± SD
	0,19
	0,13
	0,05
	0,05
	0,03
	0,05
	0,01
	0,02
	0,01
	0,05



Supplementary Table 3: Gentamicin mass released per specimen in mg/specimen, for each interval.
	Days
	0.208
	1
	2
	4
	7
	14
	21
	28
	35
	42

	Reference group (mg)
	1,02
	1,23
	0,51
	0,61
	0,43
	0,58
	0,28
	0,20
	0,15
	0,10

	Mean ± SD
	0,28
	0,19
	0,09
	0,08
	0,05
	0,13
	0,06
	0,05
	0,04
	0,01

	

	Surface group 1 (mg)
	1,08
	0,70
	0,50
	0,53
	0,57
	0,75
	0,31
	0,30
	0,22
	0,15

	Mean ± SD
	0,11
	0,08
	0,12
	0,11
	0,12
	0,26
	0,08
	0,04
	0,08
	0,04

	

	Surface group 2 (mg)
	1,45
	0,90
	0,68
	0,52
	0,47
	0,69
	0,53
	0,51
	0,28
	0,22

	Mean ± SD
	0,19
	0,06
	0,13
	0,08
	0,08
	0,17
	0,18
	0,15
	0,07
	0,05

	

	Surface group 3 (mg)
	1,37
	1,39
	0,83
	0,69
	0,68
	0,98
	0,52
	0,48
	0,31
	0,21

	Mean ± SD
	0,31
	0,16
	0,07
	0,12
	0,09
	0,13
	0,05
	0,09
	0,05
	0,02
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