| Table S1: Diagnostic tests for melanin identification produced by different filamentous fungi |  |  |
| --- | --- | --- |
| Test | Producer fungal strain |  |
|  | A. flavus | A. carbonarius |
| Solubility in water | In Soluble | In Soluble |
| Color | Dark Brown | Black |
| Solubility in KOH | Soluble | Soluble |
| Precipitation in 3N HCL | Precipitated readily | Precipitated readily |
| Solubility in organic acid solvent (chloroform, acetone, ethyl acetate) | In Soluble | In Soluble |
| Reaction with H2O2 | Decolorized | Decolorized |
| Reaction with Fecl3 (Reaction for polyphenols test) | Brown precipitate | Brown precipitate |
| Reaction with sodium dithionite and potassium ferricyanide | Decolorized and turned brown with addition of potassium ferricyanide | Decolorized and turned brown with addition of potassium ferricyanide |

| Table S2: FTIR for control melanin and melanin (15 mg) adsorption Cd |  |  |  |  |
| --- | --- | --- | --- | --- |
| Peaks | Control | Sample | Shift | Functional group |
| 1 | 3736 | 3785 | 49 | Alcohol group (O-H) stretch, free, strong and sharp |
| 2 | 3434 | 3408 | 26 | Alcohol group (O-H), stretch, H-bonded, strong and broad |
| 3 | 2924 | 2922 | 2 | Alkane group C-H (stretch, strong) |
| 4 |  | 2853 | - | Alkane group C-H (stretch, strong) |
| 5 | 2363 | 2361 | 2 | C≡ N stretching mode |
| 6 | 1632 | 1623 | 10 | C=C stretching mode, N-H bending in primary amine, or C=o stretching mode (amide) |
| 7 |  | 1710 | - | C=O stretching mode (Ketone) Or C=O stretching mode (carboxylic acid) |
| 8 | 1456 | 1406 | 50 | C=C stretching mode (Aromatic ring) |
| 9 | 1260 | 1252 | 8 | C-O-H bending mode C-O stretching mode (Alcohol) C-O stretching mode (ether) C=O bending mode C-O carboxylic acid |
| 10 | 1147 | 1148 | 1 | C-O stretching mode (Alcohol) C-O stretching mode (ether) C-O stretching mode |
| 11 | 1028 | 1037 | 9 | C-O stretching mode (Alcohol) C-O stretching mode (ether) C-O stretching mode C- F stretching mode |
| 12 | 928 |  | - | C=C bending, alkene, |
| 13 | 873 | 849 | 24 | Halo compound C-Cl, stretching |
| 14 | 815 |  | - | =C-H out of plane bending mode (Aromatic ring) or N-H, bending mode |
| 15 |  | 596 | - | C- Cl, C-Br, C-I (halo compound) |
| 16 | 541 | 542 | 1 | C- Cl, C-Br halo compound |
| 17 | 471 | 473 | 2 | C-Br, C-I (halo compound) |
| 18 |  | 447 | - | C-Br, C-I (halo compound) |

| Table S3: FTIR for control melanin and melanin (15 mg) adsorption Cr |  |  |  |
| --- | --- | --- | --- |
| Control | sample | Shift | Functional group |
| 3736 | 3785 | 49 | Alcohol group (O-H) stretch, free, strong and sharp |
| 3434 | 3430 | 4 | Alcohol group (O-H), stretch, H-bonded, strong and broad |
| 2924 | 2923 | 1 | Alkane group C-H (stretch, strong) |
|  | 2853 | - | Alkane group C-H (stretch, strong) |
| 2363 | 2361 | 2 | C≡ N stretching mode |
|  | 1712 | - | C=O stretching mode (ketone) C=O Stretching mode (carboxylic group ) |
| 1632 | 1626 | 6 | C=C stretching mode , N-H bending in primary amine , or C=o stretching mode (amide) |
| 1456 | 1405 | 51 | C=C stretching mode (Aromatic ring) |
| 1260 | 1258 | 2 | C-O-H bending mode C-O stretching mode (Alcohol) C-O stretching mode (ether) C=O bending mode C-O carboxylic acid |
| 1147 | 1151 | 4 | C-O stretching mode (Alcohol) C-O stretching mode (ether) C-O stretching mode |
|  | 1081 |  |  |
| 1028 | 1038 |  | C-O stretching mode (Alcohol) C-O stretching mode (ether) C-O stretching mode C- F stretching mode |
| 928 |  |  | C=C bending , alkene, |
| 873 |  |  | Halo compound C-Cl , stretching |
| 815 |  |  | =C-H out of plane bending mode (Aromatic ring) or N-H, bending mode |
|  |  |  | C- Cl , C-Br , C-I ( halo compound ) |
| 541 |  | - | C- Cl, C-Br halo compound |
|  | 601 | - | C- Cl , C-Br , C-I ( halo compound |
|  | 538 | - | C-Br, C-I ( halo compound ) |
| 471 | 448 | 23 | C-Br, C-I ( halo compound ) |

Fig. S1 Melanin productivity by the isolated fungal strains. Data are presented as mean ±SEM from three independent experiments P ≤ 0.05.

Fig. S2 Phylogenetic tree based on ITS sequences of 18S rDNA of the fungal strain isolated in the present study (AUMC14796-MZ314535, arrowed) aligned with closely related sequences accessed from the GenBank. (A. = Aspergillus).