Additional File 1 -  Composition of the restorative materials

| Groups | Restorative Material | Manufacturer | Composition |
| --- | --- | --- | --- |
| Hand Mixed | Fuji IX Gold Label® | GC Corp | Powder: fluoroaluminosilicate glass, polyacrilyc acid powder |
|  |  |  | Liquid: polyacrilyc acid, polybasic carboxilic acid |
| Encapsulated | Equia Fil® |  | Powder: 95% strontium fluoralumino-silicate, 5% polyacrilyc acid |
|  |  |  | Liquid: 40% aqueous polyacrilyc acid |