Table 1. Atomic percentage of nanorods. nHAEA; modified nanohydroxyapatite via EA extract, nHA; nanohydroxyapatite

| Types of nanorods | Ca (at. %) | P (at. %) | O (at. %) | Ca/P (at. %) |
| --- | --- | --- | --- | --- |
| nHA | 19.59 | 12.73 | 67.68 | 1.54 |
| nHAEA | 21.45 | 14.99 | 63.56 | 1.43 |

Table 2. Mean and standard deviation (SD) values of cell viability in MTT assay. Ctrl; Control, DMEM, PCL; Polycaprolactone, P/nHA; Polycaprolactone/nanohydroxyapatite, P/nHAEA; Polycaprolactone/ modified nanohydroxyapatite via EA extract

| SD | Mean | Groups | Time |
| --- | --- | --- | --- |
| 1.834 | 99.53 | Ctrl | 1 day |
| 4.928 | 100.5 | PCL |  |
| 5.270 | 97.23 | P-nHA |  |
| 3.953 | 97.12 | P-nHAEA |  |
| 5.429 | 100.0 | Ctrl | 3 days |
| 3.402 | 108.9 | PCL |  |
| 9.793 | 108.3 | P-nHA |  |
| 6.232 | 111.4 | P-nHAEA |  |
| 4.398 | 100.0 | Ctrl | 7 days |
| 7.187 | 100.3 | PCL |  |
| 3.122 | 109.7 | P-nHA |  |
| 7.613 | 115.3 | P-nHAEA |  |

Table 3. Mean and standard deviation (SD) values of relative gene expression in q-PCR assessment.

| SD | Mean | Groups | Targeted gene |
| --- | --- | --- | --- |
| 0.1018 | 0.9280 | Ctrl | BMP2 |
| 0.3111 | 1.260 | PCL |  |
| 0.1414 | 2.360 | P-nHA |  |
| 0.7920 | 4.260 | P-nHAEA |  |
| 0.1287 | 0.9090 | Ctrl | Runx2 |
| 0.1442 | 0.9180 | PCL |  |
| 0.2192 | 1.715 | P-nHA |  |
| 0.2475 | 2.395 | P-nHAEA |  |
| 0.04950 | 1.000 | Ctrl | DSPP |
| 1.103 | 2.350 | PCL |  |
| 4.844 | 17.55 | P-nHA |  |
| 2.793 | 43.91 | P-nHAEA |  |

Table 4. Mean and standard deviation (SD) values of ALP activity assessment.

| SD | Mean | Groups | Targeted gene |
| --- | --- | --- | --- |
| 0.4907 | 5.347 | Ctrl | ALP activity |
| 0.2121 | 6.350 | PCL |  |
| 0.1414 | 8.400 | P-nHA |  |
| 0.2121 | 9.950 | P-nHAEA |  |

Table 5. Mean and standard deviation (SD) values of ARS assessment.

| SD | Mean | Groups | Targeted gene |
| --- | --- | --- | --- |
| 0.1051 | 0.8663 | Ctrl | ARS |
| 0.1481 | 1.927 | PCL |  |
| 0.3477 | 6.833 | P-nHA |  |
| 0.7731 | 8.812 | P-nHAEA |  |