

Gingival index score
	
Material
Used

	
At base line
	
After 6 months
	
After 1 year
	
After 2 years
	
After 5 years

	
	0
	1
	2
	3
	0
	1
	2
	3
	0
	1
	2
	3
	0
	1
	2
	3
	0
	1
	2
	3

	

Zirconia
Implant
	
14
	
--
	
--
	
--
	
13
	
1
	
--
	
--
	
11
	
3
	
--
	
--
	
11
	
3
	
--
	
--
	
11
	
3
	
--
	
--

	

Titanium
Implant

	
14
	
--
	
--
	
--
	
13
	
1
	
--
	
--
	
11
	
3
	
--
	
--
	
11
	
2
	
1
	
--
	
11
	
2
	
1
	
--








Plaque index score

	
Material
Used

	
At base line
	
After 6 months
	
After 1 year
	
After 2 years
	
After 5 years

	
	0
	1
	2
	3
	0
	1
	2
	3
	0
	1
	2
	3
	0
	1
	2
	3
	0
	1
	2
	3

	

Zirconia
Implant
	
14
	
--
	
--
	
--
	
14
	
--
	
--
	
--
	
11
	
3
	
--
	
--
	
11
	
3
	
--
	
--
	
11
	
3
	
--
	
--

	

Titanium
Implant

	
14
	
--
	
--
	
--
	
14
	
--
	
--
	
--
	
11
	
3
	
--
	
--
	
10
	
3
	
1
	
--
	
11
	
2
	
1
	
--







Periodontal depth
	After 5 years
	After 2 years
	After 12 months
	After 6 months
	At base line
	No.
	Material used

	3.3
	3.2
	3.1
	2.7
	2.7
	1
	






Zirconia implant




	3.3
	3.2
	3
	2.8
	2.8
	2
	

	3.5
	3.3
	3.1
	2.6
	2.6
	3
	

	3.4
	3.4
	3
	2.9
	2.9
	4
	

	3.3
	3.3
	3.1
	2.6
	2.6
	5
	

	3.5
	3.3
	3
	2.8
	2.8
	6
	

	3.1
	3.2
	3
	2.7
	2.7
	7
	

	3.3
	3.1
	3.1
	2.9
	2.9
	8
	

	3.5
	3.5
	3.4
	2.6
	2.6
	9
	

	3.2
	3.1
	3
	2.5
	2.5
	10
	

	3.5
	3.5
	3.3
	2.7
	2.7
	11
	

	3
	3
	2.9
	2.6
	2.6
	12
	

	3.2
	3.2
	3.1
	2.7
	2.7
	13
	

	3.4
	3.4
	3.2
	2.9
	2.9
	14
	

	[bookmark: _GoBack]3.3
	3.3
	3.2
	2.9
	2.9
	1
	





Titanium implant




	3.1
	3.1
	3.1
	2.9
	2.9
	2
	

	3.5
	3.5
	3.2
	2.6
	2.6
	3
	

	3.3
	3.3
	3.2
	2.8
	2.8
	4
	

	3.4
	3.4
	3.2
	2.5
	2.5
	5
	

	3.5
	3.3
	3.2
	2.8
	2.8
	6
	

	3.3
	3.2
	3.1
	2.9
	2.9
	7
	

	3.4
	3.3
	3.1
	2.9
	2.9
	8
	

	3.3
	3.2
	3
	2.5
	2.5
	9
	

	3.2
	3.2
	3
	2.7
	2.7
	10
	

	3.2
	3.2
	3.1
	2.6
	2.6
	11
	

	3.5
	3.5
	3.2
	2.7
	2.7
	12
	

	3.3
	3.3
	3.1
	2.5
	2.5
	13
	

	3.4
	3.2
	3
	2.7
	2.7
	14
	


Marginal bone loss
	
Zirconia implant 

	After 5years
	After2
years
	After 1 year
	after 6 months
	At 3months

	D.
	M.
	D.
	M.
	D.
	M.
	D.
	M.
	D.
	M.
	

	1.8
	1.7
	1.6
	1.5
	1.3
	1.3
	0.7
	0.6
	0.4
	0.3
	1

	1.7
	1.8
	1.5
	1.6
	1.2
	1.4
	0.7
	0.5
	0.2
	0.4
	2

	1.7
	1.9
	1.6
	1.5
	1.2
	1.3
	0.6
	0.7
	0.3
	0.3
	3

	1.9
	1.8
	1.5
	1.5
	1.2
	1.3
	0.7
	0.6
	0.3
	0.2
	4

	1.8
	1.7
	1.6
	1.5
	1.4
	1.3
	0.6
	0.5
	0.2
	0.3
	5

	1.7
	1.8
	1.5
	1.6
	1.3
	1.4
	0.8
	0.7
	0.3
	0.2
	6

	1.8
	1.8
	1.5
	1.5
	1.3
	1.3
	0.7
	0.8
	0.4
	0.2
	7

	1.8
	1.7
	1.6
	1.5
	1.3
	1.3
	0.7
	0.6
	0.4
	0.3
	8

	1.7
	1.8
	1.5
	1.6
	1.2
	1.4
	0.7
	0.5
	0.2
	0.4
	9

	1.7
	1.9
	1.6
	1.5
	1.2
	1.3
	0.6
	0.7
	0.3
	0.3
	10

	1.9
	1.8
	1.5
	1.5
	1.2
	1.3
	0.7
	0.6
	0.3
	0.2
	11

	1.8
	1.7
	1.6
	1.5
	1.4
	1.3
	0.6
	0.5
	0.2
	0.3
	12

	1.7
	1.8
	1.5
	1.6
	1.3
	1.4
	0.8
	0.7
	0.3
	0.2
	13

	1.8
	1.8
	1.5
	1.5
	1.3
	1.3
	0.7
	0.8
	0.4
	0.2
	14

	Titanium implant 

	After 5years
	After2
years
	After 1 year
	after 6 months
	At 3months

	D.
	M.
	D.
	M.
	D.
	M.
	D.
	M.
	D.
	M.
	

	1.9
	1.7
	1.5
	1.5
	1.2
	1.3
	0.6
	0.7
	0.3
	0.3
	1

	1.8
	1.8
	1.5
	1.5
	1.3
	1.3
	0.7
	0.8
	0.4
	0.2
	2

	1.8
	1.9
	1.6
	1.5
	1.2
	1.3
	0.7
	0.6
	0.3
	0.2
	3

	1.8
	1.8
	1.6
	1.5
	1.4
	1.3
	0.6
	0.5
	0.2
	0.3
	4

	1.8
	1.8
	1.5
	1.6
	1.3
	1.4
	0.8
	0.7
	0.3
	0.2
	5

	1.8
	1.8
	1.6
	1.5
	1.3
	1.3
	0.7
	0.6
	0.4
	0.3
	6

	1.7
	1.8
	1.5
	1.6
	1.2
	1.4
	0.7
	0.5
	0.2
	0.4
	7

	1.9
	1.7
	1.5
	1.5
	1.2
	1.3
	0.6
	0.7
	0.3
	0.3
	8

	1.8
	1.8
	1.5
	1.5
	1.3
	1.3
	0.7
	0.8
	0.4
	0.2
	9

	1.8
	1.9
	1.6
	1.5
	1.2
	1.3
	0.7
	0.6
	0.3
	0.2
	10

	1.8
	1.8
	1.6
	1.5
	1.4
	1.3
	0.6
	0.5
	0.2
	0.3
	11

	1.8
	1.8
	1.5
	1.6
	1.3
	1.4
	0.8
	0.7
	0.3
	0.2
	12

	1.8
	1.8
	1.6
	1.5
	1.3
	1.3
	0.7
	0.6
	0.4
	0.3
	13

	1.7
	1.8
	1.5
	1.6
	1.2
	1.4
	0.7
	0.5
	0.2
	0.4
	14



