Table S1 Solutions used in this study

	Solutions
	Form
	Manufacturer
	Compositions
	Immersion time/cycle

	1. 0.5% NaClO
	liquid
	MDent, Faculty of Dentistry, Mahidol University
	Dilution from 2.5% (v/v) Sodium hypochlorite
	10 min

	2. 0.12% (CHX) Chlorhexidine gluconate
	liquid
	MDent, Faculty of Dentistry, Mahidol University
	0.12% (v/v) Chlorhexidine gluconate
	20 min

	3. Polident® (POL)
	Tablet
	Stafford-Miller Limited, Ireland
	Potassium Monopersulfate, Sodium carbonate, Sodium benzoate, Sodium bicarbonate, Citric acid, PEG-180, Sodium Lauryl Sulfate, Tetraacetylethylenediamine 
	15 min

	4. Geraniol (GE) solution 
	Tablet
	This study
	Sodium Bicarbonate, Citric acid, Tartaric acid, Geraniol, Ethylene diamine tetra-acetic acid, Sodium Lauryl Sulfate, Sodium hexametaphosphate, Mannitol
	3 hours

	5. Thymol (TM) solution
	Tablet
	This study
	Sodium Bicarbonate, Citric acid, Tartaric acid, Thymol, Ethylene diamine tetra-acetic acid, Sodium Lauryl Sulfate, Sodium hexametaphosphate, Mannitol
	3 hours
















Table S2 Comparison of antibiofilm efficacy between different chemical methods using one way ANOVA

	Substances 
	Medium (control)
	CHX         20 min
	NaClO 10 min
	POL            30 min
	POL            3 h
	POL   6 h
	GE               30 min   
	GE          3 h
	GE          6 h
	TM           30 min
	TM               3 h

	CHX_20 min
	0.010
	 
	 
	 
	 
	 
	 
	 
	 
	 
	 

	NaClO_10 min
	<0.001
	<0.001
	 
	 
	 
	 
	 
	 
	 
	 
	 

	POL_30 min
	<0.001
	0.017
	<0.001
	 
	 
	 
	 
	 
	 
	 
	 

	POL_3 h
	<0.001
	<0.001
	0.458
	0.029
	 
	 
	 
	 
	 
	 
	 

	POL_6 h
	<0.001
	<0.001
	0.458
	0.029
	1.000
	 
	 
	 
	 
	 
	 

	GE_30 min
	<0.001
	<0.001
	0.161
	0.127
	1.000
	1.000
	 
	 
	 
	 
	 

	GE_3 h
	<0.001
	<0.001
	1.000
	<0.001
	0.475
	0.475
	0.170
	 
	 
	 
	 

	GE_6 h
	<0.001
	<0.001
	0.690
	<0.001
	0.003
	0.003
	0.004
	0.673
	 
	 
	 

	TM_30 min
	<0.001
	<0.001
	0.208
	0.095
	1.000
	1.000
	1.000
	0.219
	0.006
	 
	 

	TM_3 h
	<0.001
	<0.001
	1.000
	<0.001
	1.000
	1.000
	0.732
	1.000
	0.139
	0.803
	 

	TM_6 h
	<0.001
	<0.001
	0.110
	<0.001
	<0.001
	<0.001
	<0.001
	0.104
	1.000
	<0.001
	0.007

















Table S3 Comparison of tea stain removal efficacy at 3 and 6 months of immersions between different chemical methods using one way ANOVA

	Substances for 3 months
	Distilled water
	0.12% CHX
	0.5% NaClO
	GE solution
	TM solution

	0.12% CHX
	<0.001
	 
	 
	 
	 

	0.5% NaClO
	0.001
	<0.001
	 
	 
	 

	GE solution
	0.311
	<0.001
	0.239
	 
	 

	TM solution
	0.805
	<0.001
	0.039
	0.961
	 

	Polident®
	0.979
	<0.001
	0.009
	0.744
	0.994




	Substances for 6 months
	Distilled water
	0.12% CHX
	0.5% NaClO
	GE solution
	TM solution

	0.12% CHX
	<0.001
	 
	 
	 
	 

	0.5% NaClO
	0.001
	<0.001
	 
	 
	 

	GE solution
	0.018
	<0.001
	0.955
	 
	 

	TM solution
	0.020
	<0.001
	0.945
	1.000
	 

	Polident®
	0.022
	<0.001
	0.935
	1.000
	1.000
















Table S4 Comparison of coffee stain removal efficacy at 3 and 6 months of immersions between different chemical methods using one way ANOVA

	Substances for 3 months
	Distilled water
	0.12% CHX
	0.5% NaClO
	GE solution
	TM solution

	0.12% CHX
	<0.001
	 
	 
	 
	 

	0.5% NaClO
	1.000
	<0.001
	 
	 
	 

	GE solution
	0.374
	<0.001
	0.554
	 
	 

	TM solution
	0.950
	<0.001
	0.992
	0.881
	 

	Polident®
	1.000
	<0.001
	0.988
	0.209
	0.826




	Substances for 6 months
	Distilled water
	0.12% CHX
	0.5% NaClO
	GE solution
	TM solution

	0.12% CHX
	<0.001
	 
	 
	 
	 

	0.5% NaClO
	<0.001
	<0.001
	 
	 
	 

	GE solution
	0.050
	<0.001
	0.576
	 
	 

	TM solution
	0.282
	<0.001
	0.155
	0.961
	 

	Polident®
	0.260
	<0.001
	0.170
	0.970
	1.000




