Table 2: TWO Way Repeated ANOVA assessing the effect of material and thermocycling on Vickers Hardness (HV)

| Variables | Df | Mean Square | F test | P value | Ƞ2 |
| --- | --- | --- | --- | --- | --- |
| Material | 1 | 78.400 | 81.215 | <.001 | 0.819 |
| Thermocycling | 1 | 78.400 | 106.715 | <.001 | 0.856 |
| Interaction | 1 | 10.816 | 14.722 | .001 | 0.450 |

*Statistically significant difference at P<.05. Ƞ2: Partial Eta Squared