Table 4: TWO Way Repeated ANOVA assessing the effect of material and thermocycling on surface roughness

| Variables | Df | Mean Square | F test | P value | Ƞ2 |
| --- | --- | --- | --- | --- | --- |
| Material | 1 | 5.882 | 589.502 | <.001* | 0.970 |
| Thermocycling | 1 | 0.462 | 101.893 | <.001* | 0.850 |
| Interaction | 1 | 0.641 | 141.439 | <.001* | 0.887 |

*Statistically significant difference at P<.05. Ƞ2: Partial Eta Squared