Table 4: TWO Way Repeated ANOVA assessing the effect of material and thermocycling on surface roughness
	Variables
	Df
	Mean Square
	F test
	P value
	Ƞ2

	Material
	1
	5.882
	589.502
	<.001*
	0.970

	Thermocycling
	1
	0.462
	101.893
	<.001*
	0.850

	Interaction
	1
	0.641
	141.439
	<.001*
	0.887


*Statistically significant difference at P<.05. Ƞ2: Partial Eta Squared


