Table 6: TWO Way ANOVA assessing the effect of material and thermocycling on fracture toughness.

| Variables | df | Mean Square | F test | P value | Ƞ2 |
| --- | --- | --- | --- | --- | --- |
| Material | 1 | 1.855 | 445.701 | <.001 | 0.925 |
| Thermocycling | 1 | 87.174 | 20944.070 | <.001 | 0.998 |
| Interaction | 1 | 0.086 | 20.772 | <.001 | 0.366 |

*Statistically significant difference at P<.05. Ƞ2: Partial Eta Squared

Model summary: Adjusted R2: 0.998, P value<.001, Ƞ2: 0.998