Table 6: TWO Way ANOVA assessing the effect of material and thermocycling on fracture toughness.
	Variables
	df
	Mean Square
	F test
	P value
	Ƞ2

	Material
	1
	1.855
	445.701
	<.001
	0.925

	Thermocycling
	1
	87.174
	20944.070
	<.001
	0.998

	Interaction
	1
	0.086
	20.772
	<.001
	0.366


*Statistically significant difference at P<.05. Ƞ2: Partial Eta Squared
Model summary: Adjusted R2: 0.998, P value<.001, Ƞ2: 0.998

