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Figure S1 Categorization of materials (in scores) according to their effect on NHI/3T3 cell viability. Score I: non-cytotoxic (more than 90% cell viability), Score II: slightly cytotoxic (60-90 % cell viability), Score III: moderately cytotoxic (30-59% cell viability); Score IV: severely cytotoxic (less than 30% cell viability) [23]. Placebo varnish (PLA), fluoride varnish (FLU); nanoparticulate sodium trimetaphosphate varnish (TMP); universal adhesive (SBU); surface pre-reacted glass-ionomer filler-containing varnish (SPRG); bioactive ceramic solution (BIOS) and protein from enamel solution (AMTN).
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Figure S2 Categorization of materials (in scores) according to their effect on MDPC-23 cell viability. Score I: non-cytotoxic (more than 90% cell viability), Score II: slightly cytotoxic (60-90 % cell viability), Score III: moderately cytotoxic (30-59% cell viability); Score IV: severely cytotoxic (less than 30% cell viability) [23].
Placebo varnish (PLA), fluoride varnish (FLU); nanoparticulate sodium trimetaphosphate varnish (TMP); universal adhesive (SBU); surface pre-reacted glass-ionomer filler-containing varnish (SPRG); bioactive ceramic solution (BIOS) and protein from enamel solution (AMTN).


Table S1 Correlations between data from cell viability and total protein analysis obtained for NIH/3T3 cells considering each extract dilution separately (100% - extract, 50% diluted, 25% diluted, 12.5% diluted in DMEM)

	 
	L3T3
	PLA
	FLU
	TMP
	SBU
	SPRG
	BIOS
	AMTN
	DMEM

	100%

	Spearman
	-0.371
	-0.058
	-0.714
	0.9
	0.928
	1
	0.029
	-0.714

	
	p-valor
	0.497
	0.913
	0.136
	0.083
	0.008
	0.003
	1
	0.068

	50%

	Spearman
	0.348
	-0.257
	0.257
	-0.086
	0.371
	1
	0.377
	

	
	p-valor
	0.499
	0.658
	0.658
	0.919
	0.497
	0.003
	0.461
	

	25%
[bookmark: _GoBack]
	Spearman
	0.829
	0.771
	-0.886
	0.116
	1
	1
	0.143
	

	
	p-valor
	0.058
	0.103
	0.033
	0.827
	0.003
	0.003
	0.803
	

	12.5%
	Spearman
	0.6
	-0.543
	-0.9
	-0.314
	0.543
	1
	-0.314
	

	
	p-valor
	0.242
	0.297
	0.083
	0.564
	0.297
	0.003
	0.564
	


Table S2 Correlation between data from cell viability and total protein analysis of MDPC-23 cells considering each extract dilution separately (100% - extract, 50% diluted, 25% diluted, 12.5% diluted in DMEM).


	
	MDPC
	PLA
	FLU
	TMP
	SBU
	SPRG
	BIOS
	AMTN
	DMEM

	100%

	Spearman
	-0.543
	0.116
	0.406
	-0.257
	0.986
	0.543
	-0.143
	-0.8

	
	p-valor
	0.297
	0.827
	0.425
	0.658
	<0.001
	0.297
	0.803
	0.333

	50%

	Spearman
	-0.609
	-0.6
	-0.145
	-0.257
	-0.314
	0.257
	-0.551
	

	
	p-valor
	0.2
	0.242
	0.784
	0.658
	0.564
	0.658
	0.257
	

	25%

	Spearman
	-0.714
	-0.714
	-0.429
	-0.203
	-0.029
	0.029
	-0.314
	

	
	p-valor
	0.136
	0.136
	0.419
	0.7
	1
	1
	0.564
	

	12.5%

	Spearman
	-0.6
	0.657
	-0.429
	0.086
	0.371
	-0.812
	-0.771
	

	
	p-valor
	0.242
	0.175
	0.419
	0.919
	0.497
	0.05
	0.103
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