Supplementary Information for

Microscale bone interlocking enhances osseointegration strength on the rough surface of 3D-printed titanium implants: experimental and finite element analysis

Tianyu Shu1,2†, Haoyu Shi1†, Meng Li1, Yu-Chia Lin1, Ang Li1*, and Dandan Pei1*

1Key Laboratory of Shaanxi Province for Craniofacial Precision Medicine Research, College of Stomatology, Xi’an Jiaotong University, Xi’an 710049, China.

2State Key Laboratory for Manufacturing System Engineering, School of Mechanical Engineering, Xi'an Jiaotong University, Xi'an 710054, China.

† Tianyu Shu and Haoyu Shi contributed equally to this work and share first authorship.

*Correspondence:

Ang Li

drliang@xjtu.edu.cn

Dandan Pei

peidandan@xjtu.edu.cn

# Supplementary Fig. 1 Shape of experimental implants.

# Supplementary Table 1 Surface element composition (weight percentage).

|  | Ti | O | Al | V | C |
| --- | --- | --- | --- | --- | --- |
| SLM | 76.64% | 11.16% | 5.72% | 3.94% | 2.53% |
| CNC-SLA | 80.83% | 4.92% | 6.84% | 4.27% | 3.13% |

# Supplementary Fig. 2 Implant installation at the femoral condyle of New Zealand rabbit. (A) Skin preparation. (B) Skin disinfection. (C) Surgical field. (D) Incision at skin and joint capsule. (E) Cavity preparation. (F) The implant position.

# Supplementary Fig. 3 The removal torque analysis.

# Supplementary Fig. 4 The microscale finite element model of the bone-implant interface. (A) The SLM group. (B) The CNC-SLA group.

# Supplementary Fig. 5 Mesh sensitivity analysis. The green arrow indicates the selected element number.

# Supplementary Fig. 6 Boundary conditions in the finite element model. (A) Meshed model. (B) Contact region. (C) Fixed support.