




Dear reviewer, due to the high number of groups and data in the study, we were unable to include post-hoc tables in the analysis. Our post-hoc tables are provided below. However, if you wish, we can still include them.




Table S1: Post-hoc table for ΔE
	[bookmark: _Hlk175651447]Group
	 Group
	ΔE

	Filtek Z250
	Filtek Universal
	0.266

	
	Harmonize
	0.176

	
	Vitra
	0.138

	
	Omnichroma
	0.726

	
	Essentia
	0.494

	
	Charisma Diamond One
	0.278

	Filtek Universal
	Harmonize
	0.807

	
	Vitra
	0.011*

	
	Omnichroma
	0.443

	
	Essentia
	0.665

	
	Charisma Diamond One
	0.030*

	Harmonize
	Vitra
	0.006*

	
	Omnichroma
	0.313

	
	Essentia
	0.499

	
	Charisma Diamond One
	0.016*

	Vitra
	Omnichroma
	0.069

	
	Essentia
	0.032*

	
	Charisma Diamond One
	0.686

	Omnichroma
	Essentia
	0.738

	
	Charisma Diamond One
	0.153

	Essentia
	Charisma Diamond One
	0.079


Tukey HSD Test				*p<0.05



Table S2: Post-hoc table for ΔTP
	Group
	 Group
	T0 (Initial)
	T1(After bleaching)
	ΔTP

	Filtek Z250
	Filtek Universal
	0.883
	0.066
	0.075

	
	Harmonize
	0.892
	0.437
	0.309

	
	Vitra
	0.959
	1.000
	0.084

	
	Omnichroma
	0.001*
	0.001*
	0.429

	
	Essentia
	1.000
	0.998
	0.432

	
	Charisma Diamond One
	0.216
	0.001*
	0.017*

	Filtek Universal
	Harmonize
	1.000
	0.962
	0.345

	
	Vitra
	0.316
	0.170
	0.813

	
	Omnichroma
	0.001*
	0.001*
	0.006*

	
	Essentia
	0.805
	0.016*
	0.006*

	
	Charisma Diamond One
	0.010*
	0.001*
	0.001*

	Harmonize
	Vitra
	0.328
	0.703
	0.478

	
	Omnichroma
	0.001*
	0.001*
	0.071

	
	Essentia
	0.816
	0.174
	0.072

	
	Charisma Diamond One
	0.011*
	0.001*
	0.001*

	Vitra
	Omnichroma
	0.001*
	0.001*
	0.012*

	
	Essentia
	0.984
	0.964
	0.012*

	
	Charisma Diamond One
	0.782
	0.001*
	0.001*

	Omnichroma
	Essentia
	0.001*
	0.001*
	0.996

	
	Charisma Diamond One
	0.001*
	0.003*
	0.109

	Essentia
	Charisma Diamond One
	0.294
	0.001*
	0.107


+Tukey HSD Test		++Dunn’s test		*p<0.05



Table S3: Post-hoc table for gloss
	Group
	 Group
	T0 (Initial)
	T1(After bleaching)

	Filtek Z250
	Filtek Universal
	1.000
	0.987

	
	Harmonize
	1.000
	0.985

	
	Vitra
	0.038*
	0.036*

	
	Omnichroma
	0.049*
	0.073

	
	Essentia
	0.001*
	0.001*

	
	Charisma Diamond One
	0.001*
	0.001*

	Filtek Universal
	Harmonize
	0.989
	0.704

	
	Vitra
	0.106
	0.217

	
	Omnichroma
	0.130
	0.353

	
	Essentia
	0.002*
	0.005*

	
	Charisma Diamond One
	0.001*
	0.001*

	Harmonize
	Vitra
	0.015*
	0.003*

	
	Omnichroma
	0.020*
	0.008*

	
	Essentia
	0.001*
	0.001*

	
	Charisma Diamond One
	0.001*
	0.001*

	Vitra
	Omnichroma
	1.000
	1.000

	
	Essentia
	0.822
	0.763

	
	Charisma Diamond One
	0.559
	0.093

	Omnichroma
	Essentia
	0.774
	0.591

	
	Charisma Diamond One
	0.500
	0.047*

	Essentia
	Charisma Diamond One
	0.999
	0.837


+Tukey HSD Test		++Dunn’s test		*p<0.05


